## Slide 1: First tests of CHERWELL, a Monolithic Active Pixel Sensor. A CMOS Image Sensor (CIS) using 180 nm technology
James Mylroie-Smith
Queen Mary, University of London
for the Arachnid Collaboration

## Slide 2: Outline
CHERWELL
4T MAPS
Deep P-Well
First Results
Future Plans
Summary

## Slide 3: Origins
Future
Present
Past
TPAC Digital Calorimiter using INMAPS CMOS technology
Linear Colider?
FORTIS
4T CMOS sensor for tracking and vertexing
CHERWELL
SuperB?
Alice?
Calorimetry
Tracking
+ ...... ?

## Slide 4: CHERWELL
For tracking/vertexing and calorimetetry
180nm CMOS image sensor
4 types of pixel:
    DECAL25
    DECAL50
    Reference Pixel
    Strixel
Internal, column-parallel ADC
12um thick epitaxial layer
Standard and High resistivity
DECAL 25
DECAL 50
Ref Pixel
STRIXEL
SUM
ADC
ADC
ADC
5mm
5mm

## Slide 5: CHERWELL
Cherwell
Digital Calorimetry (DECAL)
“4T” pixels with triggered global shutter and in-pixel CDS
25um pixel pitch 2x2 pixel summing at column base
50um pixel pitch
Vertex/Tracking
Standard “4T” pixels
Reference pixel array 12 bit ramp ADC implemented at column base
“Strixel” array 12 bit ramp ADC embedded in pixel array
DECAL 25
DECAL 50
Ref Pixel
STRIXEL
SUM
ADC
ADC
ADC
5mm
5mm

## Slide 6: 4T Technology
3T CMOS
  readout and charge collection node are the same
  No CDS
4T CMOS
  3 additional elements
  Readout and charge collection at different points
Benefits
  Low noise from capacitance of the floating diffusion
  Low noise and in pixel CDS
  High gain
3T
4T

## Slide 7: Deep P Well Implants
STANDARD CMOS
INMAPS
PMOS Transistors require an n-well
PMOS n-well competes with n-well diode reducing the charge collection
To improve charge collection efficiency a deep p-well is implanted
Reflects charge back into the epitaxial layer

## Slide 8: High Resistivity
We have sensors using standard and high resistivity epitaxial layers
Benefits of high res:
  Faster charge collection
  Reduced charge spread
  Increased radiation hardness
Typical resistivity
10-100Ωcm
High resistivity
1-10kΩcm

## Slide 9: Initial test
The sensor type:
  Standard resistivity
  Reference pixels(48x96)
Understand performance:
  PTC
  Pedestals
  Noise and Gain
  Pedestals and noise with temperature
  55Fe Spectrum

## Slide 10: Photon Transfer Curve
PTC scan controlled by computer
IR LED uses programmable generator to give uniform illumination
Sensor read back to computer and data complied into PTC and results plotted

## Slide 11: PTC Results
PTC performed using IR illumination
Results show good uniformity across the pixels
Gain ≈ 0.17 ADC/e
Noise ≈ 12e rms
Linear full well ≈ 11500e
Maximum full well ≈ 14700e
Log(Signal)
Log(Noise2)
Signal
Noise2

## Slide 12: Pedestals
Readout is performed on a column by column basis
Shows common noise in columns
Pedestal Value (ADC counts)

## Slide 13: Noise and Gain
Noise and gain are uniform across the sensor
Average noise value ~12 e rms
Average gain value 0.17 => 51𝜇V/e
Noise from each pixel
RMS Noise(e)
Gain from each pixel
Gain(ADCs)

## Slide 14: Maximum Full Well Capacity
Full well(e-)
Full well capacity ~ 14,700e
Consistent across the sensor
Linear full well ~11,500e

## Slide 15: Noise vs Temperature
Chart: 
| 26.662 | 30.817 | 35.857 | 40.69 | 45.435 | 50.366 | 48.061 | 43.314 | 38.752 | 33.688 | 21.647
Peak | 6442 | 6433 | 6426 | 6493 | 6699 | 7039 | 6841 | 6582 | 6525 | 6511 | 6597
Chart: 
| 26.662 | 30.817 | 35.857 | 40.69 | 45.435 | 50.366 | 48.061 | 43.314 | 38.752 | 33.688 | 21.647
Noise | 97.51 | 96.84 | 96.31 | 96.06 | 97.72 | 114.91 | 98.4 | 96.83 | 96.85 | 97.51 | 99.92
Chart: 
| 26.662 | 30.817 | 35.857 | 40.69 | 45.435 | 50.366 | 48.061 | 43.314 | 38.752 | 33.688 | 21.647
Noise | 97.51 | 96.84 | 96.31 | 96.06 | 97.72 | 114.91 | 98.4 | 96.83 | 96.85 | 97.51 | 99.92
At 50C the noise becomes large.
Increase in noise at 20C
Temperature (C)
Noise (ADCs)
Noise (ADCs)
ZOOM
Temperature (C)
Pedestal
Noise

## Slide 16: Fe55
Fe55 spectrum shows a sharp cut-off
Consistent with noise and gain from PTC
Good S/N up to 150

## Slide 17: Future Plans
Full test and comparison of on-chip ADC with on-board ADC
Characterisation of the STRIXELs
Comparison of different resistivity chips
Testbeam at CERN planned for November
Radiation damage studies
New chip design planned – discussions with CERN

## Slide 18: Summary
Cherwell chip is working well
Noise and gain as expected
Showing good uniformity in noise and gain
Obtained Fe55 spectrum
Measured noise as a function of temperature
Detailed characterisation is underway
On course for testbeam in November