## Slide 1: 14 T+ Cable winding/bending test
N.Peray
30/01/2024

## Slide 2: Goal :
Knowing the cables bending limits to design the shortest coil head possible
Hard way bend
Easy way bend

## Slide 3: Example of impact of the hard way bend on the coil head

## Slide 4: Target value of the test
Cable type | Easy way bending radius (mm) | Hard way bending radius (mm)
RMM | 13 | 275-300-325-350
TFD | 14.8 | 375-400-425-450

## Slide 5
The tool
Hard way bend dependent
Eight sets to be produced
Easy way bend dependent
Two sets to be produced

## Slide 6: Still on the coil head length optimization
How does the cable switch for a layer to the other?

## Slide 7: An option

## Slide 8: Questions
Thank you for your attention