## Slide 1: Study of gain of LGAD
1/31/2024
Gabriele Giacomini

## Slide 2: Gain Characterization
Use of a low-noise Charge Sensitive pre-amplifier (Amptek A250) to determine the gain of several families of LGADs exposed to different radiation sources (90Sr, 241Am, 55Fe, Alphas).
In this presentation, OLD BNL LGAD (shallow gain implant), new BNL LGAD (deeper implant), HPK (deep gain implant) - we submitted a paper on NIM (soon on arxiv.org)
All BNL fabricated LGAD/AC-LGAD will undergo the same tests.

## Slide 3
Chart: BNL 3045 - Sr - PX5 Gain = 5
Betas from 90Sr

## Slide 4
Chart: Am241 w3045
Gamma rays from 241Am

## Slide 5
Chart: Fe 55 - w3045
#REF! | 1
#REF! | 1
X rays from 55Fe

## Slide 6
Chart: alpha w3045
Alphas from 241Am

## Slide 7
Gain
Easy calibration with PIN diode or with Cinj (2.1pF)
Max gain for betas: effects of charge cloud shape clearly visible

## Slide 8
Spectroscopic parameters (55Fe)
Multiplication noise dominant at higher gains
Low-gain shoulder in spectra

## Slide 9
Laser Tests
Searching for effects of gain saturation in LGADs hit by laser
  scan in laser threshold
  Scan in voltage
  Diode and LGAD coming from same wafer
  FNAL board
  Mip generates charge along small radius track and instantaneously
  vs
  Laser focused at 15um and signal ~350ps long at high threshold (longer at lower threshold).
   Laser track is order of magnitudes less dense.
  Still, interesting to see saturation effects with laser injection.
  A lot of data acquired so far, still interpreting them.
  Much more soon.