## Slide 1: Superheating field in superconductors with nanostructured surfaces
Alex Gurevich
Old Dominion University, Norfolk VA, USA
Supported by DOE DE-SC 100387-020
Pathirana and Gurevich, Front. Electr. Mat. 3, 1246016 (2023)

## Slide 2: What are the SRF field limits and how could they be raised?
The widely used GL theory of dc superheating field Hs(T) is applicable near Tc but not at T << Tc.
Only Hs(0) = 0.84Hc at in the clean limit (Galaiko 1966, Catelani and Sethna, 2008)
and for arbitrary impurity concentration (Lin and Gurevich, 2012) have been calculated.
How different can the dynamic superheating field Hd(T,f) be from the static Hs(T) at GHz frequencies?
(Sheikhzada and Gurevich, 2020)
Increase of Hs by surface nanostructuring: dirty layers, SIS or SNS multilayers for which Hs has only been calculated in the limit of
We report GL numerical calculations of Hs at realistic finite for:
  Dirty surface layers
  SIS structures: dirty Nb-I-clean Nb, Nb3Sn-I-Nb and others
A significant boost of Hs can be achieved by optimizing SIS parameters.

## Slide 3: Superfluid pairbreaking velocity
Depairing current density at the surface:
Jd = envc = 500 MA/cm2
Thermodynamic critical field
Hc = 200 mT,  = 40 nm. In Nb cavities
the dc depairing limit at 2 GHz and 2K
has been achieved on “industrial scale”
1
100 nm
2-3 mm
Bardeen, Rev. Mod. Phys. 34, 667 (1962), deGennes, 1968
Superfluid velocity vs cannot exceed the critical value vc above which the superconducting state breaks down. In the clean limit:
RF field induces supercurrent density carried by Cooper pairs
At for Nb the moving condensate of Cooper pairs
becomes unstable but the density of Cooper pairs does not vanish.

## Slide 4: Ginzburg-Landau equations
Coupled nonlinear PDEs for the pair wave function and magnetic vector-potential A(r).
Coherence length  and magnetic penetration depth 
Thermodynamic critical field:
Boundary condition between a superconductor and vacuum Js = 0:
Phenomenological Ginzburg-Landau theory (1950, Nobel prize 2003)

## Slide 5: GL depairing current density
Uniform current-carrying state with  = 0exp (-iqx), where q is proportional to the velocity of the Cooper pairs.
The GL equations give:
Maximum J at q = 1/3 defines the GL depairing current density:
Current density as a function of q:
q
J = Jd
J < Jd
Suppression
of ns by current
At J = Jd the superfluid density
nc(J_d) = (2/3)ns does not vanish

## Slide 6: DC superheating field
Meissner state becomes unstable above the superheating field H > Hs as the
velocity of Cooper pairs exceed the critical velocity
GL region, T ≈ Tc: (Matricon and Saint-James, 1967, Chapman 1995)
Bs decreases as the GL parameter κ = λ/ξ increases and
the material gets dirtier.
No theory of Hs(T) at low T and
Nb
Extrapolation of GL results to T << Tc underestimates Hs(0) = 0.84Hc
at κ >> 1 in the clean limit (Galaiko 1966, Catelani and Sethna, 2008)
and for arbitrary concentration of nonmagnetic and magnetic impurities (Lin and Gurevich, 2012)

Why?

## Slide 7: Effect of on Hs
Large : Cooper pair reaches
the critical velocity at the surface, where
. This yields the
minimum superheating field at :
Local EM response
Nonlocal EM response
: Center of mass of Cooper pair reaches the critical velocity at J(0) > jd at higher H at the surface. As a result,
Increases as decreases.
Spinning Cooper pair → vortices.

## Slide 8: Vortices protect superconductivity at H > Hs
H0
At H < Hs screening currents are not strong enough to break the Meissner state at J(0) < Jd
z
At H > Hs vortices reduce the current density at
the surface allowing SC at higher fields
H < Hs
H > Hs
Counterflow of vortex currents against the Meissner current reduces J(0) at the surface below Jd allowing
SC to survive up to high fields Hc2 at which the vortex cores overlap
The SRF breakdown is limited by Hs but not Hc2
Vortices penetrate with supersonic velocities in
Embon et al Nat. Commun. 8, 85 (2017); Dobrovolskiy et al, Nat. Commun. 11, 3291 (2020)
Delay with penetration of vortices at H > Hs does not increase the SRF field limit but destroys SC

## Slide 9: Hs for nanostructured surfaces in the limit of
SIS London model
Gurevich, APL 88, 012511 (2006); AIP Adv. 5. 117112 (2015)
Kubo, Iwashita, Saeki, APL 104, 045006 (2014)
SIS, dirty limit, Usadel eqs
Kubo, SUST 34, 045006 (2021)
Ngampruetikorn and Sauls,
Phys. Rev. Res. 1, 012015 (2019)
Dirty surface layer
Inhomogeneous impurity
scattering rate at the surface
Enhancement of Hs by current counterflow induced in the overlaayer

## Slide 10: Instability of Meissner screening at H = Hs at finite
Partial suppression of
by
screening current at H < Hs
Growth of periodic perturbations
along the surface preceding
penetration of vortices at H > Hs
GL results for
GL numerical simulations for Nb:
Pathirana and Gurevich, Front. Electr. Mat. 3, 1246016 (2023)
Period along the surface
Decay length perpendicular to the surface
Christiansen, Solid Stat. Comm, 7, 727 (1969); Chapman
SIAM J. Appl. Math , 55, 1233 (1995); Transtrum et al, PRB
83, 094505 (2011), Liarte et al, SUST 30, 033002 (2017)
How can the instability lengths affect Hs
for nanostructured surfaces (SIS etc)?

## Slide 11: Dirty layer at the surface
Slowly ramping magnetic field:
instability

## Slide 12: Detecting superheating field
x/ξ
Order Parameter (f)
y/ξ

## Slide 13: Dirty surface layer, results
Maximum in Hs(ld) results from current counterflow induced in the dirty surface layer with larger
by the cleaner bulk with smaller , similar to that in SIS multilayers. Reduced Hs at larger ld is due to
larger GL parameter of the dirty layer,

## Slide 14: SIS with the same materials
SIS Nb3Sn with the same
parameters of the overlayer
and the the bulk
SIS Nb3Sn with dirtier overlayer
Dip in Hs(d) at small d results from suppression
of vortex perturbations by I layer over
perpendicular to the surface
Red dashed line shows Hs(d) calculated
in the London model

## Slide 15: Hs of SIS in the London model
Cusp-like maximum Hs caused by the current counterflow effect is at the optimum overlayer thickness:
Gurevich, AIP Adv. 5. 117112 (2015)
Here Hs1 and Hs2 are the superheating fields for the bulk and overlayer materials

## Slide 16: High-Tc overlayer in SIS
Nb3Sn - I - Nb
Thin Nb3Sn overlayer more
than doubles the dc
superheating field
London model works
surprisingly well
I interlayer is necessary to
prevent avalanche penetration
of vortices

## Slide 17: Nonequilibrium SRF
Numerical simulations of equations of nonequilibrium superconductivity
Kinetic equations for quasiparticles and dynamic eqs for SC condensate
Time-dependent GL equations for a gapped dirty superconductor
Sheikhzada and Gurevich, PRB 102, 104507 (2020)
Kramer and Watts-Tobin, PRL, 40. 1041 (1978)
Watts-Tobin, Krahenbuhl and Kramer, JLTP 42, 459 (1980)
Relaxation time of SC condensate:
Relaxation time of quasiparticles due to
inelastic electron-phonon collisions:
Relaxation time constant of quasiparticles can be much larger than the RF period
For Nb at 7K, we have:
Nearly instantaneous reaction of SC condensate to RF field.
Much slower relaxation of quasiparticles, which slows down greatly as T decreases

## Slide 18: Dynamic SRF breakdown
SC breakdown field Hd (T,f) increases with up to the limit:
SC breakdown caused by the time
averaged squared RF field

## Slide 19
Dynamic superheating field
High temperatures: enhancement of Hd due to slow qp relaxation:
Lin and Gurevich, PRB 85, 054513 (2012)
Low temperatures: T < 0.5Tc: the relaxation time increases greatly but the density of quasiparticles decreases exponentially in the dirty limit.
No effect of quasiparticles on SC breakdown if
In the clean limit the quasiparticle gap vanishes at H < Hs,
so the dynamic superheating field may be enhanced by slow relaxation of
quasiparticles
Sheikhzada and Gurevich, PRB 102, 104507 (2020)

## Slide 20: Conclusions
GL calculations of Hs for surface dirty layer and SIS structures were performed for arbitrary GL parameter.
In all cases we observed a maximum in Hs at optimal thickness for which Hs exceeds the superheating fields of both the overlayer and the bulk materials
Our GL results for Hs(d) at finite are qualitatively consistent with previous calculations in the London model
At GHz frequencies the dynamic superheating field in the dirty limit is close to the static Hs but in the clean limit the relation between Hd and Hs has not been investigated