## Slide 1
Dorothea Fonnesu
17.09.2024
Nb3Sn/Cu by Magnetron Sputtering for SRF cavities at INFN-LNL
This project has received funding from the European Union’s Horizon-INFRA-2023-TECH-01 under GA No 101131435 – iSAS
and from the European Union’s Horizon 2020 Research and Innovation programme under GA No 101004730 – I.FAST
Work supported by INFN CSN5 experiment SAMARA and INFN CSN1 experiments SRF and RD_FCC
Paris, September 16 – 20, 2024
Université Paris-Saclay, France
Thin Films SRF 2024
11th International Workshop on Thin Films
and New Ideas for Pushing the Limits of RF Superconductivity

## Slide 2: Outline
Nb3Sn/Cu challenges
INFN-LNL goal
Deposition recipe optimization
Nb3Sn R&D projects timeline
Conclusion

## Slide 3: Our partners
Lehrstuhl für
Oberflächen- und
Werkstofftechnologie

## Slide 4
A15 are brittle materials
Complicated phase diagram
Low melting point substrate (Cu)
Interface diffusion
Tuning of coating parameters
Substrate preparation
Target production/magnetron design
Trapped flux
Cavity tuning
Nb3Sn on Cu: multiple challenges
ESPP Accelerator R&D Roadmap

## Slide 5: INFN-LNL goal
Main R&D activities
1.3 GHz elliptical Nb3Sn/Cu prototype cavity
How?
DCMS with stoichiometric single target
(small samples)
DC Magnetron Sputtering
cylindrical target production via LTD
(6 GHz cavities)
Liquid Tin Diffusion
Easy and validated
(e.g. LHC Nb/Cu)
Deposition recipe must be optimised
Notes:   DCMS demonstrated for Nb/Cu (LEP-II, LHC, ALPI, ISOLDE)
  easy to implement with single stoichiometric target for Nb3Sn

## Slide 6: Deposition recipe optimization
apply 1&2 again for the deposition and RF test of 1.3 GHz prototype
3
1
tuning of deposition parameters based on Tc of small film samples
2
production and RF test of quadrupole resonator (QPR) sample

## Slide 7
1
Tc-driven parameter optimization

## Slide 8: Sample production
Tight-feedback driven standardized process:
deposition > characterization > parameter adjustment
    Films are deposited on different substrates:
      sapphire for reference as substrate does not affect the film
      copper without and with a niobium buffer layer (NbBL) of variable thickness
      bulk Nb

## Slide 9: Deposition temperature limit
Limited by weakening point of copper
      Cu starts weakening at ~ 450 °C (Nb3Sn requires > 930 °C)
      softening of 6 GHz cavity flanges observed at 650 °C

## Slide 10: Pressure and cathode power
sapphire substrate
copper and NbBL-1 substrate
not SC
Tc
pressure
power
Deposition temperature = 630 ºC

## Slide 11: Temperature and annealing time
2 h
5 h
sapphire substrate
Annealing detrimental for Tc

## Slide 12: Role of the NbBL
No annealing
sapphire
sapphire
copper
sapphire
copper
1 μm
sapphire
copper
1 μm
10 μm
sapphire
copper
1 μm
10 μm
30 μm
sapphire
copper
1 μm
10 μm
30 μm
40 μm
sapphire
copper
1 μm
10 μm
30 μm
40 μm
bulk Nb
600 °C
650 °C
At 600+ ºC Tc converges at ~ 17 K for NbBL-30+ (sapphire and bulk Nb)
Inductive measurement of SC transition

## Slide 13: Recap: Nb3Sn base recipe
Based on the observed results
  Low cathode power < 20 W
  Deposition pressure 2 x 10-2 mbar
  No annealing
  Deposition temperature 600 ºC – 650 ºC
NbBL thickness plays a major role

## Slide 14: NbBL effect on lattice parameter
650 °C
(002)
(012)
(112)
(011)
(111)
1 μm
30 μm
bulk Nb
X-Ray Diffraction spectroscopy (XRD)
Peaks shift toward nominal values

## Slide 15: NbBL effect: accommodation
650 °C
Nb3Sn
NbBL
A thicker NbBL promotes the formation of the A15 phase (see Tc)
30+ µm is the “saturation” thickness
bulk

## Slide 16: NbBL effect: accommodation
DCMS data comparison to literature data [A Godeke 2006 Supercond. Sci. Technol. 19 R68]
650 °C
1 μm
10 μm
30 μm
40 μm
Increasing
Sn content
Increasing Sn content and NbBL thickness
bulk Nb
25 At%

## Slide 17: NbBL effect: morphology
Nb3Sn/ Nb(1µm)/ Cu (650°C)
Nb3Sn/ Nb(9µm)/ Cu (650°C)
Nb3Sn/ Nb(30µm)/ Cu (650°C)
Nb3Sn/ Nb(40µm)/ Cu (650°C)
Nb3Sn/ bulk Nb (650°C)
Lehrstuhl für
Oberflächen- und
Werkstofftechnologie
Scanning Electron Microscopy (SEM)
500 nm
1µm
Nb3Sn/ Nb(40µm)/ Cu (650°C)

## Slide 18: NbBL effect: morphology
S. Leith – CERN TE-VSC Seminar 15/11/2022
Copper inclusions on film deposited on 1 μm NbBL
Nb3Sn/ Nb(1µm)/ Cu (650°C)
Scanning Electron Microscopy (SEM) + Energy Dispersive X-ray spectroscopy (EDX)

## Slide 19: Additional studies
  Magnetometry
  RF surface impedance in high/low DC magnetic field
  Superconducting gap
  Flash Lamp Annealing (FLA)
  laser treatment
  P. Vidal Garcia’s talk later this morning!

## Slide 20
2
RF test results

## Slide 21: Nb3Sn/bulk Nb QPR test
QPR = Quadrupole Resonator
Courtesy of O. Kugeler and S. Keckert
Fast cooldown
Slow cooldown
Rs ~ 23 nΩ
@ 4.5 K, 20 mT
Nb3Sn coating suffers from flux trapping
Cooldown procedure influence Rs
Quench > 70 mT
@ 4.5 K

## Slide 22: Nb3Sn/bulk Nb QPR test
Comparison to LHC baseline: Q0 vs. Eacc @ 4.5 K
LHC cavities
Nb/Cu 400 MHz
QPR Nb3Sn/Nb bulk
G=216 Ω
Equivalent to
Q0 ~ 9 x 109
@ 5 MV/m
@4.5 K

## Slide 23
3
Coating system for 1.3 GHz prototype

## Slide 24
Nb3Sn/Cu 1.3 GHz final prototype
Nb3Sn on bulk Nb to validate coating performances on 1.3 GHz Elliptical Cavities (2025)
Develop Nb thick barrier/accommodation layer on 1.3 GHz Elliptical Cavities (2025)
(proof of concept on 6 GHz cavities already done)
Nb3Sn on Cu with thick Nb coating
on 1.3 GHz Elliptical Cavities (2026-2028)
1.3 GHz vacuum system ready
Magnetron source commissioned
In parallel:
Study on alternative buffer layer
Study on flux trapping

## Slide 25
Timeline
2021 | 2022 | 2023 | 2024 | 2025 | 2026 | 2027 | 2028
TeFeN
TODAY
3/2024 First RF test on QPR Rs ∼ 20nΩ @ 4.5 K, 400 MHz
1/2022 First test on planar samples  Tc ∼ 10 K
1.3 GHz cavity first RF test (I.FAST)
1.3 GHz cavity optimized recipe for tuning (ISAS)
Nb3Sn
4/2021
Nb3Sn R&D started
6/2023 Thick Nb barrier layer  Tc > 17 K

## Slide 26: Conclusion
the optimization of Nb3Sn deposition recipe via DCMS is at an advanced stage on small samples
  Tc ~ 17.5 K
  deposition temperature 600 ºC - 650 ºC
  thickness of NbBL 30+ µm  accomodation effect
first RF test for film deposited on bulk Nb on QPR sample: promising Rs ~ 23 nΩ @ 4.5 K, 20 mT
parallel work on coating system for 1.3 GHz with rectangular magnetron

## Slide 27: Thank you!

## Slide 28: Standard production process
Sapphire
Cu + 1 µm Nb buffer layer (BL)
+ 24 h annealing
Set parameters:
Cathode power P
Deposition pressure pdep
Deposition temperature Tdep
1 µm Nb3Sn
Cu
10 cm
small samples on holder plate
Characterisation:
Tc measurement
SEM + EDS (Sn composition)
XRD
Tune next parameters
based on trends (step 1)
(1)
(2)
(3)

## Slide 29: Film properties
Field of first flux entry Ben

## Slide 30: DC Magnetron Sputtering

## Slide 31: Nb3Sn deposition system

## Slide 32: Nb3Sn deposition system

## Slide 33
Projects and partners:
SAMARA (INFN CSN5)
  INFN – LNL, INFN – TO, PoliTO, INFN – Roma3, INFN – LNF, Uni Roma 3, INFN – MI, INFN – LASA
I.FAST WP9 (EU’s Horizon 2020 Research and Innovation programme GA101004730)
  IEE – SAS, RTU, Piccoli S.R.L., Uni Siegen, LOT, HZB, HZDR, CEA, IJC, UKRI, Uni Lancaster, Uni Liverpool, UniPD; INFORMAL: CERN, DESY; ASSOCIATED: JLab
SRF (INFN Board for FCC R&D)
ISAS (EU’s Horizon Europe Research and Innovation programme GA101131435)
  IEE – SAS, RTU, Piccoli S.R.L., Uni Siegen, LOT, HZB, HZDR, CEA, IJC, UKRI, Uni Lancaster, Uni Liverpool, UniPD, CERN, DESY, JLab, Fermilab
SuperMAD (INFN CSN5)
  INFN – LNL, INFN – TO, PoliTO, INFN – Roma3, INFN – LNF, Uni Roma 3, ENEA