## Slide 1: Characterization of PEALD Coated Thin Films for SRF Cavity Research
11th International Workshop on Thin Films and and New Ideas for Pushing the Limits of RF Superconductivity – TFSRF2024 – Sept. 19, 2024
Lea Preece - on behalf of the SRF R&D Team Hamburg
Notes: Not like other characterization as for Siegen Talk -> AFM, XPS, EBSD, TEM, etc but MAGNETIC characterization

## Slide 2: Motivation
~ 45 MV/m
SRF cavities approach thermodynamic limit of niobium
Superconductor-Insulator-Superconductor (SIS) multilayers
  Theory shows potential to enhance Eacc and achieve lower rf losses
SIS coating of cavities creates new challenges
  Experimental realization
  Material properties of thin multilayer systems
Magnetic Characterization Study
➾ comprehensively investigate the magnetic properties of SIS layers
Notes: High Tc!!!
SIS = potential to enhance Eacc and achieve lower rf losses, new geometries comes with challenges that have to be investigated, eg. Flux pinning, has to be comprehensively investigated to understand magnetic properzies

## Slide 3: Motivation
~ 45 MV/m
SRF cavities approach thermodynamic limit of niobium
Superconductor-Insulator-Superconductor (SIS) multilayers
  Theory shows potential to enhance Eacc and achieve lower rf losses
SIS coating of cavities creates new challenges
  Experimental realization
  Material properties of thin multilayer systems
~ 70 MV/m
Magnetic Characterization Study
➾ comprehensively investigate the magnetic properties of SIS layers
Notes: SRF cavities = key component for acceleration in state-of-the-art particle accelerators
SIS = potential to enhance Eacc and achieve lower rf losses, new geometries comes with challenges that have to be investigated, eg. Flux pinning, has to be comprehensively investigated to understand magnetic properzies

## Slide 4: Thin Films and Screening Currents
‘Pancake’ Vortex
Vortex dissipation becomes energetically unfavourable
Gurevich: Vortices are energetically supressed in SC thin films for d < λL
Insulator as vortex barrier so that global vortex penetration is prevented
[Asaduzzaman M. et al., Direct measurement of the Meissner screening profile in superconductor-superconductor bilayers using low-energy muon spin rotation (2023)]
References:
A. Gurevich, APL 88 (2006),
T. Kubo, SUST 30 (2017)
Kubo: Vortex penetration shifts to Hsh>HC1 through “counter current” at interfaces
Notes: Hier noch anschauliche Abb zu pancake vortices

## Slide 5: SIS Multilayer Theory
Top superconductor sees majority of rf field → Surface resistance improves
Insulating layer creates more interfaces → More counter currents
Layers must be thinner than λL,Top → RF field is affected by counter currents
→ Optimal layer thickness dS depends on λL and HC1 of the used bulk and layer materials
Niobium (9.27 K)
cubic high-Tc superconductors NbN (17.3 K) and NbTiN (17.8 K)
AlN as insulator
Literature values
Theoretical maximum surface field a SIS coated cavity can withstand:
Reference:
T. Kubo, SUST 30 (2017)
Notes: Hier SS ohne d_I

## Slide 6: Sample Preparation
900 °C annealing for 1 hour with controlled heating and cooling rates
Post-Deposition Annealing to improve
TC and HC1
Recrystallisation and degas of impurities
[Gonzalez.I. et al., J. Appl. Phys. 134, 159902 (2023), 035301 (2023)]
μ0HC1 = 15 mT
μ0HC1 = 81 mT
μ0HC1 = 98 mT
μ0HC1,bulk ≈ 33 mT
NbTiN
Plasma mix of H2 and N2
[L. Mai, DOI: 10.13154/294-7658 (2020)]
250 °C
Precursors: TMA (AlN),TDMAT (TiN), TBTDEN (NbN)
Plasma-Enhanced Atomic Layer Deposition (PEALD)

## Slide 7: Characterization Measurements on SIS & SS samples
X-Ray Reflectivity (XRR) measurement
  Determine the PEALD growth per cycle (GPC)
Low Energy Muon Spin Rotation (LE-μSR) measurement
  Determine the London penetration depth λL
TC measurements
  Contactless Inductive Tc measurement on Nb
  Physical properties measurements on Si (electrical transport, VSM)
Magnetic Flux Lens (MFL) measurement
  Measure flux expulsion (and TC)
See also Md Asaduzzaman‘s talk on „Depth-resolved characterization of superconductor-superconductor bilayer properties beneficial for SRF applications “ ealier today
See also Daniel Turner‘s talk on „Enhancement of magnetic flux expulsion in multilayer structures“ ealier today

## Slide 8: λL and the Estimation of Hsh
SS bi-layer Nb/NbTiN (d ~ 36 nm)
Expected decrease in B with increasing E and z
Kubo’s counter current model used for fit
Hmax estimated for Nb/NbTiN SS bi-layer
Clean limit of λL
Meissner Screening Profile
Normal state (20 K)
Meissner state (2.7 K)
[Credits to Ryan McFadden]
Literature
Calculated
Fit
Notes: Meissner profile shows two decrease rates -> Nb and NbTiN contribution
N accounts for sample size and shape, here simplified and does not include any sample properties, had to be fixed because of constraints while fitting
Layer thickness as expected within two standard deviations, lambdas in agreement with literature values (clean limit for Nb otherwise kappa out of SC Type II limit!)
Lambda Nb probably between fit value and 40nm
Hsh reasonable in cpmparison with Nb3Sn -> 450mT
Bunch of assumptions made before and after Meissner profile fit → influence the interpretation of the results
λNb (λsub) and λNbTiN (λS) used to calculate Hsh,sub and Hsh,S -> used to calculate Hmax

## Slide 9: Discussion on Meissner Profile and Hmax
Estimate based on Meissner Fit → improvable!
Illustrates principle of field enhancement in an SS bi-layer
Hmax estimate visualizes Kubo’s prediction
  Hmax > Hsh,Nb
  SIS multilayers needed!
Kubo’s counter current model suitable to determine λL
Meissner Screening Profile
Normal state (20 K)
Meissner state (2.7 K)
[Credits to Ryan McFadden]
Notes: In the range where dS is thicker than lambda S, the Meissner state can only be preserved if phase transition is prevented by an energy barrier as a Bean Livingston barrier, see section 2.3.2. Consequently, multilayer coatings with multiple interfaces between the layers, i.e. more suppression by counter currents

## Slide 10: TC Measurements on Si Substrate
TC can be clearly assigned to the SC thin film
Highest TC for Si/AlN/NbTiN in both measurement modes
Measurement of an SIS Si/AlN/NbN sample → very low TC
Highest value measured
Not the same for Nb substrate!
Notes: Tc clearly assigned to thin film because of nc Si substrate

## Slide 11: TC Measurements on Nb Substrate
As-deposited: TC not higher than 7 to 8 K
Annealed SS with NbTiN behaves similar as unannealed samples
  TC ~ TC,Nb
  Two transitions?
Only annealed SIS with NbTiN → shows clear stepwise transition → reaches high Tc
(Zoomed out)
[Measurement Courtesy of Erwan Reches, CERN cryolab]
See also Daniel Turner‘s talk on „Enhancement of magnetic flux expulsion in multilayer structures“ ealier today

## Slide 12: TC Measurements with MFL
Annealed Nb SIS and SS samples
Only SIS with NbTiN → shows stepwise transition → reaches high Tc
No double transition or significant increase in Tc for → SS Nb/NbTiN → SIS Nb/AlN/NbN
All Tc measurements deliver matching results!
SIS Nb/AlN/NbTiN
Stepwise Transition
SS Nb/NbTiN
Continuous transition
SIS Nb/AlN/NbN
[Credits to Daniel Turner]
Notes: With polycrystallinity and a rising number of material defects, the transition width becomes broader [33, 68]. As presented in [69] for PEALD coated NbN thin films of high quality compared to e.g. sputtered films, Tc is in a range below 1 K. This is in good agreement with the measurements carried out in this study.

## Slide 13: Magnetic Flux Expulsion
As-deposited and bare samples
800 °C initial anneal
Annealed SS samples
As-deposited SIS and SS thin films
ER(Nb@900 °C) > ER(Nb@800 °C)
Limited spatial thermal gradient
Annealed SS thin films
Much higher flux expulsion
Greater expulsion for 900 °C initial anneal
[Credits to Daniel Turner]
See also Daniel Turner‘s talk on „Enhancement of magnetic flux expulsion in multilayer structures“ ealier today
Notes: Without annealing no influence of AlN layer

## Slide 14: Discussion on TC and Flux Expulsion
Better flux expulsion for 900 °C initial anneal (also observed in other labs)
  Increase in grain size with higher Tanneal
  Reduction in pinning sites
Post-deposition annealing enhances flux expulsion
  Even for SS Nb/NbTiN if no high TC is achieved
  Assumption: Pancake effect adding additional force that counteracts pinning force

## Slide 15: Discussion on TC and Flux Expulsion
Intermediate oxygen layer
High-T annealing required to activate the thin film and achieve high TC
Insulating layer on Nb required to ensure increase in TC
  Barrier layer prevents oxygen from diffusing into NbTiN layer
  XRD of NbTiN on Si confirm high-TC 𝛿-phase formation for SS sample
  Electron Microscopy probably shows oxygen-enriched phase with varying stoichiometry (Ongoing TEM studies with EPFL)

## Slide 16: Conclusion
Unclear if reduction of TC implies reduction of HC
  Experimental determination required
  Useful comparison with estimation of Hmax following Kubo’s model
Findings on oxygen diffusion allow new considerations on μSR data analysis
  Intermediate layer in the SS bi-layer Nb/NbTiN?
900 °C annealing of SIS Nb/AlN/NbN
  Does not form intended high-TC 𝛿-phase
  Ti as stabiliser of the cubic high-TC 𝛿-phase
  NbN excluded from SIS studies
Ito, H. et al. [arXiv: 1907.03410] (2019)
Soon: NbTiN HC1 measurement @ KEK!
?

## Slide 17: Summary
Further improvement of Nb SRF cavity performance neccessary... and possible with PEALD coated SIS multilayer!
  Coating thin high-TC superconducting and insulating layers
  Pushing the field of first flux penetration Hffp
Further characterization and experimental testing of the SIS theory required
SIS is a promising approach towards new technologies and improved future applications in SRF research!
Contact
Lea Preece PhD Student
Universität Hamburg Institute for Experimental Physics Luruper Chaussee 149 22761 Hamburg
Room 045, Bldg. 30
+49 40 8998-2394
lea.preece@desy.de

## Slide 18: Backup
PEALD System at Universität Hamburg
UHV Furnace at Universität Hamburg

## Slide 19: Sample Preparation
Uniform layer-by-layer thin film coatings
Various advantages (compared to e.g. thermal ALD)
  Low-temperature deposition
  High quality, high conformality
  Vast choice of precursors
Self-regulating process
Convenient for coating complex structures, e.g. inside of an SRF cavity
Plasma-Enhanced Atomic Layer Deposition (PEALD)
[L. Mai, DOI: 10.13154/294-7658 (2020)]

## Slide 20: Characterization Measurements
Depth-resolved near-surface magnetic properties measurement → λL
Spin polarised muon beam with energy of 0.5 to 30 keV
Resolves up to 150 nm below sample surface
X-Ray Reflectivity (XRR)
Determine thin film thickness
Reflectivity curve shows interference oscillations → periodicity related to layer thickness
Low Energy-μ Spin Rotation (μSR)
Oscillation width
Notes: NbTiN no elementary superconductor!!!
Lamor precession = the precession of the angular momentum of a particle with a magnetic dipole moment about the direction of an external magnetic field
Precession = the change in direction that the rotation axis of a rotating body (gyroscope) performs when an external force exerts a torque (Drehmoment) perpendicular to this axis

## Slide 21: Characterization Measurements
Magnetic Flux Lens (MFL)
SC/NC sample transition with pulsed heating under controlled cooling conditions
TC Measurements
Contactless Inductive Tc Measurement on Nb
Ramping-up T until SC state breaks down
Tc Measurements on Si (with PPMS)
Electrical-transport mode → measure electrical resistance R vs. T
Vibrating sample magnetometry (VSM) → measure DC magnetic moment vs. T
See also Daniel Turner‘s talk on „Enhancement of magnetic flux expulsion in multilayer structures“ ealier today
[Credits to Daniel Turner]

## Slide 22: PEALD Growth per Cycle for NbN, TiN and NbTiN
1 supercycle NbTiN = 3 x NbN + 1 x TiN
Two-fold results for NbTiN:
Growth per Cycle calculated from measured XRR NbTiN thickness
Growth per Cycle calculated from individual GPCs of NbN and TiN
Results within the expected range
XRR results
matching NbTiN GPCs

## Slide 23: Prediction of maximum surface field Hmax
Clean limit of λL

## Slide 24: Post-Deposition Annealing
1
Theory & Methods
→ Improvement of TC and HC1
[Gonzalez.I. et al., J. Appl. Phys. 134, 035301 (2023)]
[Gonzalez.I. et al., J. Appl. Phys. 134, 159902 (2023)]
μ0HC1 = 15 mT
μ0HC1 = 81 mT
μ0HC1 = 98 mT
μ0HC1,bulk ≈ 33 mT
900 °C annealing for 1 hour → heating rate 3 °C/min
→ controlled cooling rate ~ 1.45 °C/min for 8 hours to 200 °C

## Slide 25: Flux Expulsion Measurement

## Slide 26: STEM Measurements at CERN
Scanning transmission electron microscopy of Tc_6_2 Nb/NbTiN

## Slide 27: NbN Phase Diagram

## Slide 28: PEALD

## Slide 29: Deposition specifications

## Slide 30: VSM Tc Measurements Results
text

## Slide 31: Electrical-transport Tc Measurement Result for NbN
900 °C annealing of SIS Nb/AlN/NbN
  intended high-TC 𝛿-phase is not formed
  Ti as stabiliser of the cubic high-TC 𝛿-phase
  NbN excluded from SIS studies

## Slide 32: HC1 measurement at KEK
Ito, H. et al. [arXiv: 1907.03410] (2019)
Measured HC1 of Nb/SiO2/NbN samples vs. NbN thickness:
HC1 of bulk Nb
Determination of HC1(d) for SIS mandatory
Third-harmonic voltage measurement with local magnetometry at KEK in Japan
  SIS coated Nb samples with varying sc layer thicknesses
Compare results with theory!