## Slide 1
Point contact tunneling spectroscopy for SRF cavities and Qubits
Ivana Curci
CEA/IRFU

## Slide 2: Principle of tunneling spectroscopy
Dynes formula
Other models:
Shiba (magnetic impurities)
Arnold
McMillan
proximity effect
N
S
Fermi function
Superconducting DOS
Our PCT instrument has mapping capability with ~µm resolution statistics of the superconducting parameters spatial distribution
SIN junction

## Slide 3: Outline
ALD- coated Nb.
Nb-HPR-annealed.
Nb3Sn-Cu.
Nb, Ta, Ta/Nb for 2D Qubits.
SRF cavities

## Slide 4: ALD Al2O3-Nb
ALD + heat treatment decreases TLS losses and increases the quality factor at low fields.
650°C 4 h
650°C 10 h
First experiment
Second experiment

## Slide 5
ALD Al2O3-Nb
Small Δ and Γ might reveal a proximity effect.
Non- homogeneous spatial distribution of Δ and Γ.
bulk
Dynes formula
Reminder!!

## Slide 6: Correlation between PCT, XPS and TEM
McMillan:
Δn=0, Δs=1.55, g1=5, g2=0.1, Γ =0.01
T=1.8 K
d ≤ 2.3 nm
TEM and XPS reveal a 2 nm Nb oxide that might be responsible for the proximity effect.
See Y. Kalboussi talk…
N
S
Δn
Δs

## Slide 7: Outline
ALD- coated Nb
Nb-HPR-annealed
Nb3Sn-Cu
Nb, Ta, Ta/Nb for 2D Qubits.
SRF cavities

## Slide 8: Nb-HPR-annealed (Nb EP + HPR + 650°C-10hrs + HPR)
SRF cavities show Q factors ~10 times higher than Nb EP + HPR
σTLS and tan(δTLS) decreased by a factor 10.

## Slide 9: Nb-HPR-annealed
Very small Δ and Γ reveal a proximity effect. Non-homogeneus spatial variation.
McMillan predicts d ≤ 6 nm, consistent with TEM (~ 5 nm).
However, for various junctions we did not obtain good fits with McMillan/Arnold.
We want to test a new proximity effect model (Usadel).
bulk
T=1.85 K
McMillan:
Δn=0, Δs=1.2,
g1=2, g2=0.1,
Γ =0.01
d ≤ 6 nm
Dynes

## Slide 10
Nb EP + HPR
Nb EP + HPR + 650°C-10hrs + HPR
7.5 nm
4.5 nm
4.5 nm
Nb+HPR+annealed vs Nb+HPR
Nb +HPR shows higher Δ and Γ than Nb+HPR+annealed.
TEM and XPS show NbOx partially crystalline which explains the proximity effect in PCT.
At low field, the increase in the Q factor can be explained by the thinner and more cristalline oxide (less defects, less TLS).
And at higher field?
7.5 nm
4.5 nm
4.5 nm
See Y. Kalboussi talk…
bulk
bulk

## Slide 11: RS
Nb+HPR+annealed vs Nb+HPR
Same Δ but is higher for the reference. Γ ? Analysis on process
PCT reveal a reduction in Δ due to a proximity effect. How can we explain the difference in vs ??
Rres= 13(1) nΩ
Rres= 1.9 nΩ

## Slide 12: Outline
ALD- coated Nb
Nb-HPR-annealed
Nb3Sn-Cu
Nb, Ta, Ta/Nb for 2D Qubits.
SRF cavities

## Slide 13
There are current efforts aimed at obtaining cavities with high quality factors using Nb3Sn on Cu.
.
Nb3Sn
Ta
Nb3Sn
Cu
Barrier to reduce Cu diffusion.
Nb3Sn
Y2O3
Nb3Sn
Cu
CERN samples
Nb3Sn-Cu for SRF cavities:

## Slide 14: Nb3Sn-Ta-Cu and Nb3Sn-Y2O3-Cu
Small Δ and Γ (smaller values for Nb3Sn-Y2O3-Cu) Proximity effect? Nb? Cu?
Non-homogeneous spatial distribution of Δ and Γ.
bulk
bulk
Nb3Sn-Ta-Cu
Nb3Sn-Y2O3-Cu

## Slide 15
Nb3Sn-Ta-Cu
Nb3Sn-Y2O3-Cu
EDS shows 73-77 %Nb variation for
Nb3-Sn-Ta-Cu sample and 75-79% for
Nb3Sn-Y2O3-Cu.
For Nb3Sn-Y2O3-Cu, some junctions fit
with McMillan. It predicts d~3-7 nm.
EDS does not show Cu on the surface.
Not enough resolution?
EDS/SEM for Nb3Sn-Cu samples (CERN)
Nb3Sn-Y2O3-Cu
McMillan:
Δn=0, Δs=2.45,
g1=3.5, g2=0.7,
Γ =0.17
Dynes
scan
XPS?
Tuesday’s presentations!!

## Slide 16: Outline
ALD- coated Nb.
Nb-HPR-annealed.
Nb3Sn-Cu.
Nb, Ta, Ta/Nb for 2D Qubits.
SRF cavities

## Slide 17: Qubits coherence time (literature):
T1~200-300 μs
T1~100 μs
T1~ 400- 500 μs
> > Why? Oxides?
SPEC sample
SPEC sample
FNAL/SQMS sample
Nb-Sapphire
Ta-Sapphire
Ta-Nb-Sapphire
What can PCT reveal to understand the difference between Ta and Nb Qubits?

## Slide 18: PCT for Nb, Ta and Ta/Nb
T1~100 μs
bulk
T = 1.33 K
T=1.85 K
T= 1.85 K
bulk
bulk
T1~200-300 μs
T1~ 400- 500 μs
Nb-Sapphire
Ta-Nb-Sapphire
Ta-Sapphire
Small Δ and Γ on Ta/Nb proximity effect between Ta and Nb.
McMillan gives good fits for Ta/Nb. It predicts
d ≤ 10 nm and Γ ~ 0.01.
=0.01 < = 0.15.
Correlation with > ?
Losses are not dominated by Δ in Qubits.
Γ T1 ? How?
=0.26. Correlation with > ?
for our sample vs literature?
XRD reveal both α (wanted) and β (unwanted) phases.
More PCT on Ta and Nb is needed!!

## Slide 19: Conclusions
PCT can uncover various phenomena on the surface of superconducting devices correlated to their performances.
PCT on Al₂O₃-Nb reveals smaller gaps compared to the bulk. It can be attributed to the presence of Nb oxides.
PCT on Nb-HPR-annealed samples reveals a proximity effect. TEM and XPS explain this by the presence of a partially crystalline/metallic Nb oxide. We want to correlate values with Rres.
PCT on Nb₃Sn-Cu shows regions with Δ closer to the bulk, but also with smaller Δ, which may indicate the presence of a normal layer (Nb,Cu) estimated to be around ~3-7 nm.
We are trying to find a correlation between the for Ta and Nb that might help in the understanding of Qubits T1. We need more samples to find a correlations.

## Slide 20: References
Proslier, T., Zasadzinski, J., Moore, J., Pellin, M., Elam, J., Cooley, L., ... & Gray, K. E. (2008). Improvement and protection of niobium surface superconductivity by atomic layer deposition and heat treatment. Applied Physics Letters, 93(19).
Kalboussi, Y., Delatte, B., Bira, S., Dembele, K., Li, X., Miserque, F., ... & Proslier, T. (2024). Reducing two-level system dissipations in 3D superconducting Niobium resonators by atomic layer deposition and high temperature heat treatment. arXiv preprint arXiv:2402.04137.

## Slide 21: Thank you