## Slide 1: Cu Cavity Production
Seamless Cavity seams to be a must. 3 Techniques available:
Hydroforming (TRL 6)
Spinning (TRL 7)
Additive Manufacturing (TRL 4-5)
Electroforming (TRL 6)
Bulk Cavities (TRL 6)
Cu Surface Preparation
Well Established Procedures + New promising techniques
Chemical Polishing - SUBU5 (TRL 9)
Electro Polishing - EP (TRL 9)
Plasma Electrolytic Polishing - PEP (TRL 5)
Metallographic Polishing (TRL 5)

## Slide 2: CERN contribution
Surface Preparation:
  STOP Using SUBU is the objective
  Baseline:
  Electropolishing
  Validated on 1.3GHz
  PASSIVATION IS KEY FOR ADHESION
  Objective (5 months)
  EP on 400MHz cavities with HOM ports !!!!!
  QUESTION: how far should we push the efforts to reduce surface roughness? Is EP sufficient? do we need to move to PEP?

## Slide 3: CERN contribution
Manufacturing:
Current baseline: Spinning half-cells + ½ cells welding
Recent development: Internal ebeam welding: Very smooth welds: 1x 400MHz cavity produced (August 24).
Electroforming: 2 cavities produced, RF tests look very promising even without chemistry. Lack of manpower for pursuing further right now. 100% weld-free.
Bulk machined cavities: Ideal test-bed for reference. 4x 1.3GHz at CERN, 4 also at Jlab, 2x 400MHz at CERN. Some 1.3GHz to be provided to iFAST.
Cu welding: not a problem for the film: A problem because of high probability of porosities which, i f revealed by chemistry, can entirely spoil a 200kCHF worth object. Getting rid of welds is a very interesting route.
QUESTION: How low can we accept the RRR of the substrate to go? This could open the route to non studied alloys.

## Slide 4: CERN contribution
Collaborations:
  KEK for hydroforming: very high scalability potential, orange peel effect to adress
  PEP looks very attractive: trials in 2024 with INFN/KEK