## Slide 1: Replication and study of anomalies in LK-99, the alleged ambient-pressure, room-temperature superconductor
HABAMAHORO, Thacien1, BONTKE, Trevor1, CHIROM, Meiraba2, WU, Zheng1, BAO, Jiming3, DENG, Liangzi1, CHU, Ching Wu1
1 Department of Physics and Texas Center for Superconductivity at UH
2 Department of Electrical Engineering and Texas Center for Superconductivity at UH
3 Department of Chemistry and Texas Center for Superconductivity at UH
Thacien Habamahoro
Advisor: Prof. Paul Ching Wu Chu

## Slide 2: Outline
Introduction to superconductivity
Applications & Motivation
Evidence for Superconductivity in LK-99 by Lee et al./ Our comments
Replication of LK-99
Our evidence against superconductivity in LK-99
Summary

## Slide 3
Introduction to superconductivity
1911 – Heike K. Onnes,
Discovered Superconductivity
1933 – Meissner & Oschenfeld,
The Meissner effect
Expulsion of magnetic flux from the interior at T<TC
1900 - Drude’s theory for metals
1957 - BCS theory
High Temperature superconductivity
35 K in LBCO (Müller & Bednorz, 1986)
93 K in YBCO (Chu et al. 1987)
164 K in HgBa2Ca2Cu3O8+δ at 32 GPa (Chu et al. 1994)
203 K in H3S at 150 GPa (Eremets et al. 2015)
260 K in LaH10 at 190 GPa (Hemley et al. 2019)
Describes Superconductivity as macroscopic effect caused by condensation of Cooper pairs
Low Temperature superconductivity: Early predicted max Tc was 23 K

## Slide 4
Applications/Motivation
Efficient electric power transmission
Smaller but powerful magnets
Magnetic levitation
High-speed computing, etc.
MRI
Maglev train
The need of low temperature or extreme high-pressure limit the applications
Do we have a superconducting material under ambient conditions?
Example: H3S needs 203 K (-90 oC) and 150 GPa (1.5106 Atmospheres)

## Slide 5
S. Lee et al., arXiv preprint arXiv:2307.12008 (2023).
S.Lee at al., arXiv preprint arXiv:2307.12037 (2023).
July 22,2023
Motivation
July 22,2023

## Slide 6
Stable magnetic levitation of a thin slab of graphite over an assembly of magnets
Superconductor Pb10-xCux(PO4)6O showing levitation at room temperature and atmospheric pressure and mechanism
Lee et al. evidence for Superconductivity in LK-99: Our comments
Unphysical large magnetic susceptibility
One edge touching the magnet

## Slide 7
Synthesis: LK-99 Samples/Replication
XRD of Samples obtained via Lee et. al synthesis recipe

## Slide 8
Our evidence against superconductivity in LK-99

## Slide 9
Our evidence against superconductivity in LK-99:
LK-99 sample without Cu2S impurity
S3 is insulating and shows no magnetic anomaly anywhere close to 400 K
(a)
(b)
(c)

## Slide 10
Summary
Demonstrated levitation possibility in non-superconducting materials using a graphite slab on magnets.
Replicated LK-99 sample: Produced sample mirroring Lee et al.'s synthesis, showing anomalies close to 400 K, attributed to Cu2S impurity.
Pure Cu2S study: Identified a structural phase transition close to 400 K, from monoclinic to hexagonal, indicating impurity-related anomalies.
Cu2S-free LK-99 synthesis: Developed a sample without Cu2S impurity, exhibiting no anomalies and high electrical insulation, concluding impurity's role in observed anomalies, not superconductivity.

## Slide 11
Publication

## Slide 12
This work is supported by the Enterprise Science Fund of Intellectual Ventures Management, LLC; U.S. Air Force Office of Scientific Research Grants FA9550-15-1-0236 and FA9550-20-1-0068; the T. L. L. Temple Foundation; the John J. and Rebecca Moores Endowment; and the State of Texas through the Texas Center for Superconductivity at the University of Houston.
Acknowledgements
Thank you

## Slide 14
The First Room-Temperature Ambient-Pressure Superconductor
Lee et al. evidence for Superconductivity in LK-99

## Slide 15
Lee et al. LK-99 crystal structure and their bulk sample image
Supplementary slides

## Slide 16
Cu3P
LK-99

## Slide 17
Summary/Conclusion
With a video of a thin slab of graphite on top of magnets set up, we discussed the possibility of having a levitating non-superconducting material.
We successively replicated LK-99 sample following closely Lee et al. synthesis recipe. Our samples have very close XRD data to Lee’s LK-99 sample including Cu2S impurity. These samples (S1 and S2) show anomaly in magnetic and resistive data at around 380 K, but not related to superconductivity.
We studied pure Cu2S and found a first order phase transition at around 380 K related to the structural phase change from low-temperature monoclinic to high-temperature hexagonal structure.
We then synthetized LK-99 sample free of Cu2S impurity following a slightly different route. This sample does not exhibit any of the above anomaly and it’s highly insulating.
We conclude that all anomalies studied are associated with the structural transition of the Cu2S impurity in their sample and not with superconductivity.