## Slide 1: PTFE reinforced electrolyte membrane for high performance and durability in Proton Exchange Membrane Fuel Cell (PEMFC)
Subash C. Bhandari
Advisor: Dr. Anima Bose
Date: 02/24/2024
Physics Research Day - 2024

## Slide 2
Introduction on Fuel Cell
Experiment
Results and Discussion
Conclusion
Outline

## Slide 3
DOI:10.13140/RG.2.1.2579.0482
http://www.fcgroup.yamanashi.ac.jp/en/fuel-cell/index.html
1. Introduction: Fuel Cell

## Slide 4
1. Introduction: Proton Exchange Membrane Fuel Cell (PEMFC)
Anode reaction: ; ∆Va = 0.00 V
Cathode reaction: ; ∆VC = 1.229 V
Overall reaction: ; ∆Vo = 1.229 V
Proton Exchange Membrane Fuel Cell (PEMFC)

## Slide 5
1. Introduction: Proton Exchange Membrane Fuel Cell (PEMFC)
Anode reaction: ; ∆Va = 0.00 V
Cathode reaction: ; ∆VC = 1.229 V
Overall reaction: ; ∆Vo = 1.229 V
Proton Exchange Membrane Fuel Cell (PEMFC)
Over potential

## Slide 6
Excellent proton conductivity
High electric resistivity
Barrier to gas crossover
Mechanically strong
Higher chemical stability
General properties of PEM
1. Introduction: Proton Exchange Membrane (PEM)
Chemical structure of state-of-the-art Nafion® monomer

## Slide 7
Chemical structure of state-of-the-art Nafion® monomer
Proton Transport Mechanisms
Excellent proton conductivity
High electric resistivity
Barrier to gas crossover
Mechanically strong
Higher chemical stability
General properties of PEM
1. Introduction: Proton Exchange Membrane (PEM)
EnergyTechnol.2015,3,675–691

## Slide 8
Chemical structure of state-of-the-art Nafion® monomer
Proton Transport Mechanisms
Excellent proton conductivity
High electric resistivity
Barrier to gas crossover
Mechanically strong
Higher chemical stability
General properties of PEM
Pros:
Excellent proton conductivity
Good chemical stability
Thermally stable up to 160 oC
Cons:
Excessive swelling
Gas permeability
Low mechanical strength
Expensive (~ 1000 $/m2)
Nafion® Membrane
1. Introduction: Proton Exchange Membrane (PEM)
EnergyTechnol.2015,3,675–691

## Slide 9
PTFE reinforced Nafion composite membrane:
Casting Nafion solution directly on porous PTFE Substrate (PTFE/Nafion)
Casting Nafion solution on modified-PTFE substrate (modified-PTFE/Nafion)
Polytetrafluoroethylene (PTFE) chemical structure
2. Experiment

## Slide 10
Reduced swelling ratio
  Constrained by PTFE network
Increased proton conductivity
  Packed-acid mechanism
Enhanced mechanical strength
  PTFE support
3. Result and Discussion: General Properties

## Slide 11
3. Result and Discussion: PEMFC performance
Single cell PEMFC performance in (a) H2/O2 and (b) H2/air
(a)
(b)

## Slide 12
3. Result and Discussion: PEMFC performance and Durability
Single cell PEMFC performance at various RH
Membrane durability test at constant current of 0.2 A with cell temperature of 90 oC and 30% RH

## Slide 13
More than 57% lower swelling ratio
Improved mechanical strength by 1.8-fold
Improved PEMFC performance by 52% in O2 and 35% in air
Long term stability in harsh operating conditions of PEMFC
Compared to the state-of-the-art Nafion® membrane, modified PTFE/Nafion electrolyte membrane demonstrates;
4. Conclusion

## Slide 14
Acknowledgement
Dr. Anima Bose : Research Advisor
Dr. Dinh Cong Tinh Vo : Postdoctoral Researcher
Subash Bhandari :Graduate Student
Paul Byaruhanga : Joint Graduate Student
Current Lab Members

## Slide 15
Thank you for your Attention !

## Slide 17
PTFE/Nafion
Modified PTFE/Nafion
Surface SEM
Cross-section SEM

## Slide 18
Over potential
Fuel Cell Potential
Thermodynamic potential:
= Change in entropy
= number of electrons involved in the reaction
= Faraday’s Constant
= Equilibrium cell potential
= Nernst Potential
= Gas Constant
= Operating Temperature
= Partial pressure