## Slide 1: Ce-doped NiFe-LDH electrocatalysts for oxygen evolution reaction
Paul Byaruhanga
pbyaruha@cougarnet.uh.edu
Advisor : Dr. Shuo Chen
Department of Physics, College of Natural Science and Mathematics
University of Houston

## Slide 2: Why do we need hydrogen?
Energy source | Energy density (MJ/kg)
Li-ion battery | 0.54
Gasoline | 46.90
Hydrogen | 120.00
Department of Energy target
$2/kg H2 by 2025
$1/kg H2 by 2030
~ 220 times more energy density than batteries
~ 54 times more energy density than gasoline
https://www.bp.com/en/global/corporate/energy-economics/statistical-review-of-world-energy.html

## Slide 3: How to produce green H2?
H2O → H2 + ½ O2
Energy Diagrams, Catalysts, and Reaction Mechanisms on Make a GIF
Uncatalyzed
Catalyzed
Cathode : 2H2O + 2e- → H2 + 2OH-
Anode : 4OH- → O2 + 2H2O + 4e-
Ni foam
Ni foam
+
catalyst layer
periodic table - Search Images (bing.com)

## Slide 4: What does our electrocatalyst look like?
5µm

## Slide 5
How does the electrocatalyst perform?
in 1 M KOH

## Slide 6: Is our electrocatalyst stable?

## Slide 7
Conclusion

## Slide 8
Acknowledgement
Thank you
Mr. Yu Wang
Ms. FNU Vidhi
Mr. Haroon Muhammad Khan
Mr. Minghui Ning
Dr. Song Shawei
Dr. Dezhi Wang
Prof. Zhifeng Ren
My meme of the year so far…
Sometimes I shake my head to see if I still have my brain because you in Physics anything can happen

## Slide 9
Additional slides

## Slide 10
Effect of Ce doping
Liao, Yuanyuan, et al. (2023)

## Slide 11
Challenges
Pure Ni foam
Ce doped layer with NH4Cl
Synthesis possible
Good perfprmance
Ce doped layer without NH4F
Synthesis possible
Poor perfprmance
Ce doped layer with NH4F
Difficult to synthesize.
Poor performance

## Slide 12
Element | Line Type | k Factor | k Factor type | Absorption Correction | Wt% | Wt% Sigma | Atomic %
O | K series | 1.032 | Theoretical | 1.00 | 19.28 | 0.36 | 46.82
Fe | K series | 0.602 | Theoretical | 1.00 | 21.15 | 0.29 | 14.72
Ni | K series | 0.621 | Theoretical | 1.00 | 57.07 | 0.40 | 37.77
Ce | L series | 1.059 | Theoretical | 1.00 | 2.51 | 0.26 | 0.70
Total: |  |  |  |  | 100.00 |  | 100.00
Composition analysis

## Slide 13
Performance results of our catalysts

## Slide 14
NiFe0.95Ce0.05
NiFe-LDH