## Slide 1
NiMo based bifunctional catalysts for water electrolysis
Navmi Naik
Research Day
February 24, 2024

## Slide 2
Outline
Water electrolysis
Bifunctional catalyst
Performance
Morphology study
Conclusion

## Slide 3
Water electrolysis
https://earth.org/countries-with-water-scarcity/

## Slide 4
Bifunctional catalyst
Bifunctional – Performs HER and OER simultaneously
Reduces cost of the technology
Simplifies the setup
HER – Hydrogen evolution reaction
OER – Oxygen evolution reaction

## Slide 5
Synthesis
Hydrothermal
Deposition
Immersed in a solution of Ni(NO3)2 and FeSO4
for 1-5h.
Annealed
Nickel Foam (NF)
NiMoO4/NF
NiFe LDH/NiMoO4/NF
In H2/Ar
precursor
NiMo
NiFe LDH
Step 1
Substrate
10.1016/j.mtphys.2021.100419, 2021 MTP
Step 2
NiFe/MoNi4/MoO2/NF
OER

## Slide 6
Optimizing Step 2 – OER layer
323mV
431mV
81mV
112mV
Voltage (V)
Notes: Add Overpot for 0h and 1h. All figures on same level …resize

## Slide 7: Comparison with benchmarks
Voltage (V)
Notes: Every thing must be inside.

## Slide 8: Tests under industrial conditions
1.87V
2x2cm2
Beaker electrolyzer
AEM electrolyzer
1.63V
Voltage (V)
With IR compensation
Without IR compensation
0.5x0.5cm2
Notes: IR compensation with and without.
Why left better than right … IR compensation. Wtrite it out
Mention working area left panel
Substrate NF
Beaker electrolyzer, AEM electrolyzer

## Slide 9
Stability
∆ = 30mV
Notes: Dashed line to show difference on left panel.. Differnece 123mV…….. Remove dashed line

## Slide 10
Morphology
0.5 µm
0h
200 nm
1h
https://doi.org/10.1016/j.mtphys.2022.100841
Fanghao Zhang, 2022
10.1038/ncomms15437 Jian Zhang, 2017
https://doi.org/10.1038/s41467-023-37091-x
Panlong Zhai, 2023

## Slide 11: Conclusions and further research
A bifunctional catalyst with performance comparable to benchmarks was synthesized.
An industrial AEM electrolyzer was built.
The catalyst was found to be stable for over 100h.
Future work will focus on improving the performance further using different methods, especially with electrodeposition to build a core shell structure.

## Slide 12: Acknowledgements
Dr. Zhifeng Ren
Dr. Dezhi Wang
Minghui Ning
Yu Wang
Dr. Luo Yu
Thank you!

## Slide 13: Supplementary information
1a
1b
0a
0b
Electrodeposition?
NiMoO4
NiFe LDF/NiMoO4
 | O | Mo | Fe | Ni
At. % | 19.2 | 33.1 | 14.9 | 32.9
Wt. % | 50.5 | 14.5 | 11.2 | 23.6
Notes: Remove figure 2x5