## Slide 1
Junaid Ur Rehman
Thermoelectric Properties of N type Mg3Bi2-N type Bi2Te3 Composites

## Slide 2: Outlines
Introduction
Applications
Characterization and Results
Conclusion

## Slide 3: Introduction
1. Basic Principles
2. Figure of Merit
3. Motivation
Power stations
65% of energy wasted to environment
Green house effect

## Slide 4: Applications
1. Radioisotope Thermoelectric Generator(RTG)
Used by NASA
Apollo-I
Pioneer
Viking
Voyager-I
2. Niche applications for solid state Technology
Peltier coolers based on Bi2Te3-Sb2Te3 used for
Optoelectronic devices
Small refrigerators
Seat heat and cooling system

## Slide 5: Why I choose Composite?

## Slide 6: N type-N type makes N-type Composites
(1-x)(Mg3.2Bi1.498Sb0.5 Te0.002 + x(Bi2Te2.7Se0.3) Composite
Mg3.2Bi1.498Sb0.5 Te0.002
Bi2Te2.7Se0.3
N type
N type
Mixing after Hot Pressing
Direct Mixing Method
N type Composite

## Slide 7: Mixing after Hot Pressing
Powder 1
Powder 2
Mixing in mortar for 5 mins
Hot Pressing at 700⁰C for 5 mins
Bi2Te2.7Se0.3
Ball Milling for 6 mins
The Tube in furnace for 12hrs at 750⁰C
Mg3.2Bi1.498Sb0.5 Te0.002
Hot Pressing at 750⁰C for 5 mins
Measurements
Step 1
Step 2
Hot Pressing at 450⁰C for 3 mins
Ball milling for 6 mins
Ball milling for 8 hrs

## Slide 8: Mg3.2Bi1.498Sb0.5 Te0.002
Bi2Te2.7Se0.3
Results

## Slide 9: (1-x)(Mg3.2Bi1.498Sb0.5 Te0.002+x(Bi2Te2.7Se0.3)
1% Bi2Te2.7Se0.3
Got p type
ZT at 300K is 0.1 and at 500K is 0.3

## Slide 10: Composite Direct Mixing
Bi2Te2.7Se0.3
Ball Milling for 6 mins
The Tube in furnace for 12hrs at 750⁰C
Powder 1
Mixing in mortar for 5 mins
Mg3.2Bi1.498Sb0.5 Te0.002
Hot Pressing at 750⁰C/800⁰C for 5 mins
Measurements
Step 1
Step 2
Ball milling for 8 hrs
Powder 2

## Slide 11: (1-x)(Mg3.2Bi1.498Sb0.5 Te0.002+x(Bi2Te2.7Se0.3)
Higher ZT at 300K is 0.54 and 500K is 1.1
N type composite

## Slide 12: (1-x)(Mg3.2Bi1.499Sb0.5 Te0.001+x(Bi2Te2.7Se0.3)
Reduce the Te amount and increase Bi
ZT at 300K is 0.81 for 0.25% BTS and at 525K is 1.34 for 1% BTS

## Slide 13
Higher ZT is 0.73 at 300K and 1.25 at 500K
Reproducible
(1-x)(Mg3.2Bi1.499Sb0.5 Te0.001+x(Bi2Te2.7Se0.3)

## Slide 14: Conclusion
Successfully synthesized the Pure Compounds and reproduced the composites
Got the N type composite by changing the synthesis process
Increase the performance by reducing the extra dopant Te by 0.001 for medium range temperature

## Slide 15: Work In Progress
For Bi2Te2.7Se0.3 confirmation I will check best composites at different temperature.
SEM to check the morphology of composite with temperature and composition and EDS to confirm the wt%

## Slide 16: Thanks for your Attention

## Slide 17: Acknowledgment
Advisor: Pro Zhifeng Ren
Dr Shaowei Song
Xin Xi
Suraj Pardan
Navmi Naik
Haroon Khan
Rui Shu

## Slide 18: STRATEGIES TO ACHIEVE A HIGH FIGURE-OF-MERIT (ZT)
To improve the electrical transport properties via optimizing n.
To optimizing band engineering which cause higher power factor
Yang, Lei (2018). Emerging Materials for Energy Conversion and Storage

## Slide 19: Outline
Introduction
Seebeck effect and Peltier effect
Thermoelectric Efficiency
Types of Thermoelectric Materials(TEMs)
Problems to enhance the efficiency of TE materials
Applications of TE materials
Synthesis to make high quality TE materials
Conclusion and discussion

## Slide 20: Thermoelectric Effect
Used for harvesting and recovering heat which is directly converted into electrical energy using thermoelectric generators (TEGs) Conversely,
Peltier coolers and heaters are utilized to convert electrical energy into heat energy for cooling and heating purposes
[Ssennoga Twaha, 2016]

## Slide 21: Thermoelectric Performance
Dimensionless figure of merit zT
Where S, σ, T, and κ are the Seebeck coefficient, electrical conductivity, absolute temperature, and total thermal conductivity
Where k= k(electron) + k(lattice)
[Fujiwara, R, 2023]

## Slide 22: Types of Thermoelectric Materials
Inorganic TE materials (N and P type)
Bismuth telluride (Bi2Te3) and its alloys
Lead telluride (PbTe) and its alloys
Silicon-germanium (SiGe) alloys,
Antimony telluride (Sb2Te3)
Tin selenide (SnSe)
The abundancy of tellurium (Te) in the earth’s crust is only around 0.001 ppm which is less than gold 0.004ppm
MgAgSb
Organic TE materials (N and P type)
Organic TE materials, including polymers, carbon nanotubes (CNTs), and graphene
Low zT values
Advantages of being inexpensive and recyclable
The intrinsic flexibility of organic TE materials
In general, organic TE materials possess low thermal conductivity
ZT value depends on the power factor
Inorganic-organic TE composites(N and P type)
Organic TE materials contain lower electrical conductivity and Seebeck coefficient
Organic TE materials benefits from low thermal conductivity, low density, low cost, low environmental impacts, and good mechanical flexibility
Achieving all these requirements in one TE material is of importance

## Slide 23: Groups of TE materials and Performance
Present Thermoelectric material for Commercial Use
Bismuth Telluride (Bi2Te3), 1950s
Lead Telluride (PbTe), 1970s
Silicon Germanium (SiGe), 1970s
Skutterudittes, 1990s
TE properties at 300K

## Slide 24: zT values Inorganic and organic TE materials
Inorganic TE materials (N and P type)
Organic TE materials (N and P type)
TE properties of some typical polymer based TE materials at 300K

## Slide 26: Types of Thermoelctric Materials(TE)
There are three types of TE materials
Inorganic TE materials (N and P type)
Organic TE materials (N and P type)
Organic-Inorganic TE materials (N and P type)

## Slide 27: History of Thermoelectric (TE)
Thermoelectric(TE) materials and devices, convert the direct energy between heat and electricity.
Thermoelectrics.matsci.northwestern.edu/thermoelectrics/history.html
First TE effect in 1821-3 by Thomas seebeck
1834 J A. Peltier
20 years later 1854 Willium Thomson(Kelvin Relationship)
?