## Slide 1: Silicon Photonics Circuits for the optical readout of CERN detectors
CERN EP-ESE-BE
3rd October 2024
carmelo.scarcella@cern.ch
Carmelo Scarcella, D. Alfiero, A. Cristiano, S. Detraz, H. Muthuganesan, L. Olantera, I. Quintana, C. Sigaud, C. Soos, J. Troska
TWEPP 2024

## Slide 2: Outline
Silicon Photonics links for High Energy Physics
Ring modulator design optimization and characterization
Radiation-tolerant ring modulator driver (DART28) demonstrator
Fiber coupling to Silicon Photonics circuits
Conclusions
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024

## Slide 3: Silicon Photonics links for High Energy Physics
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024
Particle sensor
PIC
>> 100 m Single-mode fiber
System concept
Photodiode
Modulator
Fiber coupler
Photonic Integrated Circuits (PICs)
  Chiplet fabricated using CMOS process
  Fiber couplers, optical waveguides, modulators, photodiodes
  Radiation tolerant
Wavelength division multiplexing:
  Lane: 25 Gbps NRZ
  Fibre: 100 Gbps
Laser sits outside of radiation environment
  Wavelength 1300 nm
  Transparent window for Silicon
Low power / Low mass

## Slide 4: Silicon photonics integrated circuits (PICs)
Two test PICs, designed at CERN, and received in Q1 2024
PackagingPIC (IMEC SiPh Passive+)
  Fiber edge-coupling devices supporting photonic packaging activity
  Passive optical components: optical filters, waveguide structures, etc.
SystemPIC (IMEC SiPh iSiPP50G)
  Optical ring modulators, photodiodes
  4-channel wavelength division multiplexing (WDM) demonstrators
  Assess performance and radiation tolerance
Neutron and X-ray irradiation tests carried out in 2024, showing tolerance to
  High neutron fluence levels (> 3 ·1016 20 MeV n/cm2)
  Total Ionizing Dose (TID) up to 1 Grad
  Most recent published results by Lauri Olantera at RADECS 2024
SystemPIC
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024
PackagingPIC
5 mm

## Slide 5: SystemPIC ring modulator characterization results
~ 3 dB
28 nm CMOS driver provides limited modulation voltage swing Vmod
Need to increase modulator efficiency (ƞ) for margin in link power budget
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024
1550 nm legacy PICv2
CW laser
p-n junction
r
Coupling gap
Multiple ring modulators sweeping the design parameter space
  Radius (r), p-n junction type, coupling gap
  Trade-off between efficiency and bandwidth

## Slide 6: Ring modulator high-speed test
CERN high-efficiency modulator supporting 25 Gb/s data rate
  Modulation voltage swing from 1 Vpp to 4 Vpp
  CW laser power Pin = 2 mW
EP R&D WP6 phase II
  Positive link power margin with ~ 0.8 mW OMA
  Driver targeting ~2 Vpp modulation voltage swing
1 Vpp ƞ ~ 20%
2 Vpp ƞ ~ 40%
3 Vpp ƞ ~ 50%
4 Vpp ƞ ~ 60%
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024
PIC
2.92 mm coaxial connector
CERN custom design
10 µm
OMA

## Slide 7: DART28-NRZ
25.6 Gb/s - Electrical
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024
4 High-speed
outputs
Demonstrator ASIC for Radiation-Tolerant Transmitter in 28 nm CMOS
  Quad modulator driver 4x25.6 Gb/s NRZ
  Embedded data generators, no data inputs
Macrocell to be integrated in sensor Read-Out-Chips (ROCs)

## Slide 8: DART28 Driving SiPh Ring Modulator
Wire bond length is crucial for signal integrity at 25 Gb/s data rate
Connection inductance proportional to the wire bond length
  PIC thinned from the native 720 µm to ~ 300 µm
  Wire bond length reduced to ~ 500 µm
  Gold wire, 25 µm diameter, wedge-wedge bonding
Wide open optical eye diagram at 25.6 Gb/s with fast edges
25.6 Gb/s PRBS7 data
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024
SystemPIC
DART
Fibers
~ 500 µm
Ring modulator
Fiber coupler
CW laser

## Slide 9: Fiber coupling to Silicon Photonics Circuits
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024
Si waveguide
Grating coupler
Angle of incidence
~ 10° off-vertical
Optical fiber
Edge coupler
Optical fiber
Vertical-coupling: planar gratings etched into the Silicon
  Lithographic step not requiring post-processing
  Wavelength selective: bandwidth ~ 30 nm @ - 1 dB
Edge-coupling: requires chip singulation and facet finishing
  Wideband, flat response in the CWDM4 wavelength range
  Clear advantage in targeting edge-coupling in our project
Notes: Add filter

## Slide 10: CERN fiber attachment machine for PICs
R&D fiber attachment machine for PICs purchased by CERN
  Installation and commissioning in May 2024
To support the R&D activity and build internal knowhow on photonic assembly
Fully automated station for optical probe testing on the die level
Active alignment and vision-based processes fully customisable by the user
Build assembly recipes to transfer to contract manufactures
6-axis alignment
engine
Fiber array
Epoxy dispenser
PIC
UV LED
Camera
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024
GUI
Optical power meters

## Slide 11: First fiber edge-coupled PICs at CERN
8-channel fiber arrays attached to the SystemPIC using UV-cure epoxy
Test vehicle for 4-channel coarse wavelength division multiplexing (CWDM4) transmitter
4 ring modulators in the O-band coupled to a single bus waveguide
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024
8-channel
fiber arrays
DC laser COMB
Modulated outputs
5 mm
Edge-couplers
8-channel
250 µm pitch

## Slide 12: Conclusions and next steps
Demonstrated custom ring modulators compatible with 28 nm CMOS driving circuits
Successful co-packaging of the SystemPIC with the radiation tolerant ring modulator driver (DART28)
  Wide open optical eye diagram at 25.6 Gb/s ‒ Wire bonding length minimized to ~ 500 µm
Fiber coupling to Silicon Photonics circuits activity
  Fiber attachment machine for PICs, installed and commissioned at CERN in Q2 2024
  First samples of SystemPIC using edge-coupling been assembled
DRD7: R&D Collaboration on Electronics and On-detector Processing, approved in June 2024
  WP7.1.a Silicon Photonics transceiver development
  About 14 universities and institutes joined the collaboration
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024

## Slide 13
Back-up slides

## Slide 14: Si µ-ring modulator
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024
Selective wavelength filters
Small footprint (radius ~ 5µm)
Small driving voltage amplitude (down to 1 Vpp)
Optically narrowband (< 1nm)
Thermally sensitive (< 1 K)
Input
laser
CERN custom design
10 µm
V
Waveguide cross-section
Reverse biased pn Junction
+
-
Electrical contacts
Waveguide
V0
V1
Electrical
data
Optical data
Input laser
Δλ(V)
p-n junction
OMA

## Slide 15: Radiation tolerance
Silicon photonics Ring Modulators
Integrated Ge Photodiodes
> 10 MGy
> 3.5x1016 n/cm2
> 3x1016 n/cm2
Carried out X-ray & neutron irradiation test with varying ring modulator temperatures
  Neutron irradiation less damaging, independent of temperature
  TID potentially more damaging, can be fully annealed with elevated temperature using on-chip heaters
High-ﬂuence neutron irradiation of integrated Ge-photodiodes
    Limited impact, appear more tolerant than current discrete devices
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024
M. Lalović et al., "Ionizing Radiation Effects in Silicon Photonics Modulators," in IEEE Transactions on Nuclear Science, vol. 69, no. 7, pp. 1521-1526, July 2022
L. Olanterä et al., "Effects of High Fluence Particle Irradiation on Germanium-on-Silicon Photodiodes," in IEEE Transactions on Nuclear Science, vol. 71, no. 4, pp. 728-735, April 2024

## Slide 16: Fiber alignment tolerances
Mode field diameter (MFD) at the single-mode fiber (SMF) facet ~10 µm
Sub-micron MFD into the Si waveguide
Tapered waveguide adapting the two MFDs
Sub-micron alignment tolerances ± 0.6 µm for 1 dB insertion loss
Similar alignment tolerances for vertical coupling and edge coupling
Fiber attachment to PICs requires machines based on active alignment
carmelo.scarcella@cern.ch 03 October 2024
TWEPP 2024
~10 mm
single mode optical fiber core
Silicon waveguide
(o.22 mm x 0.45 mm)
Z
Y
X
Edge coupler
Optical fiber