## Slide 1: Resonant Ultrasound Spectroscopy (RUS) A Study of the Vortex Lattice Phase Diagram of Niobium
Swiss Physical Society meeting 2024
Dang Xuan Dang :: Ph.D. student
ETH Zurich, 10 September 2024
xuan.dang@psi.ch
Notes: Thanks for your introduction.
Today, I will present first results that I obtained with a RUS setup that I built as part of my PhD project. I have measured the vortex phase diagram of the well known superconductor niobium and I hope to convince you that RUS is an excellent tool to study vortex dynamics.

## Slide 2: Vortex Matter in Superconductors
Type II superconductor
    𝜅 > 1/√2
    External magnetic field allows passing via quantised vortex lines
Repulsive interaction between vortices.
Pinning of vortex lines.
Notes: Superconductivity is characterized by its ability to transport electric currents without resistance and by its ability to repel magnetic fields. Superconductors are perfect diamagnets. For a type II superconductor this definition is slightly altered.
When a type II superconductor experiences a magnetic field, it will allow for some magnetic flux to penetrate the superconducting phase. However, the field enters the superconductor only in flux quanta which are very localized lines.

## Slide 3: Vortex Matter in Niobium
T. Reimann et al Physical Review B 96, 144506 (2017)
Type II Superconductor
  Superconducting Transition Temperature 9.2K
  Bc2 ~ 0.5T
Vortex matter in Niobium
  Immediate Mixed phase 0.1T < B < 0.2T
  Shubnikov phase
Notes: Niobium is a conventional s-wave superconductor, and low k.
There is immediate mix phase can be observed by FC and ZFC, which shows vortex arrange like island, before end up filled out in Shubnikov phase.

## Slide 4: Resonant Ultrasound Spectroscopy (RUS) and Elasticity of Crystals
S. Ghosh et al, Science advance. 6, 10 (2020)
RUS measures Eigenmodes of the sample
Depend on sample dimensions, density and elastic modulus
RUS measures all elastic moduli simultaneously.
RUS is highly sensitive to changes in lattice strength.
For example:
BCC crystal has 3 components to the elastic tensor
c11 .. compression
c12 .. torsion
c44 .. shear
Notes: RUS spectra can identify all elastic moduli, which present in the list of resonant frequencies.
Each frequency can deform the crystal in serval elastic mode.
For example.

## Slide 5: Spectrum computation
J. Torres et al., JASA 151, 3547 (2022)
Calculate Eigen frequencies
by Rayleigh-Ritz method.
Compare calculation to experiment
Adapt input parameters
Get the new initial cij*
Notes: Model deal with the forward and inverse problem, while the problem enables the calculation resonant frequencies by give some physical properties.
The inverse problem can deal with determining the physical properties (here is elastic moduli) from resonant frequencies.

## Slide 6: Spectrum computation
J. Torres et al., JASA 151, 3547 (2022)
Calculate Eigen frequencies
by Rayleigh-Ritz method.
Compare calculation to experiment
Adapt input parameters
Get the new initial cij*
We use the package RUScal
https://github.com/RUS-ORNL/RUScal
Notes: Model deal with the forward and inverse problem, while the problem enables the calculation resonant frequencies by give some physical properties.
The inverse problem can deal with determining the physical properties (here is elastic moduli) from resonant frequencies.

## Slide 7: RUS experimental setup
Crystal is clampled by transmitter and receiver transducers.
F.G controls the frequency of excitation.
Amplifier gain the response signal.
DAQ records data and plotting in screen of PC.
Notes: Single crystal was clamped by transmitted and receiver transducers.
The sound wave is propagated through crystal and signal was detected another corner.
Before recording, we gain the response by amplifier.

## Slide 8: RUS Spectrum of Niobium (Nb)
Nb crystal in stick
(*): By K. J. Carroll thesis, 1962
Rectangular shape.
Dimensional: 3.84 x 4.10 x 9.40 mm3
Mass: 1.2528 g
c11 = 245.6 GPa, c12 = 138.7 GPa, c44 = 29.3 GPa (*)
RUS spectrum of Nb at T = 16K

## Slide 9: Comparison measured and calculated Spectrum
C11 ~ 124.38
C11 ~ 132.67
C44 ~ 188.49
2 compression modes
1 shear mode

## Slide 10: Eigenmodes as function of tuning parameters
Frequency (kHz)
Temperature (K)
B = 0 T
Tc ~9.25(7)K
T = 2K
Notes: In term of cooling down the crystal, All resonant frequencies change the slope at temperature critical point cause of elastic sensitive to electron DOS.
In term of tuning the magnetic field, at 2K, dots of freq. show the responding when B field goes up to 600mT
However, they show the difference the sensitive response cause strong in coupling to vortex lattice.

## Slide 11: Phase transition of Niobium by RUS measurement.
Meissner
IMS
Shubnikov
S. Mühlbauer et al, PRL 102, 136408 (2009)
Notes: Phase transition of Nb can be extracted by collect all the ZFC curve in the bias temperature range in 2K to 10K.
Our result is compare about with publication in 2009, which has done by neutron method.

## Slide 12: Conclusion
Developed RUS experiment successful investigate the phase transition of Niobium cause the change of elasticity.
RUS useful tool for the investigation vortex phases and phase transitions

## Slide 13: Acknowledgments
M. Janoschek
J. Philippe
M. Bartkowiak
M. Zolliker
F. Fautz
UZH
C. Klauser

## Slide 14: Supplementary Information
In the second-order phase transition, Landau theory:
Robert G. Leisure et al. Ultrasonic spectroscopy. chapter 5
Adding the term for order parameter (Q) and elastic strain (e) coupling (Fc) and elastic energy

## Slide 15: Supplementary Information

## Slide 16: Elastic tensor computing