## Slide 1: NI HTS magnet projects at PSI
J. Kosse, D. Araujo, B. Auchmann, A. Brem, M. Duda, T. Michlmayr, H. Garcia Rodrigues
SPS2024
This work was performed under the auspices of and with support from the Swiss Accelerator Research and Technology (CHART) program

## Slide 2: Contents
18 T technology demonstrator
18 T split solenoid
RIXS manipulator head magnet
Positron capture solenoid

## Slide 3
Non-insulated (NI) HTS
100 mm
Single-layer pancake coil wound from bare HTS tape
Solder-impregnated

## Slide 4
Non-insulated (NI) HTS Technology Solenoid
100 mm
4x 12 mm wide coil
Solder-potted
Rapidly develop infrastructure
via license agreement with
Tokamak Energy
18 T by PSI 4 stack at 2 kA, 12 K

## Slide 5
NI coil electrical representation:
Inductor (HTS spiral path)
Resistor (turn-turn contact)
Charging time constant
Large NI magnets (large L) take a long time
Non-insulated (NI) HTS Technology Solenoid
18 T by PSI 4 stack at 2 kA, 12 K

## Slide 6
NI coil electrical representation:
Inductor (HTS spiral path)
Resistor (turn-turn contact)
Charging time constant
Large NI magnets (large L) take a long time
Non-insulated (NI) HTS Technology Solenoid
S. Hahn, D. Park, J. Bascuñán, and Y. Iwasa,
“HTS Pancake Coil without Turn-to-Turn Insulation,” IEEE TAS, 2011.

## Slide 7: Experiment vs model
Example: 1.8 kA at 15 K in cryogen-free setup
Turn-turn resistance used a fitting parameter
Works reasonably over a 15-77 K range

## Slide 8: Contents
18 T technology demonstrator
18 T split solenoid
RIXS manipulator head magnet
Positron capture solenoid

## Slide 9: Split Solenoid for Neutron Scattering
18 T NI HTS solenoid
Bore field 18 T at 2 kA, 12 K
4 coils
~Bore field 18 T at 1.8 kA 6 coils
10 mm split NI HTS solenoid
10 mm
Predict with simulation

## Slide 10: Contents
18 T technology demonstrator
18 T split solenoid
RIXS manipulator head magnet
Positron capture solenoid

## Slide 11
R’Equip RIXS Manipulator Solenoid
Planned upgrade of the manipulator used in the RIXS beamline at SLS for soft X-ray scattering experiments. Funded, planned to start design 11/24
Supply a high magnetic field (up to 6 T) on the target via compact solenoid
3.6 cm

## Slide 12: Contents
18 T technology demonstrator
18 T split solenoid
RIXS manipulator head magnet
Positron capture solenoid

## Slide 13: PSI Positron Production () Experiment @ SwissFEL
Aims to demonstrate high yield positron source in 2026. Relevant for FCC-ee
SwissFEL

## Slide 14: PSI Positron Production () Experiment
N. Vallis, https://doi.org/10.1103/PhysRevAccelBeams.27.013401
Aims to demonstrate high yield positron source
Magnet to be tested by end of 2024
experiment operational 2026

## Slide 15: Upscaled version of 18 T PSI NI solenoid
18 T 50 mm cold bore
4 coils
Built & tested
15 T 72 mm warm bore
5 coils
Under construction

## Slide 16: Radiation
P3 (unshielded) | FCC-ee (2 cm Tungsten)
18 kGy/year | 23 MGy/year
DPA/year | DPA/year
P3 (unshielded) | FCC-ee (2 cm Tungsten)
18 kGy/year | 23 MGy/year
will demonstrate high yield,
but not radiation robustness
B. Humann, doi:10.18429/JACoW-IPAC2022-THPOTK048

## Slide 17
Conduction-cooled system
15 T bore, 20 T conductor @ 1.2 kA, 15 K
HTS coils
Target
Thermal shield
G10/SS support
MLI
Current terminals
72 mm
Solenoid stack
Cryocooler
Current leads
Pb mass
1.07 m

## Slide 18
Fault scenario:
Coolers stop
Open circuit
Stored energy gets dissipated
in coils+buffers
R_turnturn
HTS path

## Slide 19: Magnet under construction
Coils being manufactured
Lead buffer casting
Cryostat being assembled

## Slide 20: Conclusions
Several no-insulation HTS magnet projects ongoing at PSI
18 T split solenoid
RIXS manipulator compact solenoid
Positron capture solenoid
Leaning on experience gained via 18 T solenoid
No-insulation HTS magnets ideally suited for
DC applications
Loose magnetic field quality requirements
Compact solutions

## Slide 21
NI HTS Technology Solenoid
Rapidly develop infrastructure
via license agreement with
Tokamak Energy
terminal
terminal
Current
HTS tapes
Axial joint
Insulator
100 mm
Single-layer solder-impregnated pancakes
modular

## Slide 22: Mechanical
Stress [MPa]
Hoop
Mises
Axial
Radial
Frictional
interface
Field’s metal
Axial plate
HTS tapes
Stainless steel flange
Copper terminal plate
Stainless steel
overband
Tape structure explicitly modeled to capture
-differential thermal contraction
-plasticity
Max radial stress 2 MPa
Min axial stress -155 MPa
Max hoop stress (substrate) 450 MPa

## Slide 23: Cryogen-free test stand
18 T by 4 stack at 2 kA, 12 K
stack of 4 NI HTS coils with
connectors
HTS leads
1st cryocooler
4 K coldhead
2nd cryocooler
radiation shield
top plate
Central bore field [T]

## Slide 24: Electromagnet/thermal simulation
2D axisymmetric -formulation,
homogenized winding pack,
Anisotropic resistivity matrix with off-diagonal terms
to account for the spiral nature of the coils [1]
+2D thermal
+ Lumped thermal network
[1] R Mateira, DOI 10.1088/1361-6668/ab9688

## Slide 25: Predicted obtainable field strongly depends on thermal aspects
17 T reachable*, but magnet at risk of quenching during failure
*Not considering mechanical
[K]
1200 A nominal

## Slide 26: Buffer sizing
Slow ramp-down
Quench
Buffer size (220kg Pb) chosen by parametric study