## Slide 1: High Field Magnet Roadmap at PSI/CHART
Douglas Araujo1, Bernhard Auchmann1,2, Andre Brem1, Michal Duda1, Jaap Kosse1, Thomas Michlmayr1, Colin Müller1, Henrique Garcia1, Dmitry Sotnikov1, Anna Stampfli1, J. Van den Eijnden 1, and Ariel Haziot2
1Paul Scherrer Institute 2CERN
This work was performed under the auspices and with support from the Swiss Accelerator Research and Technology (CHART) program.
SPS Annual Meeting, Zürich, September 2024
Roadmap overview and progress report

## Slide 2
Agenda
High Field Magnets
Roadmap
Progress
High Temperature
Superconductors
Coming soon…

## Slide 3: High Field Magnets
https://indico.cern.ch/event/1298458/timetable/
MagDev
https://www.psi.ch/en/cas/chart-magdev

## Slide 4: Roadmap | CHART Environment
MagRes: resins
WireChar: conductor
MagComp: mechanics
MagAM: 3D printing
MagNum: numerics
J. Ferchow
P. Müller
X. Kong
C. Senatore
A. Brem
M. Maciejewski
https://chart.ch/chart-projects/

## Slide 5: Roadmap | R&D Vehicles small samples
BOX and cBOX
Big
BOX
Sub scale SMCC
SMACC 13 T
11 T background field
Assessing training and degradation
Multi turn
9 T background field, assessing
training and degradation

## Slide 6: Standard BOX – addressing training in Nb3Sn
Solenoid
Conductor
I
Fin
Fout
evaluate impregnation systems
22 samples tested in the last 3 years
Courtesy, S. Olten et al.

## Slide 7: Compression BOX – degradation due to stress
9.4 T
evaluate impregnation systems
reversible and irreversible degradation in external field
6 samples tested, 2 currently under testing
Courtesy, S. Olten et al.

## Slide 8: BigBOX: multi turn Nb3Sn coil
Assessing coil performance
  Superconductor margin
  Conductor degradation
  Coil training behaviour
Validating technologies
  Preload free coil
  Interface conditions
  Wax and filled wax impregnated coils
  Stress-management
  Ceramic Insulation Coating
DCC17
Magnet
BigBOX inside DCC17
Cross-section illustration
Test Results: 6 times power-up to short sample limit without training behavior
BigBOX2 (impregnated with filled-wax )was manufactured, delivered to BNL and it is waiting to be tested
Courtesy, M. Kumar et al.

## Slide 9: Subscale SMCC | Concept
4 common-coils, coil-pack assembly and splice region
Outer pads
End pads
Cable manufactured
by LBNL

## Slide 10: Subscale SMCC | Innovations
Stress-Management
Common-Coils Former
Winding Technique
Former Coating
Instrumentation routing
First stand alone impregnated with
Filled Wax system to be tested
Impregnation Technique
Re-use of tooling through winding,
reaction and impregnation
2 coils reacted at CERN, SMT Section
2 coils reacted at PSI

## Slide 11
Performance | 22 | mm |  |  | 
T = 4.5 K | iss = 9.0 kA | imax = 8.85 kA | B0 = 4.9 T | Bpeak = 6.04 T | Imax/iss = 0.98
T = 1.9 K | iss = 10.0 kA | imax = 9.39 kA | B0 = 5.2 T | Bpeak = 6.41 T | Imax/iss = 0.94
Quench number
Courtesy, G. Willering et al.

## Slide 12: HTS Challenges and Opportunities
HTS technology
HTS coil manufacturing
Modelling
HTS cable models
HFM concepts
sensitive to mechanical strain
sensitive to thermal load
HTS tape operation
Noise cancellation and Protection
Modelling validation
FEM software for electro-magnetics
postprocessing measured data
AC losses prediction
Soldered stack based - HTS cable
14 T at 20 K
16 T at 20 K
Illustration from
Little beast engineering

## Slide 13: Production and measurements
Single tape
Pancake coils
Validation (w/ U. Twente)
Results:
48 measurements done in LN2
Co-wound coil works for protection
Signal recorded to 1 uV
Several samples of pancake production:
1 single tape pancake
2 double-tape stack pancake
1 single tape double pancake
Bending and twisting of tape:
Set of bending experiments showed degradation of HTS tapes
Twisting on 15-mm former for double pancake with 4-mm twist pitch (tape width)
Coil voltage validation
Criteria for validation:
Voltage on coil (done)
AC losses (ongoing)
Magnetic field (ongoing)

## Slide 14: Modelling
HTS cable
14 T HTS dipole
16 T HTS dipole
Comsol
Quanscient
HTS straight soldered stack cable has several benefits:
Shape fits to racetrack design
Fits to Block-coil and Common coil
Highest packing factor
Highest oriented critical current
Little Beast collaboration
Type: Block coil
Target field: 14 T
Temperature: 20 K
Goal: comparison with LTS projects
AC losses optimization
Type: Block coil
Target field: 16 T
Temperature: 20 K
Goal: getting AC losses prediction with different computation software
Courtesy J. van Nugteren

## Slide 15
Coming soon…
LTS and HTS samples for testing new impregnation systems, AC losses study and modelling validation
2024: LTS subSMCC2: testing new protection systems that could be suitable for both LTS and HTS
2025: HTS subSMCC3: insulated ReBCO - based cable
2025: SMACC: 13 T demonstrator with field quality