## Slide 1
Shideh Davarpanah
Supervisor: Prof. Dr. Teresa Montaruli
Radiation Hardness and Annealing Strategies
for SiPMs of the Terzina Telescope
on board the NUSES space mission
Swiss Physical Society
Annual Meeting 2024

## Slide 2
THE NUSES SPACE MISSION
1/10
Neutrino and Seismic Electromagnetic Signals
to limb
ZIRÈ
TERZINA
S. Davarpanah
3 years mission
launch in mid-2026
Low Earth Orbit - 535 km
sun-synchronous
Technology pathfinder for New processing, Low power, High speed electronics of novel silicon photosensors and radiation hardness
ZIRÈ
Calorimeter - Low Energy fluxes
TERZINA
1st observation of Cherenkov light
emitted by atmospheric showers from
space!
Université de Genève

## Slide 3
TERZINA DETECTOR
Schmidt–Cassegrain Telescope
2 x 5 = 10 tiles (each tile: 24.9 x 24.9 mm2)
each 8 x 8 pixels (each pixel: 3 x 3 mm2)
sensitive area for each pixel = 6.58 mm2
full camera size : 120 x 48 mm2
S. Davarpanah
2/10
Martina D’Arco (talk on Friday)
Terzina Telescope: Pioneering the Detection of Cherenkov Light from Extensive Air Showers in Space
Université de Genève
~ 430 mm
~ 450 mm

## Slide 4
SiPM SPECIFICATION
S. Davarpanah
3/10
Université de Genève
FBK SiPM, 30 µm cell size, 3x3 mm2
Photon Detection Efficiency
Waveform sample for different bias voltages
Clear separation between amplitudes corresponding to the different number of photoelectrons

## Slide 5
No atmospheric shield
S. Davarpanah
Background radiation
e
p
Energy loss
Absorption
Multiple Scattering
Radiation damage
Sensor noise
Image quality
Energy threshold
Flux from SPENVIS
trapped electrons, trapped protons, solar protons
RADIATION BACKGROUND AT THE NUSES ORBIT
4/10
Université de Genève

## Slide 6
Silicon lattice before irradiation
Radiation damage (displacement, non-ionizing dose)
Silicon lattice after irradiation (radiation hardness)
Silicon lattice after annealing
RADIATION DAMAGE AND ANNEALING
Radiation damage increase the Dark Count Rate
Mitigation: by heating them; measuring efficiency of treatment at temperature comparable to the power consumption
S. Davarpanah
expected radiation background
5/10
Université de Genève

## Slide 7
ELECTRON AND PROTON IRRADIATION CAMPAIGN
Proton irradiation: 50MeV proton beam
Electron irradiation: β-source strontium-90, up to 2.2MeV
FBK NUV-HD_MT ( 3x3 mm2, 30um cell size )
Realistic simulation with Geant4 gives us Non-ionizing dose
Dark Count Rate
SiPM response to the irradiation
+
non-ionizing dose
+
SiPM specification
S. Davarpanah
IV measurement during irradiation
6/10
Université de Genève

## Slide 8
BACKGROUND MEASURMENT RESULTS
S. Davarpanah
Inferred DCR per pixel for Terzina SiPMs sensitive area from IV measurement during the irradiation
Electrons cause at least two orders of magnitude smaller change in the DCR compared to protons, despite the much higher fluence of trapped electrons
7/10
Université de Genève

## Slide 9
Annealing model
Conclusion:
  at T > 50°C
  annealing cycle ~ 84 hours
  recovery up to 40%
ANNEALING CYCLE
S. Davarpanah
Placing the devices in a climatic chamber
at fixed temperature for a set period of time
8/10
Université de Genève

## Slide 10
SUMMARY AND CONCLUSION
S. Davarpanah
Terzina at LEO of 535 km
Irradiation of SiPMs and radiation damage
Higher fluence of trapped electrons, especially low-energy electrons
Protons cause at more change in the DCR compared to electrons
Annealing model
This information allows us to adjust the trigger energy threshold throughout the 3-year mission to optimize the observation of Cherenkov signals, ensuring the best signal-to-noise ratio.
9/10
Université de Genève

## Slide 11
ACKNOWLEDGMENT
Prof. Dr. Teresa Montaruli
Dr. Matthieu Heller
Dr. Leonid Burmistrov
Dr. Caterina Trimarelli
Dr. Christoph Toennis
Martina D'Arco
10/10
Université de Genève
S. Davarpanah

## Slide 12
thank you for your attention!
S
Swiss Physical Society
Annual Meeting 2024
Shideh Davarpanah
Supervisor: Prof. Dr. Teresa Montaruli