## Slide 1: Influence of Oxygen Source on the High Magnetic Field Behavior of Nb3Sn Wires Manufactured via Internal Oxidation
Department of Quantum Matter Physics, University of Geneva, Switzerland
Department of Nuclear and Particle Physics, University of Geneva, Switzerland
Gianmarco BOVONE, Florin BUTA, Francesco LONARDO, Marco BONURA, and Carmine SENATORE
Simon C. HOPKINS and Thierry BOUTBOUL
CERN, Switzerland
Camelia N. BORCA and Thomas Huthwelker
PSI, Phoenix Beamline, Switzerland
David LeBoeuf and Xavier Chaud
CNRS - LNCMI Grenoble, France

## Slide 2
Outline
Why low temperature superconductors have still their word to say!
The internal oxidation process
Enhancement of Nb3Sn superconducting properties
High magnetic field measurements (done and to do)
Morphological overview of Nb3Sn and precipitates
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
1

## Slide 3
Magnetic field for material research and materials for high-magnetic fields
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
2
OK, maybe not so soon!
- Wilson M. N. IEEE TAS (2012) 22 3
- Finnemore D. K. et al. Physical Review 118 1 (1960)
“The solution of the problem of obtaining a field of 100000 Gauss (10 T) could then be obtained by a coil of say 30 cm in diameter and the cooling with a plant which could be realized in Leiden with a relatively modest financial support”
H. K. Onnes, 3rd International Congress on Refrigeration (1913)
Discovery of superconductivity in 1911
Heike Kamerlingh Onnes
Superconductivity will make possible high-field magnets soon!
Notes: Cambia imagine tape

## Slide 4
Nb3Sn: an old material still to be unraveled
- Matthias B. T. et al. Physical Review 95.6 (1954): 1435.
- Rosner H. et al. IEEE-CSC ESAS Eur. Supercond. News Forum. No. 9. (2012)
- Barzi E and Zlobin A.V. Nb3Sn Wires and Cables for High-Field Accelerator Magnets(2019)
First Nb3Sn magnet to generate 10 T (1963)
Superconducting properties discovered in 1954
Nb or Ta barrier
NbTa filaments
Cu
Bronze wire
Cu
Magnet, fabricated and tested by: L. Martin, C. Bruch, M. Benz and C. Rosner (left to right)
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
Initially fabricated as tape
Rod-type wire manufacturing process (e.g. RRP)

## Slide 5
The Niobium-Titanium alloy (Nb-Ti) was discovered to be a superconductor in 1965, two years after the first Nb3Sn magnet operating at 10 T
Since then, Nb-Ti is the backbone of MRI magnets
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
4
Nb-Ti has lower properties compared to Nb₃Sn, but is easier to wind and manufacture
Nb-Ti is and alloy, ductile
Nb₃Sn is an intermetallic compound, brittle
The dominion of Low Temperature Superconductors
Notes: LTS dominates applications… menzionare duttile e brittle
Grafico performance NbTi – Nb3Sn

## Slide 6
LHC dipole magnet
Fabricated using NbTi wires
Fabricated using Nb3Sn wires
LHC had to be updated using Nb3Sn magnets to have a higher beam focus and enhance the number of collisions
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
5
The dominion of Low Temperature Superconductors
Hi Luminosity LHC quadrupole magnet
Notes: Ripensare un po a sta slide…

## Slide 7
The future of Nb3Sn
FCC-hh
100 km, 16 T
100 TeV (c.o.m.)
~10’000 tons Nb3Sn
LHC
27 km, 8.33 T
14 TeV (c.o.m.)
1’300 tons NbTi
Doubling the operating current density reduces the superconductor area to one-third!
B [T] | 16
Jop [A/mm2] | 300
w [mm] | 76
Acoil [mm2] | 20’000
16
600
38
7’000
2x
How to enhance the Jc of Nb3Sn?
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
6
- Parrell et al. AIP Conf. Proc. 711 (2004) 369
- Boutboul et al., IEEE TASC 19 (2009) 2564

## Slide 8
The pinning mechanism in Nb₃Sn is due to grain boundary pinning, and grain refinement can enhance Jc
Movement of flux lines causes dissipation, detrimental for power applications. The flux line lattice must remain pinned to pinning centers (e.g., grain boundaries, or defects)
Higher the pinning force, higher the critical current density
Grain refinement induced by ZrO2 precipitation
The process is called Internal Oxidation
Nanometrical control of Nb3Sn grains
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
7

## Slide 9
Internal oxidation process
Cu
During heat treatment, grains continue to grow and join together when their boundaries are in contact
Nb or Ta barrier
NbTa with ternary element (Zr or Hf)
Cu
What happens during heat treatment
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
8

## Slide 10
Internal oxidation process
First proposed in 1968 for tape samples due to the easier introduction of oxygen. It was “impossible” to implement in round conductors: oxygen in alloy is detrimental to wire deformation
Oxygen reacts with the third element (with a higher affinity for oxidation)
The first wire with internal oxidation was fabricated in 2014, using a separate oxygen source to allow wire deformation
ZrO₂ (or HfO₂) nanoparticles prevent grains from joining together, keeping the grain size small
- Benz M. G. Transaction of the Metal. Soc. of AIME 242 (1968)
- Xu X. et al. Applied Physics Letters 104.8 (2014): 082602)
Nb or Ta barrier
NbTa with ternary element (Zr or Hf)
Cu
What happens during heat treatment
Oxygen
Oxide
Low performances at high field
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
8

## Slide 11
Evolution of layer Jc at high magnetic field
New wires designs
Multifilamentary wires
Introduction of Ta in Nb alloy
Enhancement of Jc, Fp (max) and Bc2
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
9

## Slide 12
Simplified multifilamentary wires layout and fabrication process
Oxide powder inside the Nb-alloy filaments
Oxide powder between the Nb-alloy filament and the copper jacket
AnnularOS
CoreOS
Ta Barrier
Cu OFE
Nb filaments in Cu jacket
Sn core in Cu jacket
Alloys:
Nb, 7.5%wt Ta
Nb, 7.5% wt Ta, 1% wt Zr
Nb, 7.5% wt Ta, 2% wt Hf
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
10

## Slide 13
Effects of the internal oxidation on the superconducting properties
Bovone G. et al. Superconductor Science and Technology 36.9 (2023): 095018.
Layer Jc above FCC target of 2500 A/mm2, at 4.2 K and 16 T
The FCC target for layer Jc is calculated based on the area fraction of reacted Nb₃Sn in a typical rod-type wire
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
11

## Slide 14
High magnetic field measurements
High-field measurements were performed at the Laboratoire National des Champs Magnétiques Intenses (LNCMI) in Grenoble
Bc₂ results at low magnetic fields overlap with measurements in Geneva, but high-field results are higher than extrapolated values
Magnetic field in Geneva limited to 19 T
1
2
3
4
Thermometer 1
Thermometer 2
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
12
WHH Model

## Slide 15
Nb alloy | Bc2 (T) 4.2 K, 99 % R no-OS | Bc2 (T) 4.2 K, 99 % R Core-OS | Bc2 (T) 4.2 K, 99 % R Annular-OS
Nb 7.5%wt Ta 1%wt Zr | 28.0  0.60 | 28.97  0.38 | 29.20  0.38
Nb 7.5%wt Ta 1%wt Hf | 28.9  0.56 | 29.0  0.36 | 29.32  0.36
Nb 7.5%wt Ta | 28.01  0.85 | N/A | 
T = 4.2 K
Bc2 enhancement
Very high Bc2 values measured for samples with internal oxidation
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
13
Notes: Qualche foto della probe

## Slide 16
Pinning mechanism
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
14
M(H) loop from VSM SQUID in the temperature range 4.2 -14 K and Bc2 from R(B) (1 % criteria)
pinning force FP
magnetic field B
Additional of artificial pinning centers i.e. modify the pinning mechanism
0.2
Grain boundary pinning
0.33
Point defect pinning
Modification of pinning mechanism when an oxygen source is added in presence of Hf and Zr
Increase the grain boundary density i.e. refine the grain size
Grain boundary pinning
Point defect pinning
Notes: Qualche foto della probe

## Slide 17
What drives the enhancement?
Nb3Sn grain size reduction induced by precipitates (HfO2)
100 nm
Hf-noOS
100 nm
Hf-annularOS
110 nm
45 nm
Bovone G, et al. Superconductor Science and Technology 36.9 (2023): 095018
Modification of the pinning mechanism
Enhancement of Bc2
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
15
Jc enhancement due to precipitated oxides
Notes: Rivedere animazioni line Fp

## Slide 18
Zr L3 edge
SnO2
O diffusion
direction
Nb3Sn reaction layer
5
1
Zr – coreOS
ZrO2–like spectrum found only in Nb3Sn! Different Zr spectrum in residual alloy, despite oxygen diffusion
Two peak fingerprint suppressed
XANES investigation on precipitates
Bovone G et al. IEEE Transactions on Applied Superconductivity 34.3 (2024),6000205.
Atomic specific technique, sensitive to the chemistry and to crystal environment
Investigation of Zr spectrum in different region of the reacted (and unreacted) wires
Phoenix Beamline
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
16
Notes: Logo nuovo PSI

## Slide 19
What did we learn from XANES?
Zr in Nb3Sn is fully oxidised to ZrO2
Zr in the residual alloy is not in the form of ZrO₂, but changes in the spectra suggest modifications induced by oxygen diffusion. Clusters?
ZrO₂ precipitates due to the lower solubility of Zr and O in Nb₃Sn compared to Nb
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
17
Notes: Aggiungere una slide di summary su XAS

## Slide 20
Precipitates at the interface
Uniform distribution of ZrO2 precipitates
No observable precipitates and no ZrO₂ fingerprint from XAS. However, Zr-O clusters may be present
Nb3Sn – residual alloy interface
Residual alloy
Nb3Sn
Hall, Ernest L., et al. MRS Online Proceedings Library (OPL) 205 (1990).
Courtesy of Stephan Pfeiffer, CERN
No observable ZrO₂ in the Nb₃Sn area next to the residual alloy interface. Are the precipitates too small to be detected with the microscope used?
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
18
Notes: Se non ci sto con I tempi taglio

## Slide 21
50 µm
50 µm
Drastic reduction of Nb3Sn layer thickness when OS is added
Heat treatment (HT):
550°C × 100 h + 650°C × 200 h
Higher temperature to enlarge Nb3Sn layer thickness keeping grain size low
Heat treatment optimization:
reaction layer thickness
Significant increase of layer thickness at 700 °C
No OS
With OS
50 µm
50 µm
700 °C × 50 h
700 °C × 100 h
With OS
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
19
Notes: Scrivere del fit usato con formula

## Slide 22
50 µm
50 µm
Drastic reduction of Nb3Sn layer thickness when OS is added
Heat treatment (HT):
550°C × 100 h + 650°C × 200 h
Heat treatment optimization:
reaction layer thickness
Significant increase of layer thickness at 700 °C
No OS
With OS
50 µm
50 µm
700 °C × 50 h
700 °C × 100 h
With OS
Significant increase of layer thickness at 700 °C, but modest grain growth
52 nm
56 nm
58 nm
150 nm
110 nm
Higher temperature to enlarge Nb3Sn layer thickness keeping grain size low
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
19

## Slide 23
Criterion 0.1 µV cm−1
Lonardo F. et al. IEEE Transactions on Applied Superconductivity 34.5 (2024), 6000305
Heat treatment optimization:
layer-Jc
Why Jc is lower despite the small grain size?
Fp (max) shift to 0.2 when HT at 700°C
Lower interaction between flux lines and precipitates due to size mismatch
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
20
Notes: Cambiare spiegazione

## Slide 24
Problems in pinning mechanism analysis
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
21
To determine the pinning mechanism, we need to precisely locate the position of the Fp peak in the reduced field (b)
Notes: Mettere le istereresi per far capire meglio il discorso.

## Slide 25
Problems in pinning mechanism analysis
New campaign for VSM measurements up to 30 T at EMFL in Nijmegen
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
21
To determine the pinning mechanism, we need to precisely locate the position of the Fp peak in the reduced field (b)
At high temperature the hysteresis loop closes (Bc2)
At 4.2 K the loop doesn’t close. We need to extrapolate
Or use Bc2 values measured with different techniques
Notes: Mettere le istereresi per far capire meglio il discorso.

## Slide 26
Conclusions
We successfully enhanced the layer Jc above the FCC specifications, record-high Bc2 and change of pinning mechanism (point defect) when Oxygen Source is present, for wires reacted at 650 °C
X-Rays Absorption Near Edge Structure (XANES) on Nb3Sn wires with and without OS show the presence of ZrO2 only in the Nb3Sn layer and not in the unreacted alloy
The layer Jc (16 T, 4.2 K) is strongly enhanced by the shift of Fp(max) to a higher magnetic field, due to Bc2 enhancement and/or a modified pinning mechanism
Internal oxidation is the most effective way to reduce grain size, enhance Bc2 and modify the pinning mechanism
Despite its “age”, Nb3Sn can still play a role in the future generation of high magnetic field magnets
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
22

## Slide 27
Thank you for your attention

## Slide 28
But are precipitates necessary?
Precipitates reduce Nb₃Sn grain size through the Zener drag effect
Some groups observed grain refinement without the addition of an oxygen source
Maximum Nb3Sn grain radius
precipitates radius
precipitates volumetric fraction
Is the refinement observed here enough to reach the FCC target?
- Bovone G et al. IEEE Transactions on Applied Superconductivity 34.3 (2024),6000205.
- Xu X et al. Scripta Materialia 186 (2020): 317-320.
- Asai K et al. IEEE Transactions on Applied Superconductivity 34.5 (2024), 8600105
- Balachandran S et al. Journal of Alloys and Compounds 984 (2024): 173985.
100 nm
Hf-noOS
100 nm
Hf-annularOS
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
21

## Slide 29
How to reach the FCC target
- Bovone G et al. Superconductor Science and Technology 36.9 (2023): 095018
- Lonardo F et al. IEEE Transactions on Applied Superconductivity (2024).
- Xu X et al. Scripta Materialia 186 (2020): 317-320.
- Xu X et al. arXiv preprint arXiv:1411.5397 (2014)
Samples that overcome the FCC target
- Godeke A. Superconductor Science and Technology 19.8 (2006): R68.
- Fischer C. Master’s Thesis Univ. of Wisconsin-Madison (2002).
- Balachandran S et al. Superconductor Science and Technology 32.4 (2019): 044006.
Not only grain refinement enhance the layer Jc (16 T, 4.2 K)
Samples with internal oxidation below FCC target
Shift of Fp(max) towards higher field largely enhance the layer Jc
Refinement window with only Hf addition
Bc2 value and pinning mechanism play a role in the enhancement of Jc (16 T, 4.2 K)
FCC target
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
22

## Slide 30
Combined behavior
The FCC target at 16 T and 4.2 K is reached when both grain size is refined and Fp(max) is shifted at higher magnetic field
- Balachandran S et al. Superconductor Science and Technology 32.4 (2019): 044006.
- Xu X et al. Scripta Materialia 186 (2020): 317-320..
- Fischer C. Master’s Thesis Univ. of Wisconsin-Madison (2002).
- Bovone G et al. Superconductor Science and Technology 36.9 (2023): 095018
- Lonardo F et al. IEEE Transactions on Applied Superconductivity 34.5 (2024), 6000305
- Xu X et al. arXiv preprint arXiv:1411.5397 (2014).
Internal oxidation is fundamental to reach the FCC target due to grain refinement, Bc2 enhancement, and modification of pinning mechanism
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
3
FACULTY OF SCIENCES
DEPARTMENT OF QUANTUM MATTER PHYSICS
23