## Slide 1
Uranium Carbide Material Developments
at CERN-ISOLDE
Alexander Gottberg

## Slide 2
Actinide Targets Online
Actinide targets in 2010 (2009)
244 shifts out of 350  72% (282  over 60% of total)
12 new and 2 old units (12 new)
Numbers from M. Kowalska

## Slide 3: Actinide Targets Online
Numbers from M. Kowalska
Actinide targets in 2010 (2009)
244 shifts out of 350  72% (282  over 60% of total)
12 new and 2 old units (12 new)

## Slide 4: Material Production
Production Process:
Blending UO2 and carbon powder
Cold pressing into pills
Carbothermal reduction of UO2
      UO2 + 6C → UC2 + 2C + 2CO(g)
conventional UC pills used at ISOLDE, 3.5g/cm3, grain size 3 μm to 50 μm, high porosity

## Slide 5: Current UCx at ISOLDE
bulk= 3.5 g/cm3
L. Biasetto et al.

## Slide 6: ActiLab in FP7-ENSAR

## Slide 7: ActiLab in FP7-ENSAR
Task 1: Synthesis of new actinide targets (CERN, INFN, IPNO)
Subtask 1: Sol-gel synthesis in complex fluids
Subtask 2: Nanostructures
Task 2: Characterization of actinide targets (CERN, INFN)
Subtask 1: Microstructure, porosity, specific surface, crystalline phase
Subtask 2: Emissivity, thermal conductivity at high temperature
Task 3: Actinide targets properties after irradiation (CERN, PSI)
Subtask 1: Post-irradiation examination of target prototypes
Task 4: Online tests of actinide targets (CERN, GANIL, IPNO)
Subtask 1: Impact of pulse time structure on release and ageing properties
Subtask 2: Analysis of the results-effusion and diffusion phenomena

## Slide 8: High Density UC Target at CERN
Importation from Russia of HD-UC pellets to CERN & online tests in Nov. 2010:
Set 1: 100 pills
UC (235U:0.38%), 13.2mm diam., 1mm thick, 12.3g/cm3, avg. grain 10 m , UC2<4%
Set 2: 300 pills
UC (235U:0.38%), 13.2mm diam., 1mm thick, 12.7g/cm3, avg. grain 6 m , UC2<4%

## Slide 9: Yields from HD UC
Comparable absolute yields (Gatchina 91g/cm2, conventional ISOLDE ≈45g/cm2)
HD absolute yields @ ISOLDE (241g/cm2) x2 to x10 lower than from conventional UC targets
[1] V. N. Panteleev, et al.,
Eur. Phys. J. A 42,
495-501 (2009)

## Slide 10: Micro Spot Material Mapping at SLS
Beamline X05LA @ SLS, PSI offers: hn= 5 – 20 keV, DE/E=210-4, 1 x 1 µm2
XRD
XFS
X-ray absorption fine structure (XAFS, NEXAFS, EXAFS)

## Slide 11: Micro Spot Material Mapping at SLS
Fluorescence
EXAFS
Results from first X-ray absorption experiments on UC
Beamline X05LA @ SLS, PSI offers: hn= 5 – 20 keV, DE/E=210-4, 1 x 1 µm2
XRD
XFS
X-ray absorption fine structure (XAFS, NEXAFS, EXAFS)

## Slide 12: Team and Collaboration
Team:
Richard Catherall
Thierry Stora
Tim Giles
Pekka Suominen
João Pedro Ramos
Christoph Seiffert
Bernard Crepieux
Gunvor Koldste
Marc Guichard
Thanks to:
Daniel Grolimund (PSI)
Claude Degueldre (PSI)
Ines Günther-Leopold (PSI)
Daniel Stracener (ORNL)
Vladimir Panteleev (PNPI)
Stefano Sgobba (EN-MME)
Yorick Blumenfeld
Magdalena Kowalska

## Slide 13: Some first results
Follow up:
Simulation tests
Advance sample preparation
Using post-irradiated UCx pellets
Beamtime and Actinet request for 2012

## Slide 14: Some first results
Peter Kunz: First UCx Target Run at TRIUMF
UC2+x
sintered UCx/C on exfoilated graphite
target thickness 15g/cm2
IProton = 2μA (license limit)
TTarget= 1950˚C
Close to ISOLDE process:
Carbothermal reduction of UO2
Fabrication of target disks (under inert gas atmosphere)
Conditioning / Sintering of target material
UCx after carbonization procedure
(step 1)
Sintered UCx on targe disc
(step 3)
10mm

## Slide 15: Yields from HD UC