## Slide 1
GRAiNITA: fine sampling crystal grain calorimetry
On Behalf of thr GRAiNITA Group:
IJCLab: S.Barsuk, I.Boyarintseva, D.Breton, S. Monteil, J.Lefrançois, MH.Schune;
ISMA: A.Boyarintsev, I.Tupitsyna,
LP-Clermont: H.Chanal, Y.Hou, M.Magne, S.Monteil, D.Picard, M.Yeresko;
TSNUK: O.Bezshyyko, A.Dubovik, A.Kotenko, N.Semkiv.
Giulia Hull,
Université Paris-Saclay, CNRS/IN2P3, IJCLab

## Slide 2
GRAiNITA: mix of scintillator grains soaked in a high-density liquid
GRAiNITA concept
Shashlik calorimeter: alterning layers of scintillator and absorber
is expected
Inspired by LiquidO technique for neutrino detector
(A. Cabrera et al. LiquidO Commun Phys 4, 273 (2021) )
High granularity
Modest energy resolution
High granularity
Good energy resolution

## Slide 3
GRAiNITA prototype: the “Troll”
Development of two medium-size GRAiNITA prototypes, employing respectivement BGO and ZnWO4 grains and equipped with 16 WLS fibres and SiPMs for the read-out of the scintillation light
ZnWO4
LY= 10 000 ph/MeV
Zeff=61
Density 7.62 g/cm3
n=2.1-2.3
𝜏 = 20 𝜇s
= 490 nm
Bi4Ge3O12 (BGO)
LY= 10 000 ph/MeV
Zeff=74
Density 7.13 g/cm3
n=2.1
𝜏 = 300 ns
= 480 nm

## Slide 4
GRAiNITA cosmic rays test-bench
16 WLS fibers coupled to 16 SiPMs plugged on a PCB to amplify the signals
Two 8-ch WaveCatchers for the signal readout
Since ZnWO4 has a long decay time τ≈20 μs, a special program has been implemented allowing to count the number of the single phe pulses on a time scale of 25 μs
Before and after each run with cosmic rays, we acquire 1000 ev. illuminating the grain volume with the green LED
Volume filled with:
Air
ZnWO4
ZnWO4 + water
ZnWO4 + ethylene glycol

## Slide 5
Light yield
Ignored in the fit
LY = O(400phe/40MeV)
10000 phe/GeV
 statistical contribution = 1% for 1 GeV high energy photon
Can be improved as the fiber ends are not covered with reflector
Registered signals from cosmic rays
Peut être amélioré car les extrémités des fibres ne sont pas recouvertes de réflecteur
20-25% more light when we add liquide

## Slide 6
Light confinement
Green LED light injected in the center of the prototype
Ratio between the sum of the signal in the 4 central channels and the total
Using just grains in the volume the scintillation light is more confined, this confinement decreases adding liquid with increasing refractive index
16 WLS fibers
Top view
Green LED
Sum of the signals in the 16 channels

## Slide 7
At present: the constant term
Non-uniformities and escaping energies are among the sources of energy resolution degradation  muon test beam and simulation
Accurate (1mm at 15 cm) knowledge of the muon trajectory in the prototype thanks to a Si telescope prototype(TPX3)
Aim at measuring the response of the GRAiNITA prototype as a function of the actual (length) passage of the particle, the distance to the fibre etc…
Start to address the non-uniformities
To be used further in muon test beam
Test beam (hopefully) before the summer

## Slide 8
For the future: the GRAiNITA Demontrator
We are working at the proposal for the funding request
Full size demonstrator: 17cm x 17 cm x 40 cm:
45 kg ZnWO4 grains, heavy liquid, 576 fibers, 36 SiPMs
Study of the PSD discrimination capability