## Slide 1: SC steady magnet concept and design studies
1 INFN – Genova, 2 Università degli Studi di Genova, 3 CERN, 4 Sapienza Università di Roma
T. Maiello1,2, L. Alfonso 1, A. Bersani1, L. Bottura3, B. Caiffi1, S. Fabbri3, S. Farinon1,
A. Gagno1,2 , D. Novelli1,4 , A. Pampaloni1

## Slide 2: Accelerator Superconducting Magnets
Main characteristics:
Open midplane dipole
10 T in the bore
Rectangular aperture 100 mm x 30 mm
Field quality: units in beam radius of 10 mm
Field homogeneity 1% in the good field region
Considerations:
HTS windings
High current density
Operation at high temperature
HTS cable properties | 
Bare height [mm] | 12.00
Bare width [mm] | 1.65
Insulation [mm] | 0.10
Number of tapes | 15
Fukjikura cable

## Slide 3: Field Quality and Homogeneity Evaluation
The field quality was evaluated in four harmonic coils with a radius 10mm in order to cover the affected portion of the aperture.
Field homogeneity was calculated in a rectangular area of 10mm height and 50mm width.
100 mm
mm
mm
mm
30 mm
30 mm
100 mm
10 mm

## Slide 4: CONFIGURATIONS
We have realized two 10 T configurations:
Configuration 1: the first one has a very good field quality but is more difficult to realize for mechanical reasons because the blocks are not aligned;
Configuration 2: the second one has two aligned racetracks but has a worse field quality.

## Slide 5: Configuration 1 @ 10 T
B [T]
100 mm
30 mm
1
2
3
A
B
Block no. | X [mm] right lower corner | Y [mm] right lower corner | No. of conductors | No. of tapes
1 | 142.6 | 20.0 | 40 | 600
2 | 150.0 | 42.2 | 39 | 585
3 | 106.4 | 71.4 | 31 | 465
Iron yoke | 
Radius [mm] | 300
A [mm] | (170.0; 103.6)
B [mm] | (34.1; 68.4)
Tot. Structure [k€/m] | 25.9
Tot. Assembly [k€/m] | 20.0
Tot. Conductor [k€/m] | 127.1
Tot. Cost [k€/m] | 173.0

## Slide 6: Configuration 1 @ 10 T
Operative temperature [K] | 17.5
Margin [K] | 2.5
Current [A] | 12130
Current density [A/mm2] | 537.44

## Slide 7: Configuration 1 @ 10 T
Chart: Odd harmonics
| 0 | 5 | 15 | 25
b3 | 1.4933 | 1.3769 | 0.19956 | -3.8646
b5 | -0.07554 | -0.08808 | -0.2164 | -0.65163
b7 | -0.00325 | -0.00384 | -0.00938 | -0.02529
Chart: Even harmonics
| 0 | 5 | 15 | 25
b2 | 0 | 1.4549 | 3.2997 | 0.40609
b4 | 0 | -0.15934 | -0.7091 | -2.2852
b6 | 0 | 0.01032 | -0.04648 | -0.14329

## Slide 8: Configuration 1 @ 10 T
Homogeneity (x=25mm) = 0.097%

## Slide 9: Configuration 1 @ 10 T
FL [N/m]
Block no. | Fx [kN/m] | Fy [kN/m]
1 | 1753 | 246
2 | 928 | -1433
3 | 2213 | -1288
TOTAL | 4893 | -2475
x
y
Preliminary concept: the mechanical structure we want to study consists of stainless steel containers to house racetracks. The sketch on the left is only an indication to understand the concept.

## Slide 10: Configuration 2 @ 10 T
100 mm
30 mm
1
2
3
A
B
Block no. | X [mm] right lower corner | Y [mm] right lower corner | No. of conductors | No. of tapes
1 | 146.0 | 20.0 | 40 | 600
2 | 146.0 | 42.2 | 40 | 600
3 | 106.4 | 71.4 | 31 | 465
Iron yoke | 
Radius [mm] | 300
A [mm] | (170.0; 103.6)
B [mm] | (34.1; 68.4)
Tot. Structure [k€/m] | 25.9
Tot. Assembly [k€/m] | 20.0
Tot. Conductor [k€/m] | 128.3
Tot. Cost [k€/m] | 174.2
B [T]

## Slide 11: Configuration 2 @ 10 T
Operative temperature [K] | 18.5
Margin [K] | 2.5
Current [A] | 12000
Current density [A/mm2] | 531.68

## Slide 12: Configuration 2 @ 10 T
Chart: Odd harmonics
| 0 | 5 | 15 | 25
b3 | -1.128 | -1.3 | -2.83 | -7.25
b5 | -0.1099 | -0.21 | -0.222 | -0.54
b7 | -0.0027 | -0.003 | -0.01 | -0.02
Chart: Even harmonics
| 0 | 5 | 15 | 25
b2 | 0 | -1.18 | -4.999 | -14.39
b4 | 0 | -0.23 | -0.866 | -2.29
b6 | 0 | -0.01 | -0.04 | -0.1

## Slide 13: Configuration 2 @ 10 T
Chart: Homogeneity
| 0 | 10 | 20 | 25 | 30 | 40 | 50
 | 0 | 0.025 | 0.074998 | 0.135 | 0.22495 | 0.61499 | 1.715
Homogeneity (x=25mm) = 0.13%

## Slide 14: Conclusions
We were able to find a solution for an open midplane dipole that generates 10T in the center with excellent homogeneity and good field quality.
There are simpler solutions for mechanics with good homogeneity but loosing in terms of field quality.

## Slide 15: Thank you for your attention!
1 INFN – Genova, 2 Università degli Studi di Genova, 3 CERN, 4 Sapienza Università di Roma
T. Maiello1,2, L. Alfonso 1, A. Bersani1, L. Bottura3, B. Caiffi1, S. Fabbri3, S. Farinon1,
A. Gagno1,2 , D. Novelli1,4 , A. Pampaloni1