## Slide 1: How to reduce hysteresis loss* in ReBCO based RCS super-ferric dipole magnets
Simon Otten, Anna Kario, Herman ten Kate
15th of May 2024
*in theory

## Slide 2: Presented at MuCOL annual meeting
Hysteresis loss calculations for two ReBCO designs for RCS fast-ramping dipoles
Values in the range 200-500 W/m-magnet at 15-40 K found, but heat is deposited at cold!
Is it acceptable? How to reduce it?
1. ReBCO magnet by FNAL
(H. Piekarz et al.)
2. ReBCO magnet using Unibo/CERN yoke design (Breschi et al.)

## Slide 3: What level of AC loss acceptable for energy saving?
Chart: Temperature [K]
| 1 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 | 120 | 130 | 140 | 150 | 160 | 170 | 180 | 190 | 200 | 210 | 220 | 230 | 240 | 250 | 260 | 270 | 280 | 290 | 300
P_res [W/m] | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000
P_max (ideal cooling) [W/m] | 6.6666 | 66.6664 | 133.3329 | 199.9993 | 266.6658 | 333.3322 | 399.9987 | 466.6651 | 533.3316 | 599.998 | 666.6644 | 733.3309 | 799.9973 | 866.6638 | 933.3302 | 999.9967 | 1066.6631 | 1133.3296 | 1199.996 | 1266.6624 | 1333.3289 | 1399.9953 | 1466.6618 | 1533.3282 | 1599.9947 | 1666.6611 | 1733.3276 | 1799.994 | 1866.6604 | 1933.3269 | 1999.9933
P_max (realistic cooling) | 1.9093 | 19.5121 | 39.9999 | 61.5382 | 84.2102 | 108.1077 | 133.3328 | 159.9994 | 188.2345 | 218.1809 | 249.9989 | 283.8697 | 319.9985 | 358.619 | 399.998 | 444.4421 | 492.305 | 543.997 | 599.9965 | 660.8655 | 727.2681 | 799.9947 | 879.9938 | 968.4139 | 1066.6584 | 1176.4609 | 1299.9886 | 1439.9866 | 1599.984 | 1784.5962 | 1999.9767
Chart: Temperature [K]
| 1 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 | 120 | 130 | 140 | 150 | 160 | 170 | 180 | 190 | 200 | 210 | 220 | 230 | 240 | 250 | 260 | 270 | 280 | 290 | 300
P_res [W/m] | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000
P_max (ideal cooling) [W/m] | 6.6666 | 66.6664 | 133.3329 | 199.9993 | 266.6658 | 333.3322 | 399.9987 | 466.6651 | 533.3316 | 599.998 | 666.6644 | 733.3309 | 799.9973 | 866.6638 | 933.3302 | 999.9967 | 1066.6631 | 1133.3296 | 1199.996 | 1266.6624 | 1333.3289 | 1399.9953 | 1466.6618 | 1533.3282 | 1599.9947 | 1666.6611 | 1733.3276 | 1799.994 | 1866.6604 | 1933.3269 | 1999.9933
P_max (realistic cooling) | 1.9093 | 19.5121 | 39.9999 | 61.5382 | 84.2102 | 108.1077 | 133.3328 | 159.9994 | 188.2345 | 218.1809 | 249.9989 | 283.8697 | 319.9985 | 358.619 | 399.998 | 444.4421 | 492.305 | 543.997 | 599.9965 | 660.8655 | 727.2681 | 799.9947 | 879.9938 | 968.4139 | 1066.6584 | 1176.4609 | 1299.9886 | 1439.9866 | 1599.984 | 1784.5962 | 1999.9767
Conductor loss for resistive Cu option
Maximum cryogenic heat load with ideal cooling
Maximum cryogenic heat load with more realistic cooling
Initial AC loss calculations
Hysteresis AC loss has to be reduced by an order of magnitude at least.

## Slide 4: Hysteresis loss in a single tape
Chart: Magnetic field amplitude [T]
| 1E-3 | 1.2589254117941701E-3 | 1.58489319246111E-3 | 1.9952623149688798E-3 | 2.5118864315095799E-3 | 3.1622776601683798E-3 | 3.9810717055349699E-3 | 5.0118723362727298E-3 | 6.3095734448019303E-3 | 7.9432823472428103E-3 | 0.01 | 1.2589254117941699E-2 | 1.58489319246111E-2 | 1.9952623149688799E-2 | 2.5118864315095801E-2 | 3.1622776601683798E-2 | 3.9810717055349699E-2 | 5.0118723362727199E-2 | 6.3095734448019303E-2 | 7.9432823472428096E-2 | 0.1 | 0.12589254117941701 | 0.15848931924611101 | 0.199526231496888 | 0.25118864315095801 | 0.316227766016838 | 0.39810717055349698 | 0.50118723362727302 | 0.63095734448019303 | 0.79432823472428105 | 1 | 1.2589254117941699 | 1.58489319246111 | 1.99526231496888 | 2.5118864315095801 | 3.16227766016838 | 3.98107170553497 | 5.01187233627273 | 6.3095734448019298 | 7.9432823472428096 | 10
I = 0 A | 5.2684e-11 | 1.5211e-10 | 3.4221e-10 | 8.5397e-10 | 2.1659e-09 | 5.2618e-09 | 1.2712e-08 | 3.151e-08 | 7.6749e-08 | 1.866e-07 | 4.5521e-07 | 1.1105e-06 | 2.7095e-06 | 6.5972e-06 | 1.6054e-05 | 3.8991e-05 | 9.4542e-05 | 0.00022845 | 0.00054944 | 0.001312 | 0.0030994 | 0.0072071 | 0.016381 | 0.036042 | 0.07601 | 0.15185 | 0.28428 | 0.49654 | 0.80944 | 1.2397 | 1.8066 | 2.5351 | 3.4623 | 4.6411 | 6.1396 | 8.0353 | 10.4566 | 13.5076 | 17.4091 | 22.3652 | 28.6467
I = 100 A | 6.8058e-06 | 6.8001e-06 | 6.8124e-06 | 6.8577e-06 | 6.9828e-06 | 7.2921e-06 | 7.7271e-06 | 8.623e-06 | 1.0399e-05 | 1.2787e-05 | 1.6011e-05 | 2.1669e-05 | 3.2093e-05 | 4.7816e-05 | 7.6805e-05 | 0.00013026 | 0.00023153 | 0.00043543 | 0.00086319 | 0.0017864 | 0.0038178 | 0.0082794 | 0.01796 | 0.038356 | 0.079323 | 0.15638 | 0.29057 | 0.5047 | 0.81953 | 1.253 | 1.8229 | 2.5549 | 3.4855 | 4.6675 | 6.1687 | 8.0758 | 10.4978 | 13.5729 | 17.4776 | 22.4301 | 28.7189
I = 200 A | 9.8385e-05 | 9.8671e-05 | 9.9111e-05 | 9.9865e-05 | 0.00010095 | 0.00010244 | 0.00010438 | 0.00010687 | 0.0001113 | 0.00011959 | 0.0001333 | 0.00015226 | 0.00018546 | 0.00023693 | 0.00032433 | 0.00046549 | 0.00070442 | 0.0011164 | 0.0018687 | 0.0032776 | 0.0060248 | 0.011559 | 0.022788 | 0.045348 | 0.089203 | 0.1701 | 0.30885 | 0.52869 | 0.85037 | 1.2917 | 1.8704 | 2.6093 | 3.5433 | 4.7296 | 6.2361 | 8.1497 | 10.5817 | 13.6683 | 17.5874 | 22.5633 | 28.8776
I = 300 A | 0.00048118 | 0.00048216 | 0.00048333 | 0.0004853 | 0.00048782 | 0.00049112 | 0.00049535 | 0.00050144 | 0.00050972 | 0.00052554 | 0.00055589 | 0.0005986 | 0.0006636 | 0.00077547 | 0.00094917 | 0.0012277 | 0.0016863 | 0.002446 | 0.0037178 | 0.0059285 | 0.0098938 | 0.017202 | 0.030982 | 0.057114 | 0.1059 | 0.19301 | 0.33974 | 0.56895 | 0.90168 | 1.3558 | 1.9483 | 2.691 | 3.6307 | 4.824 | 6.3407 | 8.2681 | 10.7154 | 13.8244 | 17.7705 | 22.7804 | 29.1399
I = 400 A | 0.0015012 | 0.0015024 | 0.0015035 | 0.0015052 | 0.0015078 | 0.0015131 | 0.0015205 | 0.0015313 | 0.0015505 | 0.001579 | 0.0016238 | 0.0016976 | 0.0018126 | 0.001997 | 0.0022881 | 0.0027572 | 0.0035102 | 0.0047333 | 0.0067271 | 0.010046 | 0.015686 | 0.025464 | 0.042851 | 0.074037 | 0.12955 | 0.22558 | 0.38311 | 0.62552 | 0.97384 | 1.4455 | 2.0475 | 2.7957 | 3.7437 | 4.9483 | 6.4796 | 8.4258 | 10.8986 | 14.0376 | 18.0241 | 23.0821 | 29.5046
I = 500 A | 0.0036623 | 0.0036631 | 0.0036634 | 0.0036646 | 0.0036674 | 0.0036732 | 0.0036836 | 0.0037017 | 0.0037344 | 0.0037803 | 0.0038437 | 0.003954 | 0.0041344 | 0.0044038 | 0.0048459 | 0.0055532 | 0.0066726 | 0.0084603 | 0.011368 | 0.016082 | 0.023828 | 0.036783 | 0.058777 | 0.096412 | 0.16068 | 0.26803 | 0.43969 | 0.6989 | 1.0669 | 1.5591 | 2.1649 | 2.9214 | 3.8809 | 5.1009 | 6.6521 | 8.6238 | 11.1283 | 14.3094 | 18.3483 | 23.471 | 29.9737
Halse-Brandt | 4.1666e-11 | 1.0466e-10 | 2.6289e-10 | 6.6034e-10 | 1.6586e-09 | 4.1661e-09 | 1.0464e-08 | 2.6281e-08 | 6.6002e-08 | 1.6574e-07 | 4.1611e-07 | 1.0444e-06 | 2.6202e-06 | 6.5688e-06 | 1.6449e-05 | 4.1117e-05 | 0.00010249 | 0.00025434 | 0.00062684 | 0.0015286 | 0.0036682 | 0.008595 | 0.019463 | 0.042064 | 0.08564 | 0.16247 | 0.28567 | 0.46643 | 0.71343 | 1.0356 | 1.4457 | 1.9634 | 2.6153 | 3.436 | 4.4693 | 5.77 | 7.4076 | 9.4692 | 12.0646 | 15.332 | 19.4455
Norris | 6.6935e-06 | 6.6935e-06
Norris | 0.00010841 | 0.00010841
Norris | 0.00056043 | 0.00056043
Norris | 0.0018263 | 0.0018263
Norris | 0.0046496 | 0.0046496
Tape
Halse: https://doi.org/10.1088/0022-3727/3/5/310
Brandt: https://doi.org/10.1103/PhysRevB.48.12893
Norris: https://doi.org/10.1088/0022-3727/3/4/308
Tape with width w exposed to applied current and magnetic field
Self-field loss (Norris)
Low amplitude magnetization (Halse/Brandt)
Example calculation for:
Ic = 1000 A
w = 2 mm
Ec = 100 µV/m
n = 30
f = 500 Hz
Halse-Brandt magnetization loss
Norris self-field transport loss

## Slide 5: Hysteresis loss of a single round sub-cable
Chart: Magnetic field amplitude [T]
| 1E-3 | 1.2589254117941701E-3 | 1.58489319246111E-3 | 1.9952623149688798E-3 | 2.5118864315095799E-3 | 3.1622776601683798E-3 | 3.9810717055349699E-3 | 5.0118723362727298E-3 | 6.3095734448019303E-3 | 7.9432823472428103E-3 | 0.01 | 1.2589254117941699E-2 | 1.58489319246111E-2 | 1.9952623149688799E-2 | 2.5118864315095801E-2 | 3.1622776601683798E-2 | 3.9810717055349699E-2 | 5.0118723362727199E-2 | 6.3095734448019303E-2 | 7.9432823472428096E-2 | 0.1 | 0.12589254117941701 | 0.15848931924611101 | 0.199526231496888 | 0.25118864315095801 | 0.316227766016838 | 0.39810717055349698 | 0.50118723362727302 | 0.63095734448019303 | 0.79432823472428105 | 1 | 1.2589254117941699 | 1.58489319246111 | 1.99526231496888 | 2.5118864315095801 | 3.16227766016838 | 3.98107170553497 | 5.01187233627273 | 6.3095734448019298 | 7.9432823472428096 | 10
I = 0 A | 3.8334e-09 | 4.6002e-09 | 1.2987e-08 | 4.5527e-08 | 1.1468e-07 | 3.2076e-07 | 7.6855e-07 | 1.8745e-06 | 4.6024e-06 | 1.123e-05 | 2.7054e-05 | 6.4734e-05 | 0.00015414 | 0.00036139 | 0.00083458 | 0.0018876 | 0.0041002 | 0.0087923 | 0.018726 | 0.037881 | 0.074688 | 0.14281 | 0.26632 | 0.48443 | 0.85645 | 1.4688 | 2.4422 | 3.9065 | 6.0341 | 9.0005 | 12.99 | 18.2553 | 25.0719 | 33.7895 | 44.9097 | 59.0538 | 77.0506 | 99.9517 | 129.068 | 166.0317 | 212.9486
I = 1200 A | 1.9307e-06 | 2.1372e-06 | 2.4234e-06 | 2.8956e-06 | 3.7426e-06 | 5.0354e-06 | 7.3609e-06 | 1.1264e-05 | 1.8331e-05 | 3.156e-05 | 5.7829e-05 | 0.00010428 | 0.00022881 | 0.0004475 | 0.0010262 | 0.002067 | 0.0046159 | 0.0097282 | 0.019742 | 0.039559 | 0.07727 | 0.14745 | 0.27385 | 0.49548 | 0.87399 | 1.4954 | 2.4783 | 3.9585 | 6.1045 | 9.0909 | 13.11 | 18.3927 | 25.2217 | 33.9541 | 45.0761 | 59.2235 | 77.229 | 100.1406 | 129.2582 | 166.2382 | 213.1885
I = 2400 A | 2.9359e-05 | 2.9786e-05 | 3.0576e-05 | 3.2578e-05 | 3.581e-05 | 4.0059e-05 | 4.5549e-05 | 5.2788e-05 | 6.3264e-05 | 9.5765e-05 | 0.00016559 | 0.00028101 | 0.0004411 | 0.00082865 | 0.0015091 | 0.0030479 | 0.0058595 | 0.011569 | 0.023059 | 0.044819 | 0.085886 | 0.16099 | 0.2954 | 0.52961 | 0.92631 | 1.5735 | 2.5915 | 4.1163 | 6.3171 | 9.3648 | 13.471 | 18.8141 | 25.6873 | 34.4786 | 45.64 | 59.8409 | 77.9318 | 100.9521 | 130.2263 | 167.3923 | 214.5676
I = 3600 A | 0.0001189 | 0.00011899 | 0.00011906 | 0.00011969 | 0.00012154 | 0.00012951 | 0.00014967 | 0.00018461 | 0.00023732 | 0.00030839 | 0.00040571 | 0.00057205 | 0.00092384 | 0.0014985 | 0.0026022 | 0.0044683 | 0.00833 | 0.015565 | 0.029121 | 0.054551 | 0.10099 | 0.185 | 0.33348 | 0.58969 | 1.017 | 1.7079 | 2.7856 | 4.3828 | 6.6748 | 9.8315 | 14.0494 | 19.4662 | 26.4228 | 35.2855 | 46.5277 | 60.8444 | 79.0613 | 102.2284 | 131.7088 | 169.152 | 216.6972
I = 4800 A | 0.00039431 | 0.00039665 | 0.00040162 | 0.00041144 | 0.00042768 | 0.00045136 | 0.00048323 | 0.00052533 | 0.00058242 | 0.0006877 | 0.00090131 | 0.0012508 | 0.0017417 | 0.0026672 | 0.0041658 | 0.0070715 | 0.012042 | 0.021176 | 0.038014 | 0.068595 | 0.12382 | 0.2214 | 0.39034 | 0.67838 | 1.1514 | 1.9055 | 3.0658 | 4.7683 | 7.187 | 10.4876 | 14.8044 | 20.3238 | 27.3995 | 36.353 | 47.708 | 62.1704 | 80.5942 | 104.0214 | 133.7824 | 171.5707 | 219.5763
I = 6000 A | 0.0010556 | 0.0010559 | 0.0010574 | 0.001062 | 0.0010715 | 0.0010976 | 0.0011501 | 0.0012372 | 0.0013685 | 0.0015669 | 0.001853 | 0.0023375 | 0.0031909 | 0.0045229 | 0.0069001 | 0.010746 | 0.017638 | 0.029816 | 0.0513 | 0.089569 | 0.1567 | 0.27308 | 0.47114 | 0.80241 | 1.3384 | 2.1759 | 3.4447 | 5.2835 | 7.8604 | 11.312 | 15.7199 | 21.3723 | 28.5702 | 37.6428 | 49.1706 | 63.8376 | 82.5054 | 106.2541 | 136.4261 | 174.7221 | 223.3099
Halse-Brandt | 1.875e-10 | 4.7097e-10 | 1.183e-09 | 2.9715e-09 | 7.464e-09 | 1.8748e-08 | 4.709e-08 | 1.1827e-07 | 2.9704e-07 | 7.4593e-07 | 1.8729e-06 | 4.7015e-06 | 1.1798e-05 | 2.9586e-05 | 7.4125e-05 | 0.00018544 | 0.00046281 | 0.0011508 | 0.0028452 | 0.0069722 | 0.016856 | 0.039938 | 0.091924 | 0.20328 | 0.42677 | 0.8416 | 1.5488 | 2.658 | 4.2765 | 6.5074 | 9.4614 | 13.2732 | 18.1202 | 24.2414 | 31.9529 | 41.662 | 53.8851 | 69.2731 | 88.6454 | 113.0338 | 143.7369
Norris | 8.0322e-05 | 8.0322e-05
Norris | 0.0013009 | 0.0013009
Norris | 0.0067252 | 0.0067252
Norris | 0.021916 | 0.021916
Norris | 0.055796 | 0.055796
Chart: Magnetic field amplitude [T]
| 1E-3 | 1.2589254117941701E-3 | 1.58489319246111E-3 | 1.9952623149688798E-3 | 2.5118864315095799E-3 | 3.1622776601683798E-3 | 3.9810717055349699E-3 | 5.0118723362727298E-3 | 6.3095734448019303E-3 | 7.9432823472428103E-3 | 0.01 | 1.2589254117941699E-2 | 1.58489319246111E-2 | 1.9952623149688799E-2 | 2.5118864315095801E-2 | 3.1622776601683798E-2 | 3.9810717055349699E-2 | 5.0118723362727199E-2 | 6.3095734448019303E-2 | 7.9432823472428096E-2 | 0.1 | 0.12589254117941701 | 0.15848931924611101 | 0.199526231496888 | 0.25118864315095801 | 0.316227766016838 | 0.39810717055349698 | 0.50118723362727302 | 0.63095734448019303 | 0.79432823472428105 | 1 | 1.2589254117941699 | 1.58489319246111 | 1.99526231496888 | 2.5118864315095801 | 3.16227766016838 | 3.98107170553497 | 5.01187233627273 | 6.3095734448019298 | 7.9432823472428096 | 10
I = 0 A | 3.8334e-09 | 4.6002e-09 | 1.2987e-08 | 4.5527e-08 | 1.1468e-07 | 3.2076e-07 | 7.6855e-07 | 1.8745e-06 | 4.6024e-06 | 1.123e-05 | 2.7054e-05 | 6.4734e-05 | 0.00015414 | 0.00036139 | 0.00083458 | 0.0018876 | 0.0041002 | 0.0087923 | 0.018726 | 0.037881 | 0.074688 | 0.14281 | 0.26632 | 0.48443 | 0.85645 | 1.4688 | 2.4422 | 3.9065 | 6.0341 | 9.0005 | 12.99 | 18.2553 | 25.0719 | 33.7895 | 44.9097 | 59.0538 | 77.0506 | 99.9517 | 129.068 | 166.0317 | 212.9486
I = 1200 A | 1.9307e-06 | 2.1372e-06 | 2.4234e-06 | 2.8956e-06 | 3.7426e-06 | 5.0354e-06 | 7.3609e-06 | 1.1264e-05 | 1.8331e-05 | 3.156e-05 | 5.7829e-05 | 0.00010428 | 0.00022881 | 0.0004475 | 0.0010262 | 0.002067 | 0.0046159 | 0.0097282 | 0.019742 | 0.039559 | 0.07727 | 0.14745 | 0.27385 | 0.49548 | 0.87399 | 1.4954 | 2.4783 | 3.9585 | 6.1045 | 9.0909 | 13.11 | 18.3927 | 25.2217 | 33.9541 | 45.0761 | 59.2235 | 77.229 | 100.1406 | 129.2582 | 166.2382 | 213.1885
I = 2400 A | 2.9359e-05 | 2.9786e-05 | 3.0576e-05 | 3.2578e-05 | 3.581e-05 | 4.0059e-05 | 4.5549e-05 | 5.2788e-05 | 6.3264e-05 | 9.5765e-05 | 0.00016559 | 0.00028101 | 0.0004411 | 0.00082865 | 0.0015091 | 0.0030479 | 0.0058595 | 0.011569 | 0.023059 | 0.044819 | 0.085886 | 0.16099 | 0.2954 | 0.52961 | 0.92631 | 1.5735 | 2.5915 | 4.1163 | 6.3171 | 9.3648 | 13.471 | 18.8141 | 25.6873 | 34.4786 | 45.64 | 59.8409 | 77.9318 | 100.9521 | 130.2263 | 167.3923 | 214.5676
I = 3600 A | 0.0001189 | 0.00011899 | 0.00011906 | 0.00011969 | 0.00012154 | 0.00012951 | 0.00014967 | 0.00018461 | 0.00023732 | 0.00030839 | 0.00040571 | 0.00057205 | 0.00092384 | 0.0014985 | 0.0026022 | 0.0044683 | 0.00833 | 0.015565 | 0.029121 | 0.054551 | 0.10099 | 0.185 | 0.33348 | 0.58969 | 1.017 | 1.7079 | 2.7856 | 4.3828 | 6.6748 | 9.8315 | 14.0494 | 19.4662 | 26.4228 | 35.2855 | 46.5277 | 60.8444 | 79.0613 | 102.2284 | 131.7088 | 169.152 | 216.6972
I = 4800 A | 0.00039431 | 0.00039665 | 0.00040162 | 0.00041144 | 0.00042768 | 0.00045136 | 0.00048323 | 0.00052533 | 0.00058242 | 0.0006877 | 0.00090131 | 0.0012508 | 0.0017417 | 0.0026672 | 0.0041658 | 0.0070715 | 0.012042 | 0.021176 | 0.038014 | 0.068595 | 0.12382 | 0.2214 | 0.39034 | 0.67838 | 1.1514 | 1.9055 | 3.0658 | 4.7683 | 7.187 | 10.4876 | 14.8044 | 20.3238 | 27.3995 | 36.353 | 47.708 | 62.1704 | 80.5942 | 104.0214 | 133.7824 | 171.5707 | 219.5763
I = 6000 A | 0.0010556 | 0.0010559 | 0.0010574 | 0.001062 | 0.0010715 | 0.0010976 | 0.0011501 | 0.0012372 | 0.0013685 | 0.0015669 | 0.001853 | 0.0023375 | 0.0031909 | 0.0045229 | 0.0069001 | 0.010746 | 0.017638 | 0.029816 | 0.0513 | 0.089569 | 0.1567 | 0.27308 | 0.47114 | 0.80241 | 1.3384 | 2.1759 | 3.4447 | 5.2835 | 7.8604 | 11.312 | 15.7199 | 21.3723 | 28.5702 | 37.6428 | 49.1706 | 63.8376 | 82.5054 | 106.2541 | 136.4261 | 174.7221 | 223.3099
Halse-Brandt | 1.875e-10 | 4.7097e-10 | 1.183e-09 | 2.9715e-09 | 7.464e-09 | 1.8748e-08 | 4.709e-08 | 1.1827e-07 | 2.9704e-07 | 7.4593e-07 | 1.8729e-06 | 4.7015e-06 | 1.1798e-05 | 2.9586e-05 | 7.4125e-05 | 0.00018544 | 0.00046281 | 0.0011508 | 0.0028452 | 0.0069722 | 0.016856 | 0.039938 | 0.091924 | 0.20328 | 0.42677 | 0.8416 | 1.5488 | 2.658 | 4.2765 | 6.5074 | 9.4614 | 13.2732 | 18.1202 | 24.2414 | 31.9529 | 41.662 | 53.8851 | 69.2731 | 88.6454 | 113.0338 | 143.7369
Norris | 8.0322e-05 | 8.0322e-05
Norris | 0.0013009 | 0.0013009
Norris | 0.0067252 | 0.0067252
Norris | 0.021916 | 0.021916
Norris | 0.055796 | 0.055796
Numerical
Low amplitude magnetization loss higher than sum of tape loss
Norris formula not valid
Circular cable of 12 2-mm-wide tapes on an 8 mm diameter core
Solovyov et al.: https://doi.org/10.1088/1361-6668/acb08e

## Slide 6: Effect of tape width/filamentization
Chart: Magnetic field amplitude [T]
| 1E-3 | 1.2589254117941701E-3 | 1.58489319246111E-3 | 1.9952623149688798E-3 | 2.5118864315095799E-3 | 3.1622776601683798E-3 | 3.9810717055349699E-3 | 5.0118723362727298E-3 | 6.3095734448019303E-3 | 7.9432823472428103E-3 | 0.01 | 1.2589254117941699E-2 | 1.58489319246111E-2 | 1.9952623149688799E-2 | 2.5118864315095801E-2 | 3.1622776601683798E-2 | 3.9810717055349699E-2 | 5.0118723362727199E-2 | 6.3095734448019303E-2 | 7.9432823472428096E-2 | 0.1 | 0.12589254117941701 | 0.15848931924611101 | 0.199526231496888 | 0.25118864315095801 | 0.316227766016838 | 0.39810717055349698 | 0.50118723362727302 | 0.63095734448019303 | 0.79432823472428105 | 1 | 1.2589254117941699 | 1.58489319246111 | 1.99526231496888 | 2.5118864315095801 | 3.16227766016838 | 3.98107170553497 | 5.01187233627273 | 6.3095734448019298 | 7.9432823472428096 | 10
2x12 mm | 0.0056252 | 0.0056254 | 0.0056257 | 0.0056263 | 0.0056271 | 0.0056282 | 0.0056306 | 0.0056341 | 0.0056425 | 0.0056633 | 0.0057488 | 0.006164 | 0.0071322 | 0.0087399 | 0.011209 | 0.014551 | 0.020975 | 0.030531 | 0.047848 | 0.078556 | 0.13426 | 0.2412 | 0.43619 | 0.81462 | 1.5172 | 2.7833 | 5.1373 | 9.8985 | 18.1813 | 30.5666 | 47.5423 | 70.4774 | 100.992 | 140.0109 | 190.626 | 254.9476 | 336.7179 | 440.996 | 573.4177 | 741.5689 | 954.4633
3x8 mm | 0.0038854 | 0.0038858 | 0.0038856 | 0.0038862 | 0.0038874 | 0.0038887 | 0.0038915 | 0.0038991 | 0.0039223 | 0.0040149 | 0.004316 | 0.004926 | 0.0058752 | 0.0071414 | 0.0089822 | 0.012639 | 0.018709 | 0.029363 | 0.047452 | 0.081228 | 0.14509 | 0.26887 | 0.51231 | 0.99729 | 1.9531 | 3.7504 | 6.8936 | 12.0456 | 20.3184 | 32.4168 | 49.6102 | 72.5178 | 101.6104 | 138.5304 | 185.3514 | 244.8991 | 320.5742 | 416.7355 | 539.1611 | 694.6645 | 892.1525
4x6 mm | 0.0029761 | 0.002976 | 0.0029765 | 0.0029774 | 0.0029789 | 0.0029817 | 0.0029884 | 0.0030114 | 0.0030955 | 0.0033252 | 0.0037589 | 0.0043749 | 0.0052122 | 0.0064882 | 0.0091936 | 0.013144 | 0.020012 | 0.032261 | 0.0542 | 0.094101 | 0.16787 | 0.30568 | 0.55877 | 1.0272 | 1.8861 | 3.4381 | 6.1153 | 10.4201 | 17.1327 | 27.357 | 41.4054 | 59.4438 | 82.3515 | 111.5288 | 148.6793 | 195.862 | 255.7087 | 331.7911 | 428.5081 | 551.4114 | 707.5956
6x4 mm | 0.0020354 | 0.0020363 | 0.0020368 | 0.0020379 | 0.0020402 | 0.0020463 | 0.0020655 | 0.002128 | 0.0022807 | 0.0025538 | 0.0029869 | 0.0035633 | 0.0043406 | 0.0058932 | 0.0085662 | 0.012766 | 0.020333 | 0.033734 | 0.05847 | 0.10296 | 0.18404 | 0.33354 | 0.60195 | 1.0749 | 1.881 | 3.2026 | 5.2806 | 8.4507 | 13.1937 | 19.9513 | 28.9334 | 40.7602 | 56.058 | 75.5549 | 100.0816 | 131.1788 | 170.6384 | 220.8658 | 284.6179 | 365.6766 | 468.5581
8x3 mm | 0.0015515 | 0.0015521 | 0.0015531 | 0.0015545 | 0.0015593 | 0.0015725 | 0.0016104 | 0.0016955 | 0.0018474 | 0.0020978 | 0.002463 | 0.0029715 | 0.0038804 | 0.0054121 | 0.0078914 | 0.012234 | 0.019864 | 0.033022 | 0.05698 | 0.10035 | 0.1782 | 0.31736 | 0.56247 | 0.98501 | 1.694 | 2.8365 | 4.6019 | 7.22 | 10.9408 | 15.9816 | 22.4799 | 30.9057 | 41.882 | 55.9123 | 73.755 | 96.4305 | 125.2501 | 161.9365 | 208.4771 | 267.57 | 342.5756
12x2 mm | 0.0010556 | 0.0010559 | 0.0010574 | 0.001062 | 0.0010715 | 0.0010976 | 0.0011501 | 0.0012372 | 0.0013685 | 0.0015669 | 0.001853 | 0.0023375 | 0.0031909 | 0.0045229 | 0.0069001 | 0.010746 | 0.017638 | 0.029816 | 0.0513 | 0.089569 | 0.1567 | 0.27308 | 0.47114 | 0.80241 | 1.3384 | 2.1759 | 3.4447 | 5.2835 | 7.8604 | 11.312 | 15.7199 | 21.3723 | 28.5702 | 37.6428 | 49.1706 | 63.8376 | 82.5054 | 106.2541 | 136.4261 | 174.7221 | 223.3099
24x1 mm | 0.00054468 | 0.00054705 | 0.00055108 | 0.00055993 | 0.00057691 | 0.00060541 | 0.00064679 | 0.00070379 | 0.00078798 | 0.00091267 | 0.0011245 | 0.0015043 | 0.0020721 | 0.0030742 | 0.0047047 | 0.0075912 | 0.012539 | 0.021153 | 0.036061 | 0.061724 | 0.10558 | 0.17879 | 0.29956 | 0.49307 | 0.79521 | 1.2539 | 1.9246 | 2.8769 | 4.1798 | 5.8845 | 8.0559 | 10.8261 | 14.3576 | 18.8507 | 24.5763 | 31.8395 | 41.0662 | 52.7906 | 67.6889 | 86.6239 | 110.7124
48x0.5 mm | 0.00028315 | 0.00028507 | 0.00029146 | 0.00030044 | 0.00031342 | 0.00033183 | 0.00035604 | 0.00038785 | 0.00043444 | 0.00051219 | 0.00065885 | 0.00088345 | 0.0012427 | 0.0018638 | 0.0029043 | 0.0046666 | 0.0077072 | 0.012943 | 0.021893 | 0.03701 | 0.062196 | 0.10363 | 0.17022 | 0.27497 | 0.43557 | 0.6744 | 1.0194 | 1.5019 | 2.1543 | 2.9959 | 4.0655 | 5.4271 | 7.1596 | 9.364 | 12.1676 | 15.7336 | 20.2732 | 26.0478 | 33.4008 | 42.7707 | 54.7276
120x0.2 mm | 0.00012172 | 0.00012427 | 0.00012794 | 0.00013257 | 0.0001385 | 0.00014696 | 0.00015753 | 0.00017075 | 0.00019162 | 0.000234 | 0.00030276 | 0.0004039 | 0.0005843 | 0.00087096 | 0.0013658 | 0.002205 | 0.0036268 | 0.0060419 | 0.010104 | 0.01689 | 0.028045 | 0.046059 | 0.074597 | 0.11885 | 0.18558 | 0.28368 | 0.42338 | 0.61676 | 0.87551 | 1.205 | 1.6235 | 2.1558 | 2.8333 | 3.6961 | 4.7949 | 6.1015 | 7.8843 | 10.1757 | 13.1256 | 16.9292 | 21.8828
2x12 mm
3x8 mm
4x6 mm
12x2 mm
6x4 mm
24x1 mm
etc.
Serious potential for loss reduction, but filaments must be uncoupled by high-resistive barriers and twisting
Applied current amplitude I0 = 6000 A for all calculations

## Slide 7: Effect of critical current density (12x 2 mm tapes)
Chart: Magnetic field amplitude [T]
| 1E-3 | 1.2589254117941701E-3 | 1.58489319246111E-3 | 1.9952623149688798E-3 | 2.5118864315095799E-3 | 3.1622776601683798E-3 | 3.9810717055349699E-3 | 5.0118723362727298E-3 | 6.3095734448019303E-3 | 7.9432823472428103E-3 | 0.01 | 1.2589254117941699E-2 | 1.58489319246111E-2 | 1.9952623149688799E-2 | 2.5118864315095801E-2 | 3.1622776601683798E-2 | 3.9810717055349699E-2 | 5.0118723362727199E-2 | 6.3095734448019303E-2 | 7.9432823472428096E-2 | 0.1 | 0.12589254117941701 | 0.15848931924611101 | 0.199526231496888 | 0.25118864315095801 | 0.316227766016838 | 0.39810717055349698 | 0.50118723362727302 | 0.63095734448019303 | 0.79432823472428105 | 1 | 1.2589254117941699 | 1.58489319246111 | 1.99526231496888 | 2.5118864315095801 | 3.16227766016838 | 3.98107170553497 | 5.01187233627273 | 6.3095734448019298 | 7.9432823472428096 | 10
250 A/mm | 0.012487 | 0.012531 | 0.012602 | 0.012719 | 0.012905 | 0.013198 | 0.013658 | 0.014386 | 0.015546 | 0.017379 | 0.020295 | 0.024902 | 0.032212 | 0.043801 | 0.062047 | 0.090662 | 0.13498 | 0.20269 | 0.30421 | 0.45314 | 0.66606 | 0.9602 | 1.3574 | 1.8722 | 2.5098 | 3.3097 | 4.3051 | 5.5482 | 7.0967 | 9.0588 | 11.5261 | 14.647 | 18.6272 | 23.6958 | 30.1369 | 38.3067 | 48.6586 | 61.7791 | 78.4212 | 99.5297 | 126.3092
500 A/mm | 0.0010556 | 0.0010559 | 0.0010574 | 0.001062 | 0.0010715 | 0.0010976 | 0.0011501 | 0.0012372 | 0.0013685 | 0.0015669 | 0.001853 | 0.0023375 | 0.0031909 | 0.0045229 | 0.0069001 | 0.010746 | 0.017638 | 0.029816 | 0.0513 | 0.089569 | 0.1567 | 0.27423 | 0.45834 | 0.79836 | 1.338 | 2.1427 | 3.4685 | 5.2545 | 7.8149 | 11.1972 | 15.475 | 20.9962 | 28.0212 | 36.9212 | 48.2327 | 62.6324 | 80.9098 | 104.1021 | 133.5714 | 171.0174 | 218.6199
750 A/mm | 0.00033732 | 0.00033843 | 0.00034006 | 0.00034345 | 0.00035167 | 0.00037057 | 0.00040606 | 0.00046088 | 0.00053528 | 0.00063336 | 0.00076296 | 0.00094565 | 0.0012179 | 0.0018293 | 0.0028419 | 0.004459 | 0.0075777 | 0.013171 | 0.02352 | 0.043573 | 0.080643 | 0.15226 | 0.2697 | 0.47596 | 0.89984 | 1.5258 | 2.6601 | 4.4493 | 7.0708 | 11.2656 | 16.982 | 24.5866 | 34.7517 | 47.753 | 64.3973 | 85.5879 | 112.5671 | 146.8921 | 190.6021 | 246.0669 | 316.5155
1000 A/mm | 0.00028661 | 0.00028675 | 0.0002867 | 0.00028675 | 0.00028699 | 0.0002872 | 0.00028746 | 0.00028817 | 0.00029017 | 0.00030298 | 0.00033656 | 0.00045475 | 0.00069024 | 0.0010594 | 0.0015439 | 0.0023901 | 0.0042366 | 0.0073821 | 0.014159 | 0.026503 | 0.050795 | 0.082301 | 0.18253 | 0.35603 | 0.6313 | 1.2028 | 2.1871 | 3.6871 | 6.5085 | 10.5157 | 16.6426 | 26.211 | 38.7558 | 55.4995 | 77.5215 | 105.6492 | 141.4226 | 186.9526 | 244.9121 | 318.6934 | 412.442
1250 A/mm | 0.00015929 | 0.00015836 | 0.00015842 | 0.00015902 | 0.00016032 | 0.00016473 | 0.00017381 | 0.00018922 | 0.00021071 | 0.00023886 | 0.00027571 | 0.00032454 | 0.00038965 | 0.00054602 | 0.00095941 | 0.001675 | 0.0026818 | 0.0049463 | 0.0090694 | 0.018293 | 0.03511 | 0.071755 | 0.12488 | 0.25533 | 0.51457 | 0.96073 | 1.7873 | 3.2973 | 5.6139 | 9.8737 | 16.1881 | 25.5518 | 40.4182 | 60.34 | 86.4939 | 121.479 | 166.0645 | 222.7793 | 294.9097 | 386.7689 | 503.7218
1500 A/mm | 9.9627e-05 | 9.9761e-05 | 0.00010005 | 0.00010103 | 0.00010307 | 0.00010702 | 0.00011267 | 0.00012039 | 0.00013046 | 0.00014451 | 0.00017337 | 0.00022942 | 0.00031979 | 0.00044582 | 0.00069429 | 0.0011048 | 0.0019356 | 0.0035185 | 0.0066471 | 0.013102 | 0.026364 | 0.053641 | 0.10889 | 0.21835 | 0.42946 | 0.82798 | 1.5611 | 2.8762 | 5.1723 | 9.0624 | 15.4206 | 25.2943 | 39.999 | 62.6159 | 93.1683 | 133.0994 | 186.398 | 254.2908 | 340.637 | 450.4563 | 590.3391
1750 A/mm | 5.4822e-05 | 5.5766e-05 | 5.7389e-05 | 6.0041e-05 | 6.3999e-05 | 6.9497e-05 | 7.6885e-05 | 8.6399e-05 | 9.8765e-05 | 0.00011487 | 0.00013562 | 0.00016437 | 0.00022518 | 0.00033713 | 0.00051237 | 0.00084295 | 0.0013963 | 0.0026173 | 0.0050223 | 0.0099527 | 0.020252 | 0.042014 | 0.086902 | 0.178 | 0.3582 | 0.70535 | 1.3568 | 2.5475 | 4.6717 | 8.3539 | 14.5369 | 24.5652 | 39.8737 | 62.6818 | 96.8604 | 142.5256 | 202.4415 | 281.4251 | 381.9841 | 509.8163 | 672.4913
2000 A/mm | 5.2145e-05 | 5.2216e-05 | 5.2239e-05 | 5.2212e-05 | 5.238e-05 | 5.2669e-05 | 5.4017e-05 | 5.8419e-05 | 6.801e-05 | 8.3307e-05 | 0.00010446 | 0.00013372 | 0.00017428 | 0.0002438 | 0.00039219 | 0.00063692 | 0.0011215 | 0.0019767 | 0.0038607 | 0.0077879 | 0.016036 | 0.03378 | 0.070933 | 0.14803 | 0.30343 | 0.60823 | 1.1905 | 2.2752 | 4.2416 | 7.712 | 13.6652 | 23.2997 | 39.2151 | 62.9764 | 98.0397 | 148.9993 | 215.7564 | 304.2105 | 418.8769 | 564.7879 | 750.2195
2250 A/mm | 4.9999e-05 | 4.9996e-05 | 5.0058e-05 | 5.002e-05 | 5.0077e-05 | 5.0139e-05 | 5.022e-05 | 5.029e-05 | 5.1026e-05 | 5.6413e-05 | 7.3549e-05 | 0.00010447 | 0.00014711 | 0.00020184 | 0.00029499 | 0.00050357 | 0.00086054 | 0.0016323 | 0.0030762 | 0.0061749 | 0.012973 | 0.027655 | 0.059118 | 0.12505 | 0.26009 | 0.53017 | 1.0544 | 2.0462 | 3.8694 | 7.1391 | 12.8417 | 22.2847 | 37.8144 | 62.7234 | 98.7383 | 152.2567 | 226.6339 | 323.1423 | 451.3649 | 615.2363 | 823.6231
2500 A/mm | 6.9082e-05 | 6.8932e-05 | 6.9227e-05 | 7.0125e-05 | 7.1167e-05 | 7.2515e-05 | 7.4588e-05 | 7.7517e-05 | 8.2242e-05 | 8.967e-05 | 0.00010311 | 0.00012381 | 0.00015626 | 0.00021178 | 0.0003046 | 0.00046381 | 0.00074964 | 0.0012922 | 0.0023546 | 0.0045517 | 0.0092406 | 0.019479 | 0.042115 | 0.092017 | 0.20092 | 0.43416 | 0.92261 | 1.9206 | 3.9102 | 7.7813 | 15.1248 | 28.6427 | 52.5842 | 92.9292 | 157.1111 | 253.6253 | 392.8985 | 591.1944 | 869.6367 | 1246.0035 | 1736.7406
Circular cable of 12 tapes with 2 mm width, on 8 mm diameter core
Increasing Jc decreases loss at low amplitudes.
(reduced penetration of B near edges)
In saturated tapes, loss increases with Jc. (magnetization limited by Jc)
Jc =
Applied current amplitude I0 = 6000 A for all calculations

## Slide 8: Effect of critical current density (120x0.2 mm)
Chart: Magnetic field amplitude [T]
| 1E-3 | 1.2589254117941701E-3 | 1.58489319246111E-3 | 1.9952623149688798E-3 | 2.5118864315095799E-3 | 3.1622776601683798E-3 | 3.9810717055349699E-3 | 5.0118723362727298E-3 | 6.3095734448019303E-3 | 7.9432823472428103E-3 | 0.01 | 1.2589254117941699E-2 | 1.58489319246111E-2 | 1.9952623149688799E-2 | 2.5118864315095801E-2 | 3.1622776601683798E-2 | 3.9810717055349699E-2 | 5.0118723362727199E-2 | 6.3095734448019303E-2 | 7.9432823472428096E-2 | 0.1 | 0.12589254117941701 | 0.15848931924611101 | 0.199526231496888 | 0.25118864315095801 | 0.316227766016838 | 0.39810717055349698 | 0.50118723362727302 | 0.63095734448019303 | 0.79432823472428105 | 1 | 1.2589254117941699 | 1.58489319246111 | 1.99526231496888 | 2.5118864315095801 | 3.16227766016838 | 3.98107170553497 | 5.01187233627273 | 6.3095734448019298 | 7.9432823472428096 | 10
250 A/mm | 0.0022462 | 0.002256 | 0.0022744 | 0.0022982 | 0.0023345 | 0.0023961 | 0.0024943 | 0.0026462 | 0.0028879 | 0.0032647 | 0.0038528 | 0.0047625 | 0.0061538 | 0.0082695 | 0.011424 | 0.016056 | 0.022715 | 0.032133 | 0.04522 | 0.063012 | 0.086677 | 0.1175 | 0.15565 | 0.20329 | 0.26352 | 0.33963 | 0.43471 | 0.55488 | 0.7056 | 0.89472 | 1.1036 | 1.4024 | 1.7825 | 2.2667 | 2.8848 | 3.677 | 4.701 | 6.0498 | 7.8731 | 11.3917 | 28.8482
500 A/mm | 0.00012172 | 0.00012427 | 0.00012794 | 0.00013257 | 0.0001385 | 0.00014696 | 0.00015753 | 0.00017075 | 0.00019162 | 0.000234 | 0.00030276 | 0.0004039 | 0.0005843 | 0.00087096 | 0.0013658 | 0.0021984 | 0.0036283 | 0.0060346 | 0.010098 | 0.016876 | 0.028038 | 0.044873 | 0.074663 | 0.11803 | 0.18457 | 0.28437 | 0.42032 | 0.61609 | 0.87106 | 1.1933 | 1.5663 | 2.077 | 2.7284 | 3.557 | 4.6117 | 5.9516 | 7.653 | 9.8148 | 12.5686 | 16.1949 | 21.162
750 A/mm | 3.8132e-05 | 3.9719e-05 | 4.2001e-05 | 4.4863e-05 | 4.86e-05 | 5.4247e-05 | 6.0149e-05 | 6.8316e-05 | 7.8839e-05 | 9.2276e-05 | 0.00011416 | 0.00016347 | 0.00024182 | 0.00035846 | 0.00059157 | 0.00096814 | 0.001693 | 0.0029502 | 0.005303 | 0.0094494 | 0.016666 | 0.027606 | 0.049081 | 0.08583 | 0.1396 | 0.23133 | 0.36949 | 0.57472 | 0.88084 | 1.3018 | 1.9126 | 2.6587 | 3.6183 | 4.8472 | 6.4151 | 8.4135 | 10.955 | 14.1885 | 18.2946 | 23.509 | 30.1337
1000 A/mm | 2.9609e-05 | 3.0258e-05 | 3.0307e-05 | 3.0515e-05 | 3.0724e-05 | 3.1008e-05 | 3.1296e-05 | 3.1462e-05 | 3.4417e-05 | 4.5556e-05 | 6.5183e-05 | 9.3453e-05 | 0.00013199 | 0.00019468 | 0.00033542 | 0.00053538 | 0.0010091 | 0.0017923 | 0.0034049 | 0.0062206 | 0.011703 | 0.021396 | 0.037924 | 0.063659 | 0.1174 | 0.20031 | 0.32395 | 0.54142 | 0.85374 | 1.3095 | 2.0351 | 2.988 | 4.2329 | 5.8409 | 7.9069 | 10.5497 | 13.9194 | 18.2128 | 23.6719 | 30.6143 | 39.4305
1250 A/mm | 2.1566e-05 | 2.166e-05 | 2.1685e-05 | 2.1609e-05 | 2.1773e-05 | 2.2051e-05 | 2.3049e-05 | 2.48e-05 | 2.7429e-05 | 3.0976e-05 | 3.5918e-05 | 4.8545e-05 | 8.2238e-05 | 0.00013541 | 0.00021024 | 0.00037774 | 0.00065946 | 0.0012095 | 0.0023823 | 0.0045192 | 0.0087275 | 0.014384 | 0.030012 | 0.055247 | 0.096358 | 0.17366 | 0.30131 | 0.49015 | 0.82174 | 1.3098 | 2.0112 | 3.1148 | 4.6087 | 6.5701 | 9.1091 | 12.3758 | 16.5595 | 21.8986 | 28.7016 | 37.3536 | 48.3597
1500 A/mm | 3.131e-05 | 3.874e-05 | 4.9003e-05 | 8.2104e-05 | 0.00015332 | 0.00022463 | 0.00048563 | 0.00090614 | 0.0016735 | 0.0035106 | 0.0067043 | 0.012908 | 0.022278 | 0.045823 | 0.085162 | 0.15241 | 0.27079 | 0.46599 | 0.76839 | 1.2779 | 1.9729 | 3.1077 | 4.7882 | 7.0627 | 10.0477 | 13.9139 | 18.8873 | 25.2574 | 33.387 | 43.7452 | 56.9176
1750 A/mm | 2.4801e-05 | 3.3392e-05 | 4.44e-05 | 5.853e-05 | 9.6629e-05 | 0.00016975 | 0.0003072 | 0.00070559 | 0.0013342 | 0.0026431 | 0.0055335 | 0.011451 | 0.020727 | 0.036259 | 0.073515 | 0.13885 | 0.24496 | 0.43329 | 0.73672 | 1.2199 | 1.9969 | 3.078 | 4.8279 | 7.3537 | 10.7462 | 15.1819 | 20.9222 | 28.299 | 37.7393 | 49.7826 | 65.1263
2000 A/mm | 1.7324e-05 | 2.6255e-05 | 3.8348e-05 | 5.3924e-05 | 7.4188e-05 | 0.0001557 | 0.00023104 | 0.00049352 | 0.0011097 | 0.0020692 | 0.004511 | 0.0094416 | 0.019263 | 0.033338 | 0.061559 | 0.12189 | 0.23081 | 0.39783 | 0.69909 | 1.187 | 1.9653 | 3.1377 | 4.8073 | 7.4874 | 11.2296 | 16.2032 | 22.6774 | 31.0381 | 41.7692 | 55.4854 | 72.9694
2250 A/mm | 3.0654e-05 | 4.7697e-05 | 6.9177e-05 | 0.00013609 | 0.00021564 | 0.00035525 | 0.0008596 | 0.0018087 | 0.0035624 | 0.0071695 | 0.017089 | 0.032137 | 0.053702 | 0.10651 | 0.211 | 0.38137 | 0.65697 | 1.1382 | 1.8856 | 3.1472 | 4.8754 | 7.5186 | 11.5323 | 16.9918 | 24.1724 | 33.4882 | 45.4826 | 60.849 | 80.4725
2500 A/mm | 3.9667e-05 | 6.2453e-05 | 0.00011199 | 0.00019582 | 0.00032112 | 0.00063334 | 0.0015261 | 0.0030683 | 0.0050936 | 0.01438 | 0.030128 | 0.05249 | 0.092625 | 0.1879 | 0.3627 | 0.62202 | 1.0844 | 1.8686 | 3.0526 | 4.9335 | 7.759 | 11.7628 | 17.5416 | 25.3338 | 35.5408 | 48.7333 | 65.6814 | 87.3647
Jc =
Applied current amplitude I0 = 6000 A for all calculations
Circular cable of 120 tapes/filaments with 0.2 mm width on 8 mm diameter core
0.2 mm
0.2 mm
0.2 mm
0.2 mm
0.2 mm

## Slide 9: Effect of operating temperature
Used measured Jc(B,T) data for SuperPower tape from Robinson Research Institute https://htsdb.wimbush.eu/dataset/4256624
Chart: Magnetic field amplitude [T]
| 1E-3 | 1.2589254117941701E-3 | 1.58489319246111E-3 | 1.9952623149688798E-3 | 2.5118864315095799E-3 | 3.1622776601683798E-3 | 3.9810717055349699E-3 | 5.0118723362727298E-3 | 6.3095734448019303E-3 | 7.9432823472428103E-3 | 0.01 | 1.2589254117941699E-2 | 1.58489319246111E-2 | 1.9952623149688799E-2 | 2.5118864315095801E-2 | 3.1622776601683798E-2 | 3.9810717055349699E-2 | 5.0118723362727199E-2 | 6.3095734448019303E-2 | 7.9432823472428096E-2 | 0.1 | 0.12589254117941701 | 0.15848931924611101 | 0.199526231496888 | 0.25118864315095801 | 0.316227766016838 | 0.39810717055349698 | 0.50118723362727302 | 0.63095734448019303 | 0.79432823472428105 | 1 | 1.2589254117941699 | 1.58489319246111 | 1.99526231496888 | 2.5118864315095801 | 3.16227766016838 | 3.98107170553497 | 5.01187233627273 | 6.3095734448019298 | 7.9432823472428096 | 10
15 K | 6.1797e-06 | 8.3374e-06 | 1.2289e-05 | 2.0325e-05 | 3.4789e-05 | 5.8683e-05 | 9.3646e-05 | 0.00014133 | 0.00020368 | 0.00028502 | 0.000389 | 0.00052242 | 0.00069203 | 0.00091418 | 0.0013605 | 0.0024973 | 0.0042979 | 0.0068332 | 0.011274 | 0.019371 | 0.031147 | 0.051385 | 0.08279 | 0.1295 | 0.2021 | 0.30315 | 0.45012 | 0.64648 | 0.88916 | 1.1868 | 1.5449 | 1.9816 | 2.5073 | 3.1218 | 3.8487 | 4.7245 | 7.5554 | 43.9542 | 176.0199
20 K | 0.00010524 | 0.00011338 | 0.00012386 | 0.00013955 | 0.00015979 | 0.00018694 | 0.00022242 | 0.00026879 | 0.00032791 | 0.00040294 | 0.00049859 | 0.00062064 | 0.0007915 | 0.0012068 | 0.0020835 | 0.003398 | 0.0052376 | 0.0086135 | 0.014457 | 0.022937 | 0.037521 | 0.05994 | 0.093931 | 0.14577 | 0.21897 | 0.32599 | 0.46856 | 0.64446 | 0.85986 | 1.1239 | 1.446 | 1.8299 | 2.2852 | 2.8288 | 3.6075 | 11.6003 | 53.1033 | 463.6252 | 20861.6823
25 K | 0.00041044 | 0.00041035 | 0.00041213 | 0.00041178 | 0.00041171 | 0.0004134 | 0.00042221 | 0.00044055 | 0.00047852 | 0.00053678 | 0.00063275 | 0.00086567 | 0.0013406 | 0.002052 | 0.003034 | 0.0045627 | 0.0075085 | 0.011928 | 0.01871 | 0.030067 | 0.046696 | 0.073297 | 0.11091 | 0.16611 | 0.24446 | 0.34551 | 0.47107 | 0.62896 | 0.82084 | 1.052 | 1.3281 | 1.6617 | 2.1187 | 4.9236 | 26.173 | 179.9769 | 4387.3241 | 96466.4671 | 269647.2134
30 K | 0.00064312 | 0.00064455 | 0.00064589 | 0.00064878 | 0.00065243 | 0.00066105 | 0.00068212 | 0.00073005 | 0.00083031 | 0.0010095 | 0.0012966 | 0.0017047 | 0.0022799 | 0.0032671 | 0.004968 | 0.0074553 | 0.011391 | 0.017639 | 0.026744 | 0.041148 | 0.061882 | 0.091989 | 0.13426 | 0.19082 | 0.26324 | 0.3545 | 0.46702 | 0.60382 | 0.77082 | 0.9792 | 1.424 | 4.0063 | 24.6495 | 223.4424 | 5507.0033 | 77080.7156 | 210065.7628 | 403582.5462 | 565309.1717
35 K | 0.0018151 | 0.0018188 | 0.0018239 | 0.0018331 | 0.001849 | 0.0018793 | 0.0019383 | 0.0020543 | 0.0022677 | 0.0026254 | 0.0031636 | 0.0039317 | 0.0051098 | 0.0070433 | 0.0099117 | 0.014156 | 0.020452 | 0.02946 | 0.042717 | 0.06108 | 0.085905 | 0.11936 | 0.16075 | 0.21208 | 0.27675 | 0.3611 | 0.50528 | 0.92577 | 2.7087 | 10.2757 | 54.1454 | 698.4412 | 13911.4955 | 90798.2032 | 222366.168 | 391061.8173 | 527626.3201 | 646828.0938 | 727582.8836
40 K | 0.02015 | 0.020169 | 0.020203 | 0.020255 | 0.020338 | 0.020466 | 0.020667 | 0.020978 | 0.021464 | 0.022218 | 0.023392 | 0.02518 | 0.027868 | 0.031825 | 0.037545 | 0.045636 | 0.056589 | 0.071138 | 0.09111 | 0.11994 | 0.16622 | 0.2541 | 0.45327 | 0.95907 | 2.2309 | 5.5636 | 16.4703 | 68.9377 | 561.9789 | 5446.8247 | 38064.1253 | 124212.8165 | 258610.6881 | 402714.5357 | 530080.7601 | 640209.6639 | 716776.1062 | 760680.2089 | 773475.139 | 754392.3007
45 K | 5.3198 | 5.3202 | 5.3198 | 5.3203 | 5.3173 | 5.3181 | 5.3207 | 5.3252 | 5.3351 | 5.3581 | 5.3953 | 5.4488 | 5.5369 | 5.6739 | 5.8996 | 6.2742 | 6.8503 | 7.8048 | 9.3968 | 12.0822 | 16.9628 | 26.67 | 49.2694 | 115.4899 | 359.0105 | 1504.5773 | 7840.0226 | 33073.8642 | 97221.9115 | 191810.4099 | 308912.9953 | 428059.3925 | 545051.5856 | 643176.3128 | 714967.5458 | 760714.7807 | 783145.2819 | 775222.9638 | 746858.2613 | 694774.4601
Loss increases with temperature due to decreasing Jc
Big loss increase when
I0 = 6 kA > Ic
Applied current amplitude I0 = 6000 A for all calculations
Circular cable of 120 tapes/filaments with 0.2 mm width on 8 mm diameter core
0.2 mm
0.2 mm
0.2 mm
0.2 mm
0.2 mm
T =

## Slide 10: Extrapolation to a full ReBCO based RCS fast-ramping dipole magnet
Chart: Temperature [K]
| 15 | 20 | 25 | 30 | 35 | 40 | 45
Q [J/m] | 0.1295 | 0.14577 | 0.16611 | 0.19082 | 0.21208 | 0.95907 | 115.4898
Case:
Jc(B,T) of SuperPower tape (RI data)
Layout 120 tape/filaments, 0.2 mm wide
Applied current 6 kA, applied field 0.2 T
Loss/cycle per sub-cable 0.1-0.2 J for T < 35 K
Full magnet power:
Multiply with number of sub-cables in the cross-section (24) and 5 Hz repetition rate
This value is conservative as not all turns experience 0.2 T
Achieving 15 to 25 W in 15 to 30 K range
Slight increase with T due to Jc drop
Large increase when
Ic < I0 = 6 kA
Chart: Temperature [K]
| 15 | 20 | 25 | 30 | 35 | 40 | 45
P [W/m] | 15.5403 | 17.4928 | 19.9332 | 22.899 | 25.4492 | 115.0882 | 13858.7805
B0 = 0.2 T, I0 = 6 kA
B0 = 0.2 T, I0 = 6 kA

## Slide 11: What level of AC loss acceptable for energy saving?
Chart: Temperature [K]
| 1 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 110 | 120 | 130 | 140 | 150 | 160 | 170 | 180 | 190 | 200 | 210 | 220 | 230 | 240 | 250 | 260 | 270 | 280 | 290 | 300
P_res [W/m] | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000 | 2000
P_max (ideal cooling) [W/m] | 6.6666 | 66.6664 | 133.3329 | 199.9993 | 266.6658 | 333.3322 | 399.9987 | 466.6651 | 533.3316 | 599.998 | 666.6644 | 733.3309 | 799.9973 | 866.6638 | 933.3302 | 999.9967 | 1066.6631 | 1133.3296 | 1199.996 | 1266.6624 | 1333.3289 | 1399.9953 | 1466.6618 | 1533.3282 | 1599.9947 | 1666.6611 | 1733.3276 | 1799.994 | 1866.6604 | 1933.3269 | 1999.9933
P_max (realistic cooling) | 1.9093 | 19.5121 | 39.9999 | 61.5382 | 84.2102 | 108.1077 | 133.3328 | 159.9994 | 188.2345 | 218.1809 | 249.9989 | 283.8697 | 319.9985 | 358.619 | 399.998 | 444.4421 | 492.305 | 543.997 | 599.9965 | 660.8655 | 727.2681 | 799.9947 | 879.9938 | 968.4139 | 1066.6584 | 1176.4609 | 1299.9886 | 1439.9866 | 1599.984 | 1784.5962 | 1999.9767
120x0.2 mm cable, with SuperPower Jc(B,T) | 15.5403 | 17.4928 | 19.9332 | 22.899 | 25.4492 | 115.0882 | 13858.7805
120x 0.2 mm layout yields AC loss below maximum cryogenic heat load for 15 K < T < 35 K !
Conductor loss for resistive option
Maximum cryogenic heat load with ideal cooling
Maximum cryogenic heat load with more realistic cooling
Initial AC loss calculations
120x 0.2 mm AC loss

## Slide 12: Conclusion & outlook
We calculated hysteresis loss by analytical an numerical methods. There will be other contributions to the cryogenic heat load: coupling loss, eddy current loss, heat leaks, etc.
Hysteresis loss strongly increases with perpendicular field, to be minimized through optimal conductor placement and yoke design
Further reduction by reducing tape width and/or use filamented conductors as
Hysteresis loss decreases with increasing Jc for low field amplitudes and increases with increasing Jc for high amplitudes of magnetic field
Case presented: round conductor with 120 filaments, 0.2 mm wide yields < 30 W hysteresis loss showing potential for saving energy compared to the resistive option