## Slide 1: Metallurgy and Material Science at CERN
Anité Pérez CERN EN-MME-MM

## Slide 2: Metallurgy and Materials Science at CERN
  It covers metals, ceramics, polymers, composites…These materials are crucial for advancing technologies in all fields (energy, medicine, transport, computing…) and in accelerators
  The Materials service at CERN assists colleagues in studying existing materials (bulk, powder, 3D printed, coatings) and developing new ones to address engineering challenges within the scientific community
  Our main task as materials experts at CERN is to understand the structure and properties of the materials and predict/understand their performance in the accelerator environment as a function of their processing
Materials, Metrology and Non-Destructive Testing (MM) Section | EN-MME-MM (cern.ch)

## Slide 3
SEM-based microanalysis: Energy Dispersive X-ray Spectroscopy (EDS)
Requirements:
Specimen SEM inspectable
Non volatile/ hazarous particles
Nanometric to micrometric
Particles analysis at CERN
Microscopic characterization at CERN
Chemical analysis
Some examples of techniques
Topography analysis
Cross section
3D FIB Tomography
At CERN we need to characterize this internal structure (that can be crystalline or amorphous) and we need tools able to image in the nanometric to millimetric range
What is Microstructure?
What is Microscopy?

## Slide 4
100 µm
  Sometimes the optical microscopy is enough to visualize what we want (~ 1 µm), and sometimes more resolution is needed
4
Microscopic characterization at CERN: Topography
OM

## Slide 5
  Sometimes the optical microscopy is enough to visualize what we want (~ 1 µm), and sometimes more resolution is needed
  Scanning Electron Microscopes (SEMs) are used to evaluate the surface at the nanometric level including analysis of X-rays emitted by the matter in response to being hit with charged particles  Energy Dispersive X-ray Spectroscopy (EDS)
5
Microscopic characterization at CERN: Topography
100 µm
Microscopy
SEM
SAMPLE
Detector
OM

## Slide 6
  Sometimes the optical microscopy is enough to visualize what we want (~ 1 µm), and sometimes more resolution is needed
  Scanning Electron Microscopes (SEMs) are used to evaluate the surface at the nanometric level including analysis of X-rays emitted by the matter in response to being hit with charged particles  Energy Dispersive X-ray Spectroscopy (EDS)
6
Microscopic characterization at CERN: Chemical analysis
100 µm
SEM
2 mm
OM
Investigation of the phases present into welds that are working at 4 K
EDS
Superconducting Nb3Sn cables before reaction as part of the QA/QC at CERN

## Slide 7
  Sometimes the optical microscopy is enough (~ 1 µm) to visualize what we want, and sometimes more resolution is needed
  Scanning Electron Microscopes (SEMs) are used to evaluate the surface at the nanometric level including analysis of X-rays emitted by the matter in response to being hit with charged particles  Energy Dispersive X-ray Spectroscopy (EDS)
  Focused Ion Beam (FIB) combined with SEM is used to characterize near surface microstructure and features
7
Microscopic characterization at CERN: FIB cross section
Installation of Laser Engineered Demonstrator Chamber in the LHC | High Luminosity LHC Project (cern.ch)
Surface treated with laser (LESS) as a novel solution for the in-situ treatment of the LHC beam screens for HL-LHC project to reduce the secondary electron yield (SEY)

## Slide 8
  Sometimes the optical microscopy is enough (~ 1 µm) to visualize what we want, and sometimes more resolution is needed
  Scanning Electron Microscopes (SEMs) are used to evaluate the surface at the nanometric level including analysis of X-rays emitted by the matter in response to being hit with charged particles  Energy Dispersive X-ray Spectroscopy (EDS)
  Focused Ion Beam (FIB) combined with SEM is used to characterize near surface microstructure and features
8
Microscopic characterization at CERN: FIB cross section
Installation of Laser Engineered Demonstrator Chamber in the LHC | High Luminosity LHC Project (cern.ch)
SEM
FIB
SAMPLE

## Slide 9
  Sometimes the optical microscopy is enough (~ 1 µm) to visualize what we want, and sometimes more resolution is needed
  Scanning Electron Microscopes (SEMs) are used to evaluate the surface at the nanometric level including analysis of X-rays emitted by the matter in response to being hit with charged particles  Energy Dispersive X-ray Spectroscopy (EDS)
  Focused Ion Beam (FIB) combined with SEM is used to characterize near surface microstructure and features
9
Microscopic characterization at CERN: 3D FIB-tomography
20 µm
Installation of Laser Engineered Demonstrator Chamber in the LHC | High Luminosity LHC Project (cern.ch)
SEM
FIB
SAMPLE

## Slide 10
Microscopic characterization at CERN: Other applications
Testing of new materials: Carbon foams for the new Inner Tracking System (ITS3) for ALICE ITS upgrade. The goal is to use ultra-lightweight spacers, made of carbon foam to reduce the total weight of the experiment
Reverse Engineering: To analyse and gain knowledge about the way something works, and which materials were used to build it because we need to manufacture it again or to evaluate the irradiation effect (ex. commercial CMOS)
Failure analysis: Technical procedure to investigate the root cause of failure of a product or equipment during the design, manufacturing or service process (ex. Silicon module on ATLAS ITK stave failed during cooling test)

## Slide 11
304L stainless steel with 23% deformation at 4K
316LN stainless steel with 32% deformation at 4K
The strain-induced martensitic content in the grades 316LN at a given temperature and for the same level of plastic strain, is much lower than in the grade 304 L.
Martensite (BCC)
Austenite (FCC)
Microscopic characterization at CERN: Cryogenic studies
observation of the dislocation substructure in the vicinity of a shear band formed in the single crystal during deformation

## Slide 12: Summary
GENERAL:
The Materials service provides support to anyone at CERN that wants to study or control materials.
Metals, polymers, ceramics and composites are the most frequent in bulk, powder or coating format.
MICROSCOPY TECHNIQUES:
Different systems and techniques are available in the service to extract precise information in the nanometric to micrometric scale about morphology, chemistry and internal structure
APPLICATIONS:
Quality control, new materials research, new developments and technology, medical devices, reverse engineering, failure analysis…
19-Mar-24
Notes: For FCC, simulations are required to understand if such small macro-particles could cause unacceptable beam losses.

## Slide 13
Thanks for your attention!