## Slide 1: Joint Modelling Updates
D. Rinaldoni, B. Bordini
02/08/2024

## Slide 2
Analytic Study on Contact Resistance
wCu=10 µm, hCu=15 µm
RRR | Rct (µΩ cm2)
1 | 0.679
5 | 0.224
10 | 0.134
20 | 0.075
40 | 0.040
hCu
hCu
wCu
Chart: Rct (µΩ cm2)
| 1 | 5 | 10 | 20 | 40
R_ct | 6.7889e-11 | 2.241e-11 | 1.3384e-11 | 7.4824e-12 | 3.9717e-12
Values for HTS tape ~ 10 µΩ cm2 (Yoon et al.)
We lose 2-3 orders of magnitude
Thickness 80 µm
Width 4 mm
T = 4.2 K

## Slide 3
Analytic Study on Contact Resistance
wCu=10 µm, hCu=15 µm
RRR | Rct (µΩ cm2)
1 | 0.679
5 | 0.224
10 | 0.134
20 | 0.075
40 | 0.040
Chart: Rct*RRR
| 1 | 5 | 10 | 20 | 40
R_ct*RRR | 6.7889e-11 | 1.1205e-10 | 1.3384e-10 | 1.4965e-10 | 1.5887e-10

## Slide 4
wCu=10 µm, hCu=15 µm
RRR | Rct (µΩ cm2)
1 | 0.679
5 | 0.224
10 | 0.134
20 | 0.075
40 | 0.040
Changing the Copper thickness:
wCu=20 µm, hCu=25 µm
RRR | Rct (µΩ cm2)
1 | 0.481
5 | 0.084
10 | 0.048
20 | 0.024
40 | 0.013
wCu=30 µm, hCu=35 µm
RRR | Rct (µΩ cm2)
1 | 0.293
5 | 0.022
10 | 0.012
20 | 0.006
40 | 0.003
Analytic Study on Contact Resistance

## Slide 5
wCu=0 µm , hCu=15 µm
Analytic Study on Contact Resistance
wCu=10 µm, hCu=15 µm
RRR | Rct (µΩ cm2)
1 | 0.679
5 | 0.224
10 | 0.134
20 | 0.075
40 | 0.040
RRR | Rct (µΩ cm2)
1 | 0.691
5 | 0.616
10 | 0.616
20 | 0.616
40 | 0.615
We gain at maximum 1 order in the case of etched tape.
Remark: True only for joints (Cu+Ha), not for the HTS tape  In that case Rct increases more because of the buffer layers.

## Slide 6
RRR | Rin (µΩ) | Rout (µΩ)
1 | 0.727 | 0.239
5 | 0.240 | 0.079
10 | 0.143 | 0.047
20 | 0.080 | 0.026
40 | 0.046 | 0.014
We can estimate the radial resistance of the entire joints:
Analytic Study on Contact Resistance
N | Rin (µΩ) | Rout (µΩ)
5 | 0.060 | 0.020
10 | 0.111 | 0.036
20 | 0.214 | 0.069
30 | 0.321 | 0.101
50 | 0.543 | 0.165
Njoints = 7
RRR = 20

## Slide 7
Ongoing Studies
Currently working on the fully 3D model aiming to know the current distribution in the joints in 3D.

## Slide 8: Thank you for your attention. Questions?