## Slide 1: Pancakce 1&2 and Stacks 01&02 measurements High-field solenoid technology for the Muon Collider
ABDEL HAFIZ Mahmoud
02/08/2024

## Slide 2: Stacks
Stack 01 & 02
132 tapes
Stack soldered to copper plate with BiSn solder (melting temperature 137°C)
4 insulating screws to apply small pressure and prevent from delamination
Stack 02 showed that screws are unnecessary
Magnetic stirrer
Ohmmeter self-resistance 40
Crocodile plug for stack 01
Soldered voltage tape for stack 02

## Slide 3: Stack 02 – resistance before etching
Resistance mesured before etching
Sample in LN
Value here has a low reliability has it is a 2 points measurements.
Please consider evolution of the resistance

## Slide 4: Stack 01 – transverse resistance during the etching
Program shut down for a few minutes
Part 1

## Slide 5: Stack 01 & 02 – resistance during etching
Stack 02
Stack 01

## Slide 6: Stack 01 & 02 – cycles after etching
Stack 02
Stack 01

## Slide 7: Stack 01 & 02 – Microscopic observations
Stack 01 after etching ~ 500
Stack 02 after etching ~ 0.5

## Slide 8: Stack 01 – Microscopic observations
Stack 02 after etching + brushing ~ 15
Stack 02 after etching + (more) brushing ~ 150

## Slide 9: Pancakes set up
R_Shunt
R_series
R_T
L
Hall probe
U3
R_cables
R_cables_2
U1
U2
In case of protection needed

## Slide 10: Pancake 1

## Slide 11: Pancake 2
Longer copper plates (current leads)
Plates welded to copper ring
Voltage tape slots dedicated
Copper inner ring soldered to mandrel (highly improving joint resistance)

## Slide 12: Pancake 1 & 2 – Compare IC

## Slide 13: Pancake 1 & 2 – Compare Time constant
 | Pancake 2 | 
 | Charge | Discharge
5 A | 4.87 | 4.92
10 A | 4.70 | 5.05
20 A | 4.78 | 5.02
50 A | 4.60 | 4.83
 | Pancake 2 | 
 | Charge | Discharge
5 A | 4.87 | 4.92
10 A | 4.70 | 5.05
20 A | 4.78 | 5.02
50 A | 4.60 | 4.83
 | Pancake 1
 | Charge
20 A | 4.85
40 A | 4.27
60 A | 4.18
80 A | 4.06
 | Pancake 1
 | Charge
20 A | 4.85
40 A | 4.27
60 A | 4.18
80 A | 4.06

## Slide 14: Pancake 1 – Compare Time constant
Etching
  Whole pancake drowned into iron chloride
  Cleaned into water
  Dried with pressurized air
Brushing
  Brushed after ~ 1 month with electrical drill like brush

## Slide 15: Pancake 1 – Compare IC
Slow ramp rate
  0.02 A/s to 0.1 A/s
  Cleaned into water
  Dried with pressurized air

## Slide 16: Pancake 1 – Shape of voltage during ramp
Before brushing
After brushing

## Slide 17: Pancake 2 – Compare Time constant
Etching
  Parts protected with silicon coating
  Whole pancake drowned into iron chloride
  Cleaned into sodium becarbonate
  Dried with pressurized air
  Cleaned with acetone
  Cleaned with water
  Dried with pressurized air
 | Pancake 2 after etching |  |  | 
 | Charge | Discharge | Charge 2 | Discharge 2
5 A | 41.8 | 28.2 | 42.2 | 29.8
10 A | 40.6 | 51.4 |  | 
20 A | 30.4 | 43.1 |  | 
30 A | 36.4 | 40.7 | 34.1 | 41.1
40 A | 50.4 | 45.4 | 44.8 | 41.2
50 A | 51.8 | 50.5 |  | 
 | Pancake 2 after etching |  |  | 
 | Charge | Discharge | Charge 2 | Discharge 2
5 A | 41.8 | 28.2 | 42.2 | 29.8
10 A | 40.6 | 51.4 |  | 
20 A | 30.4 | 43.1 |  | 
30 A | 36.4 | 40.7 | 34.1 | 41.1
40 A | 50.4 | 45.4 | 44.8 | 41.2
50 A | 51.8 | 50.5 |  | 
 | Pancake 2 | 
 | Charge | Discharge
5 A | 4.87 | 4.92
10 A | 4.70 | 5.05
20 A | 4.78 | 5.02
50 A | 4.60 | 4.83
 | Pancake 2 | 
 | Charge | Discharge
5 A | 4.87 | 4.92
10 A | 4.70 | 5.05
20 A | 4.78 | 5.02
50 A | 4.60 | 4.83

## Slide 18: Pancake 2 – Compare IC
Post treatment to be continued …