## Slide 1: Overview of tests of ReBCO stacks and coils
C. Accettura
Final Cooling Progress Meeting
https://indico.cern.ch/event/1390350/
22/11/2024, CERN

## Slide 2: Tomography
3 additional stacks were tested
  S5 133 stacked tapes from THEVA
  S7107 stacked tapes from Fujikura
  S8123 stacked tapes from Fujikura
Results significantly worst compared to the previous one (THEVA)
EDMS 3181512

## Slide 6: Tomography
What is the origin of the problem?
  Difference status of copper surface (oxidation, grain size) impact the adhesion of coating
  Coating process not reproducible
  Problem during thermal treatment

## Slide 7: Planning of test
Stacks:
  Sample 2 THEVA (good)--> optical to check where is the failure, solder quantity
  Sample 7 Fuji (bad)--> optical to check where is the failure, solder quantity
Tape:
  Theva uncoated 10cm--> SEM+FIB copper structures, impurities, oxide
  Fuji uncoated--> SEM+FIB copper structures, impurities, oxide
  Theva coated A--> XRF to check homogeneities, coating thickness
  Theva coated B--> XRF to check homogeneities, coating thickness
  Fuji coated A--> XRF to check homogeneities, coating thickness
  Fuji coated B--> XRF to check homogeneities, coating thickness