## Slide 1
Thin Film Superconducting Cavities For Sustainable Accelerators
Daniel Seal
daniel.seal@stfc.ac.uk

## Slide 2
1. Our Goal
2. Thin Film Development
3. Thin Film Testing
4. Future
Agenda

## Slide 3
1. Our Goal

## Slide 4
Bulk Nb Dominates SRF
Image © STFC John Dawson
Courtesy of C. Antoine (CEA)
Bulk Nb
  Highest Tc, Bc1, Bsh of any element
  Large Q0 (1010- 1011)
  CW operation
Bulk Nb has reached limits:
Q0 > 1010
Eacc > 50 MV/m
(1.3 GHz, 2 K)
Q0
Eacc
Nb : Limits @ 2 K, 1.3 GHz :
Accelerating gradient, Eacc ~ 55 MV/m (± 5 MV/m)
(Geometry : B/Eacc ~ 4.2 mT/(MV/m))
Surface resistance, Rs = RBCS + Rrés.
High field dissipations
Quench
P = const, ↑
Investment +
Power consumption
Q0 ↑ Costs ↓
Investment
Eacc ↑ Costs ↓
Aimed performance
Present state
Eacc  BRF  Bsh
Notes: SC cavity are intensively used for accelerating charged particles, but bulk Nb cavities are ay their performance limit Eacc  BRF  BSH and Q0  1/RS .
We aim to increase both Eacc and Q0. for this we have to look for new solutions.

## Slide 5
From Bulk Nb To Thin Films
Image © STFC John Dawson
Image courtesy: C. Antoine
Protection, low secondary emission yield
High Tc SC
S-I-S multilayers
Structure, high thermal conductivity (Copper ?)
External layer, optimized for thermal transfer
High purity Niobium Optimized only for thermal conduction
Native oxide
Unstable upon annealing
RF side
Helium side
Today
Future ?
Niobium or…
Native oxide
Not optimized for thermal transfer
Courtesy of C. Antoine (CEA)
Notes: Shallow penetration depth of RF fields
Can decouple RF surface from cavity support structure
Drastic cost reduction

## Slide 6
Superconductors Being Considered
Material | Tc (K) | Bsh (mT)@ 0 K
Pb | 7.1 | 100
Nb | 9.2 | 219
NbTiN | 17.3 | 439
V3Si | 17.0 | 490
NbN | 17.3 | 214
Nb3Sn | 18.3 | 425
Nb3Al | 18.5-19.1 | 
MgB2 | 39.0 | 170
High Bsh  High Eacc  fewer cavities
High Tc  High Q0  less cooling
Why thin film on copper?
Cheaper than Nb
Higher thermal conductivity
Easily machinable
Courtesy of C. Antoine (CEA)
Notes: Add different materials beyond Nb

## Slide 7
Saving Energy For Future Accelerators
Image © STFC John Dawson
Moving from 2 K to 4.5 K reduces cryogenic power by factor 3!
S. Posen, Supercond. Sci. Technol. 30 (2017) 033004
2 K (Bulk Nb)
4.5 K (Thin Film)
Infrastructure
Operation
C. Z Antoine: IPAC2023
Estimated cryogenic costs of ESS (M€):
40
25
4
11
Notes: Nb3Sn low surface resistance operation at higher temperatures than Nb
Inverse coefficient of performance – watts of wall power to remove 1 watt of heatn- accounts for Carnot efficiency (4.5 K more efficient than 2 K)
Liquid helium system rather than superfluid helium makes cryogenic system simpler, easier maintenance, fewer pumps, no 2K return line etc – infrastructure cost
Decrease plug power by factor 3 - operation cost
Reduce cost of cryogenic plant – 2 K He not needed

## Slide 8
2. Thin Film Development

## Slide 9
Thin Film Pathway
Cavity Forming
Surface Polishing
SC property evaluation
RF test
SC Film Coating &
Surface Analysis
Post Treatments
Initial testing on planar samples
Aim: Produce a prototype, high performance 1.3 GHz thin film SRF elliptical cavity Q0 > 1010 @ 4.5 K

## Slide 10
Surface Polishing
At STFC:
  Some mechanical polishing
  Diamond turning (DT)
IFAST Partners:
  Mechanical polishing;
    Tumbling
    Metallographic (MP)
  Chemical polishing
    SUBU
    Electropolishing (EP)
    Plasma Electrolytic Polishing (PEP)
MP Cu Disk
In development at STFC
Green alternative
MP Nb Disk
DT Cu Disk
SUBU Cu Choke Cavity
PEP Quadrupole Resonator (QPR)
PEP 6 GHz Cavity
Courtesy of E. Chyhyrynets & C. Pira (INFN)

## Slide 11
Thin Film Depositions - Planar Samples
QPR samples for high RF field analysis
Sample disks for mass parameter optimisation
Planar samples provide a cost-effective pathway for thin film R&D
X-ray Photoelectron Spectroscopy
Scanning Electron Microscopy
Secondary Ion Mass Spectrometry
White Light Interferometry
Notes: Characterisation facilities

## Slide 12
Thin Film Depositions - Planar Samples
Nb3Sn on 50-100 mm substrates
  Theoretical Tc = 18 K
  DC, HiPIMS
  Effect of magnetron power, deposition temperature
Chart: T (K)
 | 17.449 | 0.012
 | 0.01
 | 17.449 | 0.012
 | 0.01
  Can Nb3Sn sputtering match or exceed performance of Sn vapour diffusion into bulk Nb?
Chart: Magnetron power (W)
| 200 | 100 | 50
RF | 16.4 | 16.5 | 17.4
VSM (RAL) | 16.05 | 16.5 | 16.95
VSM (IEE) | 16.8 | 16.8
Effect of DC magnetron power
XPS comparison of Nb3Sn/Cu (~ few nm depth)
SIMS on 100 W HiPIMS
Nb
Sn
Cu
SEM – high grain density
~ 2 μm
Four point probe
Notes: To reduce fabrication cost

## Slide 13
600 c
800 c
800 c
Thin Film Depositions - Planar Samples
V3Si on 10 mm substrates
  Theoretical Tc = 17 K
  Initial steps to improve Tc and consistency of growth
  Post-annealing required – furness, laser, flash lamp
C. Benjamin et al. V3Si: An alternative thin film material for superconducting RF cavities, IPAC 24
  Is V3Si a viable alternative material?
Effect of heater power on Tc
Effect of post-deposition annealing
XRD V3Si/Nb
SEM – small crystallites

## Slide 14
Thin Film Depositions – 6 GHz Cavities
  Are performances on flat geometries repeatable on curved geometries?
  Closed Seamless Cavities
  Open Split Cavities
Nb, NbTiN, Nb3Sn, V3Si
ms-Flash Lamp Annealing at HZDR
Planar magnetron
Cylindrical magnetron
Deposition facility
Courtesy of S. Prucnal & S. Zhou (HZDR)
Nb target with Ti wire
Notes: Copper drawn from a single sheet rather than welded

## Slide 15
Thin Film Depositions – 1.3 GHz Cavities
Optimising thin film deposition parameters
  Mainly Nb thin films so far
  Comparing deposition techniques (DCMS, HiPIMS)
  Plasma diagnostic studies
  Can we achieve uniform coatings on larger cavity structures?
S. Simon et al. Tailoring the production of Nb superconducting films for SRF cavities: mass/energy spectroscopy and film characterisation, IPAC 24
Mass scan at 10-3 mbar
Ion energy distribution function of Nb+ at 10-3 mbar
Notes: Analysis of positive ions for DC and HiPIMS deposition techniques – lower pressure favours production of positive ions with higher ion energy

## Slide 16
3. Thin Film Testing

## Slide 17
DC Superconducting Properties
Rapid sample tests with multiprobe inserts
Is the sample superconducting?
What is its Tc?
What is its behaviour under high magnetic fields?
Four-point probe measurements with alternative materials
Magnetic field penetration with Nb
Four-point probe
Magnetic Tc
Magnetic Field Penetration
20 tests per week!
D. Seal et al. Upgraded multiprobe sample inserts for thin film SRF cavity developments, IPAC 24
Notes: All systems are closed cycle cryocoolers

## Slide 18
DC Magnetic Field Penetration
Cavity-like DC fields applied:
  Parallel
  From one side (unlike SQUID VSM)
  B < 600 mT
Recently upgraded facility:
  Test 10 cm samples size and 6 GHz split cavities
  Magnetic shields
  Minimal damage to films
V3Si/Nb/Cu Sample
Meissner state when R = 1
3 tests per week!
Is there a correlation between DC & RF performance?

## Slide 19
RF Test With Choke Cavity
7.8 GHz Choke Cavity
Low field measurements:
  Rs vs Bsample, pk
  Rs vs Tsample
  Penetration depth vs Tsample
Mass parameter optimisation prior to:
  High field/low frequency tests with QPR
  Cavity tests
3 tests per week!
Chart: Deposition Temperature (°C)
| 23 | 240 | 339 | 465 | 555 | 614
Target 1 (4 hr) | 55.0265 | 87.2169 | 31.4215 | 21.0079 | 13.1185 | 41.7822
Target 2 (4 hr) | 39.2252 | 14.6783 | 11.8812 | 16.5761 | 7.2629 | 16.6009 | 4.3344
BCS | 1.533 | 1.533 | 1.533 | 1.533 | 1.533 | 1.533
Effect of magnetron power on Nb3Sn/Cu
Effect of deposition temperature on Nb/Cu
Most importantly, how does the thin film perform under RF conditions?

## Slide 20
Low Power Cavity Testing
Courtesy of O. Poynton & J. Rigby
Cryocooler based facility
P < 2.5 W, T > 4 K (est.)
Quick first cavity test
Good cavities will have high power test in LHe
4 types of cavity
1.3 GHz closed
1.3 GHz split (in development)
6 GHz closed
6 GHz split
First tests autumn 2024!
Feedthroughs for RF, wiring etc
1.3 GHz cavity
6 GHz split cavity
Adapter for heat links
Cold head

## Slide 21
High Power Cavity Testing
Courtesy of T. Sian & C. Hill
Full Q0 vs Eacc test with LHe
Testing with existing STFC/DL LHe infrastructure mainly used for ESS & PIP-II cavity tests
Upgrades now allow for:
A RF single system for 650 MHz, 700 MHz and 1.3 GHz
P ≤ 200 W, T = 2 K & 4.2 K
Capability for 9-cell tests
Existing SRF Test Facilities at Daresbury Laboratory
First tests summer 2024!

## Slide 22
4. Future

## Slide 23
The Future of Thin Film SRF in the UK
Continuing R&D
Thin film coatings
Post-processing
Quick sample testing
Split cavities
Multi cells
Cavity testing
UK XFEL
ISIS II
FCC
ILC
Loaded test in CLARA
Reduce capital and running costs of accelerators!

## Slide 24
Acknowledgements
STFC/CI: O. B. Malyshev, R. Valizadeh, C. Benjamin, O. Poynton, J. Rigby, A. Akintola, T. Sian, L. Smith, J. Conlon, C. Benjamin, S. Pattalwar, G. Miller, A. Blackett-May, A. Vick, C. Hill, M. Pendleton, M. Jones, P. Smith, A. Wheelhouse, D. Mason
Lancaster University/CI: G. Burt, N. Leicester, H. Marks, A. Mogheyseh
University of Liverpool/CI: S. Simon, J. Bradley
INFN: C. Pira, E. Chyhyrynets​, D. Ford, A. Salmaso
IJCLAB: D. Longuevergne, O. Hryhorenko​
CEA: C. Antoine
IEE: E. Seiler, R. Ries
HZDR: S. Prucnal, S. Zhou

## Slide 25
@STFC_matters
Science and Technology Facilities Council
Science and Technology Facilities Council