## Slide 1
Alvaro Romero Francia, Tina Griesemer, Rui Franqueira Ximenes, Mike Parkin [SY-STI-TCD]
[HI-ECN3 BDF Target & target complex initial review]:
Looking ahead – Target alternative designs

## Slide 2: HI-ECN3 BDF target initial review
Baseline design.
Alternative designs:
    Removed water channels.
    The full W target.
    The full W target – exploring other options.
    In-beam tests
Conclusions.

## Slide 3: WP3 – BDF Target design
BDF Target water cooling layout (20bar, 5m/s)
13 x TZM blocks (580 mm)
5x W blocks (780 mm)
1.5 mm
⌀250 mm
25-350 mm
Ta2.5W cladding
Baseline beam parameters of the BDF Target operation.
~ 4.0×1019 p+/y
Target will become an extremely radioactive device!
~100 Sv/h after few hours of cool-down
Baseline design
Baseline design is robust with thorough design report https://doi.org/10.23731/CYRM-2020-002, representative in-beam tests, PIE plus HIP & other testing.

## Slide 4: WP3 – BDF Alternative Target design requirements
4
Physics drivers
Particle production
    Want particle interactions with High Z materials, especially in the shower region –large effect. W > TZM > Cu
    -Replacing upstream TZM with W would be beneficial, even if this needs more cooling channels
      Overall density of target (including water channels) is not so important
  Background signal
    Capture all electromagnetic shower particles in the target – Need sufficient target ø and density
Operations drivers
Activation products of water
Production of Hydrogen
Thermal management & engineering drivers
Want lots of cooling channels in the shower region! (reduces overall ρ)
Want lots of high thermal conductivity materials in the shower region, eg copper (reduces ρ & Z)
Want to reduce target ø.
Want to reduce plate thicknesses (reduces overall ρ)
Want improved Tungsten grain structure
Now is an opportunity to explore alternative designs.
Reduce volume of water, especially in the beam & shower

## Slide 5: WP3 – BDF Target design
Alternative design – proven concepts

## Slide 6: WP3 – BDF Target design
→ Using what the section’s learnt experience
Drivers:
Reduce the amount radiolysis-produced free hydrogen gas (ATEX)
Reduce activation of the water (less water) and of the target (less Ta), and decay heat (less Ta)
Reduce contamination risk of water & W spallation products -(stronger and thicker external shroud instead of thin cladding)
Shorter target will simplify waste packaging and disposal.
Increase physics performance. (overall denser without water channels)
Alternative designs
Next slides
Based on L4 main dump
Based on SPS internal dump
TZM
TZM
W
W

## Slide 7: WP3 – BDF Target design
Alternative design – Initial approach
1. Is it beneficial to have the blocks in contact or not?
Contact (perfectly bonded)
Gap (not bonded)
Diluted beam
Sweep
OR
…These options were explored in the 26th SHiP Collaboration Meeting, by T.Griesemer
Contact (not bonded)
PREMATURE MODELS with assumptions and simplifications
2. Diluted or sweep beam?

## Slide 8: WP3 – BDF Target design
Contact (perfectly bonded): the stress distribution along the beam axis is homogeneous. On average, the equivalent stresses are lower.
Contact (not bonded): High stress gradients in single blocks.
Gap (not bonded): Higher temperatures, stress reduction is negligible compared to the perfectly bonded case.
→ Having the blocks bonded is best option
Blocks in Contact with perfect thermal bonding
Cooling water at circumference uses 10 000 W/m2.K calculated using original water flow rate of baseline.
Temperature after 1 pulse [°C]
Equivalent stresses after 1 pulse [MPa]
PREMATURE MODELS with assumptions and simplifications
Alternative design – TZM&W blocks, TZM shell
Contact (perfectly bonded)
Gap (not bonded)
Contact (not bonded)
Steady State + One Pulse
35mm centre beam

## Slide 9: WP3 – BDF Target design
Sweep
Diluted beam
Position in radial axis [mm]
Temperature [°C]
Maximum Temperature in Block 6
Diluted beam Sweep
Max Temp: 700 °C
Max Temp: 900 °C
Alternative design – TZM&W blocks, TZM shell
1000
0
120
PREMATURE MODELS with assumptions and simplifications
Transient models
At plane of location of highest temperature

## Slide 10: WP3 – BDF Target design
The sweep significantly reduces the peak temperature compared to the diluted beam (Δ200⁰C)
The sweep reduces peak equivalent stresses by 70 MPa (down to 130 MPa) compared to diluted centrebeam
Equivalent stresses after 1 pulse
Center
Shell
Equiv. Stress [MPa]
Equiv. Stress [MPa]
Position in beam axis [mm]
Position in beam axis [mm]
Diluted beam Sweep
Diluted beam Sweep
PREMATURE MODELS with assumptions and simplifications
It is beneficial to have the blocks in contact.
The swept beam reduces the peak temperatures & stresses.
How would a full W target behave using this design?...
Alternative design – Initial approach
350
0
400
0

## Slide 11: WP3 – BDF Target design
Alternative design – The full W target
Max energy deposition (J/cm^3)

## Slide 12: WP3 – BDF Target design
Alternative design – The full W target
Water cooling
Water cooling
Beam direction
All W! 10-mm slices
TZM shell
Full W compact target, encased in an actively cooled TZM shell.
The TZM discs in the baseline design are replaced with W. – Good for physics
The water-cooling channels in the baseline design are removed. – Good for operations
To achieve efficient heat evacuation, the W slices and the TZM shell are diffusion bonded by means of hot isostatic pressing (HIP). – better grain structure for mechanical properties
The thickness of the W slices is limited to the maximum capability through cold rolling.
TZM
W
W
TZM

## Slide 13: WP3 – BDF Target design
Thermal simulation
W recrystallizes at 1200-1300
Plastic deformation
Eq.Stress [MPa]
Eq.Plastic strain [mm/mm]
Steady state simulations!
These are steady state simulations. After each spill from steady state temperature, the temperature may raise up to 1100
Structural simulation
Very high mechanical stresses, with beam-induced plastic deformation in the upstream W
Alternative design – The full W target
Temperature [Cº]

## Slide 14: WP3 – BDF Target design
Alternative design – The full W target
A full W target core has improved physics performance…
..but the temperature in the W discs, and the beam-induced mechanical stresses must be reduced
- Currently, we are exploring alternatives to optimize the design of the full W target…

## Slide 15: WP3 – BDF Target design
Alternative design – The full W target (exploring other options)
Water cooling
Water cooling
Beam direction
Single core W-target TZM shell
To improve the mechanical behavior in the W core.
W-target – Ta shell
To improve the mechanical behavior in the shell.
W-target – TZM shell
+ Upstream cooling
To reduce the upstream temperatures and therefore, beam-induced stresses.
Alternative designs: Full W core
H2O
H2O
H2O
H2O

## Slide 16: WP3 – BDF Target design
Water cooling
Water cooling
Beam direction
Single core W-target TZM shell
Similar stresses in core.
Ta shell
Unacceptable mechanical stresses for Ta.
TZM shell + Upstream cooling
Temperature reduction.
Temperature [Cº]
Eq.Stress [MPa]
Eq.Stress [MPa]
Alternative design – The full W target (exploring other options)
Alternative designs: Full W core

## Slide 17: WP3 – BDF Target design
Beam direction
Gold sheets in peak energy density deposition
Enhance heat evacuation with two gold sheets in the location with the highest peak energy density deposition, while keeping the interaction length.
1-mm Copper slices between each W sheet
Enhance the heat evacuation in the upstream of the target
The full Gold target
Enhance heat evacuation a full gold target while increasing the interaction length
Water cooling
Water cooling
Alternative design – The full W target (exploring other options)
H2O
H2O
H2O
Alternative designs: Full W core with internal sheets

## Slide 18: WP3 – BDF Target design
Beam direction
Gold sheets in peak energy density deposition
Temperature reduction
1-mm Copper slices between each W sheet
Temperature reduction
The full Gold target
Temperature reduction
Temperature [Cº]
Temperature [Cº]
Temperature [Cº]
Water cooling
Water cooling
Alternative design – The full W target (exploring other options)
Alternative designs: Full W core with internal sheets

## Slide 19: WP3 – BDF Target design
Beam direction
Ta pipe in the center with Water cooling
To enhance the heat evacuation by introducing a HIP Ta pipe in the center of the target.
Copper insert in the center
To conduct the heat towards the downstream of the target, where it could be evacuated by means of alternative cooling systems.
Water cooling
Water cooling
Alternative design – The full W target (exploring other options)
Alternative designs: Full W core with inserts
H2O
H2O
H2O

## Slide 20: WP3 – BDF Target design
Beam direction
Ta& H2O pipe in the center
Temperature reduction
Copper insert in the center
Temperature reduction
Temperature [Cº]
Temperature [Cº]
Water cooling
Water cooling
Alternative design – The full W target (exploring other options)
Alternative designs: Full W core with inserts

## Slide 21: WP3 – BDF. More Alternative Target designs -Helium cooling
21
beam
W
Ta cladding
Helium
Water
W
Helium cooling on faces
Water cooling (with Ta cladding) at edges
Helium cooled blocks
Removes need for cladding
  In baseline design, Tantalum has high stress: residual from HIPing + thermal expansion in beam
  Tantalum bad for accident cases
Allows higher next-to surface local coolant temperatures (no risk of boiling)
-But HTC is lower than water
-Added cooling system complexity and cost
Studies are ongoing
W (non-clad) helium cooled, or mix of Helium and Water cooling

## Slide 22: Target Alternative Designs testing
Scaled representative target(s) will be tested in 400GeV beam in 2025.
Using the Test Stand base, and design of Test Stand top from the Baseline test in 2024
Option exists to test multiple alternative designs in beam.
Test Target
Instruments
Water
Test Stand
Beam
Connections
Test stand moved in/out of beam
Test stand setup in 2018.
Alternative options for test/stand in 2025
22
Test stand movement
Device movement

## Slide 23: Conclusions
New alternative designs are being explored.
Target with increased W has improved physics
The elimination of the water cooling channels between the core discs:
  High stresses in cladding & issues of water in beam (with water channels) will have to be balanced against higher W temperatures and stresses in W (without water channels)
The introduction of high thermal conductivity materials such as Copper or Gold:
  Promising to reduce the temperature within the core.
  Issues of thermal expansion mismatch, gold has cost implication
We are also exploring “exotic” designs, such as cooling from the centre, or with helium. These studies are in a preliminary phase and may not be viable.
Variations on beam sigma & sweep radius, and target diameter will also be explored.