## Slide 1: Nichrome Electrodes

## Slide 2: Received to CERN
Received electrode appeared in good shape.

## Slide 3: Short circuit during first conditioning, 50um
During our first condtioning trial, there became a short circuit at one point, turning the electrodes from a capacitor into a resistor.

## Slide 4: Change to 80um gap, current gap for conditioning
Carefully increasing the frequency from 100 to 500Hz, we are currently condtioning at 25MV/m (not shown) and are starting to locate the breakdowns.

## Slide 5: Breakdown Locations
So far, the breakdowns are observed in close proximity.

## Slide 6: Summary
Continue conditioning
At 25MV/m.
Starting to locate breakdowns.
Comments: The electrode can go far beyond what is required of it with regards to field holding. We also see the pressure be heavily linked with the applied voltage.