## Slide 1: VELO U2 cooling substrates
Oscar Augusto on behalf of the VELO Upgrade 2 group

## Slide 2: VELO Module/Cooling concepts (FTDR)
Smaller microchannel coolers to reduce the overall cost
More challenging to integrate (interface between pipes and coolers)
Cooling structure could be potentially re-used (NA62 talk)
Better cooling performance
Cheaper and more flexible design
Easier to integrate (cooling plant)

## Slide 3: VELO Module/Cooling concepts (NIKHEF)
Kazu/Yutaro presentation

## Slide 4
3D metal
Exploration phase
Considering evaporative as baseline solution
Considering evaporative CO_2 as baseline solution
Power dissipation of up to
Power dissipation of up to 2W/cm^2
Largest variation of temperature on the sensor part around (with respect to the inner side wall)
Largest variation of temperature on the sensor part around 25℃ (with respect to the inner side wall)
Alternative strategy to cooldown off-chip electronics would have to be improved (cooling routing lines)
U-like design
Different designs submitted to the Royce Institute (Sheffield)
More aggressive designs (larger ) would require lower operating temperature (Krypton?) to keep the max. sensor temperature
More aggressive designs (larger ΔT) would require lower operating temperature (Krypton?) to keep the max. sensor temperature <−20℃
At the moment, considering different designs which could lead to a material budget reduction compared to plan-Z
3D metal
U-like design
U-like design

## Slide 5
3D metal: LHCb VELO
Different designs
Squared tube and connector prototypes
X-ray tomography via NXCT
U-shaped design
0.5mm
1.0mm
Fill factor
Printing distortion and blockage
X-ray 2D tomography (one projection)
New round of printing:
Filling factor being improved
Different printing parameters to improve distortions and fill factor
Half of the samples will be electro-polished (easier integration?)
Samples are being post-processed

## Slide 6
Ceramics
Why?
Robustness, reliability, stability in ultra-high-vacuum
Manufacturing at IKTS Fraunhofer (Germany)
Possible to embed conductive layers in between ceramics layers and metalize the surface
Potential to integrate electronics or high conductivity elements
Mechanically robust and compatible with high ultra vacuum
Different base materials: YSZ, , … including SiC and AlN
Different base materials: YSZ, Al_2 O_3, … including SiC and AlN
Manufacturing based on several layers
Ceramics
©Fraunhofer IKTS

## Slide 7
Ceramics
Experience with fluidic applications
First prototype based on the early VELO Upgrade I CERN design
Initial channel with width (restrictions)
Initial channel with 70μm width (restrictions)
Channels height
Channels height 100𝜇𝑚
Overall dimensions:
Overall dimensions: 40×60mm^2
Based on LTCC
Possible to move to SiC or AlN
Al_2 O_3/Glass ~1:1
HTCC at a later stage ( )
HTCC at a later stage (Al_2 O_3 ~96%)
Ceramics
©Fraunhofer IKTS
Restrictions
Main
channels
Input
Output
40 mm
60 mm

## Slide 8
Ceramics: Goal and status
Very encouraging first manufacturing round!!!
Goal:
Manufacture first samples (IKTS)
Second round being prepared
Validate initial prototypes to high pressure, leak tightness and cooling performance
Benchmark: LHCb VELO Upgrade 2 requirements (High pressure 186 bar, leak tight (vacuum operation) and excellent thermal performance
Miniaturized version (2x smaller in-plane)
Expected 35um and 100um width restrictions and main channels respectively!
First samples in-house
(eagerly waiting to be tested)
Fraunhoffer ©
IKTS Fraunhoffer ©
IKTS Fraunhoffer ©
IKTS Fraunhoffer ©

## Slide 9: Metrology
Measurements done using the smartscope
Planarity deviation of order of tenths of
  An additional layer can be deposited and machined for better planarity as we scale it up (Massimo thesis)
  Discussion with the manufacturer this week
The microchannels pattern can be seen in the surface survey
  Cross section analysis on-going

## Slide 10: Simplified FEA
Sensor + ASIC (400um Silicon)
->
Cooling structure in Al2O3 (20W/m.K)
Overhang of 5 mm as in the VELO U1

## Slide 11: FEA (Alumina LTCC)
Sensor + ASIC (200um Silicon)
->
Cooling structure in LTCC Al2O3 (5W/m.K)
Overhang of 5 mm as in the VELO U1

## Slide 12: FEA (Alumina LTCC)
Sensor + ASIC (200um Silicon)
->
Cooling structure in LTCC Al2O3 (5W/m.K)
Overhang of 8 mm as in the VELO U1

## Slide 14: VELO U1 TDR
VELO Upgrade I TDR
Cooling substrate at baby prototypes level
  SNAKEI, 40 mm x 60 mm
  Main channel 200 um x 70 um (Restriction 30 um x 70 um)
Robustness tests running
  High pressure and cycling

## Slide 15: VELO U1 TDR
VELO Upgrade I TDR
Cooling substrate at baby prototypes level
  SNAKEI, 40 mm x 60 mm
  Main channel 200 um x 70 um (Restriction 30 um x 70 um)
Robustness tests running
  High pressure and cycling
Fluidic and cooling performance test ()

## Slide 16: VELO U1 TDR
Cooling substrate at baby prototypes level
  SNAKEI, 40 mm x 60 mm
  Main channel 200 um x 70 um (Restriction 30 um x 70 um)
Robustness tests running
  High pressure and cycling
Fluidic and cooling performance test ()
Finite element analysis (FEA) to optimize the channels distribution and cooling performance
VELO Upgrade I TDR

## Slide 17: VELO U1 TDR
VELO Upgrade I TDR
Cooling substrate at baby prototypes level
  SNAKEI, 40 mm x 60 mm
  Main channel 200 um x 70 um (Restriction 30 um x 70 um)
Robustness tests running
  High pressure and cycling
Fluidic and cooling performance test ()
Finite element analysis (FEA) to optimize the channels distribution and cooling performance
Scale the cooling substrate to module size
Connector attachment at the very early stages

## Slide 18: VELO U1 TDR
VELO Upgrade I TDR
 | Ceramics | 3D metal
Baby prototypes | Thinner channels were already manufactured Nominal samples by End/July | Samples produced show distortion and fill factor issues Second round should have better fill factor (TBC)
Robustness tests | Miniaturized connector glueing at the moment (based on the CERN design) – High pressure test in-house New connector for nominal size Cyclic tests | Connector is required (see last row)
Cooling performance | Heaters ordered and vacuum tank/CO2 in place (To be recommissioned) | In principle, same heaters/set-up can be used
Cooling FEA | On-going (large contribution due to the overhang) | On-going (large contribution due to the overhang)
Module scaling and Mod0 | Aiming for timepix4 prototype by mid/2025 (40 mm x 60 mm – nominal size) | Pursuit another manufacturer in parallel (Terms and conditions?)
Connector | IKTS has experience with integration, soldering, Hyperbar bonding (CPPM), brazing(?) | More samples are required (smoother finishing would be beneficial)

## Slide 19
Summary
Scaling up towards the final design (highly dependent on the geometry – not defined yet!)
Cooling plates
Ceramic plates
Miniaturized samples in-house (20 x 30 mm2)
Nominal dimension expected by end of July () – compatible with the first prototypes specs (timepix4 single board)
Nominal dimension expected by end of July (40×60 mm^2) – compatible with the first prototypes specs (timepix4 single board)
Robustness validation (high pressure / cyclic tests?)
Connector being assembled
Finite element analysis of the sample ( including design optimization)
Connector: different approaches can be considered
IKTS integration, soldering, hyperbar bonding (CPPM), brazing, …
Summary

## Slide 20
Summary
Cooling plates
3D metal printing
First run shows fill factor issue and distortions
Additional samples produced to understand better the printing (straight samples)
Second run should have better fill factor
Connector R&D requires more samples
Another manufacturer to be identified (Alloyed, BA systems, ?)
Smoother surface is desirable
Thank you for your attention

## Slide 21: Ceramics 3D printing
Experience with fluidic applications
First prototype based on the SNAKEI design
  Restrictions of instead of
  Channels height 100
  Overall dimensions: 40x60
  Based on alumina ()
    Possible to move to SiC afterwards
Currently, initial quote being discussed
©Fraunhofer IKTS
SNAKEI based design to optimize printing parameters/test feasibility
Simplified FEA focusing on the 5 mm overhang. Substrate in alumina and heat conduction on one side of the cooling plate and Stycast (100um). For , .

## Slide 22: Cooling material budget (U1)
VELO U1 cooling material budget
Not all services are present (no cables)
Material budget for perpendicular incidence
Inner most region has only the contribution from the sensor+ASIC (~0.4% X0)
Second innermost region contains the contribution from sensor, cooling plate and glue layer
(~1.0% X0)

## Slide 23: Materials considerations ()

## Slide 24: Materials considerations (Minimum wall, OD 1 mm / 200 bar)
Exercise to take into account the resistance to stress of the material
Rounded tubes maximum pressure (Barlow equation):
: yield strength
: wall thickness
D: outer diameter
Very small in some cases (should be taken with a pint of salt)
Same exercise will be repeated using flexural strength

## Slide 25: Materials considerations (Minimum wall, OD 1 mm / 200 bar)
This is just an initial exercise for the selection of materials
Indicates that diamond/ceramics would be good candidates for the substrate
Taking into account the capacity to deal with high pressure and material budget
Those number should still take into account thermal conductivity and thermal expansion mismatch
Preference for Diamond, SiC, (3D) Alumina, 3D titanium and BeO

## Slide 26: Materials considerations (Minimum wall, OD 1 mm / 200 bar)
Kapton
Preference for BeO, Diamond, Graphite, PyroidHT, SiC, Aluminum, Si and 3D AlSi10Mg based on thermal conductivity
To be as inclusive as possible, all possibilities below Kapton thermal expansion or below 10ppm/K (?)

## Slide 27: Materials considerations
SiC
Diamond
(3D) Alumina
3D
titanium
BeO
Graphite/
Pyroid HT
3D AlSi10Mg
Si
Invar36
Material budget
Thermal conductivity
Thermal expansion

## Slide 28: Metal 3D printing
Collaboration with the Royce Institute (UK) based on Selective Laser Melting
Revisit the plan-Z alternative and try to further reduce the material budget contribution
  Main motivation: design flexibility and replaceability/price
Three prototypes manufactured with different wall thicknesses (250 um, 150um and 100um)
  To be tested for high pressure, leak tightness, …
  A quarter of a module approach (sensor, hybrid and GBTx region)
Sensor tile
Hybrid
GBTx

## Slide 29: Metal 3D printing (FEA)
Ti cooling tubes: with 250 um wall thickness
Two cooling tubes under the silicon tile (similar to U1)
  Silicon tile (400 um thick)
  12 W (2x higher than U1)
Hottest region of the tile
  About 3x higher than the plan-Z U1 measurements (around 8C)
On the same model, TPG or graphene layer (1200 W/m.K) was considered to remove the heat of the GBTx
  GBTx on top of Kapton/stycast layer (600um total, 1.25W/m.K)
  Simulated as silicon 0.5x0.5cm and 5W
  High
Silicon tile
GBTx
TPG/PyroidHT
Kapton/Stycast

## Slide 30: 3D metal printing + Pyroid HT (Very preliminary FEA)
Soldered interface
(NanoFoil?)

## Slide 31: VELO U1 (TDR stage)
VELO Upgrade I TDR
Production of cooling/fluidic prototypes
Robustness tests
Cooling performance
Cooling performance

## Slide 32: VELO Module/Cooling concepts (CERN)
Jan Buytaert (CERN)

## Slide 33: VELO Module/Cooling concepts (Oxford)
Malcolm and Adam (Oxford)

## Slide 34: Simplified FEA

## Slide 35: VELO Module/Cooling concepts (NIKHEF)
Kazu/Yutaro presentation

## Slide 36: VELO Module/Cooling concepts (NIKHEF)
Kazu/Yutaro presentation

## Slide 37: VELO Module/Cooling concepts (CERN)
Jan Buytaert (CERN)

## Slide 38: VELO Module/Cooling concepts (CERN)
Jan Buytaert (CERN)

## Slide 39: VELO Module/Cooling concepts (Oxford)
Malcolm and Adam (Oxford)

## Slide 40: VELO Module/Cooling concepts (NIKHEF)
Kazu/Yutaro presentation