## Slide 1
Emilio Bellingeri
Tl-1223 Superconducting Films for Beam Screen Coatings in FCC: Synthesis and Performance Validation

## Slide 2
OUTLINE
    Project
    Why Thallium-based?
    Phase diagram study
    Precursor coating deposition and reaction
    Structural characterization
    DC and RF superconducting properties
    High vacuum compatibility
    Conclusions
Notes: I will start by outlining the project, then proceed to explain the reasons behind the study of Thallium and describe our collaboration. Finally, in the second part, I will discuss the development of this material that we carried out.

## Slide 3: FCC beamscreen projects @SPIN
First project: Tl based HTS preparation
              PI Emilio Bellingeri
              Addendum FCC-GOV-CC-0049 (EDMS1580502, KE3112)
New project: New project for assessing Tl (1223) superconducting coating feasibility
              PI Alessandro Leveratto
      Addendum FCC-GOV-CC-0217 (KE5072/TE)
2016-2019
2021- 2024
Structural and Transport Characterization: TEM, SEM, EBSD, Jc (T, B), SHPM,…
Sigrid Holleis, Florian Semper Michael Eisterer
Andreas Steiger-Thirsfeld , Johannes Bernardi
Sample preparation, structural characterization, DC measurements, theory
Alessandro Leveratto, Aisha Saba, Cristina Bernini, Federico Matteo, Cialone, Ruggero Vaglio
Accelerator environment compatibility, theory
Marcel Himmerlich, Bernard Henrist ,Stephanie Fernandez-Peña Mauro Taborelli, Guillaume Rosaz, Sergio Calatroni, Massimo Giovannozzi
RF measurements
Andrea Alimenti, Alessandro Magalotti, Nicola Pompeo, Kostyantin Torokhtii, Pablo Vidal García, Enrico Silva

## Slide 4
T = 50 B = 16 T
 = 1GHz 100 TeV High syncrotron
radiation intensity
Work condition:
B=14 T (or 16 T)
T=50K (or 100 K)
Jc > 104 Acm-2
In FCC-hh Beam screen is foreseen to work at T>50K. The surface resistance of copper at 50 k may not be sufficiently low to guarantee a safe operational margin for the fcc-beams (in particular at injection energy).
Idea: superconducting coating!
ReBCO (Cu1212)
Tl1212
c=12.7Å
Tc=80 108K

## Slide 5
Already demonstrated the possibility to deposit via electrochemistry thanks to the high out-of-stoichiometry tolerance with respect to RE-123
Cheap and scalable technique, which could be considered for a direct deposition on tubes or arbitrarily shaped templates
Tc ~ 120 K
E. Bellingeri et al. IEEE 2001
G. Gritzner et al. SUST 2004
D.Y. Jeong et al SUST 2007
Why Thallium-1223 ?

## Slide 6
TOXIC LAB CONSTRUCTION
POWDER AND BULKS REALIZATION
PRECURSOR DEPOSITION
HIGH PRESSURE REACTION
CHARACTERIZATION

## Slide 7
955 °C
940 °C
938 °C
Tl-based cuprated
PHASE DIAGRAM STUDY
ON VARYING MANY PARAMETERS:
TEMPERATURE
INITIAL PRESSURE
FINAL PRESSURE
O2 PARTIAL PRESSURE
High Ar pressure syntesis in order to prevent Tl evaporation
    Phase diagram study

## Slide 8: Precursos layer Reacted film
Nd:YAG 1064 nm
5 Hz 90 min
Substrate LAO 001
T substrate = RT
p(O2) = 8.7-9.3 10-2 mbar
HT-HP REACTION
950 °C
50 bar Ar+ p(O2)
3 h

## Slide 9
FWHM= 0.6 °
SE
BSE
500 µm
500 µm
Very pure Tl(1223) phase, policristalline but fully (c and ab ) oriented
Structural properties

## Slide 10
  Microscopy–SEM EBSD TEM

## Slide 11
VTI – 16 T
R(T, B) > HC2, Hirr

## Slide 12
VTI – 16 T
Critical current density Jc
Nominal channel geometry
Length lV+V- = 300 µm
Width d = 100 µm
Thikness z = 0.5 µm
s = 50 10-8 cm2
Jc = 2 105 A/cm2
H3PO4 8.5%
Transport current measured 4 wire on patterned samples to reduce Ic

## Slide 13
VTI – 16 T
Critical current, critical current density, Pinning Force
Critical current density Jc

## Slide 14: Microwave characterization
Measurement technique
Dielectric-loaded resonator Surface perturbation method
VNA
S21
H
Transm. coeff.
sample
Vortex motion resistivity ρvm
VNA
Sample thickness ≈ 1 µm
Tc = 116 K (Tl-1223), no signs of a second phase
“Higher” Q-factor compared to the previous sample
10600
GHz

## Slide 15: Microwave characterization
Vortex motion resistivity ρvm
Wrt YBCO SuperPower CC:
(computed assuming a thickness of ~3 µm) within a factor of 1.5-2
is the dominant factor in difference @ 70 K
Promising results:
  constant in the T-B range reported (crucial for high B applications)
  Ample margins for optimization
Bands refer to different assumed values for
λL(0) = [150,600] nm

## Slide 16
Requirements inherent of the particle accelerator environment.
Vacuum: Pumping test of degassing RGA from surface after 24 h pumping are
The RGA after 24 h of pumping was readily within CERN's acceptance criteria for unbaked components. In addition, XPS analysis revealed that no high atomic mass elements (Tl, Pb, Bi) are released by the pellet.
Secondary Electron Yield (SEY): the bare Tl-1223 surface has a rather high initial δmax at room temperature. The application of a thin amorphous carbon coating
(150 nm thick Ti buffer layer followed by addition of a 100 nm thick a-C top layer). dropped the SEY to 0.77, very promising result for further development of this approach.

## Slide 17
Thank you for your attention
Tl-1223 coatings approach the performances required, in terms of critical current and irreversibility field, by FCC application.
Conclusion
A reliable method based on amorphous precursor deposition followed by a high temperature/high pressure thermic treatment to produce almost pure Tl(1223) superconducting coating has been demonstreated
Tl(1223) sample exhibits a vortex flux-flow resistivity (𝜌_ff) that is nearly comparable to ReBCO tapes. The observed lower surface resistance is due to a lower pinning constant (k_p), (that in ReBCO tapes has been artificially increased through the introduction of controlled defects)
Results are on LaAlO3 single crystal:
a suitable substrate need to be optimized (Reaction temperature is too high for pure silver)
Pinning force shoul be increased
Thikness increased up to few micometers
Electrochemical deposition of precursors is possible but give less dense layers:To be optimized
Notes: let's go back the way we came

## Slide 18
Istituto SPIN
Genova, L’Aquila, Napoli, Roma, Salerno
Electrochemical deposition
Pulsed Laser Deposition
Film Deposition Of Thallium Based Precursors
CONSTANT POTENTIAL
PULSED POTENTIAL
SUBSTRATES
EMPLOYED
LAO (001)
STO (001)
Frequency | 5 Hz
Laser energy | 1-3 J/cm2
Vacuum | 8 × 10-8 mbar
O2 pressure | 10-2 – 10-1mbar
d target - substrate | 3-4 cm

## Slide 19
Thicker
(2 h dep.)
Thinner
(1 h dep.)
Istituto SPIN
Genova, L’Aquila, Napoli, Roma, Salerno
2.2 um
875 nm
700 nm
120 nm

## Slide 20
Thicker
Thinner
Istituto SPIN
Genova, L’Aquila, Napoli, Roma, Salerno
Alessandro Leveratto, CNR-SPIN Genova SPIN Seminar series – October 24, 2024

## Slide 21
Istituto SPIN
Genova, L’Aquila, Napoli, Roma, Salerno
VTI – 16 T
R(T, B) > U0
with n ≈ 0.48;
with n ≈ 0.77.

## Slide 22
Alessandro Leveratto, CNR-SPIN Genova Joint Workshop UniGe – IFW– Genoa – June 10, 2024
Istituto SPIN
Genova, L’Aquila, Napoli, Roma, Salerno
955 °C
Increasing T 850 to 950°C
Decreasing p(O2) 1 to 0.1 bar at RT

## Slide 23: Measurement technique – dual mode dielectric loaded resonator
VNA
Dielectric loaded resonators
f1,2 = [8; 14],[16; 27] GHz
at
Q-factor
Res. frequency
Effective surface
impedance
Vortex motion resistivity
Modified Lorentzian fit
TMQF - fit
e.m. simulation
geometrical factors estimation
Classical
electromagnetism + vortex motion
K. Torokhtii et al., Acta IMEKO 9(3), 2020
K. Leong et al., IEEE Trans. Microw. Theory Techniq., 50(9), 2002
TE021 - mode
N. Pompeo et al., Measurement, 184, 109937, 2021
A. Alimenti et al., IEEE Instrum. Meas. Mag., 24(9), 2021
K. Torokhtii et al., Measurement: Sensors 18, 2021 A. Alimenti et al., Meas. Sci. Technol, 30(6), 2020
Flux flow resistivity
Pinning frequency
Single vortex physical model

## Slide 24: Measurement technique
Measurement technique = Dielectric-loaded cylindrical resonator. Note: this is essentially a bulk technique, meaning that the surface impedance (a kind of AC electrical resistance) is measured as an average over the entire sample, both in terms of surface area and thickness.
Superconducting sample = Placed inside the resonator, between one of its end plates and the internal dielectric crystal (see schematic in slide 2).
Resonator = Acts as a source of electromagnetic radiation → induces RF currents on the sample surface, allowing us to measure its resistivity.
The measurement = A differential surface impedance measurement (ΔZₛ), calculated from variations (typically induced by the magnetic field) in the quality factor Q and resonant frequency f of the resonator with respect to a reference value*.
Theoretical/physical models = Allow us to extract vortex parameters (such as the flux-flow resistivity ρ_ff, pinning frequency fₚ, etc.).
Measurements = Performed at a fixed frequency; either at constant magnetic field and varying temperature ("transitions"), or at fixed temperature and varying magnetic field ("field ramps", used to extract the vortex parameters mentioned above).
* For example, in measurements with varying magnetic field and fixed temperature, the reference values Q(B=0) and f(B=0) are compared to the experimental values Q(B>0) and f(B>0).

## Slide 25: Measured Samples
Sample thickness ≈ 1 µm
RF measurements show two different Tc [116 K (Tl-1223); 80 K (Tl-1212)]
“Low” Q-factor  large losses (high )
Tc1
Tc2
7 GHz
Sample NdYAG012 (03/2024)
Sample thickness ≈ 1 µm
Tc = 116 K (Tl-1223), no signs of a second phase
“Higher” Q-factor compared to the previous sample
Sample NdYAG031 (12/2024)
10600
GHz

## Slide 26: Temperature sweeps at constant B
Estimated normal state resistivity ≈ 100 µΩ cm
Normal state resistivity from literature [1,2,3,4] ≈ 300-500 µΩ cm
f = 14.9 GHz
[1] G. Triscone, Physica C 272, 21-25 (1996).
[2] R. Awad, et al., Supercond. Sci. Technol,17 35 (2004).
[3] S. Isber, Supercond. Sci. Technol. 18 311 (2005).
[4] A.I. Abou Aly, J Supercond Nov Magn, 23 (2010).

## Slide 27: Magnetic field sweeps at constant T (Surface impedance)
From the magnetic field sweep:
Rs increases with field -> dissipation due to increased number of fluxons in the sample
Rs (surface resistance) and Xs (surface reactance) allow for the determination of the vortex parameters (an estimation of of λL is needed)

## Slide 28: Magnetic field sweeps at constant T (Desired thickness)
To be in the bulk regime (no substrate contribution to Rs),
the required coating thickness is computed from the e.m. penetration depth.
This estimation depends on the actual λL
At T < 70 K, B = 12 T and f = 14.9 GHz:
If λL = 150 nm  Thickness ≥ 3.1 µm
At lower frequencies, a thicker sample is needed.
In the worst case (pure flux flow), with the present data, at T < 70 K, B = 12 T and f = 2 GHz:
Rs( f2) ≈ Rs( f1) sqrt( f2/f1)  thickness ~ 9 µm

## Slide 29: Magnetic field sweeps
Dimensional crossover = Depending on the values of magnetic field and temperature, the sample transitions between different electromagnetic geometries (bulk, thick film, thin film). This complicates both data analysis and interpretation, making the London penetration depth λL a particularly critical parameter.
λL = Leaving aside the strictly physical aspects, the analysis was carried out by treating λL as a free parameter. As a result, the extracted microscopic parameters are accompanied by a "confidence range" (shaded areas) that reflects the possible variations of λL. Clearly, the range is wide (λL up to 600 nm), yet the confidence intervals remain relatively narrow.
Desired thickness = In view of a potential FCC application, and in order to avoid dimensional crossovers, the system must operate in the bulk regime. To achieve this with the current performance of the superconductor, a minimum thickness of 4–5 μm at 70 K and 12 T is required. If the material performance is improved, a thinner layer will be sufficient to stay in the bulk regime (and thus effectively shield electromagnetic radiation).

## Slide 30: Magnetic field sweeps at constant T (Pinning Parameters)
Bands refer to different assumed values for
λL(0) = [150,600] nm
(full dots correspond to 150 nm)
Gittleman-Rosenblum pinning parameters, with the estimation of the maximum creep factor , see:
N. Pompeo, et al., Physical Review B 78.9 (2008): 094503.
Considering pinning, at T < 70 K, B = 12 T and f = 2 GHz:
If λL(0) = 150 nm  thickness ~ 4 µm
If λL(0) = 600 nm  thickness ~ 5.5 µm

## Slide 31
Wrt YBCO SuperPower CC:
(computed assuming a thickness of ~3 µm) within a factor of 1.5-2
is the dominant factor in difference @ 70 K
Promising results:
  constant in the T-B range reported (crucial for high B applications)
  Ample margins for optimization
Bands refer to different assumed values for
λL(0) = [150,600] nm

## Slide 32: Pinning parameters comparison, magnetic field sweeps at constant T
The recent sample (NdYAG031) clearly shows improved performances both in and compared to the old one (NdYAG012)

## Slide 33: Vortex motion resistivity
:
Minimize the flux-flow resistivity (dissipation)
Increase the pinning frequency (pinning strength)
Low losses
High losses
: flux-flow resistivity (dissipation)
(or ): pinning frequency (pinning strength)
: creep factor (thermal activation)
Resistività di vortice (grandezza complessa)