## Slide 1
Status of HFM development
at INFN
Alessandra Pampaloni
On behalf of the INFN Genova and LASA collaboration
May 22, 2025

## Slide 2: Outline
12 T Nb3Sn Falcon Dipole
  Electromagnetic Design
  Winding Tests
  Mechanical Design
  Mechanical Mockup
Toward the 14 T Program
  LTS Technology
  HTS Technology
Conclusion

## Slide 3: 12 T Nb3Sn Falcon Dipole
The FalconD program, signed in 2018, is being developed in accordance with the CERN/INFN KE 4102 agreement
An amendment was issued in March 2023 to update the project's scope and schedule
The project involves the development and construction of a short model Nb3Sn dipole with the following specifications:
  Single aperture with an inner bore of 50 mm
  2-layer cos-theta coil providing a bore field of 12 T at 1.9 K
  Mechanical assembly using bladder & key technology
  The total coil length is 1.5 m

## Slide 4: 12 T Nb3Sn Falcon Dipole
The FalconD project includes the following activities:
  At ASG Superconductors, manufacturing of:
    1 dummy pole wound with copper cable
    2 practice poles wound with Nb3Sn cable
    5 poles wound with Nb3Sn cable for the single aperture
  At INFN LASA, assembly and testing @ 4.2 K of the magnet
ASG is responsible for manufacturing the coils, which include 7 Nb3Sn coils and 1 dummy copper coil
CERN supports all activities and supplies the magnet components, including the cable, spacers and other necessary items
INFN is responsible of the magnet design, B&K assembly and preliminary test @ 4.2 K at LASA laboratory

## Slide 5: Electromagnetic Design
The 2D and 3D electromagnetic design is completed.
1.38 mm
1.98 mm
1.17 mm
9.85 mm
Reacted cable:
Width +2%
Mid-thick +4.5%
21.42 mm
1.89 mm
40 strands Ø 1 mm
Parameter | Value
Cu/NCu | 0.9
Joverall [A/mm2] | 424
JSC [A/mm2] | 1220
weqv [mm] | 37
Number of turns | 12+24
Unit length [m] | 150
  * intended as mechanical limit
Courtesy of R. U. Valente
Bore Field | Operating Current | Margin on loadline @ 1.9 K **
12 T | 20180 A | 24.4%
13.5 T * | 23000 A | 15%
  ** margins are calculated with the EuroCirCol JC curve scaled to JC(16 T, 4.2 K) = 1200 A/mm2

## Slide 6: Winding Tests
Courtesy of R. U. Valente
  A significant detachment (protrusion) of the accumulated turns from the mandrel has been observed (accumulation is nearly 1 mm/turn)
Winding tests have been performed using bare Cu cable, insulated Cu cable and insulated Nb3Sn revealing significant differences in the results
Key findings include:
  Turns closer to the pole are less critical, as most of the bending occurs in the easy way
  The most critical turns are those near the midplane, where significant hard way bending is combined with pronounced twisting
  The natural turn angles did not correspond to that designed for the end spacers

## Slide 7: Winding Tests
Courtesy of R. U. Valente
Free bending tests of the midplane turn have been performed
These tests confirmed the challenges, particularly for short coil ends (~ 100 mm); however, extending the coil end to ~ 200 mm appears to mitigate or solve the issue
To further refine the design, we have been working to extend the end spacers and align them with the natural conductor angles measured during the winding tests
The new design of the end spacers is very promising, but modifications to the winding machine are necessary, so we will repeat the winding tests as soon as the new tooling is finalised

## Slide 8: Mechanical Design
Courtesy of N. Sala
The 2D and 3D mechanical design was optimised and finalised
We are working on the definition of the assembly procedure

## Slide 9: Mechanical Mockup
Courtesy of A. Bersani and A. Gagno
Consolidation of mechanical FEA to predict stress and strain conditions during B&K assembly
Determining the most efficient assembly sequence
Personnel training to gain specific skills in B&K assembly
The mockup also served as a test of the 8-channel bladder pumping system that we will use for the final assembly of FalconD
500 mm

## Slide 10: Mechanical Mockup
Courtesy of A. Bersani and A. Gagno
The mock-up is instrumented with several strain gauges
The measured outer diameter, obtained using a caliper, is in line with FEM model expectations
Analyses on the recorded data by the strain gauge are in progress and will be available in the near future

## Slide 11: Toward the 14 T Program – LTS Technology
Presently it is in advanced approval phase a new INFN – CERN collaboration to finalizing a 6-year proposal within the HFM R&D Program framework
One of the main goals is to construct a 14 T demonstrator in a cos-theta configuration
The construction will take place at the new IRIS program facility at the LASA laboratory in the consolidated joint work between Milan & Genoa INFN sections
Courtesy of E. De Matteis

## Slide 12: Toward the 14 T Program – HTS Technology
The proposal within the HFM R&D Program framework under discussion with CERN also includes activities focused on HTS
  Study and evaluate multiple configurations of HTS-based (REBCO-type) dipole magnets designed with characteristics suited for accelerator applications
  Design, construct and test a single-aperture, subscale HTS dipole model targeting a central field of 10 T, operating at temperatures between 10 and 20 K
Courtesy of M. Statera

## Slide 13: Conclusion
The 2D and 3D electromagnetic and mechanical design of FalconD has been finalized
We are working on the assembly procedure and manufacturing drawings
Through the mockup construction we are getting familiar with the bladder & key assembly procedure, and we are validating our finite element models
As soon as the new winding tooling is available in ASG we will repeat the winding tests with the final optimized design of the end spacers
  If these tests are also successful, we will begin the production of the dummy coil
The program will continue with the new agreement toward a 14 T INFN demonstrator Nb3Sn dipole and a 10 T demonstrator in REBCO

## Slide 14
Thank you for your attention!