## Slide 1
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC
Electropolishing of large copper substrates for FCC
FCC-ee 400 MHz double cell

## Slide 2
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025
Content
Tools and expertise
  Electropolishing set-up, Interfaces and Simulation
Simulation vs real data
Main issues and achievements
Preparation for the 2-cells 400 MHz FCC-ee cavities
Main challenges & strategies
Conclusions

## Slide 3
Electropolishing set-up & Interfaces
Tools and expertise
Bath handling chemical facility
Cavities handling machine
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025

## Slide 4
Simulation
Tools and expertise
# working parameters
j = f(U, T, vb, Sc/Sa, σl, [b])
- j, Current density
- U, Overall applied tension
- Tb, Bath temperature
- vb, Bath fluid dynamics
- Sc/Sa, Cathode geometry & Cathodic/Anodic surface ratio
- σl, Bath conductivity
- [b], Bath composition
Anode: Cu(s) → Cu2+(aq) + 2e- 2H2O(l) → O2(g) + 4H+(aq) + 4e-
Cathode: Cu2+(aq) + 2e- → Cu(s) 2H+(aq) + 2e- → H2(g)
Mass transport controlled
Charge transfer controlled
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025

## Slide 5
Simulation
Tools and expertise
Shear rate () is the rate of change in velocity at which one layer of fluid passes over an adjacent layer
RDE model data
RDE experimental data
Shear rate
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025

## Slide 6
Simulation
Tools and expertise
Creation of a new anodic current density function to be used for any geometry, using the results obtained with the RDE:
Shear rate (τ)
Overpotential (η)
Current
density (j)
Shear rate (τ)
Overpotential (η)
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025

## Slide 7
Simulation vs Real data
Current density (A/m2)
POLISHING
Overpotential (V)
POLISHING & OXYGEN FORMATION
jlim
Benchmarking on 1.3 GHz copper monocell
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025

## Slide 8
Simulation vs Real data
Data from 400 MHz monocell processing
Cavity | Tension / V | Current / A | Temperature / °C *
PC04#1 | 21 | 81.8 | 15.4
PC04#2 | 21 | 72.5 | 14.0
PC06#1 | 21 | 75.0 | 15.2
PC06#2 | 21 | 75.9 | 14.8
Simulation total current, corrected to estimated
wet surface: 84 A at 21 V
*) Temperature readings from the chemical
facility are not in line with the ones measured
on the test cavity (~10 °C). dT within the chemical
facility is below 1.6 °C.
Data from simulation:
400 MHz Current density distribution at 10 °C
Average polishing rate: 0.1 µm/min
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025

## Slide 9
1st Ever electropolishing of a 400 MHz monocell copper cavity
Main issues and achievements
1st Ever electropolishing of a 400 MHz LHC monocell copper cavity
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025

## Slide 10
Main issue: Passivate the copper
Main issues and achievements
  Neutralisation before disassembly
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025

## Slide 11
Main challenges
  Power input (+ surface & + distance)
Preparation for the 2-cells 400 MHz FCC-ee cavities
Strategy
  Cathode optimisation
  Increase bath flow
  Exploit existing working window
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025

## Slide 12
Main challenges
Strategy
  Reduce retentions
  Reduce back flow
  Keep neutralisation step
  Passivation of copper
Existing
New
Preparation for the 2-cells 400 MHz FCC-ee cavities
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025

## Slide 13
Main challenges
Strategy
  Assemble 2nd contact ring
  Electropolishing of ports
Preparation for the 2-cells 400 MHz FCC-ee cavities
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025

## Slide 14
Conclusions
Electropolishing process is well mastered
Data from 400 MHz monocell processing ensures 2-cell geometry EP feasibility
Main challenge remains the copper surface passivation
Impact of non electropolished (EP) ports still to be assessed
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025

## Slide 15
Thank you for your attention
L. Ferreira, FCC Week 2025 | Electropolishing of large copper substrates for FCC 21st of May 2025