## Slide 1: TEM analysis of coatings for RF cavities
J. Bernardi, A. Steiger-Thirsfeld – USTEM / TU Wien
S. Leith, G. Rosaz, C. P. A. Carlos - CERN
F. Semper, M. Asiyaban and M. Eisterer –Atominstitut / TU Wien

## Slide 2: Thin film Nb3Sn RF cavities
Vapor diffusion coating
High Power Impulse Magne-
tron Sputtering (HiPIMS)
M.Liepe, Cornell University, FCC Week 2015
Challenges:
Homogeneity, constant Sn concentration
Surface roughness
Localized defects

## Slide 3: The perfect cavity coating
Cu
Nb3Sn
Thin Nb3Sn coating
  higher operating temperature than pure Nb
  low surface resistance
  high acceleration gradients
Homogeneous microstructure, no defects
Smooth surface
Constant Nb:Sn ratio
No Cu diffusion into A15 film
Ta interlayer
Low costs
Cu substrate with high heat conductance

## Slide 4: Preparation conditions
Ta Interlayer Kr atmosphere, 0.001 mbar
  High temperature Deposition @ 750 °C + annealing @ 750 °C
  Low temperature Deposition @ 175 °C
Nb-Sn target Sn 25 at% or Sn 27 at%
Nb-Sn coating pressure
  High pressure 2.50x10-2 mbar
  Low pressure 7.00x10-4 mbar
Annealing of Nb-Sn
  reaction during coating Deposition @ 750 °C / 2 hrs
  reaction after coating Deposition @ 260 °C / 2 hrs + annealing @ 750 °C / 24 hrs

## Slide 5: A perfect microstructure?
Ta-M
Cu-L
Nb-K
Sn-L
Ta
Nb3Sn
SUBU, 25% Sn, Ta 750°C, Nb3Sn 8.0E-03, reaction during coating (at 750 °C)
EDX maps
ABF

## Slide 6: The real surface (microscopically)
A15
Ta
Cu
Voids
Cracks
Rough surface
Rough surface
Rough surface
Voids and cracks
Smooth surface
Smooth surface
Smooth surface

## Slide 7: The surface (macroscopically)
low pressure coating reaction after annealing
high pressure coating
high pressure coating
low pressure coating
high pressure coating reaction after annealing
What‘s beneath the surface?
What causes the defects (hillocks, hollows, cracks)?
FoV 20 µm
FoV 40 µm
FoV 20 µm
FoV 40 µm
FoV 40 µm
FoV 40 µm
high pressure coating

## Slide 8: Hillocks and hollows
Hollows in the Nb3Sn caused by voids in the Cu substrate.
Sn 25%
Reaction during coating
Medium pressure

## Slide 9: Damages in Cu substrate
Cu
Ta
Nb3Sn
FoV: 830 µm
FoV: 20 µm
FoV: 200 µm

## Slide 10: Homogeneity of Nb3Sn film
Nb:Sn
3.03
3.05
3.2
3.2
3.5
DarkField
Ta
Cu
Ta
Nb3Sn
Ta
Nb3Sn
3.0
2.9
2.9
2.8
2.8
2.9
Smooth surface
Large columnar grains
No Cu at GB
But: Inhomogeneous Nb:Sn ratio
Rougher surface
Defects on Cu  surface defects
Homogeneous Nb:Sn ratio

## Slide 11: Remnant (trapped) field at one edge
Applied Field:
10 mT
T: 5 K
Superconducting
Surface
Cu Substrate
Damages due to
sample preparation
Superconductor
Porosity of copper substrate
Trapped field
Points of preferred flux entry
Cu
Nb3Sn
Defect in Ta layer
1.6 mm
Scanning Hall measurements
Macroscopically homogeneous sample

## Slide 12: Damaged Ta interlayer
Crack in Ta layer  interdiffusion of Cu
High pressure coating  rough surface
Cu and Sn enriched areas on the surface
NbL
SnL
CuK
TaL
Interdiffusion zones
Cu-Sn enriched spots
CuK
CuSn
Ta
Cu
A15
A15

## Slide 13: Imperfect Ta interlayer
Ta
Cu
A15
Ta
A15
Imperfect
Ta layer
TEM
HAADF
DF
Ta
A15
Ta
A15
TlL map

## Slide 14: Microstructure of Nb3Sn layer
Columnar growth
Columnar growth
Smooth surface
Columnar growth with voids along columns
Rough surface
Ta grain influence A15 formation
Fine A15 grains

## Slide 15: Ta - A15 interface
DF TEM
DF TEM
TaL
NbK
SnL
DF TEM
Ta
A15
Cu
Ta
A15
The orientation of the Ta grains appears to influence the orientation of the A15 grains.

## Slide 16: Summary RF cavities
Bipolar HIPIMS: suitable technique for producing good Nb3Sn layers
Homogeneous Nb3Sn layers can be formed
Surface quality depends on pressure during coating
Quality of the Ta interlayer is decisive for homogeneous Nb3Sn layers
Purity of the Cu surface is the top priority