## Slide 1: HIGHEST: high-gradient, high-temperature superconductors
Sergio Calatroni, on behalf of the Collaboration.
This project has received funding from the European Union’s Horizon 2020 Research and Innovation programme under GA No 101004730.

## Slide 2: A view on Linear Colliders

## Slide 3: The Compact Linear Collider (CLIC)
  Timeline: Electron-positron linear collider at CERN for the era beyond HL-LHC
  Compact: Novel and unique two-beam accelerating technique with high-gradient room temperature RF cavities (~20’500 structures at 380 GeV), ~11km in its initial phase
  Expandable: Staged programme with collision energies from 380 GeV (Higgs/top) up to 3 TeV (Energy Frontier)
  CDR in 2012 with focus on 3 TeV. Updated project overview documents in 2018 (Project Implementation Plan) with focus 380 GeV for Higgs and top.
Accelerating structure prototype for CLIC: 12 GHz (L~25 cm)
The CLIC accelerator studies are mature:
Optimised design for cost and power
Many tests in CTF3, FELs, light-sources and test-stands
Technical developments of “all” key elements
  Recent talks: eeFACT-I1 and eeFACTI2
From: Steinar Stapnes

## Slide 4: The ILC250 accelerator facility
e- Source
e+ Main Liinac
e+ Source
e- Main Linac
Damping Ring
Beam dump
Interaction point
Physics Detectors
Bunches of ~1010 e+/e-
Creating particles Sources
  polarized elections/positrons
High quality beam Damping ring
  low emittance beams
Acceleration Main linac
  superconducting radio frequency (SRF)
Collide them Final focus
  nano-meter beams
Go to Beam dumps
Undulator positron source
Electron driven positron source
  Recent talks: eeFACT-I1 and eeFACTI2
From: Steinar Stapnes

## Slide 5: From JoAnne Hewett, FCC week 2024

## Slide 6: Power and energy: future colliders
From: Steinar Stapnes
Linear collider studies predict roughly similar power consumption for equivalent machines (ILC vs CLIC)

## Slide 7: How can SC and NC have the same power consumption?
Linear collider RF systems fall in two categories
Despite the ~106 difference in quality factor, (~103 considering cryo efficiency), pulsing at low duty factor allows reducing the average consumption for NC accelerating structures down to the SC level – which cannot be effectively be pulsed
We want to verify whether HTS in pulsed RF mode allows a further power gain compared to both Nb and Cu
SC niobium, Q01010, 35 MV/m, CW
NC copper, Q0104, 100 MV/m, pulsed

## Slide 8: C3, a new kid on the block?
More info on C3 here
From: Emilio Nanni
Improvements in Q factor compared to copper could pave the way for energy savings

## Slide 9: Background of HIGHEST

## Slide 10: HTS for the FCC-hh beam screen
FCC-hh, a proposed 100 TeV p-p collider at CERN, with 16 T dipoles operated at 1.9 K
A beam screen held at 50 K, to protect the dipoles from synchrotron radiation ~30 W/m/beam (LHC < 0.2 W/m)
HTS materials instead of copper in the FCC-hh beam screen, to improve beam stability (-> impedance) at 50 K
Bunched particle beams produces RF fields, up to ~1 GHz
Extremely challenging requirements:
  HTS must operate at 50 K and 16 T
  Critical fields Hc2 , Hirr >> 16T
  Jc > 25 kA/cm2 (2.5x108 A/m2)
  Surface resistance Rs better than for copper
Compatible with accelerator environment
  Minimize dipole field distortion due to persistent currents
  UHV compatible, low SEY, lifecycle assessment, etc..
16 Tesla !
Calatroni, IEEE TAS 26, 3500204 (2016)
Calatroni et al, SuST 30, 075002 (2017)

## Slide 11: Two material choices
Coat the inside of the screen
with Tl-1223 films
Manufacture the screen using REBCO tapes soldered to the screen

## Slide 12: Development of soldering technology
CC
Solder
Beamscreen
HTS tapes
Solders based on Sn / Pb / Cu / Bi & In temperatures < 220ºC
2x80 km of beam screens to be coated with HTS

## Slide 13: Validation of RF performance (UPC - ICMAB)
In house developed 8.05 GHz cavity resonator compatible with 25mm bore 9 T magnet at ICMAB
REBCO CCs outperform Cu at 50K and up to 9T
RS is microstructure dependent
Puig et al, SuST 32, 094006 (2019)
Surface currents equivalent to 0.1 MV/m of a typical accelerating cavity

## Slide 14: First real cavity, f9 GHz
We have developed a technology for applying 2D HTS tapes to 3D RF “RADES” cavities demonstrating the potential of HTS for RF applications J. Golm et al., IEEE TAS, Vol. 32, No. 4, (2022) 1500605
2x improvement of RF quality factor compared to copper
(newer prototype 5x improvement)
RADES cavity for axion searches
12 mm-wide HTS tapes

## Slide 15: First published physics results with an HTS coated cavity
arXiv:2403.07790

## Slide 16: Other results from CAPP
From: D. Ahn, CAPP. More info at Patras Workshop
2.2x10-5 
3.5x10-5 

## Slide 17: Goals of HIGHEST

## Slide 18: ICMAB – UPC: testing at higher RF power
Patrick Krkotic, PhD dissertation, UPC Barcelona 2022
THEVA inclined deposition
0 T external field
HTS coated conductors at 8 GHz (dielectric resonator) and 50 K

## Slide 19: Literature review
There are very few measurements on HTS at high RF currents (mostly microstrip resonators). But physics is proven.
~1011 A/m2 RF current (microstrip resonator, 200 µm, 350 nm thick, 8 GHz)
Powell et al. Journal of Applied Physics 86, 2137 (1999)
For 1 µm thickness this is equivalent to 105 A/m ( 0.1 T  25 MV/m)
Entering the “high-gradient” range

## Slide 20: Literature review - II
From: M. Hein, “High-Temperature-Superconductor Thin Films at Microwave Frequencies” (Springer Tracts in Modern Physics, 155)

## Slide 21: High-gradient testing at SLAC – supported by I.FAST IIF
“Mushroom” cavity. Can achieve Hpeak of about 360 mT – 2.9x105 A/m (equivalent to ~80 MV/m in a standard accelerating cavity) using 50 MW XL-4 Klystron at 11.4 GHz.
Zero E-field on the sample
Maximum H-field on the sample
Sample accounts for ⅓ of total cavity loss
Goal: demonstrate and qualify high-gradient pulsed operation of HTS, at cryo-temperatures

## Slide 22
Work plan from 4/2023 to 4/2025

## Slide 23
Segmented cavities
CERN
Segmented
cavity for
axion
detection
SLAC
Segmented
cavity for
RF pulse
compressor

## Slide 24
Industrial application prospect
At the end of this study, we aim at consolidating TRL4.
Prototype pulse compressor with SLAC will demonstrate TRL6.
  Timescale: 2-3 years after completion of this study
  Need a further round of funding
  This will include the design, fabrication and coating, and its validation in a high-power RF bench test bench.
Future accelerator projects will drive achieving further TRLs and drive commercialization.
  Industry will be involved for construction of devices
  Other companies may be involved for hardware manufacturing

## Slide 25
Addressing the European Green Deal
Benefits
Actions
New-generation collider linacs are expected to use hundreds of MW of electricity
Energy savings from HTS are in line with current policies of societal impact minimization

## Slide 26
Resources and budget
CERN:
  Provided resources: two senior physicist (scientific coordination, 0.2 FTE) and one senior Fellow (follow up, measurements, 0.5 FTE)
  Requested resources: 10 kEUR (sample manufacturing)
KCT:
  Provided resources: one senior scientist (design, procurement, coating, 1 FTE)
  Requested resources: 100 kEUR (80 kEUR manpower for coating operations, 20 kEUR sample holder manufacturing)
CSIC-ICMAB:
  Provided resources: one senior scientist (0.2 FTE), and one PhD student (0.5 FTE)
  Requested resources: 50 kEUR (40 kEUR PhD student and manpower for coating and characterization work, 10 kEUR consumable)
Ratio for the requested IIF funds: 120 kEUR personnel and labour / 40 kEUR material
Final deliverable is a report on the demonstrated achieved performance, and on the prospects for scalability to accelerator-scale RF devices.

## Slide 27
Budget table
 | Manpower | Materials | Total
CERN |  | 10 kEUR | 10 kEUR
KCT | 80 kEUR | 20 kEUR | 100 kEUR
CSIC-ICMAB | 40 kEUR | 10 kEUR | 50 kEUR
 |  |  | 160 kEUR

## Slide 28: A possible future ?

## Slide 29: Muon Collider
From: Chris Rogers

## Slide 30: Muon collider
Muon cooling system requires RF cavities operating at high-gradient AND in a strong magnetic field.
Normal conducting copper, possibly cryo: baseline option
A dream: High-Temperature Superconductors ?

## Slide 31: Final remarks
No data exist for modern HTS at high-gradient RF (either samples or cavities): experiments needed
Fabrication technologies for real cavities must be developed: wider soldered tapes within the iFAST collaboration “HIGHEST”
Eventually, develop a direct HTS coating technique on copper

## Slide 33: High-temperature Superconductors

## Slide 34: Superconductors zoo
By PJRay - Own work, CC BY-SA 4.0, https://commons.wikimedia.org/w/index.php?curid=46193149

## Slide 35: Zoo of superconductors
https://nationalmaglab.org/magnet-development/applied-superconductivity-center/plots
Jc may vary of orders of magnitude.
Hc2 has much smaller variation.
YBCO most promising candidate
NbTi – NbTiN possible candidates at B < 10T
Nb3Sn for B < 15 T

## Slide 36: Zoo of superconductors
https://nationalmaglab.org/magnet-development/applied-superconductivity-center/plots
Pinning force

## Slide 37: First: a caveat
Bulk Nb
HiPIMS +DC Bias
Nb/Cu samples
HIE-ISOLDE
JC decrease is guiding the development of Nb/Cu films
Rationale:
Results from HIE-ISOLDE and bulk Nb
Modelling of losses as hysteretic losses from RF fluxons penetration
Existing HTS Coated Conductors might not be the best choice at high-gradient RF, being optimized for flux pinning
4K, 250mT
From: Carlota Pereira Carlos

## Slide 38: REBCO coated conductors
REBCO crystal structure
Charge transport in planes
High anisotropy
Extreme sensitivity to oxygen content
Large and small
Electronic features:
Scheme of Coated Conductor (CC)
Buffer layers allow biaxial epitaxial REBCO growth
Metallic substrate makes tape ductile
Artur Romanov, PhD dissertation, UA Barcelona 2022

## Slide 39: Type II superconductors
Magnetic phase diagram
for type II SC
Vortex length scales:
Distance upon which magnetic field decays.
Distance upon which the order parameter decays.
Vortex in type II SC
Characterized by mixed phase
with vortex penetration.
Abrikosov lattice
Distribution into hexagonal lattice in homogenous material.
Artur Romanov, PhD dissertation, UA Barcelona 2022

## Slide 40: Vortex pinning
Defects: Strategy to pin vortices
Lorentz-like force provokes vortex movement
Defect landscape:
0D: Impurity atoms, interchanged atoms
1D: Dislocations, columnar defects
2D: Twin boundaries, grain boundaries
3D: Nanoparticles, associated strained regions
Critical current density
The maximum value of without moving the lattice, without presenting resistance.
Scales with current density and magnetic field
Artur Romanov, PhD dissertation, UA Barcelona 2022

## Slide 41: Various producers of CCs
CCs differ in architecture and REBCO microstructure.
YBCO (1.6 ) + BZO nanorods
EuBCO (2.5 ) + BHO nanorods
GdBCO (1.5 )
YBCO (3 ) + Y2O3 nanodots
Bruker
Fujikura APC
SuNAM
SuperOx 2
Artur Romanov, PhD dissertation, UA Barcelona 2022

## Slide 42: HTS coating technologies
Patrick Krkotic, PhD dissertation, UPC Barcelona 2022

## Slide 43: Some theory background: fluxon motion in RF
The motion of the rigid fluxon lattice behaves as a harmonic damped oscillator
(neglecting thermal creep)
The “depinning frequency”
Gittleman and Rosenblum: Phys Rev. Lett. 16, 734 (1966)
Calatroni and Vaglio, IEEE Trans. Appl. Supercond. 27 (2017) 3500506
Coffey, Clem PRL 67, 386 (1991)
Brandt PRL 67 2219 (1991)
Silva et al, PRB 78, 094503 (2008)
d
Chart: 
Pinning centers
B field is normal to surface: worst case
Surface resistance

## Slide 44: RF when an external magnetic field is present
Vortex pinning
  Artificial pinning centres
Vortex lattice
  cylindrical normal conducting regions tens of nm diameter
  Each vortex carries one flux quantum
Apply RF Current
  Motion of vortices  dissipation
    The motion of the rigid vortex lattice behaves as an harmonic damped oscillator with quadratic potential
Simplified model valid for estimates and scaling
Gittleman and Rosenblum: Phys Rev. Lett. 16, 734 (1966)
Calatroni and Vaglio, IEEE Trans. Appl. Supercond. 27 (2017) 3500506
Coffey, Clem PRL 67, 386 (1991)
Brandt PRL 67 2219 (1991)
Silva et al, PRB 78, 094503 (2008)
Patrick Krkotic, PhD dissertation, UPC Barcelona 2022

## Slide 45: Coating process I
2) Edge removal
1) Pre-tinning
Ag
Substrate
Buffer layers
Ag
REBCO
Cu
Solder
Ag
Substrate
Buffer layers
Ag
REBCO
Cu
Solder
Developed in the context of FCC-hh impedance reduction by coating the beam screen with HTS tapes

## Slide 46: Coating process II
3) Soldering
Ag
Substrate
Buffer layers
Ag
REBCO
Cu
Solder
4) Substrate extraction
Solder
Cu
Ag
REBCO
Cu
Surface to coat
Cu
Substrate
Buffer layers
Ag
Cu
Solder
Cu
Ag
REBCO
Substrate
Buffer layers
Ag
Cu
Surface to coat
Cu
N. Lamas et al., to be published

## Slide 47: Scaling to lower frequency
REBCO scaled to 1 GHz at 50 K
x100 improvement over Cu at 50 K
Romanov et al, SciRep 10:12325 (2020)
For HTS Rs scales as
For Cu Rs scales as
GHz
38x12 mm samples
50 mm bore
16 T
at all frequencies
A parallel-plate resonator is being commissioned to test samples at ~1 GHz
Will demonstrate real experimental frequency scaling on samples

## Slide 48: Surface impedance: the key
RS Surface resistance (property of the surface)
: instabilities rise-time
: betatron tune-shift
Ib: bunch current
M: number of bunches
E: beam energy
L: bunch length
R: accelerator radius
c: speed of light
b: vacuum chamber radius
f: wakefields frequency
: electrical resistivity
 Risetime of beam instabilities
ZT Transverse impedance (property of the beam)
What could be better than copper at 50 K?
High-Temperature Superconductors (HTS)

## Slide 49: New kid on the blocks: the C3 study @ SLAC
8 km footprint for 250/550 GeV CoM ⟹ 70/120 MeV/m
Large portions of accelerator complex compatible between LC technologies
Beam delivery / IP modified from ILC (1.5 km for 550 GeV CoM), compatible w/ ILC-like detector
Damping rings and injectors to be optimized with CLIC as baseline
Cryogenically cooled – 77 K (liquid nitrogen)
C3 - 8 km Footprint for 250/550 GeV (to scale)
From: Emilio Nanni
Cooling allows for increase in accelerating gradient, and savings in RF power infrastructure
C3 Parameters
More info here

## Slide 50: Flux pinnining
Typical SRF accelerator cavities are made of niobium
Effect of external magnetic field on SRF accelerating cavities is mostly due to flux pinning, weak pinning in bulk Nb and strong in Nb/Cu
Earth magnetic field should not be an issue for HTS (to be verified)
Strong magnetic shielding needed
Limited or no magnetic shielding

## Slide 51: HTS tape at 8 GHz (dielectric resonator) and 50 K
Patrick Krkotic, PhD dissertation, UPC Barcelona 2022

## Slide 52: Effect of magnetic field: fluxon losses in RF
Surface resistance, reactance due to vortex motion
To maximize f0 and minimize fluxon losses we need high Jc materials
“safe” zone
“unsafe” zone

## Slide 53: Predicted surface resistance of HTS in 16 T field
YBCO | Tc=92K | T=50K | B0=16T | Jc(50,16)=7.5x109Am-2 | Bc2(50)=40T | n=60cm | f0=10GHz
Tl-1223 | Tc=125K | T=50K | B0=16T | Jc(50,16)=1x1010Am-2 | Bc2(50)=80T | n=80cm | f0=14GHz
For HTS the Rs scales as
For Cu the Rs scales as

## Slide 54: Cryogenic losses: SRF aimed at energy saving compared to NRF
Carnot efficiency
Cryoplant efficiency
30%
Power consumption for 1 W @ 77 K | 13 W
Power consumption for 1 W @ 20 K | 50 W
Power consumption for 1 W @ 4.2 K | 230 W
Power consumption for 1 W @ 1.9 K | 920 W
Thanks to T. Koettig, CERN

## Slide 55: Low-power RF measurements
An improvement larger than x10 compared to copper (Rs=8m) has been measured on samples of tapes (8 GHz) at low RF power
Adapted from Romanov et al, Sci. Rep. (2020) 10:12325
Cu

## Slide 56: HTS for axion searches
Increase Q
copper coating  superconducting coating
Requirement: High quality factor in a high magnetic field
Motivation:
Axion haloscope

## Slide 57: First results at SLAC, at low gradient
Two HTS measurements, after calibration measurements with Cu and Nb
Rs Cu  17 m
Rs REBCO tapes  1.7 m
Rs REBCO PVD  1.0 m
Directly grown REBCO on MgO and on copper+MgO (CERACO)
Soldered REBCO-CCs on copper (Fujikura by CSIC-ICMAB)

## Slide 58: Preliminary SLAC results at high-gradient I
From: Mitch Schneider

## Slide 59: Preliminary SLAC results at high-gradient II
From: Ankur Dhar
Shaded area: change from 100 W to 1.6 kW of forward power

## Slide 60: First device validation – supported by I.FAST Innovation Fund
Next goals: develop large-size tapes (50 mm wide) in collaboration with KCT, to be first tested on discs at SLAC. Two-years plan funded by IIF
(Ideally: REBCO coating directly on 3D objects)
Device validation: X-band pulse compressor (SLAC) as first “real” RF device
Coating will be performed by CSIC-ICMAB
Courtesy Greg LeSage, SLAC
Pulse compressor

## Slide 61: Axion cavity as earlier demonstrator
Approach being validated also for axion detection cavities in RADES collaboration having a similar geometry
Copper body manufactured at Mainz University, adapted to 12 mm wide coated conductors, coated by CSIC-ICMAB
Axion cavity
Q0 = 268 520 (75%)
    Surface currents
    E-field
    f= 9.3 GHz
Q0 = 356 070

## Slide 62
Summary of milestones and deliverables: WP2 KCT
M1 - Design and fabrication of sample holder system (due 3/2024). Achieved well in advance
D1 - HTS coating of large samples (due 3/2025). On track and well under way, first 40 mm wide tape already coated (final goal is 50 mm, but 40 mm is enough for our final goal)
KCT confidential
Do not disclose
Roll to roll coater for HTS tapes
40 mm wide HTS tape

## Slide 63
Summary of milestones and deliverables: WP3 CSIC
D1 - Coating on discs and segmented cavities for benchmarking (small tapes) (due 3/2024). Achieved for discs, already high-power tested at SLAC (presented at EUCAS 2023 / IPAC 2024) waiting for readiness of segmented cavity
D2 - Measurement of superconducting properties of large size tapes (due 3/2025). On track and well under way, first 40 mm wide tape already characterized
CSIC confidential
Preliminary results
Do not disclose
Copper disc coated with 12 mm tapes
First tests of 40 mm tape

## Slide 64: Possible practical implementation of HTS tape-coated cavities
How could a future cavity look like? Bimetallic cavities
J. Haimson, WEPMS085, PAC07 (s.steel inserts)
CLIC Mo-iris prototype
P. McIntyre et al., IEEE TAS 19 (2009) 1380
Composite cavities exist and have been demonstrated.
Joints at low-current regions are standard practice even in SRF cavities (ie QWRs)
Segmentation at zero-current region is possible, see device being designed at SLAC
SC
NC
B