## Slide 1
HTS soldering & preliminary characterization
HIGHEST” High-Temperature High-Gradient Superconductors
2024 – 07 – 05 CERN

## Slide 2
3 – R&D and lessons learned
1 – Alternatives to commercial CC
Outline
D-Nano 40 mm-wide CC tape “batch #1”
Jena YBCO thin film
2 – Coating a RADES cavity
4 – Plan of action
Solder thickness
Pressure homogeneity

## Slide 3
3 – R&D and lessons learned
1 – Alternatives to commercial CC
Outline
D-Nano 40 mm-wide CC tape “batch #1”
Jena YBCO thin film
2 – Coating a RADES cavity
4 – Plan of action
Solder thickness
Pressure homogeneity

## Slide 4
3D HTS coatings will benefit from having wider tapes
40mm-wide D-Nano tape from batch #1

## Slide 5
3D HTS coatings will benefit from having wider tapes
40mm-wide D-Nano tape from batch #1

## Slide 6
40mm-wide D-Nano tape from batch #1 is unsuitable as low Rs coating
40mm-wide D-Nano tape from batch #1
& n = 8 GHz
40mm-wide D-Nano tape from batch #1 shows rather high Rs values

## Slide 7
40mm-wide D-Nano tape from batch #1
& n = 8 GHz
40mm-wide D-Nano tape from batch #1 shows rather high Rs values
Based on previously reported low Jc values, the high Rs (H=0) could arise from “high-angle” grain boundaries
40mm-wide D-Nano tape from batch #1 is unsuitable as low Rs coating

## Slide 8
3 – R&D and lessons learned
1 – Alternatives to commercial CC
Outline
D-Nano 40 mm-wide CC tape “batch #1”
Jena YBCO thin film
2 – Coating a RADES cavity
4 – Plan of action
Solder thickness
Pressure homogeneity

## Slide 9
YBCO thin film* shows encouraging results…
*MgOSC /YBCO15nm /STO20nm /YBCO400nm
m0H(T)
m0H(T)
m0H(T)
m0H(T)
m0H(T)
m0H(T)
& n = 8 GHz
& n = 8 GHz
& n = 8 GHz
& n = 8 GHz
& n = 8 GHz
& n = 8 GHz
…when compared to best CC

## Slide 10
@20K & 8GHz
RRR10 Cu
RRR50 Cu
YBCOSC
EuBCOCC
…when compared to Cu
YBCO thin film* shows encouraging results…
*MgOSC /YBCO15nm /STO20nm /YBCO400nm

## Slide 11
3 – R&D and lessons learned
1 – Alternatives to commercial CC
Outline
D-Nano 40 mm-wide CC tape “batch #1”
Jena YBCO thin film
2 – Coating a RADES cavity
4 – Plan of action
Solder thickness
Pressure homogeneity

## Slide 12
Coating process overview
2) Edge removal
1) Pre-tinning
Ag
Substrate
Buffer layers
Ag
REBCO
Cu
Solder
Ag
Substrate
Buffer layers
Ag
REBCO
Cu
Solder
REBCO (1 – 3)
Buffers (0.2 – 1 )
Metallic substrate (30 - 100 )
Protective layer
Scheme of Coated Conductor (CC)

## Slide 13
3) Soldering
Ag
Substrate
Buffer layers
Ag
REBCO
Cu
Solder
4) Substrate extraction
Solder
Cu
Ag
REBCO
Cu
Surface to coat
Cu
Substrate
Buffer layers
Ag
Cu
Solder
Cu
Ag
REBCO
Substrate
Buffer layers
Ag
Cu
Surface to coat
Cu
Coating process overview

## Slide 14
RADES cavity coating in detail
Pressure Homogenizer
Coating the Axion Cavity – May 2021– Guilherme Telles and Neil Lamas

## Slide 15
1st coating: Outperformed 100% Cu cavity
B [T] |  | 
0 | 40,000 | 80,000
11 | 40,000 | 60,000
B [T] |  | 
0 | 40,000 | 80,000
11 | 40,000 | 60,000
Q-factor measurements
Coating performed slightly worse than expected

## Slide 16
2nd coating: The coating failed under external magnetic field
B [T] |  |  | 
0 | 40,000 | 80,000 | 200,000
11 | 40,000 | 60,000 | ?
B [T] |  |  | 
0 | 40,000 | 80,000 | 200,000
11 | 40,000 | 60,000 | ?
Coated with Fujikura
Used less solder to reduce solder overflow
Promising Q values!

## Slide 17
3rd coating: The coating failed under external magnetic field
B [T] |  |  |  | 
0 | 40,000 | 80,000 | 200,000 | 100,000
11 | 40,000 | 60,000 | ? | ?
B [T] |  |  |  | 
0 | 40,000 | 80,000 | 200,000 | 100,000
11 | 40,000 | 60,000 | ? | ?
How to prevent detachment?

## Slide 18
3 – R&D and lessons learned
1 – Alternatives to commercial CC
Outline
D-Nano 40 mm-wide CC tape “batch #1”
Jena YBCO thin film
2 – Coating a RADES cavity
4 – Plan of action
Solder thickness
Pressure homogeneity

## Slide 19
Right amount of solder
Amount of solder
Too much solder
REBCO deformation
+ solder leak
Not enough solder
 no adherence
Right amount of solder

## Slide 20
At least 10 mm of solder thickness are needed
Sample ID | Solder thickness | Pressure [kg/3e-3m^2] | Kapton test | Intrusive test
1 | 6.5 | 50 |  | 
2 | 6.5 | 100 |  | 
3 | 10.3 | 50 |  | 
4 | 10.3 | 10 |  | 
5 | 10.3 | 25 |  | 
1 bar (corresponds to 30 kg) of pressure applied on 10 mm of solder
withstands at least 11 bar of pulling pressure

## Slide 21
3 – R&D and lessons learned
1 – Alternatives to commercial CC
Outline
D-Nano 40 mm-wide CC tape “batch #1”
Jena YBCO thin film
2 – Coating a RADES cavity
4 – Plan of action
Solder thickness
Pressure homogeneity

## Slide 22
Simulations of the RADES Cavity show a pulling pressure ≤ 110 bar
DC Field-induced currents
Lorentz forces
-axis
-plane maximum
-axis max pull-off force
5

## Slide 23
Lorentz Forces in REBCO-coated Cavities for Dark Matter Search – Guilherme Telles
Critical region is around the central flat portion of the cavity
-axis
-plane maximum
-axis max pull-off force
We need to better homogenize the applied pressure during soldering

## Slide 24
Pressure sensitive sheet
We can quantify the pressure & its homogeneity

## Slide 25
Longitudinally: one side of the cavity
Transversally: start of curvature
Low-pressure areas
There seems to be a correlation between locally low pressure and detachment
1.5 - 2.5 bar
0.8 - 1.2 bar
We are not achieving an homogeneous pressure in the cavity

## Slide 26
Softer pressure homogenizer without air bubbles
Custom negative piece
New high precision press
What do we need to improve homogeneity?

## Slide 27
What do we need to improve homogeneity?
Elastosil M 4601 A/B Silicone
Hardness Shore A 28
For semi-closed geometries
(RADES, KEK…)
Silicone rubber cast
Silicone rubber sheet
Hardness Shore A 20
For open geometries
(flux compressor, polyhedral cavity….)
Custom negative piece
Silicon rubber sheet
Facet to be coated
Softer pressure homogenizer without air bubbles (to be tested)
Custom negative piece
New high precision press

## Slide 28
What do we need to improve homogeneity?
Automatic pressure control
Softer pressure homogenizer without air bubbles
Custom negative piece
New high precision press (Implemented)

## Slide 29
What do we need to improve homogeneity?
We use FEM simulations to determine best negative piece geometry for a given surface
Softer pressure homogenizer without air bubbles
Custom negative piece (tested successfully)
New high precision press

## Slide 30
3 – R&D and lessons learned
1 – Alternatives to commercial CC
Outline
D-Nano 40 mm-wide CC tape “batch #1”
Jena YBCO thin film
2 – Coating a RADES cavity
4 – Plan of action
Solder thickness
Pressure homogeneity

## Slide 31
– Wait for results on the new RADES cavity and re-coat if needed using a silicone cast
– Design negative piece(s) for SLAC’s flux compressor based on COMSOL simulations
Plan of Action
– Run pressure homogeneity experiments to find best configuration
– Push R&D on pre-delaminated coatings