## Slide 2: Nb3Sn coil packs: mechanical characterization & modelling
25/04/2024

## Slide 3
Context – Nb3Sn magnets design
Issue: Degradation occurs in some magnets at computed stress below the “limit”, some other work at computed stress higher than the “limit” (e.g. 11T can degrade at simulated 60 MPa, RMM can work at simulated 200 Mpa).
  Non comprehensive list of unsolved questions in a general context
  More accurate definition of the stress limit on conductor (3D)
  Model and experimental data are not in phase during cooldown and requires fine tuning (loss of prestress at cold)
  Local structural effect (peak stresses)
  Stress during reaction
Our objectives:
  Improve modelling of the coil material during the life steps of a magnet (assembly, reaction, cooldown, powering)
  Provide harmonized and model adapted experimental data of the coil pack (ID card for each coil)
  In particular, in the context of HFM program
    12T, Cosinus theta type dipole
    14T+, Block coil type dipole

## Slide 4
A standard 10-stack sample
Standard fabrication: Identical sample configurations, repeatable and documented fabrications
  Void / pressure
  Reaction cycle
  Impregnation cycle
Standard characterization: List of measurements and measurement methods
  Stress/strain (3 directions, 2 temperatures)
  CTE (3 directions)
  Dimensions (non reacted/impregnated samples)
Focus put on the harmonization of the fabrication and the characterization

## Slide 5
Toward a standard 10-stack Id card
Phase 1: Resolve some open questions
  Relevant sample configuration
  Stress/strain measurements methods: global vs local
  Influence of sample’s length
  Effect of surface
  Load effect on CTE
Phase 2: Only then
  Characterize and compare 10-stack for different magnets/coils
  Investigate impact of resin fraction
  Investigate new fiber,
  …

## Slide 6
Toward a standard 10-stack Id card
1. Which version of the keystoned stack is more representative of the non-keystoned stack (model)?
Proposed study: Compare stress/strain curves and DIC for 3 configurations using identical samples
Cable representative
Coil representative
It is not only a difference in stress decomposition:
varying stiffness along the width of cable
Assumed reference
In models

## Slide 7
Toward a standard 10-stack Id card
2. Are global (LVDT) and local (DIC, extensometer) technics measuring the same thing?
Proposed study: Measure simultaneously the deformation under load with both LVDT and DIC.
Cable stack compression – DIC observation
(EDMS 2714314)
Wolf et al., IEEE Trans. Appl. Supercond., 29 (2019)
Fichera et al., IEEE Trans. Appl. Supercond., 29 (2019)

## Slide 8
3. Is the length of the sample influencing the measurement?
Proposed studies:
With transverse load applied, compare stress gradient on the longitudinal direction for sample of different length
After load cycles, a Vickers measurement to compare hardening of copper for different length
Toward a standard 10-stack Id card
Balachandran et al., Supercond. Sci. Technol., 34 (2021)

## Slide 9
4. Understand the effects of interfaces during measurements: surface irregularities, double stacks,…
Proposed study: DIC measurements with stacks sandwiched by different interfaces.
Toward a standard 10-stack Id card
sitting effect
Cable stack
to cable stack
Intermediary material
Cable stack
to wedge

## Slide 10
5. How does the load influence the thermal contraction of the stack?
Proposed studies:
Compare CTE (3 directions) before and after load cycles.
Measure CTE on samples under load (Reiter et al., IEEE Trans. Appl. Supercond., 11 (2001))
Toward a standard 10-stack Id card

## Slide 11
Preliminary Test plan
Keystone – non compensated
CTE (tr)
CTE (ax)
CTE (ra)
Strain (tr)
LVDT+DIC (ax)
CTE (tr)
CTE (ax)
CTE (ra)
Vickers
Strain (ax)
LVDT + DIC (ra)
CTE (tr)
CTE (ax)
CTE (ra)
Vickers
Strain (ra)
LVDT + DIC (ax)
CTE (tr)
CTE (ax)
CTE (ra)
Vickers
Vickers
Study case cable: 11T and SMC
1s
1s
2s
2s
1s
1s
2s
1s
1s
Strain (tr) – LVDT+DIC (ax)
Strain (tr) – LVDT+DIC (ra)
Vickers
1l
1l
1l
8s + 2l
CTE (tr)
CTE (ax)
CTE (ra)
Strain (tr) – LVDT+DIC (ax)
CTE (tr)
CTE (ax)
CTE (ra)
Strain (ax) – LVDT+DIC (ax)
CTE (tr)
CTE (ax)
CTE (ra)
Strain (ra) – LVDT+DIC (ax)
CTE (tr)
CTE (ax)
CTE (ra)
1s
1s
s: short sample – 15 mm
l: long sample – 50 mm
Flat (reference)
Keystone - compensated
4s
4s
Strain (tr) – LVDT+DIC (ax)
CTE (tr)
CTE (ax)
CTE (ra)