## Slide 1: Stress-Managed Asymmetric Common-Coils (SMACC)
D. Araujo, B. Auchmann, A. Brem, T. Michlmayr, C. Müller, A. Stampfli, J. Van den Eijnden
6th Common-Coils Joint Meeting – May 2024
Work supported by the Swiss State Secretariat for Education, Research and Innovation SERI.
This work was performed under the auspices and with support from the Swiss Accelerator Research and Technology (CHART) program

## Slide 2: Motivation
In respect to standard common-coils magnet, we would like to:
deal with high Lorentz forces in a different way
simplify the common-coils architecture for accelerator magnets
have a full common coils architecture and reacting & winding
D. Araujo

## Slide 3: Stress-Managed Asymmetric Common-Coils (SMACC) –Nb3Sn – hf_3
1 2 3 4
Layers | 1 | 2 | 3 | 4
Wire type | Nb3Sn RRP® 162/169 | Nb3Sn RRP® 162/169 | Nb3Sn RRP® 78/91 | Nb3Sn RRP® 60/91
N wire x dia in mm | 26 x 1.1 | 26 x 1.1 | 40 x 0.7 | 40 x 0.7
Cu/nCu | 0.9 | 0.9 | 1.2 | 1.8
Bare Cable dimensions in mm* | 15.77 x 2.06 | 15.77 x 2.06 | 14.94 x 1.3 | 14.94 x 1.3
Insulation thickness in mm | 0.155 | 0.155 | 0.155 | 0.155
Number of turns | 8 | 43 | 62 | 62
D. Araujo
* Does not include Rutherford cable core

## Slide 4: Stress-Managed Asymmetric Common-Coils (SMACC) – Nb3Sn – hf_3
1 2 3 4
B0 in T | Eop in MJ/m | Top in K | % Margin | Iop in kA
14 | 2.94 | 4.22 | 9.8 | 14.77
Layer | Bpeak in T | % Margin | Jsc in A/mm2 | Jcu in A/mm2 | Jov * in A/mm2
1 | 14.83 | 9.80 | 1135.8 | 1261.2 | 389.5
2 | 14.81 | 9.91 |  |  | 
3 | 11.24 | 11.68 | 2110.8 | 1759.0 | 605.7
4 | 9.78 | 13.98 | 2686.5 | 1492.5 | 
* Including insulation area
D. Araujo

## Slide 5: Stress-Managed Asymmetric Common-Coils (SMACC) – Nb3Sn – hf_3 - 14 T
High-Field (1 and 2) and Low-Field (3 and 4) Jc fitting
The same Jc fitting is used for ERMC and DEM-0.7
D. Araujo

## Slide 6: Stress-Managed Asymmetric Common-Coils (SMACC) - Cross-Section
The asymmetric common-coils magnet has an intra-beam distance of 250 mm, 50 mm bore, yoke diameter of 660 mm and 30 mm thick stainless-steel shell.
The magnet has 4 different types of coils (layer 1, layer 2, layer 3 and 4)
and 8 coils in total (for a double aperture magnet). The coils are placed
in the stress-management formers. The preload is transferred
towards the inner-most layers through the ribs.
The iron pole, combined with the asymmetric concept, helps on the
balance vertical force balance.
The magnet concept is based on bladder & keys technology for room
temperature preload.
D. Araujo

## Slide 7: Mechanical Analysis
Von-Mises
Von-Mises
Hoop Stress
S1
D. Araujo

## Slide 8: Mechanical Analysis
Maximum
principal stress
D. Araujo

## Slide 9: 3D Magnetic Analysis – Iop = 14.77 kA
B0 in T | Bp in T | Lss in mm
13.81 | 14.47 | 500
B0 in T | Bp in T | Lss in mm
13.98 | 14.70 | 1000
B0 in T | Bp in T | Lss in mm
14.01 | 14.71 | 1500
2D without self-field | B0 in T | Bp in T
14 | 14.00 | 14.56

## Slide 10: 3D Magnetic Analysis – Multi-poles
Multi poles | 2D | Lss = 500 mm | Lss = 1000 mm | Lss = 1500 mm
b3 | +6.45 | +5.84 | +6.29 | +6.36
b5 | -6.75 | -7.10 | -6.94 | -7.00
b7 | -6.25 | -6.45 | -6.30 | -6.38
b9 | -1.75 | -1.82 | -1.72 | -1.74
a2 | -2.87 | -16.95 | -5.86 | -4.58
a4 | -4.55 | -4.50 | -4.39 | -4.40
a6 | +6.85 | +6.91 | +6.82 | +6.83
a8 | -0.71 | -0.73 | -0.76 | -0.82
-14.08 | -2.99 | -1.71
2D

## Slide 11: SMAAC 14 T and 13 T @ 4.5 K 9.5 – 10% margin
SMACC HF 3
SMACC LF 2

## Slide 12: SMAAC 14 T and 13 T @ 4.5 K 9.5 – 10% margin
SMACC HF 3
SMACC LF 2

## Slide 13: SMAAC 14 T and 13 T @ 4.5 K 9.5 – 9.8% margin
SMACC HF 3
SMACC LF 2

## Slide 14: SMAAC 14 T and 13 T @ 4.5 K 9.5 – 10% margin
SMACC HF 3
SMACC LF 2
Re-use shell, rods, bladders, keys
re-machine yoke

## Slide 16: Stress-Managed Asymmetric Common-Coils (SMACC) –Nb3Sn – hf_3 - 14 T
Ribs and spar thickness were optimized for mechanics.
|B| including self-field
D. Araujo

## Slide 17: Mechanical Analysis
Pre-load with 0.5 mm interference on the keys.
Von-Mises
Von-Mises
Hoop Stress
D. Araujo

## Slide 18: Mechanical Analysis
Von-Mises
Von-Mises
Hoop Stress
D. Araujo

## Slide 19: Mechanical Analysis
14 T operation
Stress on coils: 135 MPa on corners, other else < 100 MPa
Von-Mises
> 30% engineering margin on the peak of stress regions.
D. Araujo

## Slide 20: Subscale – Winding
former
spool
Rotating beam
After 1st coil block
rib
Before pushing down
After pushing down

## Slide 21
D. M. Araujo

## Slide 22: Magnetic Design
Let’s consider two typical common-coils turns distribution, with racetracks on the top and bottom of apertures for field quality correction (a and b). C shows a third design without racetracks / clover-leaf coils, with an additional common-coil on the hard-way bend direction.
a: racetracks / clover-leaf coils and wide blocks
b: racetracks / clover-leaf coils and thin blocks
c: only common-coils and thin blocks
Stress-management with spars, but high vertical load
Stress-management with spars and ribs
Asymmetric design