## Slide 1
Towards ordering the cavities
CNRS/IN2P3/IJCLab
Akira Miyazaki, Patricia Duchesne, Gilles Olivier, Sebastien Blivet, Guillaume Olry

## Slide 2: Introduction : History summary and series production
1995
2000
2005
2010
2015
2020
2025
ESS
MYRRHA
PIP2
PIP2
EURISOL
He Liquefier (2008)
SPIRAL2
MYRRHA
Clean-room for cryomodule (2007)
Chemical facility (2008)
SPIRAL2
ESS
Furnace (2016)
New Assembly Hall (2020)
Klystron (2017)
Upgrade CV800 (2018)
First cryogenic test of a cryomodule at Supratech (2007)
Supratech Platform is officially recognized by IN2P3 (2017)
EU-XFEL
MAX
Creation of IJCLab, merging of equipment from LAL and IPNO in Supratech (2020)
TTF3
LHC
First cryogenic test of a Spoke resonator in Europe (2002)
Supratech Platform is created (2004)
Calibration Station (2000)
Vertical cryostat (CV800)
MYRTE
Series production
Prototyping Phase
R&D
ESS : - preparation & testing of cavities, couplers and tuners
- Integration of 14 cryomodules
LHC : Calibration of all Cernox thermal sensors (> 6000 units)
PIP-II : Testing of 33 Spoke cavities
Spiral2 : Integration and test of 7 cryomodules
MYRRHA : - preparation & testing of 60 couplers and tuners
EU-XFEL : Preparation and power testing of 800 couplers

## Slide 3: Low-b cavities for protons & heavy ions collider cavities
ILC cavities (1.3 GHz)
FCC/PERLE cavities (800 MHz)
88 MHz
352 MHz
352 MHz
325 MHz

## Slide 4: PERLE project at IN2P3/IJCLab and cavities
Ultimate goal of PERLE: first multi-turn ERL designed to operate at 10 MW (20 mA, 87250500 MeV)
A hub to explore a broad range of accelerator phenomena and to validate technical choices improving accelerators for future energy and intensity frontier machines
Target Parameter | Unit | Value
Injection energy | MeV | 7
Electron beam energy | MeV | 250 / 500
Average beam current | mA | 20
Bunch charge | pC | 500
Duty factor |  | CW
Beam Dump
800 MHz 5-cell SC cavity x 4
(22 MV/m)
800 MHz 1-cell SC cavity x 4
(9.2 MV/m)
Injector Linac
Main Linac

## Slide 5: R &D targets
P. Dhakal “Nitrogen doping and infusion in SRF cavities: A review” Phys Open 5 100034 2020
FCC/PERLE
For FCC/PERLE
Extremely high-Q at relatively high gradient in large cavities (800 MHz)
Extremely high gradient with relatively high-Q in a large # of cavities (~8000)
For ILC250
Duty cycle =100%
Duty cycle <1%

## Slide 6: FCC/PERLE RF design: different strategy to eliminate HOMs
JLab
FCCUROS5
Shahnam’s PhD thesis
Trapped mode in 5-cells damped with HOM couplers
HOM couplers tested with Cu prototype cavity
HOMs extracted through beam pipe  Beam Line Coupler or Absorber
Simulation only

## Slide 7: Strategy for successful cavity preparation
JLAB prototype 1-cell @ IJCLAB
  Mid-T baked by JLAB  no improvement
  Deep groove (1 mm) in welding found by FNAL
  repair?
JLAB prototype 5-cell @ FNAL
  Determine the best recipe for PERLE/FCC
  1st test showed bad Q0 and Q-slope
  Light EP and another test without mid-T bake
FCC prototype 1-cell from CERN
  One cavity will be provided by CERN (mid 2025)
On my desk 
Public tender for PERLE cavities (JLAB RF design): end of 2024
  1-cell bare cavity for the validation process in the vendor (end 2025)
  4 x 5-cell jacketed cavities for the accelerators (no spare, no prototype!)
  Recipes need to be determined during the fabrication process without R&D!

## Slide 8: Fabrication and preparation of the cavities
Plan A: EP + heat treatment
Plan B: BCP + heat treatment
Risk in increasing costs
Risk in lower performance
Validate EP process and its cost with the 1st single cell prototype

## Slide 9: Experiences from JLAB prototype vs series ESS cavities
P.A. Smith et al SRF2017
JLab
Step | Amount
Bulk BCP | 90+110 um
600C annealing | 10 hours
Final BCP | 20 um
Step | Amount
Bulk BCP | 200 um
800C annealing | 3 hours
Final EP | 30 um
120C baking | 12 hours
We will not reach PERLE specification with the ESS standard recipe
No safety margin from JLAB recipe
 More advanced recipe!
800 MHz
704 MHz

## Slide 10: List of the advanced recipes
P. Dhakal “Nitrogen doping and infusion in SRF cavities: A review” Phys Open 5 100034 2020
P. Sha et al. Appl. Sci. 12, 546 (2022)

## Slide 11: high-Q / high-G cavities in the world
F. Eozenou et al TTC high-Q/high-G WG Sep 2022 LINAC22 THPOGE23
120C baking @ CEA-Saclay
650 MHz
300C baking or N-doping seems like the best option for FCC/PERLE
120C or 2-step baking for higher gradient  ILC
Clean vacuum baking furnace is key in this research domain
P. Sha et al. Appl. Sci. 12, 546 (2022)
300C baking @ IHEP
J. Maniscalco TTC high-G/high-Q WG meeting 09/08/2022
2N0 doping at 800C @ LCLSII
704 MHz
1.3 GHz

## Slide 12: Clean vacuum furnace at IJCLab: same as the one in ZANON
Vacuum furnace originally used for 600C annealing of ESS spoke cavities
A cryogenic pump, pure Ar for purging etc
Never used for advanced heat treatment (mid-T bake)
Annealing at 800C with samples to see contaminations
M. Fouaidy et al., IEEE Transactions on Applied Superconductivity, vol. 28, no. 4, pp. 1-6 (2018)

## Slide 13: 300C baking of DESY 1.3 GHz cavity in IN2P3/IJCLab
13
April 3 2024
Large volume  ultimate vacuum reach is not as good as KEK
Offset between target (300C) and cavity (316C)
No clean room around
  Same as JLAB  Lid + plastic bag prepared in a clean room
  FNAL and KEK have a clean room in front
Very first mid-T bake in France

## Slide 14: 1st test is always far from ideal (CV1 at CEA Saclay on June 18 2024)
1st cooling down after long shutdown
T-sensor at the bottom broken
No info in

## Slide 15: 1st test results
2024 mid-T bake at 2 K
2022 1st EP @ 1.4 K
2022 2nd EP + 650C @1.4 K
2024 mid-T bake
2022 1st EP
2022 2nd EP + 650C
At 1 MV/m
The mid-T baked cavity showed significantly high residual resistance
 Is it due to contamination of furnace/cavity or magnetic field effect?

## Slide 16: Magnetic field sensitivity (1.3 GHz cavities)
JLab
KEK
Not optimized for mid-T!

## Slide 17: Compare to JLAB result at 2 K: 25 mG case
2022 2nd EP + 650C @1.4 K
2022 1st EP @ 1.4 K
2024 mid-T bake at 2 K
We could explain the degradation of Q due to non-optimized magnetic shield and high sensitivity to trapped flux in mid-T baked cavities
 Improving magnetic shield and installing magnetic field at CEA!

## Slide 18: 2n cooling down: temperature sensors were OK (July 18 2024)
Cavity top
Cavity bottom
800C & 600C annealed 1.3 GHz cavity with at
 No flux expulsion is expected

## Slide 19: Flux expulsion is mandatory for mid-T bake or N-doped cavities
Lower
M. Checchin TTC topical workshop 2017
Meissner State
Mixed State
Balance between thermodynamic force and pinning force in the mixed state
Higher thermal gradient  higher expulsion efficiency
 Cooling down with higher thermal gradient is a standard receipt in LCLS-II at SLAC
900C annealing
800C annealing

## Slide 20: Surface resistance at low field during cooling down
The very high residual resistance of the last measurement after mid-T bake was due to the bad ambient magnetic field
The magnetic field expulsion is still not perfect
KEK cryostat for final check
FJPPN “ERL collaboration”

## Slide 21: Q vs E and Rs vs E
20 MV/m seems like a quench limit after the mid-T bake at 316C
Maybe a small anti-Q-slope was observed
Before mid-T bake data was taken at 1.4 K

## Slide 22: 3rd test at KEK (1st week of October) being prepared
2.0 K
1.4 K
Our results so far
316C baking, no perfect magnetic field
 Extremely interesting to test this cavity at KEK

## Slide 23: Risk management of 5-cell 800 MHz cavities
The 1st constraint is budget
  We prepared public tender based on quotations from the vendors
  Niobium materials is under procurement; very expensive!
  Cavity fabrication + preparation will be soon published; super expensive!
Within the budget, we need to take a risk
  Mid-T baking is the most promising way to achieve the potential performance of PERLE
  However, magnetic field environment and flux expulsion capability will be known at the very end inside the cryomodule (deliverable of iSAS)  out of spec. can be the practical answer
  Backup 1: reset the surface with light BCP  ESS spec: 17 MV/m Q0=1010  200 MeV instead of 250 MeV
  Backup 2: reset the surface with light EP  jacket is the obstacle
EP is still under discussion
  Cold EP can achieve x100 better surface roughness than BCP Knowledge transfer was done from FNAL to a vendor with 650 MHz cavity  No technical issue
  Budget is the constraint!
  No EP  BCP at IJCLab  ESS spec or trying mid-T bake after BCP (R&D subject)
HOM damping scheme
  HOM couplers were validated with copper cavities (Carmelo’s PhD thesis)
  Risk in niobium coupler antennas  hyper expensive; challenging to cool down
  FCC’s scheme (no HOM couplers) is not yet validated  too late for the iSAS public tender
  Backup (?)

## Slide 24: Booster cavities: low gradient requirement: new proposal
MV/m & Single cell 800 MHz  Nb3Sn/Nb at 4 K is realistic!
M. Seidel iSAS workshop 2023
S.Claudet et al, CERN 2013
Timeline: 4 years  800 MHz single cell prototype for Nb3Sn test after mid-T bake
Nb3Sn booster + mid-T bake ERF  the most advanced SRF accelerator project!
Crylcooler is probably too ambitious at this moment
PIPII 650 MHz in Fermilab!
Courtesy:
Sam Posen

## Slide 25: Conclusions
IJCLab has been a world-leading laboratory of SRF cavities for proton / heavy ion linear accelerators
  R&D of Spiral2, ESS, MYRRHA, PIPII cavities are coming to the final phase
  Contributions to collider projects has been in beam dynamics and nanobeams (ATF), RF couplers (Eu-XFEL), temperature sensors (LHC), etc
Risk management is the critical issue in the iSAS/PERLE cavity procurement
  Very ambitious specification (however not impossible according to the literature)
  No sufficient R&D: time and money  international collaboration to complement it
  Limited budget (or too expensive cavities)  several options to mitigate the risks
Advanced heat treatment is the key R&D subject
  IJCLab is equipped with a clean vacuum furnace originally used for the ESS spoke cavity project
  Mid-T baking for super high-Q
  1st mid-T baked results in 1.3 GHz cavity  studies on-going
Future prospects (end 2024 – beginning 2025)
  3rd test at STF in KEK (October) with flux expulsion
  Repairing JLAB 800 MHz prototype cavity
  Procurement of Nb materials and cavities
Collaborations
  Collaboration with INFN-LASA / CEA Saclay via iSAS
  ERL collaboration with KEK via FJPPL
  FCC: collaboration with CERN/FNAL
  PERLE: collaboration with CERN/JLAB
  Potential collaboration with iHEP