## Slide 1: Topics for MD simulations

## Slide 2: SUMMARY
Dislocations vs film thickness
Dislocations vs ions energy
Dislocations vs interrupted growth
Surface smoothening vs ions energy
Cristallinity vs ions energy
Surface oxide as a barrier to Hydrogen diffusion
Toward Nb3Sn?

## Slide 3: Dislocations vs Thickness
Single layer growth
2.3.10-3 mbar, Kr
Dislocation density measured by GIXRD (incidence angle 2 degrees)

## Slide 4: Dislocations vs ions energy

## Slide 5: Dislocations vs interrupted growth
Dislocations (~ size to niobium’s coherence length) = pinning sites
3 layers, 0.67 µm each
Interrupted growth possible strategy to decrease film’s dislocation density
Change number of layers (i.e. layer thickness) but maintain total thickness 2 µm
Maintain thickness of each layer around 0.67 um, but change total number of layers
Nb
Cu
30 min
30 min
Disloc. density increases with more layers?
Interrupted growth:

## Slide 6: Surface smoothening vs ions energy

## Slide 7: Surface smoothening vs ions energy

## Slide 8: Surface smoothening vs ions energy

## Slide 9: Cristallinity vs ions energy (Nb/Cu)
0V
-50V
-75V
-85V
-100V
-125V
150C
Simulation with different Cu surface orientations?

## Slide 10: Surface oxide as a barrier diffusion to hydrogen
At the end of the coating process, 2 routes
Cavity is left cooling down from 200C to RT and then vented with dry air
Cavity is oxidized at 200C, 5.10-3 mbar O2 for 2 hours, then cooled down, tehn vented with dry air
Is the second scenario a good way to reduce residual hydrogen pumping?

## Slide 11: Toward Nb3Sn?
Much more complex system
Nb, Sn target. 75%, 25%
Bi-Polar HiPIMS
High temperature coatings (600C – 750C)
RF DATA AVAILABLE – 3 different coating pressures