## Slide 1: Materials Studies of Processes in Internal Oxidation Nb3Sn wires: TU Bergakademie Freiberg Collaboration
Simon C. Hopkins, T. Boutboul (TE-MSC-LSC)
G. Rosaz (TE-VSC-SCC)
211th TE-TM Meeting, 3 June 2024
With thanks to A. Leineweber, J. Lachmann and S. Waschull (TU Bergakademie Freiberg)

## Slide 2: Introduction
Magnet designs for proposed future energy-frontier hadron colliders impose challenging performance targets for Nb3Sn wire, including:
  non-Cu Jc ≥ 1500 A/mm2 (16 T and 4.2 K)
  deff ≤ 20 µm
Internal oxidation methods show considerable potential to achieve these targets
Collaborations in the context of the High Field Magnets (HFM) programme are developing the understanding needed to establish a scalable wire technology, and optimise wire designs and heat treatments
  UNIGE (KE4663) is working towards a rod-in-tube internal oxidation wire design, producing and characterising trial wires
  This presentation concerns a new collaboration agreement with TU Bergakademie Freiberg (KE5963) addressing the mechanisms of this process with fundamental materials studies
A. Ballarino et al., IEEE Trans. Appl. Supercond. 29 (5) 6001709, 10.1109/TASC.2019.2896469

## Slide 3: TU Bergakademie Freiberg
Prof. Andreas Leineweber, Institute of Materials Science (IWW)
  Particular expertise in phase equilibria and crystallographic analysis; intermetallics (e.g. solder systems, Nb3Sn superconductors); XRD and Rietveld analysis
  Equipment for alloy production, sintering, PVD and galvanic deposition
  Characterisation by XRD, TEM and SEM (with EBSD), thermal analysis
Also access to relevant methods in other departments:
  Institute of Experimental Physics: semiconductor deposition
  Materials Technology: Institute of Metal Forming

## Slide 4: Nb3Sn Wire Technology
2024 marks the 70th anniversary both of CERN and Nb3Sn, now finally being united for HL-LHC in accelerator magnets
  Key challenge: Nb3Sn is brittle, and multifilamentary wires with a large fraction of stoichiometric, fine-grained Nb3Sn are needed
Our present baseline wire type is a variant of the internal tin process (1974):
  Nb filaments are distributed in a Cu matrix containing a Sn core
  Nb3Sn grows by solid state reaction-diffusion
RRP® assembly sequence
C. Sanabria, A new understanding of the heat treatment of Nb-Sn superconducting wires, PhD thesis, FSU 2017
The Restacked Rod Process (RRP®, ~2001) was developed by Oxford in Carteret (NJ, USA), now Bruker OST
  Subelements are produced from an assembly of Nb rods in Cu contained within a Nb diffusion barrier, stacked, and drawn to produce the wire
  Wires are now Ti-doped (increases Bc2)
  Flexible configuration to customise Cu/non-Cu and effective filament size, and optimise Jc and RRR for the application
108/127
.
120/127
132/169
150/169
162/169
Selected RRP® wire designs (schematic)

## Slide 5: Limits on Nb3Sn Wire Performance
RRP® has been extremely successful as a magnet conductor:
  High Jc and RRR
  Long piece length production
  Low degradation on Rutherford cabling
…but Jc performance has not advanced in recent years:
  Jc decreases with smaller subelements (ds < ~50 µm)
  Flux pinning is mostly by grain boundaries, so layer Jc(B) is limited by grain size (~100 nm) and Bc2
  Influenced by Sn stoichiometry and heat treatment – but a compromise between many parameters
    (grain size, Bc2, RRR, stability, mechanical properties)
HL-LHC 108/127
ERMC-1
12 T 4.2 K
15 T 4.2 K
Non-Cu Jc vs. ds for RRP® wires of different Nb:Sn stoichiometry
M. Field et al., IEEE Trans. Appl. Supercond. 24 (3) 6001105 (2014), 10.1109/TASC.2013.2285314
Non-Cu Jc at 4.3 K for several RRP® wires (no corrections)
Degradation on cabling for two RRP® and PIT wires
S. C. Hopkins et al., IEEE Trans. Appl. Supercond. 33 (5) 6000609 (2023), 10.1109/TASC.2023.3254497
S. C. Hopkins et al., IEEE Trans. Appl. Supercond. 34 (3) 6001308 (2024), 10.1109/TASC.2024.3375274

## Slide 6: Advancing Nb3Sn: Nausite (1)
During heat treatment, Nb3Sn grows at the surface of Nb filaments – basic approximation:
  Sn diffuses through Cu-Sn and the Nb3Sn layer to the Nb interface, where Nb3Sn is formed
  For internal tin wires, we pass through all phases of the complex binary Cu-Sn phase diagram, but interactions with Nb (and Ti…) not explicitly considered
…but far from the full picture
  Rely on Cu favouring the formation of stoichiometric Nb3Sn
  Early reports of inward Cu diffusion and of Nb dissolution
  Extensive intragranular Cu found in high resolution microscopy
A ternary Cu-Nb-Sn phase was eventually identified (‘nausite’) (M. Naus et al., 2001)
  Forms a ‘membrane’ at the interface between the Nb filament bundle and the Sn-rich core, influencing Cu/Sn transport
  Associated with Nb dissolution and formation of coarse/disconnected Nb3Sn at CERN (I. Pong et al., 2011)
Cu-Sn phase diagram and (dashed) plateau temperatures in Nb3Sn wire heat treatments
RRP® subelement after the 400 °C heat treatment step
C. Sanabria, PhD thesis, FSU 2017
M. T. Naus et al., IEEE Trans. Appl. Supercond. 11 (1) 3569–3572 (2001), 10.1109/77.919835
I. Pong et al., IEEE Trans. Appl. Supercond. 21 (3) 2537-2540 (2011), 10.1109/TASC.2011.2106473

## Slide 7: Advancing Nb3Sn: Nausite (2)
Work between CERN and TUBAF began following an internship of their student Alexander Walnsch (2015)
TUBAF identified the crystal structure of nausite (Nb0.75Cu0.25)Sn2 in 2016
Meanwhile, Sanabria (at FSU) had found that optimisation of the heat treatment step at 350–400 °C could regulate nausite thickness (‘nausite control’) and improve Jc for small ds wires
The observations that:
  Heat treatment optimisation – even before Nb3Sn forms – could achieve progress towards performance targets defined for FCC
  Knowledge of the ternary Cu-Nb-Sn diagram was remarkably incomplete, but necessary for optimisation
  motivated the formulation of a collaboration agreement in 2017 (KE3985)
(a) Kikuchi pattern and (b) distribution of nausite in a PIT wire sample
S. Martin et al., Intermetallics 80 16-21 (2017) 10.1016/J.INTERMET.2016.09.008
Improvements in Jc(ds) dependence for nausite control heat treatments
C. Sanabria, PhD thesis, FSU 2017

## Slide 8: NbSn2 and Nausite
TUBAF optimised techniques (EBSD etc.) to distinguish NbSn2 and Nausite, and clarified their structural relationships
  Nausite is derived from NbSn2 by partial substitution of Nb for Cu
  Similar layered structures along [001]: lattice parameters are within ~1%, and the phase transition can be described by a change in stacking sequence
  Both phases form with {001} faceted interfaces to a Sn-rich melt, and grow perpendicular to [001], but with differences in morphology vs. temperature
Nausite
NbSn2
Atomic volume over the Cu solubility range of NbSn2 and nausite obtained from EDX and XRD of powder mixtures and diffusion couples
Examples of experimental Kikuchi patterns around [001] showing the characteristic bands with which the phases can be distinguished NbSn2 – a {022}; nausite – e {111}, f {112}
Nausite
NbSn2
J. Lachmann et al., Mater. Charact. 168 110563 (2020), 10.1016/j.matchar.2020.110563

## Slide 9: Nausite Decomposition
Thermal analysis of powder samples was used to analyse the decomposition of nausite
Corrected sample temperatures from DSC
~230 °C
~586 °C
Sn melting
η decomposition
nausite decomposition
Nausite
NbSn2
Right 
In situ XRD (Cu-Kα)
 Left
DSC
Analysis of phase transformations during heating of a nausite-containing powder sample
S. C. Hopkins et al., IEEE Trans. Appl. Supercond. 31 (5) 6000706 (2021), 10.1109/TASC.2021.3063675

## Slide 10: Cu-Nb-Sn Phase Diagram
Phase equilibria were studied by microscopy and thermal analysis of Nb-Sn and Cu-Nb-Sn samples:
  Powder pellets
  Diffusion couples: Cu and Sn sputtered on Nb
CALPHAD re-evaluation of Cu-Nb-Sn phase diagram, including nausite
Later collaboration (KE5074) extended this to consider the effects of Ta and O
  (Ta,Cu)Sn2 identified
  First steps towards analysing internal oxidation
450 °C
400 °C
370 °C
300 °C
210 °C
η (Cu6Sn5)
Nb
α Cu(Sn)
ε (Cu3Sn)
NbSn2/ nausite
Nb3Sn
Sn
J. Lachmann et al., Thermodynamic re-modelling of the Cu–Nb–Sn system: Integrating the nausite phase, CALPHAD 77 102409 (2022), 10.1016/J.CALPHAD.2022.102409

## Slide 11: Phase Transformations in Wires
CERN and TUBAF also conducted a joint study of phase transformations in wire samples
  Tested generality of Sanabria’s observations of RRP® for other RRP® designs, and for R&D distributed barrier and distributed tin wires
0 h
48 h
RRP® 1 mm
TVEL
JASTEC
BEI of samples quenched from 400 °C
η
ε
η
Nausite
S. C. Hopkins et al., Phase Evolution During Heat Treatment of Nb3Sn Wires Under Development for the FCC Study, IEEE Trans. Appl. Supercond. 31 (5) 6000706 (2021), 10.1109/TASC.2021.3063675

## Slide 12: Advancing Nb3Sn: Internal Oxidation
Flux pinning in conventional Nb3Sn wires is mostly on grain boundaries:
  Enhancing grain boundary pinning  refining grain size (compromise with Nb3Sn area, Bc2, heat treatment duration)
  Adding point pinning  adding or growing precipitates (strengthening may impede wire drawing)
‘Internal oxidation’ has been proposed by Xu et al. (2014) as the solution:
  Add a readily oxidised solute element (Hf or Zr) to the Nb alloy (e.g. Nb-Ta-Hf)
  Embed a source of oxygen (e.g. SnO2)
  Precipitates (e.g. HfO2) form only on heat treatment, in Nb3Sn, and:
    Impede Nb3Sn grain growth and/or
    Provide point pinning
X. Xu et al., Appl. Phys. Lett. 104 082602 (2014), 10.1063/1.4866865

## Slide 13: Advancing Nb3Sn: Internal Oxidation
Implemented in Hyper Tech Research (Columbus, USA) in collaboration with Ohio State University and Fermilab
  Nb3Sn grain sizes reduced to < 50 nm
  Non-Cu Jc exceeds FCC-hh target of 1500 A/cm2 at 4.2 K, 16 T
  Shifts pinning peak towards higher reduced field (B / Birr)
Hf
Zr
SEM cross-sections of reacted Hyper Tech Hf- and Zr- alloyed internal oxidation PIT wires
Non-Cu Jc (4.2 K) of internal oxidised wires compared to HL-LHC wire and FCC target
Grain boundary and point pinning contributions in APC wire
Very promising, but not yet an industrialised wire technology validated for accelerator magnet applications
  Still to be demonstrated: long length production, degradation on cabling, magnetothermal stability…
X. Xu et al., Supercond. Sci. Technol. 36 035012 (2023), 10.1088/1361-6668/ACB17A
J. Rochester et al., IEEE Trans. Appl. Supercond. 31 (5) 8000205 (2021), 10.1109/TASC.2021.3057560

## Slide 14: Internal Oxidation: Next Steps
Considerable progress with building understanding – e.g. at UNIGE (KE4663):
  Alternative oxygen source configurations have been evaluated
  Established by XANES that HfO2 precipitates form at the Nb3Sn growth front
but significant questions remain, e.g.:
  Detailed understanding of oxide decomposition, oxygen transport, and interactions with Cu/Cu-Sn
  Effects of Zr/Hf alloying on Cu-Nb-Sn thermodynamics and diffusion kinetics
  Effects of Nb alloy microstructure on Nb3Sn growth
Addressing fundamental questions is challenging in wire studies:
  Long lag between wire trials
  Complex geometry
  All processes coupled – e.g. Cu-Sn phase transformations, Nb3Sn growth, oxygen transport
Key motivation for new TUBAF collaboration:
  Use diffusion couples to decouple processes and better understand their mechanisms (SnO2 decomposition, O transport, HfO2 precipitation, influence of Hf/Ta/O on Cu-Nb-Sn, Nb3Sn formation and grain coarsening)
  Analyse wire samples to identify relevant model systems and validate applicability of conclusions
3-year collaboration (KE5963) signed in March 2024

## Slide 15: Methods: Lessons Learnt
Diffusion couple design
  Sn dewetting: use higher-melting Cu-Sn alloys and structured films
  Tune thicknesses and compositions to achieve representative Hf and O atomic fractions
Purity
  Characterisation of substrate materials and purity control during deposition to avoid the influence of other oxygen sources
    cf. wire studies with Hf alloying and without an oxygen source in which HfO2 precipitates were found
Superconducting characterisation of diffusion couple samples to close the loop with wire samples
  Prepare some samples in a form suitable for VSM at CERN
Grain size determination of very fine-grained regions challenging: multiple methods needed
Dewetting of Sn plated on Nb
C. Tarantini et al., Sci. Rep. 11 17845 (2021), 10.1038/s41598-021-97353-w

## Slide 16: Nb3Sn SRF Cavities
Cavities: transfer energy from an EM wave to the beam
Current technology at CERN: Nb/Cu (LHC, HIE-ISOLDE)
Objective: decrease by 10× the surface resistance at 4.5 K
Proposal: Replace Nb by Nb3Sn
Material validated on bulk Nb cavities (expensive, high flux sensitivity)
FCC mid-term report, cds.cern.ch/record/2887249/

## Slide 17: Nb3Sn SRF Cavities: A Comparison
Targets:
  High Eacc  high peak field
  High quality factor  low surface resistance (~0.4 nΩ), high Tc (~18.3 K)
Compared to wires:
  Many of the same parameters are influential, but the desired condition is different
  Operation in full Meissner state – flux penetration to be avoided at all costs!
  Detailed knowledge and control required of phase diagram, interdiffusion, purity/alloying, microstructure
  Temperature budget: Max 800 °C (cavity material integrity/flange brazing)
 | Wire | Cavity
Key Aim | Maximise flux pinning, optimise Fp(B) | Minimise resistance, avoid defects
Defects | Point pinning increases Jc at high field | Increase residual resistance
Refined microstructure | Fine grains (<100 nm) increase Fp and Jc | Typically ~1 µm (gb losses possible)
Alloying | Ti/Ta increase Bc2  increase Jc at high field | Increase residual resistance
Presence of Cu | Favours Nb3Sn growth | Surface Cu contamination
Stoichiometry | Optimise Tc and Bc2 | Maximise Tc, avoid secondary phases

## Slide 18: Methods Transferrable from SRF
High Power Impulse Magnetron Sputtering (HiPIMS)
  Nb and Nb alloy/composite targets (e.g. for Nb3Sn)
  Purity, cleanliness, UHV good practices (control O2 sources)
  Macrostructure control: porosity
  Microstructure control e.g. by ion bombardment energy
  Nb surface preparation (electropolishing, Buffered Chemical Polish, etc.)
Thin film characterisation:
  XPS profiling
  XRD (EN-MME)
  SHPM, VSM etc.
Materials
  RRR 300 Nb
  Microstructural control by cold work – rolling studies (EN-MME)
HiPIMS glow discharge during a quadrupolar sample coating
UHV coating setup

## Slide 19: Diffusion Couples: Basic Approach
Produce layered structures of:
  Nb and its alloys (‘Nb-X’: Nb, Nb-1Hf, Nb-4Ta-1Hf)
  Cu-Sn
  SnO2 (oxygen source)
  ‘Inert’ substrates (e.g. Y2O3, sapphire)
  using Nb-X sheets and sputtered films
Perform heat treatments for different temperatures and durations, and analyse the resulting microstructures by:
  Optical microscopy
  Scanning Electron Microscopy (SEM; cross-section and top-view)
  X-ray diffraction
  Analyse grain sizes by Electron Backscatter Diffraction (EBSD) and/or Transmission Kikuchi Diffraction (TKD)
  For selected samples:
    Transmission Electron Microscopy (TEM) – e.g. for precipitate analysis
    Vibrating Sample Magnetometry (VSM) at CERN – comparative study of Jc, Tc

## Slide 20: New Approaches: Cu-Sn and SnO2
High-melting Cu-Sn substrates:
  Prepare < 25 at.% Sn substrates by arc melting for heat treatments above 400 °C without melting
  Intermetallics (e.g. Cu3Sn) and Cu(Sn) solid solutions
SnO2 patterned films:
  Optimise sputter deposition of SnO2
  Create laterally structured SnO2 coatings, e.g. by photolithography:
    Mitigate dewetting (additional metal interfaces)
    Provide internal reference away from without oxygen source
Cu-Sn
Nb-X
SnO2
Internal oxidation
Reference

## Slide 21: New Approaches: Nb-X
Nb-X sheets
  Plates/foils ~1 mm thick
  Assess effect of microstructure with annealing and different degrees of cold work
  Tests with RRR 300 Nb (certified purity) and different rolling reductions
Nb-X sputtered films
  Coatings ~10 µm thick on ‘inert’ substrates (e.g. Y2O3 or sapphire)
  Produced at TUBAF
  Produced at CERN by HiPIMS:
    Benchmarking for purity and defect populations
    Control of microstructure

## Slide 22: Diffusion Couple Configurations
Expected configurations are shown schematically below
Designs will be finalised after trials in the first year
Cu-Sn
Nb-X
SnO2
Nb-X
SnO2
Cu
Sn
W
Nb-X
SnO2
Inert
Cu-Sn
W
These configurations are flexible enough to allow:
  Cu-rich (Cu-Sn substrate) and Sn-rich (Cu/Sn coatings) compositions
  SnO2 decomposition and O transport with (Nb-Ta-Hf) and without (Nb) Hf oxide precipitation
  Behaviour with and without an intentionally added oxygen source:
    As shown – internal reference between SnO2 patterned strips
    Samples produced with and without SnO2 layer
All with control of starting Nb alloy microstructure

## Slide 23: Wire Studies
Analysis of wire samples provided by CERN:
  Consistent comparison of microstructures (e.g. Nb3Sn grain sizes) in wires from different sources
  Comparison with diffusion couples to identify inconsistencies or interesting cases for further study
  Correlations with Ic measured at CERN  understanding of microstructural effects and heat treatment optimisation
Supported by complementary studies in TE-MSC-LSC:
  Ejection furnace: microscopy, VSM and RRR measurements of samples at different stages of the heat treatment
  Studies of rolled wire samples and cables when sufficient internal oxidation wire is available
Supports development of wire activities e.g. in UNIGE

## Slide 24: Work Plan
Activity |  |  | 24 |  |  |  | 25 |  |  |  | 26 |  |  |  | 27
 |  |  | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1 | Q2 | Q3 | Q4 | Q1
D1 | M1.1 | Cu-Sn substrate preparation |  |  |  |  |  |  |  |  |  |  |  |  | 
D2 | M2.1 | Patterning of SnO2 layers |  |  |  |  |  |  |  |  |  |  |  |  | 
 | M2.2 | Interaction of SnO2 with Nb/Nb alloys |  |  |  |  |  |  |  |  |  |  |  |  | 
D3 | M3.1 | Definition of diffusion couple designs |  |  |  |  |  |  |  |  |  |  |  |  | 
 | M3.2 | Trial samples for magnetisation measurement |  |  |  |  |  |  |  |  |  |  |  |  | 
 | M3.3 | Interim report: diffusion couple preparation and analysis |  |  |  |  |  |  |  |  |  |  |  |  | 
 | M3.4 | Samples for CERN characterisation (e.g. VSM) |  |  |  |  |  |  |  |  |  |  |  |  | 
 | M3.5 | Final report: diffusion couple preparation and analysis |  |  |  |  |  |  |  |  |  |  |  |  | 
D4 | M4.1 | Analysis of wire samples (batch 1) |  |  |  |  |  |  |  |  |  |  |  |  | 
 | M4.2 | Analysis of wire samples (batch 2) |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 25: Current Status
Visit to TUBAF in January 2024 to visit experimental facilities and discuss the planned work
Agreement signature completed 18 March 2024
Kick-off meeting by Zoom in April 2024
TUBAF hired a PhD student, Simon Waschull, who visited CERN (22-31 May) for:
  UHV system training in TE-VSC
    Sample preparation and handling
    Materials compatibility (UHV)
    Bakeout procedure
    He leak testing
    Residual Gas Analysis
  Familiarisation with superconducting wire and magnet technologies in TE-MSC
    Nb3Sn wire metallography and microscopy (103, 288)
    Nb3Sn cabling (103)
    Superconducting tests (Ic, RRR, VSM, magnetothermal stability in 163)
    Visit to UNIGE for TEM of internal oxidation sample produced for KE4663 (FIB lamella prepared by EN-MME)
    Visits to LMF (180) and the polymer lab
  Discussions with EN-MME
    Visit of microscopy facilities (112)
    Discussion of cold worked microstructures in RRR Nb

## Slide 27: Additional Slides

## Slide 28: Nb-Sn Phase Diagram
Reports of the binary Nb-Sn (and Cu-Sn) phase diagrams have not always been consistent
  The Nb-Sn phase diagram of Charlesworth was commonly used (1970), with the established stoichiometries of the Nb-Sn binary intermetallics
  …but solubility and composition ranges were wildly inconsistent between studies and evaluations
J.P. Charlesworth et al., J. Mater. Sci. 5 580-603 (1970), 10.1007/BF00554367
Comparison of Nb3Sn phase fields between different published phase diagrams (1969–2002)

## Slide 29: The Influence of Ta
Ta decreases nausite and (modestly) Nb3Sn layer growth
Note Nb-4Ta is typical for Nb3Sn wire doping
Courtesy of A. Leineweber

## Slide 30: HiPIMS Microstructural Control
0 eV
50 eV
75 eV
85 eV
100 eV
125 eV
Nb3Sn morphology in Cu/Ta/Nb3Sn coatings vs. pressure
1μm
8×10-3 mbar
1μm
2.5×10-3 mbar
1μm
7×10-4 mbar
Tuning of dislocations in Nb/Cu thin films by ion bombardment energy
C. P. A. Carlos et al., CERN SRF Workshop, 2-3 Feb 2023, https://indico.cern.ch/event/1235920/