## Slide 1: Qualification of the first Cold Powering System for the HL-LHC triplets
Amalia Ballarino for the WP6a
Genova (Italy), 7-10 October 2024
14th HL-LHC Collaboration Meeting
A. Ballarino, Y. Leclercq, C. Barth, G. Willering, V. Gahier, F. Pasdeloup,
W. Bailey*, Y. Yang*
*University of Southampton

## Slide 2: Powering the HL-LHC magnets
SC Link
SC Link
8+2 Systems
Two types
74.5 m long
117 kA DC
120 m long
40 kA DC
Vertical path  8 m

## Slide 3: Cold Powering System for HL-LHC Magnets
SC Link
DFHX
Current Leads
DFX
Itot up to 117 kA DC
mHe by design  5.5 g/s
mHe controlled by TREBCO
He mass flow rate imposed by the cooling of the current leads
SC Link: transfer line for the helium gas needed for the cooling of the current leads  Low heat load cryostat
TREBCO  60 K
TMgB2  20 K

## Slide 4: The Superconducting Link for HL-LHC
 117  kA @ 25 K
  90 mm,  25 kg/m
418 kA
122 kA (coaxial)
37 kA
19 Polarities
REBCO
MgB2
A. Ballarino
MgB2 wire produced at ASG Superconductors
Superconducting Link cryostat produced at Cryoworld
MgB2 cabling performed at ICAS/TRATOS
REBCO cabling at CERN

## Slide 5: Cold Powering System in the SM-18
LHe
DFX
Superconducting Link
DFHX
GHe recovery
Powering 18 kA, 15 kA, 2 kA, 2 kA

## Slide 6: Cold Powering System in the SM-18
Bending radius  2 m
Q  1.6 W/m
Instrumentation signals: 304 voltage taps and 105 temperature sensors
Cooling with GHe: no thermal shields
DFHX
ext  1 m
19 Current Leads
= System assembly in the SM-18
- Not a “Prototype” – spare system for HL-LHC
- Many “first time” – cryo,vacuum,
mechanical, electrical..
Ltot = 5.5 m

## Slide 7: Contributions from our collaborators
A successful collaborative effort
University of Southampton - DFX
Uppsala University/RFR – Three components of DFHX
CERN Main Workshop
Manufacturing/assembly of resistive parts of
current leads
Manufacturing of mechanical components of DFHX
Welds in the SM-18

## Slide 8: Vertical Path of Superconducting Link
SOTON

## Slide 9: Cool-down
After the pressure test (4.6 bara) and the leak test (helium leak rate better than
1.0 × 10-8 mbar·l·s-1), cool-down to nominal cryogenic conditions was performed
T  50 K
from RT to 160 K
m = 2 g/s - 3 g/s
15 K
T  70 K
from 160 K to 15 K
DFHX Temperature
DFX Temperature

## Slide 10: Layout of DFX
MgB2 to Nb-Ti
Nb-Ti
WP6a
WP3

## Slide 11: Dealing with Thermal Contractions
Two thermal cycles (from room temperature to cryogenic conditions) followed by powering of all circuits. Repetitive performance
F = Fixed Point
Movements
(up to 3 cm)
Notes: guide rollers

## Slide 12: Powering Scheme
Maximum current delivered by the power converters: 94 kA
Four power converters:
18 kA – IHL-LHC = 16.23 kA (Nb3Sn quadrupole)
15 kA – IHL-LHC = 12.11 kA (Separation dipole)
2 kA – IHL-LHC = 2 kA (Trim)
2 kA – IHL-LHC = 1.74 kA (Correctors)
T sensors on MgB2
to REBCO
T sensors on REBCO
T sensors on MgB2

## Slide 13: Cryogenic and Electrical Performance (1/2)
4.9 g/s
3.5 g/s
94 kA
0 A
Mass flow rate dominated by requirement of optimized current leads:  0.05 g/(skA)

## Slide 14: Cryogenic and Electrical Performance (2/2)
4.9 g/s
3.5 g/s
94 kA
0 A
4.9 g/s
High voltage tests (2.3 kV among polarities and between each polarity and the ground) in nominal cryogenic conditions successfully performed (leakage currents < 10 A)

## Slide 15: Room Temperature Terminations
Maximum 5 °C increase at maximum current, no condensation during any operating condition (both at zero current and with current)

## Slide 16: Splices
Stable performance, no overheating, temperature of splices independent of current ( 1 K)
REBCO to MgB2, GHe @ 20 K
MgB2 to Nb-Ti, LHe @ 4.5 K
Nb-Ti to Nb-Ti, LHe @ 4.5 K
MgB2 to REBCO
MgB2 to
REBCO
MgB2 to
REBCO
Temperature
Temperature
time
time

## Slide 17: Transient Behavior
Successfully validated:
  Cryogenic requirement during transients
Capability of operating without liquid helium supply during 10 minutes with MgB2 to Nb-Ti splices immersed in liquid helium. Capability of producing up to 10 g/s of GHe
  Electrical requirement (cross talks)
Absence of cross talk among circuits – via electro-magnetic coupling. Fast discharges (up to 100 A/s) of the 2 kA circuits do not trigger the quench protection system of any of the other circuits
  High Voltage insulation
  Each circuit tested at 5 kV in air, 2.3 kV in nominal cryogenic conditions, and 1.1 kV in GHe at room temperature. Measured leakage currents 100 times lower than specified limit

## Slide 18: Re-spooling/Transport of SC Link + DFHX
See presentation of Y. Leclercq on Wednesday (WP6a in String)
Compactness of DFHX and flexibility of the SC Link enable assembly and qualification of the
Systems at the surface (before installation in the LHC underground)

## Slide 19: Conclusions
The first Cold Powering System for the HL-LHC Triplets has been successfully validated: cryogenic, electrical and mechanical performance all met design parameters. Robustness of the system in different operating modes was proven
The system transferred up to 94 kA (maximum current delivered by power converters) in DC mode and in nominal cryogenic conditions: MgB2 @ 20 K and REBCO @ 60 K. Operation of MgB2 is up to 29 K and of REBCO up to 70 K ( 10 K temperature margin)
Components of the Cold Powering Systems have been industrialized. They are today in an advanced phase of series production, and several series productions are completed (recently DFHX components)
The system has been opened, re-spooled, transported and installed in the String. This was also a good exercise for what will have a to done for the tunnel installation

## Slide 20
A phantastic team !

## Slide 21: Thanks for your attention !
Acknowledgements:
O. Pirotte, R. Mauny and J. Gery from the TE-CRG group
G. Pichon and S. Juberg form SM-18 TE-MSC operating team
W. Maan and G. Barlow from the TE-VSC group
P. Moyret and L. Deparis from the EN CERN Main Workshop
QPS and ELQA teams from the TE-MPE group
C. Bertone and E. Richards and the EN-HE transport team
Our collaborators: University of Southampton and University of Uppsala