## Slide 1: Experience on NCRs and future expectations
Julien DEBEUX (CERN) on behalf of HL-LHC WP4
14th HL-LHC Collaboration Meeting – Genoa (Italy) – 08/10/2024

## Slide 2: Introduction
Outline
  Brief reminder on NCRs for HL-LHC WP4
  NCRs spotted during RFD-SPS CM fabrication, assembly and reception
  Conclusions + few words about LHC Series
Not part of this presentation
  Manufacturing of CRAB cavities
  NCRs linked to FPCs
Talk of E. Jordan: “RFD NCRs & future mitigation”
Talk of J. Swieszek and S. Barriere:
“RFD-CM Repair overview and highlight”

## Slide 3: NCRs for HL-LHC WP4
Nonconformity → Non fulfilment of a requirement
  Requirements are specified in Engineering specifications, drawings, procedures, standards, etc.
Courtesy of H. Garcia Gavela: EDMS 2894857

## Slide 4: NCRs for HL-LHC WP4
Useful links and documents:
  HL QA training for WP4 (H. Garcia Gavela): EDMS 2894857
  NCR Process: EDMS 1499015
  NCR Process for Collaborations: EDMS 2149457
  NCR Template: EDMS 1501109
  Launching NCR using EDMS: EDMS 1908145
Main contacts:
  HL-Quality contact for WP4: G. Prica, H. Garcia Gavela
  Standards and specifications: L. Dassa
  Manufacturing quality / Welding activities: J. Debeux, M. Benahmed

## Slide 5: NCRs for HL-LHC WP4
Persons to be contacted in case of Nonconformity on the HL-LHC WP4 Cryomodule
 | Non-critical |  | Critical
 | 1 or 2 | 3 | 4 or 5
Standards and specifications | L. Dassa |  | O. Capatina
Transport engineering and Tuner | K. Artoos |  | O. Capatina
General Design - Test - RF compliance | N. Valverde |  | R. Calaga
General Design - Design & calculations | T. Capelli |  | O. Capatina
Manufacturing & assembly & Welding & Logistics | J. Debeux / S. Barriere | M. Garlasche | 
Materials | C. Santos Maldonado | I. Aviles | S. Sgobba
Survey | V. Rude | M. Sosin | H. Mainaud
Vacuum compliance | G. Bregliozzi |  | 
Cryogenic compliance | L. Delprat/K. Brodzinski |  | 
Cleanroom & RF cavity compliance | N. Valverde |  | R. Calaga
RF Tests | K. Turaj |  | R. Calaga
Low level RF | G. Hagmann |  | R. Calaga
RF Controls | A. Butterworth |  | R. Calaga
RF Power compliance | E. Montesinos |  | 
Beam dynamics compliance | N. Mounet | R. Tomas | 
HL Quality | G. Prica | H. Garcia Gavela | 
Integration, installation | G. Cipolla | P. Fessia/M. Modena | 
HL safety | C. Gaignant |  | T. Otto
Transport and handling on site | M. Perez Ornedo | C. Bertone | 
Safety conformity | D. Tshilumba/L. Dassa |  | S. Marsh
Configuration | M. Zerlauth |  | 
EDMS 3014549
Who (from CERN) should sign the NC will depend on the component/system/domain and the level

## Slide 6: Overview of NCRs for RFD SPS
2
Between 30 to 35 NCRs reported on EDMS
12 main steps of assembly, ~1300 items (~900 drawings), etc.

## Slide 7: NCRs during RFD-SPS CM fabrication, assembly and reception
Bellows and base materials

## Slide 8: NCRs spotted during RFD-SPS CM Components fabrication
Bellows
The NCRs are linked to:
  2-ply bellows
  Design and Test Pressure
  Dents
  Base material
  Dimensional aspect
~10 NCRs in total
Biphase boxes – Level Port Bellows
Bellows proposal from subcontractor
Approval focused on dimensions and base material
Essentially discussed / approved by mail
Info on «2-ply» missed during discussions

## Slide 9: NCRs spotted during RFD-SPS CM Components fabrication
Bellows
The NCRs are linked to:
  2-ply bellows
  Design and Test Pressure
  Dents
  Base material
  Dimensional aspect
~10 NCRs in total
Bellows for cryogenic lines
Design pressure is 2.1 barg and test pressure is 2.7 barg.
The supplier used a design pressure of 1.8 barg based on test pressure 2.7 barg + coefficient of 1.5 ; while the actual coefficient in CERN Specification is 1.25.

## Slide 10: NCRs spotted during RFD-SPS CM Components fabrication
Bellows
The NCRs are linked to:
  2-ply bellows
  Design and Test Pressure
  Dents
  Base material
  Dimensional aspect
~10 NCRs in total
Bellows for cryogenic lines and CWT

## Slide 11: NCRs spotted during RFD-SPS CM Components fabrication
Parallel with LHC Series (RFD Biphase & DQW PIMs)
!
!
Notes: Expliquer les causes des dents. Activités liée au transport / manipulation pour le PIMs.

## Slide 12: NCRs spotted during RFD-SPS CM Components fabrication
Bellows
The NCRs are linked to:
  2-ply bellows
  Design and Test Pressure
  Dents
  Base material
  Dimensional aspect
~10 NCRs in total
Cryogenic lines bellows, blade support and tuner bellows
Collars in EN 1.4429 2D Forged instead of 3D Forged
Convolutions in EN 1.4404 (EN 10088-2) instead of EN 1.4435 (EN 10028-7)
Missing Cobalt assessment or Cobalt content >0.3%
No magnetic permeability values given
No inclusion content reported

## Slide 13: NCRs spotted during RFD-SPS CM Components fabrication
Bellows
The NCRs are linked to:
  2-ply bellows
  Design and Test Pressure
  Dents
  Base material
  Dimensional aspect
~10 NCRs in total
Cryogenic line bellows (extremity bellows)
The total length of the bellows is shorter than required (118.6mm instead of 131.5mm)
The number of convolutions is lower than mentioned on drawing
Holes of blank extremity collar not perpendicular

## Slide 14: NCRs spotted during RFD-SPS CM Components fabrication
Bellows
The NCRs are linked to:
  2-ply bellows
  Design and Test Pressure
  Dents
  Base material
  Dimensional aspect
~10 NCRs in total
LHC SERIES
Update of Engineering specifications
Single sourcing for each type of bellows, then dispatched to the collaborations:
  Cryogenic bellows: KOMPAFLEX AG
  Tuner and blade support bellows: MEWASA AG

## Slide 15: NCRs spotted during RFD-SPS CM Components fabrication
Base material
~8 NCRs in total
The NCRs are linked to:
  Material standard
    ASME / ASTM vs EN standards
    EN standards for pressure applications (PED harmonized)
  Material grades or properties
    Grade of austenitic stainless steels (EN 1.4429)
    Welding filler material (W Z 18 16 5 NL)
    Magnetic permeability
  Cobalt content
    Cobalt content not mentioned in the certificates
    Values are above the limit
 For LHC Series: Update of specs and drawings, procurement strategy, improvement of QA/QC
Evaluation thanks to PMA
Evaluation by experts
Evaluation with destructive testing
Non-destructive measurements
Measurements at CERN
Tracking in EDMS 2798791

## Slide 16: NCRs during RFD-SPS CM assembly
Welding

## Slide 17: NCRs during RFD-SPS CM assembly
Orbital welds on beam screen lines

## Slide 18: NCRs during RFD-SPS CM assembly
Potential root causes:
  Tolerances of the parts
  Limited access
  Difficulty of execution
  Backing gas set-up
  Actions:
  STFC and CERN performed together the repair
  Knowledge transfer between the teams
  Modifications of the design drawing
  Qualification of the welder for repair operation
Orbital welds on beam screen lines

## Slide 19: NCRs during RFD-SPS CM assembly

## Slide 20: NCRs during RFD-SPS CM assembly
Dimensional control (Blade support assy, OVV, WMS, biphase line, etc.)
Clash / Matching during assembly (HOM Cooling line, RF Coax line, etc.)
Blow-off valve (insulation vacuum)
 Evolution of assembly procedure, Engineering Specs, safety components, etc.
Other NCRs

## Slide 21: NCRs during RFD-SPS CM Reception
Other NCRs
Tightening checks:
  Lateral doors: 1 door not OK (1/4 of a turn missing)
  Cavity support system:
    1 FPC connection partially OK
    Top blade connection: locking screws not OK
  Cryogenic transport lock: Loose
  Tuner Thermal Intercept: Connexion to double pipes or braids partially OK
Courtesy of T. CAPELLI

## Slide 22: NCRs during RFD-SPS CM Reception
Other NCRs
FSI checks:
  4 lower FSI were obstructed by MLI
Cryo instrumentation:
  Labels removed / replaced
  Heaters not installed / checked
Courtesy of T. CAPELLI
MLI
Reflector

## Slide 23: Conclusions and perspectives
RFD-SPS Prototype:
  This prototype phase was highly instructive, also for QA-QC activities.
  Some difficulties to deliver and review quality and manufacturing documents in time, with a rigorous respect of approval process.
Concerning requirements:
  To prepare LHC Series, the Eng. Spec and drawings were updated.
   Few Deviation Permit Requests have been already prepared.
Concerning NCRs:
  Important step during drafting NCRs: Root causes, preventive and corrective actions and implications
 For LHC Series:
All the requirements shall be respected, any deviation must be traced and approved before continuing the production.

## Slide 24: Conclusions and perspectives
CERN:
  A new welding and quality engineer hired in April 2024 (Myriam Benahmed)
Collaborations with STFC / TRIUMF:
  Good use of HL QA tools
  Efficient raw material procurement strategy
  Transparency, respect of reviewing processes (from the procurement specification drafting)
  Some QA tools have been implemented

## Slide 25: Thank you ! Any questions ?

## Slide 26: Back-up slides

## Slide 27: Back-up slides