## Slide 1: Exploring RF Breakdown and Conditioning in High-Gradient Accelerating Cavities
03.06.2025
Pablo Martinez-Reviriego
On behalf of CERN SY-RF-MKS, SY-RF-LIS and IFIC accelerator group
pablo.martinez.reviriego@cern.ch

## Slide 2: Outline
High power conditioning and Breakdown studies:
BTW cavity for medical applications:
Publication: https://doi.org/10.1016/j.net.2024.08.033
RFQ2 for Linac4 (ongoing):
Poster: https://indico.cern.ch/event/1424597/contributions/6532647/

## Slide 3: Outline
High power conditioning and Breakdown studies:
BTW cavity for medical applications:
Publication: https://doi.org/10.1016/j.net.2024.08.033
RFQ2 for Linac4 (ongoing):
Poster: https://indico.cern.ch/event/1424597/contributions/6532647/

## Slide 4: Hadron therapy
Hadron Therapy centres are growing fast, but all of them are based on circular machines
Advantages of linacs:
Fast dose delivery.
High beam quality.
High repetition rate.
Almost 100% of transmission: low radiation levels.
Technological challenges:
Large machines.
Complexity.
Accelerator | Beam always present during treatment? | Energy variation by electronic means? | Time needed for varying the energy
Cyclotron | Yes | No | 80-100 ms (*)
Synchrotron | No | Yes | 1-2 s
Linac | Yes | Yes | 1-2 ms

## Slide 5: Linear accelerators for hadron therapy
LIGHT project by A.D.A.M
230 MeV proton beam at 200 Hz. Coupled Cavity Linac:
18-20 MV/m.
Total length ∼28 m.
TULIP project
230 MeV proton beam at 200 Hz.
BTW cavities: 40 MV/m.
Length reduced by a factor 2.

## Slide 6: IFIC High-Power S-band facility and BTW structure
Designed at CERN for MV/m:
RF conditioning evolution
Breakdown localization
Field emission electron dynamics
Radiation characterization
FC-Down
-field
-field

## Slide 7: RF conditioning
FC down signal ∼ 0.
FC up signal saturates.
Dose reduced with conditioning.
Pablo Martinez
up to 39 MV/m.
800 M pulses.
Over 25000 BDs.
Limited by lab peak power.

## Slide 8: Comparison with other tests
Normalization factor:
Structure | [GHz] | Mode
TD24 N2 | 11.994 | TM01
TD26 | 11.994 | TM01
Crab cavity | 11.994 | TM11
BTW | 2.9985 | TM01
Structure |  | Mode
TD24 N2 | 11.994 | TM01
TD26 | 11.994 | TM01
Crab cavity | 11.994 | TM11
BTW | 2.9985 | TM01

## Slide 9: BD studies
Good agreement with previous results:
BDR decreases after operating at constant power.
Double exponential: tendency of BDs to produce clusters.

## Slide 10: Enhancement factor evolution
Dark current scans were performed at different stages of conditioning.
can be fit for each scan.
evolution during conditioning.

## Slide 11: BD localization: Edge method
Search of reflection rise and transmission drop.
No hot cells detected

## Slide 12: BD localization: Short pulses
Transmitted pulse does not show a flat top: rise time must be increased.
High accumulation of BDs characterized by low reflection and similar .

## Slide 13: Dark current dynamic simulations
Electrodynamic simulations in CST for field emitted electrons:
  Ratio of reaching FC.
  Energy deposited by .
Scans:
  Emission cell.
  Input RF power.
travelling
Down
travelling
Up

## Slide 14: Radiation simulations and measurements
Simulation:
  interacting with Cu wall.
  X-rays photons produced by bremsstrahlung.
  Spectrum decays exponentially up to maximum energy of incoming e−.
Measurement challenge:
  High fluence of photons during RF pulse: huge pile-up.
Solution:
  Small CeBr3 scintillating crystal detector.
  Pb collimator system: Holes of 4 and 2 mm.
  Measurements directly from PMT.

## Slide 15: Spectrum measurement set-up
Pulse Amp
Pulse PMT

## Slide 16: Spectrum measurements
Maximum energy of photons in agreement with dark current simulations.
Measurement campaign stopped due to a klystron mulfunctioning.
4 mm hole
2 mm hole

## Slide 17: Outline
High power conditioning and Breakdown studies:
BTW cavity for medical applications:
Publication: https://doi.org/10.1016/j.net.2024.08.033
RFQ2 for Linac4 (ongoing):
Poster: https://indico.cern.ch/event/1424597/contributions/6532647/

## Slide 18: Radio Frequency Quadrupole (RFQ)
m structure that focuses, bunches and accelerates continuous beam of low energy hadrons (few MeV)

## Slide 19: The Linac4 RFQ
Critical element in CERN proton chain: No spare
Surface damage observed in Linac4 RFQ
Hypothesis:
irradiation Degradation More BDs
Solution:
New RFQ fabrication and conditioning
Great opportunity for BD studies!
Limitation: New RFQ must survive the conditioning
Serafim, C., Calatroni, S., Djurabekova, F., Peacock, R., Bjelland, V., Perez-Fontenla, A. T., ... & Sargsyan, E. (2025). Effects of H− low beam irradiation and high field pulsing tests in different metals. Physical Review Accelerators and Beams, 28(1), 013101.

## Slide 20: A very different structure
Parameter | CLIC T24 | Crab cavity | BTW (hypothetical) | RFQ
Type | Travelling wave | Travelling wave | Travelling wave | Standing wave
Mode | TM01 | TM11 | TM01 | TE210
[GHz] | 11.994 | 11.994 | 2.9985 | 0.352
Length [m] | 0.2 | 0.24 | 0.190 | 3.06
Repetition Rate [Hz] | 20 - 200 | 50 | 20 - 200 | 0.833
Pulse length [s] | 0.2 | 0.2 | 2.5 | 1000
[MW] | 42.4 | 40 | 33 | 0.4
Max. E-field [MV/m] | 220 | 154 | 281 | 34
Max. H-field [kA/m] | 410 | 505 | 319 | 5.17
Max. [MW/] | 3.4 | 5.48 | 5.13 | 0.01
[MV/m] | 123 | 105 | 115 | ?
Parameter | CLIC T24 | Crab cavity | BTW (hypothetical) | RFQ
Type | Travelling wave | Travelling wave | Travelling wave | Standing wave
Mode | TM01 | TM11 | TM01 | TE210
 | 11.994 | 11.994 | 2.9985 | 0.352
Length [m] | 0.2 | 0.24 | 0.190 | 3.06
Repetition Rate [Hz] | 20 - 200 | 50 | 20 - 200 | 0.833
 | 0.2 | 0.2 | 2.5 | 1000
 | 42.4 | 40 | 33 | 0.4
Max. E-field [MV/m] | 220 | 154 | 281 | 34
Max. H-field [kA/m] | 410 | 505 | 319 | 5.17
 | 3.4 | 5.48 | 5.13 | 0.01
 | 123 | 105 | 115 | ?
Paszkiewicz, J. (2020). Studies of breakdown and pre-breakdown phenomena in high-gradient accelerating structures (Doctoral dissertation, University of Oxford).

## Slide 21: Field distribution
E-field
H-field
Parameter | RFQ | LES
[MHz] | 352 | 0
Repetition Rate [Hz] | 0.833 | 1 - 6000
Pulse length [s] | 1000 | 1 - 1000
Gap [mm] | 2.3 | 0.1
Voltage [kV] | 78 | 7.75
Max. E-field [MV/m] | 34 | 77.5
Parameter | RFQ | LES
 | 352 | 0
Repetition Rate [Hz] | 0.833 | 1 - 6000
 | 1000 | 1 - 1000
Gap [mm] | 2.3 | 0.1
Voltage [kV] | 78 | 7.75
Max. E-field [MV/m] | 34 | 77.5
RFQ cross section:
TE210 mode
Large Electrode System (LES)
I. Profilatova, Recent progress at pulsed dc systems, 8th International Workshop on Mechanism of Vacuum Arcs, 2019.
Large separation between electric and magnetic field
RFQ might be a key to connect High Frequency and DC

## Slide 22: Local power coupling simulation
Angular dependence
Paszkiewicz, J. Local power coupling as a predictor of high-gradient breakdown performance. High Gradient Workshop 2021.
Notes: Antenna length: 1 mm
Antenna length: 1 mm
𝑘_𝑙=5.4×10^(−9) 〖"Am" 〗^(3/2) "V" ^(−3/2)

## Slide 23: Local power coupling simulation
d [mm] | [MV/m] | [MV/m] | 
2.47 | 36 | 15.0 | 0.986
2.9 | 34 | 15.5 | 1
3.47 | 29 | 15.7 | 1.12
d [mm] |  |  | 
2.47 | 36 | 15.0 | 0.986
2.9 | 34 | 15.5 | 1
3.47 | 29 | 15.7 | 1.12
Gap dependence At kW

## Slide 24: RFQ measurements
Reflected power increases: Different coupling
Antennas show different behavior: BD localization
Vnuchenko, A. (2020). High-gradient issues in S-band RF acceleration structure for hadrontherapy accelerators and radio frequency Quadrupoles

## Slide 25: RFQ conditioning (ongoing work)
How can we localize BDs?
Experimental set-up:
Incident power
Reflected power
16 antenna signals
Lack of:
Transmitted power
Dark current

## Slide 26: BD simulation
Axial symmetry
Half symmetry
No symmetry
Up
Down
Up right
Down right
Up left
Down left
Wang, F., & Adolphsen, C. (2009). Localization of rf breakdowns in a standing wave cavity. Physical Review Special Topics—Accelerators and Beams, 12(4), 042001

## Slide 27: From measurement to simulation
Normalization:
Most similar simulation
W.L. Millar. Workshop on Breakdown Science and High Gradient Technology 2023, https://agenda.infn.it/event/34253/contributions/210153/

## Slide 28: What information can be obtained?
BD longitudinal position
Measurement and simulation agreement
Most similar mode distribution

## Slide 29: Axial position
0
12
1
12 and 1 type BD can be rotated by integers of
Sum of all BDs
V4
V1
V2
V3
Power Coupler

## Slide 30: Conclusions
BTW structure:
  A maximum gradient of 39 MV/m was achieved with 800 ns pulses without saturation.
  No hot cells detected.
  Dark current simulations show good agreement with experimental observations.
  Spectroscopy measurements showed good results. Klystron malfunction stopped measurements campaign.
  Dose decreases with conditioning. HG linacs produce high radioactive dose, requiring shielding.
Radio-Frequency Quadrupole:
  Local power coupling simulations agree with BD location and field gap dependence in DC.
  First conditioning curve for an RFQ structure (ongoing).
  Testing of method to compare antenna signals and BD localization simulation.
THANK YOU!

## Slide 31
Back up

## Slide 32: Hadron therapy
Accelerator | Beam always present during treatment? | Energy variation by electronic means? | Time needed for varying the energy
Cyclotron | Yes | No | 80-100 ms (*)
Synchrotron | No | Yes | 1-2 s
Linac | Yes | Yes | 1-2 ms
Relative Biological Effectiveness (RBE)
Linear Energy Transfer (LET)
Marx, V. (2014, April 4). Sharp shooters. 508. Nature, p. 137

## Slide 33: Some pulses

## Slide 34: The S-band BTW structure

## Slide 35: Tapering
The tapering makes the structure asymmetrical in the longitudinal direction
Design direction
Opposite direction

## Slide 36: BD localization: Phase method
Search for BD phase.
Cell localization.
is highly affected by
Accumulation of BDs in agreement with short pulses

## Slide 37: Hole size impact
Small hole: Photons must pass through small Pb region. Attenuation is higher for photons of lower energy.
Big hole: Photons can reach directly to the detector.

## Slide 38: Local power coupling
time
voltage
current
power
Field emission,
no plasma, tiny currents
Onset of breakdown and plasma formation
Fully formed plasma
Voltage collapse
Peak power demand during breakdown onset!

## Slide 39: BD simulation
TE110
TE210
TE112
Input power
Before BD:
Mostly TE210 is excited
Close to critical coupling
After BD:
Different eigenmode
New field distribution

## Slide 40: Measurement normalization
Normalization 1:
Normalization 2:
Normalization 3:
Linear

## Slide 41: Simulation normalization
Normalization 1:
To dB (Normalization 2)
Linear (Normalization 3)

## Slide 42: Error minimization
Measurement
1
4
3
2

## Slide 43: Local power coupling
Antenna length: 1 mm
Angular dependence
Quadrant dependence
Longitudinal dependence

## Slide 44: BD distribution RFQ1

## Slide 45: RFQ measurements
Reflected power increases: Different coupling
Antennas show different behavior: BD localization
BD recovery and soon activation with the same antenna pattern
Consecutive BDs (1 s separation) with the same antenna pattern
Vnuchenko, A. (2020). High-gradient issues in S-band RF acceleration structure for hadrontherapy accelerators and radio frequency Quadrupoles