## Slide 1: CNPEM's First Superconducting Device Development: A Wavelength Shifter for Sirius Hard X-ray Beamline
`
Rafael Molena Seraphim
(Head of the Systems Engineering Division)
On behalf of the Technology Unit
TE-MSC Seminar
27th June 2024

## Slide 2
Brief Overview of CNPEM
CNPEM engages in superconductivity initiatives
SWLS Overview
  Electromagnetic design
  Coils fabrication
  Mechanical design
  Cryogenic design
  Electrical systems
  Magnetic characterization approach
  Assembly and Sirius Installation
  Schedule and summarized development status
Outline

## Slide 3
We are located at Campinas (a city of ~1.1 million people), about 100 km from Sao Paulo
530,000 m2

## Slide 4: CNPEM is a private, nonprofit organization, working under contract with the Brazilian Ministry of Science, Technology, Innovation (MCTI)
DSC
Technology Unit
~860 employees
~450-560 trainees, pos-docs, students and outsourced personnel
Systems Eng.
Mechanical Eng.
Materials Eng.
Electrical Eng.
Computational Eng.

## Slide 5
Sirius Highlights
(Some numbers only considering the storage ring)
520 m of fully NEG-coated vacuum chambers (developed in-house)
~85% index of nationalization
180 RF BPMs and electronics; beam scrappers etc. (developed in-house or w/ partnerships)
RF amplifier tower
4 towers of RF solid-state amplifier, 65 kW each (developed in-house)
550 W module, produced by BBEF
More than 35 power Supplies powering families of magnets (developed in-house)
More than 1000 magnets (developed in a partnership w/ WEG)
Sirius
4th gen.
E = 3 GeV
C = 520 m
40 beamlines
ε = 0.25 nm.rad

## Slide 6
Brief Overview of CNPEM
CNPEM engages in superconductivity initiatives
SWLS Overview
  Electromagnetic design
  Coils fabrication
  Mechanical design
  Cryogenic design
  Electrical systems
  Magnetic characterization approach
  Assembly and Sirius Installation
  Schedule and summarized development status
Outline

## Slide 7
Motivation:
Superconductivity Initiatives
Sirius accelerators were delivered
late 2019
The accelerator's engineering division was separated from LNLS, and the Technology Unit was created – work on other engineering projects of the center and partnerships with Brazilian industry:
Knowledge gap: lack of expertise in superconducting technology -> Need to bring this expertise to CNPEM, focusing on the center's main actuation fields
mid 2020
    An agreement was signed between CNPEM and CERN for transferring know-how and technology in superconducting magnets
late 2020
      First initiative in superconductivity was started at CNPEM with CERN’s help: build a team at CNPEM and design of the first magnet
2021
Electric motors, generators, power transmission lines, SMESs
Energy
Accelerators
Magnets, insertion devices, RF cavities
Medical
Magnetic resonance devices (MRI and NMR), cyclotrons for therapy
Materials
Low and high temperature superconducting materials development and characterization
Main fields of interest

## Slide 8
Superconductivity Initiatives – CNPEM/CERN/Universities (USP and UFSCar) partenership
Setup for testing coils
Superconducting Dipole of 6.4 T (project on hold)
2021
Superconducting Wavelength Shifter of 6.6 T (ongoing project – FDR phase)
2021
Vertical Cryostat for Testing Superconducting Coils
2022
Manufacture and Characterization of NbTi Wires (ongoing project) – CNPq InovaNióbio Project
2023

## Slide 9
Setup for testing coils
Superconducting Dipole of 6.4 T (project on hold)
2021
Superconducting Wavelength Shifter of 6.6 T (ongoing project – FDR phase)
2021
Vertical Cryostat for Testing Superconducting Coils
2022
Manufacture and Characterization of NbTi Wires (ongoing project) – CNPq InovaNióbio Project
2023
Superconductivity Initiatives – CNPEM/CERN/Universities (USP and UFSCar) partenership

## Slide 10
Sirius phase 2 - new hard X-ray beamlines -> Need for high energy photons
SWLS - Motivation
Beamline | Exp. Technique | Energy Range [keV]
SUSSUARANA | X-ray Diffraction | 30 - 200
MANATI | X-ray Tomography | 80 - 150
Two beamline candidates
Current non-superconducting magnets of 3.2 T do not produce reasonable photon flux above 100 keV
11x
49x
204x
Aperture: 1x1 mrad²
(current beamlines focus on photon energies below 70 keV)

## Slide 11
Build a superconducting magnet, cryogen-free, with magnetic field higher than 6 T and compatible with one of the Sirius low-beta straight sections
The magnet must not impact the Sirius emittance and beam dynamics
Use NbTi wires
Reuse components from a deactivated 4 T Superconducting Wiggler
4 T SCW
Cold mass
(In LHe bath)
Schematic of a Wiggler
SWLS – Design Premises
Conceito de WLS
Nova estrutura eletromagnética
SWLS NbTi wire
Ø = 0.90 mm
Cu/NbTi = 0.97
Bought from Budker Institute of Nuclear Physics
SWLS

## Slide 12
Brief Overview of CNPEM
CNPEM engages in superconductivity initiatives
SWLS Overview
  Electromagnetic design
  Coils fabrication
  Mechanical design
  Cryogenic design
  Electrical systems
  Magnetic characterization approach
  Assembly and Sirius Installation
  Schedule and summarized development status
Outline

## Slide 13
Electromagnetic Design
Proposed electromagnetic model
Ho pole (12 mm) ferromagnectic below 20 K
Parameters | Targets
Current | < 300 A
Peak field | > 6 T
FWHM of central peak | < 30 mm
1st magnetic field integral | < 200 G.cm
Margin @ 5.0 K | > 20%
  A very narrow central peak field not to impact the beam emittance
Basic Parameters
Target magnetic field profile (Accelerators Physics group)
FWHM < 30 mm
7 T

## Slide 14
6.6 T
1.4 T
29.6 mm
Electromagnetic Design
Additional results
Parameters | Results
Roll-off of peaks (± 5 mm) | 0.16%
2nd magnetic field integral | 6.7 kG.cm²
Total integrated quadrupole | 0.13 T
Total integrated sextupole | 5.7 T/m
Current sharing temperature | 6.1 K
Total AC loss during ramp-up (time = 5 min) | 0.314 W
Stored magnetic energy | 3.37 kJ
Inductance | 130 mH
Electromagnetic Design Analysis and Optimization:
Geometry of the model
Magnetic field plots
Field integrals and multipoles
Fabrication errors
Load line operating margin
Energy Losses
SME and Inductance
Photon flux emission
Iop ≈ 228 A
Field maps
Parameters | Targets | Results
Current | < 300 A | 228 A
Peak field | > 6 T | 6.6 T
FWHM of central peak | < 30 mm | 29.6 mm
1st magnetic field integral | < 200 G.cm | 72 G.cm
Margin @ 5.0 K | > 20% | 24%
Main results
Simulated field profile

## Slide 15
Independent power supplies used to central and lateral coils:
Allows correction of the field integrals during the current ramp-up
Minimize perturbations on the beam
Electromagnetic Design – Current ramp-up
Operating current

## Slide 16
Brief Overview of CNPEM
CNPEM engages in superconductivity initiatives
SWLS Overview
  Electromagnetic design
  Coils fabrication
  Mechanical design
  Cryogenic design
  Electrical systems
  Magnetic characterization approach
  Assembly and Sirius Installation
  Schedule and summarized development status
Outline

## Slide 17
The coils have slightly oval shape to better maintain the tension on the wires during winding process
Lateral coil (180 turns)
Central coil (1080 turns)
Coils fabrication
Geometry and dimensions
Notes: Slide status e validações futuras

## Slide 18: Coil prototyping – winding process
Winding structure: Mandrel + pole + support (Upper lid)
Edges insulation: 300 µm fiberglass
Winding process: layer by layer
Interlayer insulation: 150 µm fiberglass
Notes: Isa

## Slide 19: Coils fabrication – impregnation setup and procedure
Pre-impregnation process:
Room temperature pump down (24h) and bake-out (24h@80°C): pressure 10-2 mbar
Resin overnight at room temperature with vacum pump
Impregnation process:
Degass the resin: 1h@50°C
Open valve and apply 100 mbar nitrogen pressure to control the velocity of the flow
Milking and reversed milking with 1 atm pressure (about 5 – 7 times)
Used resin:
Araldite F (100 pbw)
Hardener HY 905 (100 pbw)
Flexibilizer DY 040 (10 pbw)
Accelerator DY 062 (1 pbw)
Resin curing process
(pbw = parts by weight)
Notes: Isa

## Slide 20
Impregnation process was optimized using copper prototypes
After few copper prototypes, NbTi coils were successfully prototyped
Prototyped coils were successfully tested at the vertical cryostat
Coils fabrication - prototypes
NbTi lateral coil prototype
NbTi central coil prototype
Copper prototyoes – porosity evolution
Notes: Slide status e validações futuras

## Slide 21
Vertical Cryostat
Cryostat Design and Features:
The cryostat follows the same principles as the SWLS: conduction cooling, current leads, thermal shield, etc.
Applications and tests planned
Thermal and magnetic tests of superconducting coils
Thermal performance of components at cryogenic temperatures
Mechanical component fixation at cryogenic temperatures
Splice box performance evaluation
Quench protection system testing
Control system testing and evaluation
Notes: Slide status e validações futuras

## Slide 22
Mirror yokes were designed to test the coils
PCB boards with 3 Hall sensors (HGT-2101) were used to measure the magnetic field
Coils fabrication – tests in the vertical cryostat
Simulated magnetic profile for the mirror yokes
Results: Lateral coil
Field in 300 A
Hall Probes

## Slide 23
1006 steel and Holmium poles were tested
Quench protection was also tested and validated
Coils fabrication – tests in the vertical cryostat
Quench training: central coil
Results: Central coil

## Slide 24
Brief Overview of CNPEM
CNPEM engages in superconductivity initiatives
SWLS Overview
  Electromagnetic design
  Coils fabrication
  Mechanical design
  Cryogenic design
  Electrical systems
  Magnetic characterization approach
  Assembly and Sirius Installation
  Schedule and summarized development status
Outline

## Slide 25: Mechanical design
Electromagnetic structure
1
Electron beam vacuum chamber
3
Thermal circuit
2
Supports
4
1
2
3
4

## Slide 26: Mechanical design – electromagnetic structure
Main Concepts
Large thermal contraction of Al clamps to pre-load the coils
Central coils’ clamps with conical shape to prevent magnet’s gap closing
Invar washers to prevent bolt loosening
0.6°
Central coils’ conical clamps
Simulation Results of Thermal Contraction and Magnetic Forces for Coils and Clamps

## Slide 27: Mechanical design – vacuum chamber
Main Concepts
Tripartite CuCrZr chamber
Total length of 1.2m
Very thin central part (5mm vertical aperture; 0.5mm wall)
Optimized internal profile to withstand the pressure difference at the central part
38mm
5mm
0.5mm
6mm
Pressure gradient simulation for optimization of the internal profile
(each side)
Longitudinal external profile in the assembly

## Slide 28: Mechanical design – structure supports
Main Concepts
Base frame supports the whole structure
Kevlar straps suspension:
  Minimize thermal conduction with low thermal contraction
  Provide vertical (adjustable out of vacuum) and horizontal alignment
Lateral Yoke serves as an anchoring point for the supports (unique connection between base frame, vacuum chamber and yoke)
Base frame
[304 SS]
Chamber Supports
[316L SS]
Kevlar Straps
Lateral Yoke
[316L SS]

## Slide 29: Mechanical design – chamber supports
Main concepts
  Flexures ensure high transversal stiffness and low longitudinal stiffness (to accommodate thermal contraction)
  Flexures’ anchoring points forms perpendicular lines pointing to the magnet’s center avoiding its displacement
  Materials:
    316L SS provides good mechanical strength with relatively low thermal conductivity and low heat capacity (improving cooldown)
    G10 minimizes heat transfer between 4K and 20K circuits due to its low thermal conductivity
  Hydroformed bellows with modified comb-type RF shield:
    Isolate the vacuum (cryostat/beam)
    Provide longitudinal elasticity for thermal contraction
    Minimize heat transfer between chamber (20K) and cryostat (300K) with low machine impedance impact
Hydroformed Bellows
[316L SS]
Flexures
[316L SS]
Chamber supports
[316L SS]
Thermal Insulators
[G10 / PEEK]
300K-20K Transition
Comb-type RF-shield
Thermal Contraction Analysis
1.8 mm

## Slide 30: Mechanical design – validations and next steps
Supports validation (static and dynamic studies)
Disassembly and inspection of the 4T SCW
Assembly and fiducialization
More details in the following slides
  Mechanical detachment tests of Ho poles and clamps
  Kevlar straps mechanically characterized
Validations already carried out
  Alignment procedure
  Suspension stiffness
  Vibration
  Contraction accommodation
  Stiffness
  Vibration

## Slide 31
Brief Overview of CNPEM
CNPEM engages in superconductivity initiatives
SWLS Overview
  Electromagnetic design
  Coils fabrication
  Mechanical design
  Cryogenic design
  Electrical systems
  Magnetic characterization approach
  Assembly and Sirius Installation
  Schedule and summarized development status
Outline

## Slide 32: Cryogenic concept
LHe tank for the coils ~4.2 K
Central flange – access to the central Lhe tank
SRDK-408S
(50W @ 60K & 12.5W @ 20K, 60 Hz)
SRDK-415D
(55W @ 60K & 1.5W @ 4.2K, 60 Hz)
60K
1st Thermal Shield:
Cooled by 1st stage of the 4 cryocoolers
20K
2nd Thermal shield:
Cooled by the 2nd stage of SRDK-408S
300K
Cryostat Vac Vessel 10-6 ~ 10-8 mbar
300K – 20 K
e- beam chamber transition inner: 10-10 mbar
outside: 10-8 mbar
4K
Cold mass:
Cooled by the 2nd stages of SRDK-415D
20K
E beam vac. Chamber and supports: Cooled by the 2nd stages of SRDK-408S
Kevlar supports
4 T SCW
(in bath cooling)
6.6 T SWLS
(cryogen-free cooling)

## Slide 33: Thermal links
Cold source ~4 K
Cold source ~4 K
Flexible element
Busbar
Cold bus and counterweight
Copper
Copper
Copper
Thermal links connecting the coils to the cold source
Copper

## Slide 34: Heat Loads and Cooling Circuits
Heat Source | 60 K [W] | 20 K [W] | 4 K [W]
Radiation | 7.95 | 0.3 | 0.007
Conduction | 13.82 | 0.77 | 0.17
Current leads@228A | 39 | - | 0.65
Beam Chamber | 37.2 | 8.65 | -
Total | 97.97 | 9.72 | 0.827
Cooling Capacity | 210 | 25 | 3
Design Temperatures
Cooling capacity higher than the heat loads
Heat loads
Cooling Circuits

## Slide 35: Thermal Simulaitons – main considerations
Thermal Contact Conductances
considered in the simulations
(literature and measured values)
The cooling power of the cryocoolers' stages as a function of their temperatures
(based on the models' load map)
The heat loads were considered in the model with their calculated values
and locations along each thermal circuit

## Slide 36: Temperature distribution – 60K Circuit

## Slide 37: Temperature distribution – 20K Circuit
Without 3rd Harmonic cavity – short e- beam bunch
(Power dissipated in the chamber: ~15 W)

## Slide 38: Temperature distribution – 20K Circuit
With 3rd Harmonic cavity – long e- beam bunch
(Power dissipated in the chamber: ~1.75 W)

## Slide 39: Temperature distribution – 4K Circuit
Coils’ temperature around 4.3 K
High ΔT, under evaluation to be improved*
Assymetric thermal load:
1x HTS Current Lead on the lef side
2x HTS Current Leads on the right side
* By increasing the section and improving the quality of the contacts by brazing, without compromising flexibility, assembly, and manufacturing

## Slide 40: Cooldown and warm-up time
Cooldown
Warm-up
About 75 hours to achieve operating temperature
About 30 hours for complete warm-up
Total time for a shutdown needs to fit in one week!

## Slide 41: Coils temperature after current ramp-up
AC losses heat up prevents current ramp-up shorter than 10 minutes
Temperature distribution after 10 minutes current ramp-up

## Slide 42: Tests and validations already carried out
  Vacuum sealing concept of the CuCrZr flanges at cryogenic temperatures
  Validation of fastening and tightening methods at cryogenic temperatures
  Characterization of thermal elements and their contacts at low temperatures

## Slide 43
Brief Overview of CNPEM
CNPEM engages in superconductivity initiatives
SWLS Overview
  Electromagnetic design
  Coils fabrication
  Mechanical design
  Cryogenic design
  Electrical systems
  Magnetic characterization approach
  Assembly and Sirius Installation
  Schedule and summarized development status
Outline

## Slide 44: Current leads and cryogenic electrical circuits
Current Leads: 300K – 4K
  Main heat load in the cryogenic system
Links: between SC wires and coils
  Coils wound with long extensions
  Minimize connections
Splices: electrical connection between coils
  Connections located at good cooling capacity regions
  Unique resistive part between coils
  Pre-requisite: R < 500 nΩ @ 4 K
  Next steps:
  Test the new mechanical fixture of the current leads
SC wires
Preliminary results: R < 10 nΩ @ 4 K
Current Lead
HTS (SS ballasted)
Bi-2223
Resistive Current Lead
Brass
C26800
Flexible thermoelectric link
Copper
Feedthrough
Splice box installed at the vertical cryostat

## Slide 45: Power supply
  Next steps:
  Final test of the developed power supply in the vertical cryostat with SC coils
Resonant converter (discontinuous parallel resonant converter): in-house development
  3 kW, 300 A, and 10 V, and ripple lower than 10 ppm
4T SCW power supplies: Danfysik MP8443
  3 kW, 300 A and 10 V, ripple of 25 ppm
  Obsolete hardware and software
  No technical support anymore
Control system
DC Link
(300 V)
Ripple ~ 7 ppm (1 ppm = 0.3 mA)
Can operate with the load in short-circuit
Resonant converter
Topology of the developed resonant converter
Plan A
Plan B

## Slide 46: Quench protection
Quench Detection prototype (analog circuit) and Extraction circuit
Quench protection archtecture
  Next steps:
  Validate the FPGA prototype in the vertical cryostat
  Robustness and reliability of the FPGA concept for the SWLS
Premises:
  Provide redundant detection and protection
  Design to keep max hot-spot temp < 100 K
Detection: voltage measurement – voltage taps
  Detection circuit: Analog vs Digital using FPGA:
    FPGA can be scalable and optimizable for the SWLS
Protection: Active method with external energy extraction
  The detection circuit sends a signal to the extraction circuit
  The power supply is turned off, and the contactors are activated
  Dump resistors in the extraction circuit dissipate the stored energy
Detected quench during tests of the coils
Redundant voltage taps
Detection by overvoltage and coil unbalance
Redundant extraction switches

## Slide 47
Brief Overview of CNPEM
CNPEM engages in superconductivity initiatives
SWLS Overview
  Electromagnetic design
  Coils fabrication
  Mechanical design
  Cryogenic design
  Electrical systems
  Magnetic characterization approach
  Assembly and Sirius Installation
  Schedule and summarized development status
Outline

## Slide 48: Magnetic characterization plans
Challenges: Small gap; cold vacuum chamber; high field calibration
Two proposed solutions: Characterization in air (“Plan A”); Characterization in vacuum (“Plan B”)
Measurements: Mapping of the magnetic field profile; measurement of field integrals
Plan A
Antichamber for RT* measurements
Hall sensor setup adaptations
Mechanical rod or Hall sensor carriage
Stretched wire for field integrals measurements
* Room Temperature
PCB coils and Hall sensors developments for Plan B
Plan B
Measurements inside SWLS vacuum chamber
New Hall sensor setup and calibration at CT**
New vacuum actuation system
PCB coils for field integrals measurements
** Cryogenic Temperature
Developments of mechanical rod and antichamber for Plan A
Total length of vacuum chamber: 1782 mm
Thermal and vacuum studies in progress
~ 4, 20, 60 Hz preliminary study
with Hall Sensor and Scan/Insert Coil

## Slide 49
Brief Overview of CNPEM
CNPEM engages in superconductivity initiatives
SWLS Overview
  Electromagnetic design
  Coils fabrication
  Mechanical design
  Cryogenic design
  Electrical systems
  Magnetic characterization approach
  Assembly and Sirius Installation
  Schedule and summarized development status
Outline

## Slide 50
Challenges
  Centering the magnetic field:
    Before cooldown: ensuring precise alignment with geometric references
    After cooldown: maintaining precise positioning with limited access for correction
  Cabling and thermal links integration: Planned assembling sequence to simplify the connections
Assembly

## Slide 51
Assembly
Main Concepts
  Measurement-assisted alignment concept (before cooldown):
    Geometric center alignment: assembling and measuring components in respect to fiducial points – reference points transferred from the electromagnetic structure to the external cryostat
    Magnetic center alignment: the measurement of permanent magnets center, located in fiducial points outside the cryostat, allows to correlate the magnetic center with the geometric reference – using the same magnetic measurement system
  Accommodation of thermal contraction (after cooldown):
    Position the structure considering simulated thermal contractions (validation needed)
    Vertical alignment can be adjusted using screws outside the cryostat (validation needed)
Alignment tolerances are still being defined together with the Accelerator Physics Group

## Slide 52
Sirius installation
e- beam

## Slide 53
Brief Overview of CNPEM
CNPEM engages in superconductivity initiatives
SWLS Overview
  Electromagnetic design
  Coils fabrication
  Mechanical design
  Cryogenic design
  Electrical systems
  Magnetic characterization approach
  Assembly and Sirius Installation
  Schedule and summarized development status
Outline

## Slide 54
DESIGN
Schedule

## Slide 55
Electromagnetic Design
Mechanical and Cryogenic Design
Electrical Systems
Validations and Characterizations
Simulations and analysis of the magnetic field profile
SC coils fabrication
Testing of the coils in the vertical cryostat
Final validation of the electromagnetic design of the SWLS
Development of hor/ver correctors
Simulations and analysis of temperature distribution
Simulations and analysis of force distribution in mechanical elements
Validation of refrigeration concepts using the vertical cryostat
Development of electron chamber components
Evaluation and inspection of the superconducting wiggler structure
PROGRESS
Development, testing, and validation of cryogenic electrical circuit
Manufacturing, improvement, and testing of resonant power converter
Development of quench detection and protection system
Development of hardware and software for control and monitoring
Development of setup for magnetic characterization
Integration, assembly, and fiducialization strategy
Evaluation of the impact of device vibration on the machine
Final magnetic characterization of the SWLS
Summarized development status
30% completed
70% completed
60% completed
70% completed

## Slide 56
cnpem.br
Thank you!
Acknowledgements:
CERN
David Tommasini
Gerard Willering
Salvatore Mele
Attilio Milanese
Emmanuele Ravaioli
Louis de Mallac
Miguel Cerqueira Bastos
Torsten Koettig
Carlo Petrone
Amalia Ballarino
CNPEM development team