## Slide 1
nLGAD detector gain performance in the deep and near-ultraviolet (UV) spectral range
26th International Workshop on Radiation Imaging Detectors (IWORID2025)
July 6-10, 2025, Bratislava, Slovakia
Miloš Manojlović, Neil Moffat, Pablo Fernandez-Martínez, Jairo Villegas, Enric Cabruja, Mateusz Rebarz, Giulio Pellegrini, Salvador Hidalgo
Contact e-mail: milos.manojlovic@imb-cnm.csic.es

## Slide 2: Outline
Motivation
  Why study low-penetration radiation?
Introduction to Low Gain Avalanche Diodes (LGAD)
  What are LGADs and the novel nLGAD ‘’flavour’’?
Measurement setup
  Transient Current Technique (TCT)
Spectral Gain Response
  Measurements under deep-UV and near-UV radiation
Conclusions & Future

## Slide 3
Why study low-penetration radiation?

## Slide 4: Why study low-penetration radiation?
Near-surface phenomena are challenging for traditional Si detectors due to recombination effects, which reduce quantum efficiency (depth around 1 µm)
Even more challenging is single-photon detection, which is crucial in many fields such as:
  quantum information
  fluorescence microscopy
  biomedical imaging
  soft X-ray astronomy (< 1 keV)
  deep-UV in fusion experiments etc.
p++
n++
Dead layer
Photon/Particle
Standard PiN diode
Low surface e-field &
Recombination of e-h pairs

## Slide 5
Low Gain Avalanche Diodes (LGAD)

## Slide 6: Low Gain Avalanche Detector
[1] A.G. Stewart et al. in Proc. of SPIE, Vol. 6119, 2006
No Gain
Moderate Gain
&
Proportional response
Gain > 104
Digital response
Linear mode
  Proposed by IMB-CNM in 2014
  Proportional response (linear mode operation)
  Better sensitivity (Gain)
  S/N ratio increased
  Excellent timing resolution (~ 30 ps)
  MIP detection for HEP
  Thin detector integration with the same signal and higher collection efficiency
Original paper
G. Pellegrini, et al., Technology developments and first measurements of Low Gain Avalanche Detectors (LGAD) for high energy physics applications, Nucl. Instrum. Methods A 765 (2014) 12.

## Slide 7: nLGAD Technology
In “low energy physics” - range i.e. penetration depth of the radiation decreases, so the gain starts to diminish
To mitigate this effect
  nLGAD technology
Drawbacks of standard LGAD
n+
n++
n-
p++
n-type LGAD (nLGAD)
n-substrate
Inverted implantation polarity
  Electron driven multipication when charge is generated prior to reaching the gain layer
n+
p++
(~ 2 µm)
E-profile
Cascade of multiplied e
(holes not shown)
Pellegrini, G., Salvador, H. V., David, F. G., Waleed, K., & Manfred, V. (2023). *Low-Penetrating Particles Low-Gain Avalanche Detector*. European Patent EP 3 971 997 B1.

## Slide 8: LGAD vs nLGAD

## Slide 9
Results & Measurements

## Slide 10
Reduce the suppression: Z scan is done so that laser is defocused
Band Pass Filter
Beam splitter
Photodiode
Gradient filter
Neutral-density filter
CCD
High speed oscilloscope
Trigger
(7)
DUT
Transient Current Technique (TCT)
Tunable laser
200-2500 nm

## Slide 11: 1st nLGAD run results
Concept confirmed
  lower penetration depth translates to higher gain
Single pad detectors for now
[1] Villegas, J., Torres, C., Manojlovic, M., Jimenez-Ramos, M. C., Moffat, N., Lopez, J. G., & Hidalgo, S. (2025). NLGAD gain response to low-penetrating particles. Nuclear Instruments and Methods in Physics Research Section A: Accelerators, Spectrometers, Detectors and Associated Equipment, 1072, 170208. https://doi.org/10.1016/j.nima.2025.170208

## Slide 12: 1st and 2nd nLGAD run results
The detectors are sensitivity to deep and near-ultraviolet light (UV)
  Penetration depth ≲ 10 nm
Single pad detectors for now
We acknowledge ELI Beamlines (Czech Republic)
Femtosecond optics

## Slide 13
Summary
First nLGAD productions at IMB-CNM showed good performance for low penetrating radiation, with optimal response (linear gain over 20-40) in the blue and near UV range
Medium UV region (down to 250 nm) explored: signals with gain observed. However, gain seems to be significantly lower than for the near UV range.
New designs explored and new run being fabricated to improve response in DUV range.
ELI TCT facility remarkable and helping us to develop DUV sensors for the future

## Slide 14
Application: SoftPix project

## Slide 15: SoftPix project
What was the goal?
  Production of photon counting píxellated detector with high spatial resolution (55 µm pitch)
How?
  Bumb-bond the USJ-nLGAD and AC-LGAD with Timepix4 and Medipix3 ASIIC
Graphene
n+
n++
n-
p++
Timepix3/Medipix4
ASIC
Passivation
X
│
R
A
Y
280 < E < 530 eV
Water window range
H2O
T ~ 1
A ~ 1
A – Absorptance coefficient T – Transmittance coefficient
- Carbon
- Oxygen
Medical Imaging Application
  For biopsy (for example after a mammography)
  images on the spot
  soft X-rays detected by a Timepix-LGAD device would give better contrast than hard X-rays
  adequate resolution
Preliminary tests with pulse generator

## Slide 16
Conclusions & Future

## Slide 17: Conclusions
nLGAD seems like a promising technology for deep-UV, near-UV
For Soft X-ray detection further adaptation is required
High gain is preserved for low penetrating radiation
Limited to low-energy physics
Future
Low energy proton & ion detection
Has repercussions in medical physics, particularly in ion cancer therapy using ions such as carbon
In progress…
600 keV protons
α-particle in fusion experiments
n
10B+n→7Li+α+Q
Q = 2.79 MeV
α

## Slide 18: Ultra-shallow junction nLGAD (USJ-nLGAD): A New Benchmark in Low Penetration Radiation Detection Technology – work in progress…
Moving to low diffusivity p-type implant (BF2)
Moving to ultra low implantation energies
Moving to laser annealing (minimum diffusion)
Moving to deep multiplication implant for more uniform gain response
Pixellated backside from 55 um to 220 um pitch
Antireflective coatings (MgF2)
Dead layer (entrance window) minimized!
  Quantum efficiency for Soft X-ray maximum
Preliminary...
Same magnitude of field can be obtained with higher implant dose (demonstration)
Ongoing...
October 2025
Key modifications
“Dead” layer

## Slide 19: Acknowledgements
Acknowledgements
This work has been funded by the Spanish Ministry of Science and Innovation (MCIN/AEI/10.13039/501100011033/) and by the European Union’s ERDF program “A way of making Europe”. Grant references: PID2020-113705RB-C32 and PID2021-124660OB-C22. Also, it was funded by the European Union’s Horizon 2020 Research and Innovation funding program, under Grant Agreement No. 101004761 (AIDAInnova).
Thank you!