## Slide 1: MATRIX: Simulation and Experimental Study of GaN Proton Detectors
N S T.D. Lê2, N. Arbor2, A. Wieck1, M M. Siviero3, J.Y. Duboz3
1 Lehrstuhl für Angewandte Festkörperphysik, Ruhr-Universität Bochum, D-44780 Bochum, Germany
2 Université de Strasbourg, CNRS, IPHC UMR 7178, F‐67000 Strasbourg, France
3 Université Côte d’Azur, CNRS, CRHEA, 06560, Valbonne, France

## Slide 2: Motivation: Proton therapy
A.-C. Knopf and A. Lomax, “In vivo proton range verification: a review,” Phys. Med. Biol., vol. 58, no. 15, p. R131, Jul. 2013, doi: 10.1088/0031-9155/58/15/R131.
“PTCOG - Patient Statistics.” Accessed: Jul. 04, 2025. [Online]. Available: https://www.ptcog.site/index.php/patient-statistics

## Slide 3: Why Gallium Nitride?
Total dose: 300 Mrad= 3 Mgy
24 MeV protons
25 nA beam current
Large bandgap material (3.4 eV @ 300K)
Also, large displacement energies of…
Ga: 45 eV | N: 109 eV
Large radiation hardness?!
  Matured fabrication methods from LED / high power electronics technology
  Proof of concept + first steps:
J.-Y. Duboz et al., “GaN Schottky diodes for proton beam monitoring,” Biomed. Phys. Eng. Express, vol. 5, no. 2, p. 025015, Jan. 2019
J.-Y. Duboz et al., “Proton Energy Loss in GaN,” Phys. Status Solidi B, vol. 258, no. 8, p. 2100167, 2021
M. Siviero et al., “GaN diodes comparative study for high energy protons detection,” J. Semicond., vol. 46, no. 0, 2025

## Slide 4: Detector Design
500µm and 1mm pitch
500µm pitch
250 µm x 500 µm pitch
500µm pitch

## Slide 5: Measurement facility CYRCé
TR24 cyclotron from ACSI:
16 to 25 MeV and 300uA maximum
Beamlines for isotope production or proton irradiation
About CYRCé:
E. Bouquerel et al., “Design and commissioning of the first two CYRCé extension beamlines,” Nucl. Instrum. Methods Phys. Res. Sect. Accel. Spectrometers Detect. Assoc. Equip., vol. 1024, p. 166034, Feb. 2022, doi: 10.1016/j.nima.2021.166034.

## Slide 6: Measurement Setup
1: Vacuum proton beam line
2: 200 m thick diffuser for beam homogenization
3: Object positioned in beam
4: 24 MeV proton beam, 2nA current
5: Detector array on XY-translation stage
6: Readout electronics, controller (128-channel CT imaging circuit)
1
4
5
6
3
2

## Slide 7: Measurement setup
Objects to image
Afterwards: Data processing and image generation

## Slide 8: Signal quality
0.5 x 0.5 mm2
2 x 64 diodes
Raw data
Background Subtraction
Normalization of response inhomogeneities
Round apertures in the beamline ≈ 25 mm
All array diodes are working! - Diode yields 100 %
Response inhomogeneity < 2 %
8

## Slide 9: 2D Imaging “Misc shape”
0.5 x 0.5 mm2
2 x 64 diodes
Different energy = different signal!

## Slide 10: GATE10 Simulation

## Slide 11: Energy Modulation at CYRCé

## Slide 12: MATRIX response at different energies
0.5 x 0.5 mm2
2 x 64 diodes

## Slide 13: Response vs deposited energy

## Slide 14: Extrapolation

## Slide 15: Straggling?
0.5 x 0.5 mm2
2 x 64 diodes

## Slide 16: Straggling?
0.5 x 0.5 mm2
2 x 64 diodes

## Slide 17: Undiffused Beam
0.5 x 0.5 mm2
1 x 128 diodes
0.25 x 0.5 mm2
1 x 128 diodes
Can we make a movie of how the beam changes (due to, e.g., collimation)? 

## Slide 18: Time dependent imaging
Three phases:
  Beam stability (no changes)
  Live changes of beam collimation
  Wire profiling inside the beamline
1 x 1 mm2
11 x 11 diodes
  (1 fps – currently limited by readout software)

## Slide 19
We acknowledge financial support from MATRIX (DFG/ANR-22-CE92-0047), NECTAR (ITMI/INSERM-2021), and DFH/UFA CDFA-05-06 Doctoral School.
We gratefully acknowledge ams OSRAM for providing the AS5900 readout circuit used for data acquisition.
Nico Brosda
nico.brosda@rub.de
Next up:
Measuring at different facilities
Larger multiplexed arrays
Assessing the time resolution

## Slide 20: Key Facts: Readout Electronics
ams AS5900 26-Bit 128-Channel Low Noise Current-to-Digital Converter
low noise (down to 3200 electrons for full range up to 1 µA)
Low power dissipation down to 1 mW/channel
data transfer through LVDS interface with up to 80 Mbps
Used for X-ray detectors (CT imaging)