## Slide 1
NDT Report |  | 
X-ray Computed Tomography |  | 
HFM Inspection of SMC 11T 2G 103b coil |  | 
TESTS PERFORMED BY: | DOCUMENT PREPARED BY: | DOCUMENT APPROVED BY:
M. Celuch EN/MME/MM | M. Celuch EN/MME/MM | G. Arnau Izquierdo EN/MME/MM
 |  | EN ISO 9712 level 2 Card n° BO2-020101
List of notification: Jose Ferradas Troitino (TE/MSC) Juan Carlos Perez (TE/MSC) Aleksandra Bartkowska (EN/MME) Mickael Crouvizier (EN/MME) |  | 
CERN
CH1211 Geneva 23 Switzerland
EDMS NO. 3063899
REV. 1.0
VALIDITY APPROVED
REFERENCE J. Ferradas Troitino TE/MSC
Date: 20/03/2024

## Slide 2
Aim
The main region of interest is the so-called layer jump (transition from the inner to outer conductor layer). We would like to investigate the conductor placement and any potential defect appearing in the volume.
REFERENCE D J. Ferradas Troitino TE/MSC
EDMS NO. 3063899
REV. 1.0
VALIDITY APPROVED

## Slide 3
REFERENCE J. Ferradas Troitino TE/MSC
EDMS NO. 3063899
REV. 1.0
VALIDITY APPROVED
Figure 1. Inspected sample.

## Slide 4
Testing conditions
REFERENCE J. Ferradas Troitino TE/MSC
EDMS NO. 3063899
REV. 1.0
VALIDITY APPROVED
Device | D7 LINAC |  |  |  | 
X-ray source: | Type | Voltage [MeV] | Frequency [Hz] | Voxel Size [mm] | FOD / FID [mm]
 | Siemens SILAC | 5.9 | 599.88 | 0.115 | 2700 / 3248.821
FOD – focus object distance
FID – focus imaging (flat panel) distance

## Slide 5
Results
As one popped in/out strand can induce a wave of events the numbers below show only the amount of conductors affected by the pop in/out effect. So even if there are more than one event in the same cable it is counted as one.
2 cables affected (1 in connection and 1 in non-connection side)
All results obtained are available using the link:
\\cern.ch\dfs\Projects\ZeissMetrotomCT\2024\TE\MSC\HFM\
CT data (vgl file) can be viewed using Volume Graphics software:
\\cern.ch\dfs\Projects\ZeissMetrotomCT\Public\VGViewer
Images and videos available starting from the next page.
REFERENCE J. Ferradas Troitino TE/MSC
EDMS NO. 3063899
REV. 1.0
VALIDITY APPROVED

## Slide 6
Vid. 1 – SMC 103b – top view.

## Slide 7
Fig. 2 – SMC 103b – quad view.

## Slide 8
Fig. 3 – SMC 103b – quad view.

## Slide 9
Fig. 4 – SMC 103b – quad view – affected cable on non-connection side.

## Slide 10
Fig. 5 – SMC 103b – quad view – affected cable on connection side.

## Slide 11
Vid. 2 – SMC 103b – right view.

## Slide 12
Vid. 3 – SMC 103b – right view – layer jump.

## Slide 13
Fig. 6 – SMC 103b – right view – layer jump.

## Slide 14
Fig. 7 – SMC 103b – right view – layer jump.

## Slide 15
Fig. 8 – SMC 103b – right view – layer jump.

## Slide 16
Vid. 4 – SMC 103b – rot views.