## Slide 1
UNIVERSITY OF TWENTE.
Measurement and FE modelling critical transverse loading limits of REBCO round cables for fusion
A. Nijhuis1,3 ,G. Anniballi1, J. Rietberg1, N. van Dusschoten1, V.J. Ellenbroek1,2,
R. Lübkemann3, J. Leferink3, C. Soyarslan2, A.H. van den Boogaard2, J.D. Weiss4, K. Radcliff 4, D.C. van der Laan4, H. Jin5, C. Zhou1,5, W. Yu5, J.G. Qin5, E. Garibaldi6, M. Breschi6
1 University of Twente, Faculty of Science & Technology, Enschede, The Netherlands
2 University of Twente, Faculty of Engineering Technology, Enschede, The Netherlands
3 Foundation SuperACT, Hengelo, The Netherlands
4 Advanced Conductor Technologies, Boulder, CO & University of Colorado, Boulder, CO, USA
5 Institute of Plasma Physics, Chinese Academy of Sciences, China
6 University of Bologna, Bologna, Italy
ASIPP
MT29 Boston July 2025

## Slide 2: CORC-CICC Design for fusion
Ic of REBCO tape is strain sensitive.
Fusion reactors HTS CS-Coils:
Magnetic Field ~ 18 – 20 T
Current ~ 40 – 60 kA
High Lorentz Load ~ 1,000 kN/m
T. Mulder, et al. IEEE Transactions on Applied Superconductivity, 30, no. 4, pp. 1-5, 2020, 4800605, doi: 10.1109/TASC.2020.2968251.
K Ilin et al 2015
Supercond. Sci. Technol. 28 055006
IxB | I [kA] | B [T] | F [kN/m]
BEST | 42 | 20 | 840
EU-DEMO | 60 | 18 | 1,080
2
Integrated approach:
Composite cables for high transverse load.
Experimental characterization of tape and cable properties.
CICC Conductor design optimization with FEModel.
Large transverse load deforms tape & REBCO layer.
Strain exceeding irreversibility limit  Critical current degradation
UNIVERSITY OF TWENTE.

## Slide 3: Conductor design optimization
UNIVERSITY OF TWENTE.
Single tape testing
Axial stress
Axial strain
TransverseStress
Winding
Cable transverse load testing
Critical current
Transverse stiffness d(F)
Inter tape contact resistance Rc
FE cable model
Materials
Design

## Slide 4: Single tape: Ic – mechanical testing
UNIVERSITY OF TWENTE.
U-Spring axial tensile & compressive strain Ic(B,T,e)
Axial tensile stress, mechanical properties, Ic & eirr
Transverse stress, Ic & sirr (77 K)
Winding angle Ic & min core diam. (77 K)

## Slide 5
Transverse load (10 x 4 mm2)
UNIVERSITY OF TWENTE.
Ic/Ic0 and n/n0 at zero load after applied stress.
Tape | 𝜎irr [MPa]
S-Innovation | 900
Fujikura, 22-0012-09 | 400
SSCT, ST2903-105 | 750

## Slide 6: Conductor design optimization
UNIVERSITY OF TWENTE.
Single tape testing
Axial stress
Axial strain
TransverseStress
Winding
Cable transverse load testing
Critical current
Transverse stiffness d(F)
Inter tape contact resistance Rc
FE cable model
Materials
Design

## Slide 7
Transverse load: Twente Cable Press
UNIVERSITY OF TWENTE.
7
Hydraulic press based on principle of lever mechanism and wedge
Sample length: 400 mm
Measuring: Ic, Rc, force, displacement and AC loss (only at 4.2 K).
T-operating temperatures: 4.2 and 77 K

## Slide 8
ACT CORC©-CICC Twente Press test sample
7 mm
OD
Extruded C101 Cu Keystones
Machined C110 Cu support
Central cooling tube
Selected tapes (8) for critical current and inter-tape contact resistance measurements.
Cu keystone
SS support
UNIVERSITY OF TWENTE.
8
CORC© cable used in ACT Sultan sample with 36 tapes, OD of 7.04 mm (including thin plastic tube) in groove with 7.54 mm.

## Slide 9
CORC© Twente Press ACT #1,2 & 3
9,000 cycles successive F-increases
(Ec=10 mV/m), n-value (22-21)
Irreversible degradation = critical load (CL):
ACT samples CL<~ 90 kN/m.
UNIVERSITY OF TWENTE.
9
ACT sample #1
ACT sample #2
Sub-cable parameters both samples | 
Tape Manufacturer | SuperPower
SC Tapes | 36
Tape width | 4 mm
Tape thickness | 63 m
Substrate thickness | 50 m
Copper thickness | 5 m
Spacing | 0.5 mm
Core | Cu Rod
Core OD | 5.34mm
Strain window | [-1.3%, 0.45%]
ACT sample #3

## Slide 10
Twente Press ASIPP sample #1 & #3
ASIPP sample #3, degradation for
spiral at 210 kN/m (x6=1,260 kN/m).
solid core 450 kN/m (x6=2,700 kN/m).
ACT samples ~ 90 kN/m < (x6=540 kN/m).
Main difference with ATC samples:
radius Cu profile matches to cable.
no plastic tube around cable.
cable 1,000 kN/m ~ tape 200 MPa (strans)
UNIVERSITY OF TWENTE.
10
ASIPP sample #3
Spiral core
Main parameters ASIPP |  | 
ASIPP Sultan # | #3 | #1
tape supplier | Fujikura | SSTC
Core OD | 4.0 mm | 4.6 mm
SC tape layer | 16 | 22
tape No. layer | 2x3 Cu+ SC(2x4+3x8+4x4)+4x2 Cu | SC(2x4+3x7+ 4x11)+4x1 Cu
tape No. | 48 | 73
winding angle | 33.5-49° | 36.5-56°
gap | ~0.6 mm | 0.4 mm
OD | ~8.6 mm | 9.6 mm
width | 4 mm | 4 mm
thickness | 0.11 mm | 0.10 mm
Ic @ 77K,SF | 160 -210 A | 160-190 A
ASIPP sample #1
Solid Cu core

## Slide 11
Cable outer layer damage, Press test
UNIVERSITY OF TWENTE.
11
ACT cables: < 90 kN/m
Cu groove and key-stone have larger radius than cable (stress concentration?).
ASIPP cables: Middle layers withstand 450 kN/m, more homogeneous distributed contact.
Groove and cable radius match, outer tapes squeezed (→ kinking).
r-cable
r-Cu-groove
Remedies: ACT #3
Space needed for cable to “breath”?
Press testing
ASIPP #1, layer 22
ASIPP #1, layer 10
ASIPP #1, layer 1
ASIPP #3, layer 4
ACT #1 & 2, no damage

## Slide 12
ACT #1 & 2, ASIPP #1 & 3 (spiral), Press F(d)
UNIVERSITY OF TWENTE.
12
Two stiffness regimes
ACT #1
ACT #2
ASIPP #1
22 layers
16 layers (SS spiral)
12 layers
12 layers
ASIPP #3
void/layer - sample | ACT #1 | ACT #2 | ACT #3 | ASIPP #3 | ASIPP #1
(dmeas @150kN/m) [mm] | 150 | 190 | 250 | 700 | 500
tape thickness (t) [mm] | 63 |  |  | 110 | 
void/layer: (Dout-Din)/(2N)-t [mm] | 12 |  |  | 11 | 12
void fraction cable X-section [%] | 16 |  |  | 9 | 10
K. Wang, Y. Gao, W. Luo, Y. Zhou, A. Nijhuis, Nonlinear contact behavior of HTS tapes during pancake coiling and CORC cabling, Supercond. Sci. Technol. 34 (2021) 075003 https://doi.org/10.1088/1361-6668/abf710
ACT #3
12 layers

## Slide 13
Contact resistance results: Rc(F)
Contact resistance: initial Rc and after 3,000 cycles, 2 to 10 𝜇𝛺m in all conductors (under load).
Rc evolution with cycling in qualitative agreement (peak).
UNIVERSITY OF TWENTE.
13

## Slide 14: Conductor design optimization
UNIVERSITY OF TWENTE.
Single tape testing
Axial stress
Axial strain
TransverseStress
Winding
Cable transverse load testing
Critical current
Transverse stiffness d(F)
Inter tape contact resistance Rc
FE cable model
Materials
Design

## Slide 15: Model validation – experimental data
ACT single CORC© experiment with transverse anvil loading.
Parameters | 
Tapes | 12
Layers | 6
Tape width | 3 mm
d-Tape | 44 m
d- Substrate | 30 m
d-Copper | 5 m
Gap spacing | 0.5 mm
Core | Cu/SS rod
Strain window | [-1.3 %, 0.45 %]
D.C. van der Laan et al, 2018 Supercond Sci Technol 32, DOI:10.1088/1361-6668/aae8bf
D.C. van der Laan et al 2019 Supercond. Sci. Technol. 32 015002
D.C. van der Laan, private communication.
UNIVERSITY OF TWENTE.
Good match irreversibility limits:
model versus experiment
NCR = no current sharing between tapes.
PCR = perfect current sharing between tapes.
Cu core
SS core

## Slide 16: Simulations: gap, Cu-tube, EM/ML load
Smaller gap reduces voids and tape bending.
Gap spacing = 1 mm
Gap spacing = 0.5 mm
UNIVERSITY OF TWENTE.
F
ACT cable result compared with 0.5 and 1.0 mm Cu tube.
Strain distribution with 0.5 mm Cu-wall thickness.
Left 2 plots: displacement (mm) for Mech and Electromagnetic Load at 200 kN/m (bending).
Right: Difference body load (EM) and Mechanical Load for different tape thicknesses and gap sizes.
Critical transverse EM load < mechanical load (30%).

## Slide 17: ASIPP CICC; Cu tube core, 1,080 kN/m
REBCO von Mises: 90 MPa
UNIVERSITY OF TWENTE.
17
Cu tube core, 1 mm dwall
1,200 kN/m, Cu tube, 1 mm dwall
Cu tube core, 3 mm dwall
REBCO von Mises: 108 MPa
Cu tube vM stress: 118 MPa,
near yielding stress

## Slide 18: ASIPP CICC; Cu core-SS spring, 1080 kN/m
REBCO von Mises stress:
110 MPa
UNIVERSITY OF TWENTE.
18
Solid Cu core
SS spiral core
SS spiral core
REBCO von Mises stress:
110 MPa
SS spiral peak von Mises stress:
280 MPa
Significantly below yielding limit
Improved cooling

## Slide 19: Model - SULTAN vs Twente Press results
19
2023: CORC Model EM critical EM load
prediction: 1,000 kN/m and ML 1,320 kN/m
2024 Sultan test:
L-leg: CORCs with spiral core, Tcs decreased ~1 K after 80 kA load; EM load = 825 kN/m
R-leg, with CORC cables with solid Cu-core, no degradation up to 80 kA
2025 Twente Press: ASIPP sample #3, Mechanical load degradation for spiral core at 210 kN/m (x6= 1,260 kN/m
FEModel EM load correction: 0.7 x 1,260 = 880 kN/m
ASIPP #3 with spiral core in CORC cables (HFRC)
Tcs@40kA, 10.85T
UNIVERSITY OF TWENTE.

## Slide 20: Summary
UNIVERSITY OF TWENTE.
Cable Press test in agreement with ASIPP Sultan, FEModel and measured REBCO tape properties.
Press critical transverse load CORC®-like cables (5 samples) varies from <100 to 450 kN/m (x 6 =500 to 2,700 kN/m).
Optimizations:
  Gap limit between tapes of same layer
  EM: Cu tube around CORC
  CICC central SS spiral
Contact resistance: evolution with load cycling (with maximum around 10 cycles). Initial Rc and after 3,000 cycles, 2 to 10 𝜇𝛺m (under load).

## Slide 21
UNIVERSITY OF TWENTE.
Thank you!